Owens-Corning

Commercial Insulation

ProSpec

Welcome to Owens-Corning's digitized Commercial Insulation Specifications.  ProSpec provides editable insulation specifications for a wide range of interior partition, exterior wall and roof/ceiling assembly applications.

ProSpec includes directions for the specification writer and product data that can be easily selected for insertion in your project specifications.

Directions for the specification writer and product data boxes are eliminated by turning the toggle off. (Tools, Option, Hidden Text) Turning the toggle on restores the on screen directions and product data.

To add product data from these product data boxes, choose text and insert in the specification text.

If you have questions regarding our products, applications or installation please call us at 1-800-GET-PINK.

# Section 07200

# Interior Partition

# Acoustical Insulation

Part 1 	General

# 1.01 	Summary

A.	Provide glass fiber acoustical insulation for interior partitions

as indicated in building plans.

# 1.02	Materials Provided in Other Sections

# These sections are typically cross referenced. Delete section(s) not included in project manual.

A.	Section 09250-Gypsum Board

B.	Section 09260-Gypsum Board Systems

C.	Section 09100-Metal Support Systems

# 1.03	References

A.	American Society for Testing and Materials (ASTM).

1.	C 665 Specification for Mineral Fiber Blanket Thermal

Insulation for Light Frame Construction and Manufactured

Housing.

2.	E 84 Test Method for Surface Burning Characteristics of

Building Materials.

3.	E 136 Test Method for Behavior of Materials in a Vertical

Tube Furnace at 750(C.

4.	C 518 Test Method for Steady-State Thermal Transmission

Properties by Means of the Heat Flow Meter.

- C423 Test Method for Sound Absorption Coefficient by the

Reverberation Room Method

# 1.04	Submittals

A.	Product Data: Submit Owens-Corning product literature, samples

and installation instructions for specified insulation.

# 1.05	Delivery, Storage and Handling

A.	Protect insulation from physical damage and from becoming wet,

soiled, or covered with ice or snow. Comply with manufacturer's

recommendations for handling, storage and protection during

installation.

B.	Label insulation packages to include material name,

production date and/or product code.

Delete paragraph below if section 01600 or 01620 are not included

in project manual.

C.	Deliver and store materials under provision of Section (01600) (01620).

# 1.06	Limitations

A.	Do not use unfaced insulation in exposed applications where there

is potential for skin contact and irritation.

B.	Kraft and standard foil facings will burn and must not be left

exposed. The facing must be installed in substantial contact with

the unexposed surface of the ceiling, wall or floor finish.  Protect facing

from any open flame or heat source.

Part 2 	Products

# 2.01	Manufacturer

A.	Owens-Corning.

# 2.02	Sound Attenuation Batts

A.	Type: Unfaced glass fiber acoustical insulation complying with

ASTM C 665,  Type I.

B.	Size:

Thickness___ Width___ Length___

Thickness		        Width		  Length

3½"    89mm	   16"  406mm     24"  609mm    	 96"  2438mm

2½"    64mm	   16"  406mm     24"  609mm     	 96"  2438mm

C.	Surface Burning Characteristics:

1.	Maximum flame spread: 10

2.	Maximum smoke developed: 10

When tested in accordance with ASTM E 84.

D.	Combustion Characteristics:

Passes ASTM E 136.

E.	Fire Resistance Ratings:

Passes ASTM E 119 as part of a complete fire tested

wall assembly.

F.	Sound Transmission Class:  STC___

# Select STC from Wall System Chart included in the ProSpec Introduction & Instruction Package.

G.	Dimensional Stability:

Linear Shrinkage less than 0.1%

# 2.03	Quiet Zone Acoustic Batts

A.	Type: Kraft faced glass fiber acoustical insulation complying with

ASTM C 665,  Type II, Class C.

B.	Size:

Thickness___ Width___ Length___

Thickness		        Width		  Length

3½"    89mm	   16"  406mm     24"  609mm    	 96"  2438mm

2½"    64mm	   16"  406mm     24"  609mm     	 96"  2438mm

C.	Surface Burning Characteristics:

1.	Maximum flame spread:  Not Rated

2.	Maximum smoke developed:  Not Rated

When tested in accordance with ASTM E 84.

# Kraft facing on this insulation will burn and

must not be left exposed. The facing must be installed in substantial

contact with the unexposed surface of the wall finish material.

# Protect facing from any open flame or heat source.

D.	Fire Resistance Ratings:

Passes ASTM E 119 as part of a complete fire tested

wall assembly.

E.	Sound Transmission Class:  STC___

# Select STC from Wall System Chart included in the ProSpec Introduction & Instruction Package.

F.	Dimensional Stability:

Linear Shrinkage less than 0.1%

2.04	Thermal Batt Insulation

A.	Type: Unfaced glass fiber thermal insulation

complying with ASTM C 665, Type I.

B.	Size:

# Metal Frame Insulation

# Thickness____ Width____ Length ____

Thickness			     Width		Length

3½"    89mm		16"  406mm     24"  609mm    	96"  2438mm

3½"    89mm		16"  406mm     24"  609mm     	96"  2438mm

6¼"    159mm		16"  406mm     24"  609mm     	96"  2438mm

# Wood Frame Insulation

# Thickness____ Width____ Length ____

Thickness			    Width			Length

3½"    89mm		15"  381mm     23"  584mm   	93"  2362mm

3½"    89mm		15"  381mm     23"  584mm    	93"  2362mm

3½"    89mm		15"  381mm     23"  584mm    	93"  2362mm

6¼"    159mm		15"  381mm     23"  584mm    	93"  2362mm

5½"    139mm		15"  381mm     23"  584mm     	93"  2362mm

C.	Surface Burning Characteristics:

1.	Maximum flame spread: 10

2.	Maximum smoke developed: 10

When tested in accordance with ASTM E 84.

D.	Combustion Characteristics:

Unfaced insulation passes ASTM E 136 test.

E.	Fire Resistance Rating:

Passes ASTM E 119 as part of a complete fire tested

wall assembly.

F.	Sound Transmission Class:  STC_____

# Select STC from Wall System Chart included in the ProSpec Introduction & Instruction Package.

G.	Dimensional Stability:

Linear shrinkage less than 0.1%

# 2.05	Shaftwall Insulation

A.	Type: Unfaced glass fiber acoustical insulation

complying with ASTM C 665, Type I.

B.	Size:

Thickness___ Width___ Length___

Thickness		   Width		     Length	    R-value

1½"    38mm		24"  609mm     	    96"  2438mm	       5.8

C.	Surface Burning Characteristics:

1.	Maximum flame spread: 20

2.	Maximum smoke developed: 20

When tested in accordance with ASTM E 84.

D.	Combustion Characteristics:

Passes ASTM E 136.

E.	Fire Resistance Ratings:

Passes ASTM E 119 as part of a complete fire tested

shaftwall assembly.

F.	Sound Transmission Class: STC___

# Select STC from Wall System Chart included in the ProSpecIntroduction & Instruction Package.

G.	Dimensional Stability:

Linear shrinkage less than 0.1%

2.06	Gypsum Board

A.	Refer to Section (09250) (09260) for detailed specifications.

Select appropriate construction

B.	Type: 1/2" thick, type “x” gypsum panels.

C.	Type: 5/8" thick, type “x” gypsum panels.

D.	Type: 1" thick, shaftliner.

# 2.07	Metal Framing

A.	Refer to Section (09250) (09260) for detailed specifications.

Select appropriate construction

B.	Type: 2 1/2" steel stud.

C.	Type: 3 5/8" steel stud.

D.	Type: 2 1/2" steel I-stud.

Part 3	Execution

# 3.01	Inspection and Preparation

A.	Examine substrates and conditions under which insulation work is

to be performed.  A satisfactory substrate is one that complies with

requirements  of the section in which substrate and related work is specified.

B.	Verify mechanical and electrical services within the shaftwall have been tested and inspected.

B.	Obtain installer's written report listing conditions detrimental to

performance of work in this section. Do not proceed with installation

of insulation until unsatisfactory conditions have been corrected.

C.	Clean substrates of substances harmful to insulation.

# 3.02	Installation - General

A.	Comply with manufacturer's instructions for particular conditions

of installation in each case.

B.	Batts may be friction-fit in place until the interior finish is applied.

Install batts to fill entire stud cavity. If stud cavity is less than 96"

in height, cut lengths to friction-fit against floor and ceiling tracks.

Walls with penetrations require that insulation be carefully cut to fit

around outlets, junction boxes and other irregularities.

C.	Where walls are not finished on both sides or insulation does not

fill the cavity depth, supplementary support must be provided to

hold product in place.

D.	Where insulation must extend higher than 8 feet, temporary support

can be provided to hold product in place until the finish material is applied.

# 3.03	Gypsum Board Installation

A.	Refer to Section (09250) (09260) for proper installation of gypsum board.

# 3.04	Protection

A.	Protect installed insulation as recommended by Owens-Corning.

END OF SECTION