Valspar Flooring	April, 2007

1191 Wheeling Rd

Chicago, Illinois 60090

Toll-Free: (800) 637-7793

www.valsparflooring.com

Specifier Notes: This product guide specification is written according to the Construction Specifications Institute (CSI) Format, including MasterFormat (2004 Edition), SectionFormat, and PageFormat, contained in the CSI Manual of Practice. The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code. Coordinate with other specification sections and the drawings. Delete all "Specifier Notes" when editing this section.

SECTION 09 7000

## Descoglaze-I

## Epoxy/Polyester Wall & Ceiling Surfacing

NOTE TO SPECIFIER

The purpose of this suggested specification is to assist the specifier in developing a specification for the use of DESCOGLAZE-I SYSTEM.Questions regarding the selection, installation, or intended end use of materials should be directed to a technical representative.This specification is prepared to be a part of a complete project specification.

PART 1 - GENERAL

1.01	Related Documents

A.	Drawings and general provisions of the Contract, including General and Supplementary Conditions, apply to this section.

1.02	Summary

A.	DESCOGLAZE-I is a monolithic wall and ceiling coating system able to withstand severe impact and temperature fluctuations and can be modified depending upon the agreed to requirements of this project.

1.03	References

ASTM E 96	Test Method for Water Vapor Transmission of Materials

ASTM D 1360	Test Method for Fire Retardancy of Paints

ASTM D 1864-88	Test Method for Moisture in Mineral Aggregates

ASTM D 4060-90	Test Method for Abrasion Resistance of Organic Coatings by the Taber Abraser

ASTM E 84	Test Method for Surface Burning Characteristics of Building Materials

1.04	System Performance Requirements

A.	Provide an epoxy wall and ceiling coating system that, when cured, produces the following typical properties:

PROPERTY	TEST METHOD	RESULT

Taber Abrasion	ASTM D 4060	0.025 gram loss after
			14 day cure @ 200 cycles using
			CS17 wheels with 1000 gram loads

Fire Resistance	ASTM E 1360	3.8 grams weight loss indicating
			a fire resistant product

Moisture Resistance	ASTM E 96	Less than 1 perm indicating
	Transmission		a vapor barrier

Color Retention	ASTM E 188	No fading, loss of gloss or
			effect on the film after 100

hours exposure

Hardness	Sward Hardness	35

Scrubbability	Gardner Scrubbability	No effect after 1000 cycles

Machine	Gloss before test - 86

Gloss after test - 85

Fire Resistance	ASTM E 84	Flame Spread Index:7

Smoke Development:5

Class “I” or “A”

1.05	Submittals

A.	Submit manufacturer's technical data and product literature indicating that the products comply with specified requirements.

B.	Submit two mock-up sample coupons that are representative of the finished wall and ceiling surface, texture and color.

1.06	Quality Assurance

A.	Installer Qualification:Use only a qualified installer for the wall system manufacturer of having completed a program of instruction in proper methods for preparation of substrate, possible delaminated areas, crack and joint repair and complete wall and ceiling system installation.

B.	Mock-up: On site, fabricate a panel approximately 100 sq. ft. (10 sq. m.) to demonstrate quality of finished wall and ceiling system, complying with manufacturer's instructions.Install panel where directed by architect/engineer.Maintain panel as a standard of quality for all installations.

1.07	Delivery, Storage and Handling

A.	Deliver product in factory packages, clearly marked with manufacturer's identification, printed instructions, lot numbers and shelf life expiration date for each component.

B.	Store materials at 50 C to 90 F (10 C to 32 C) in dry environment away from sunlight, heat, or other hazards.

1.08	Project Conditions

A.	Maintain minimum substrate surface temperature of 55 F (12 C) for a minimum of 48 hours before, during and after installation, or until cured.

B.	Substrate must be free of hydrostatic, capillary or moisture vapor pressure.Substrates in contact with ground must have a properly installed, effective vapor barrier to help prevent potential problems resulting from hydrostatic, capillary or moisture vapor pressure.Concrete must contain less than 3% moisture when tested per ASTM D 1864.

C.	Do not apply sealers or membrane curing agents to concrete.Moisture curing of concrete is recommended.

D.	Concretes containing lightweight aggregates are not recommended substrates.

E.	Provide ventilation, lighting and clean, drinkable water supply.

F.	Advise other trades of fixtures and fittings not to be installed until system is cured, such as: radiators, painting, decorating, floor-supported equipment or cabinetwork, caulking, plumbing, fixtures, etc.

G.	Work areas shall be kept free of traffic and no trades shall be permitted in rooms during the application and curing of the coating.

H.	Protect adjacent surfaces from damage resulting from work of this trade.If necessary, mask and/or cover adjacent surfaces, fixtures, equipment, etc. by suitable means.

I.	Gypsum drywall is only suitable for dry areas.Water-resistant Gypsum board is suitable in occasionally wet areasInstall drywall in accordance with drywall manufacturer's directions and with the factory paper bound edge 1/4 inch (6.4 mm) above floor line.Tape and fill joints; fill all fastener heads and other indentations for smooth finished surface.

PART 2 - PRODUCTS

2.01	Materials

A.	Resinous Wall and Ceiling System:DESCOGLAZE-I.

PART 3 - EXECUTION

3.01	Inspection

A.	Before starting work, ensure that environmental and site conditions are suitable for application and curing.

B.	Inspect surfaces for acceptability of levelness, moisture content and other critical factors at time of installation.

C.	Report in writing to architect/engineer, with copy to manufacturer, of deficiencies that could impair work.Surfaces must be approved prior to application of the system.

3.02	Surface Preparation

A.	Prepare surfaces in accordance with manufacturer's instructions.

B.	Remove concrete laitance by steel shot blasting, grit blasting, or other method approved by manufacturer.

C.	Surface must be clean, sound and dry prior to application.

D.	Pre-fill surface irregularities, holes and cracks in accordance with manufacturer's recommendations.

3.03	Mixing

A.	Comply with manufacturer's instructions for mixing procedures.

B.	Pre-mix each component before every batch to ensure uniformity.

C.	Carefully measure and mix the components together.

3.04	Installation

A.	Follow manufacturer's written instructions.

B.	Prime entire surface with recommended primer.

C.	Apply coating in accordance with manufacturer's instruction to a total thickness depending upon the agreed to requirements of the installation.

D.	Apply grout coat(s) and topcoat(s) at manufacturer's recommended coverage to provide uniform, dense surface.

E.	Allow proper cure time for each installation step.

F.	Allow the finished system to cure for a minimum of 7 days from completion before putting into service.

3.05	Corner Radius Application

A.	Prior to priming entire surface, apply primer to corners.

B.	 Mix a thixotropic ( fume silica ect, ). Into premixed Descoglaze to form an epoxy gel.

C.	Apply epoxy gel to wall corners and wall ceiling transitions at specified diameter using a radius trowel.

D.	After the material cures sand ridges and chatter marks and proceed with wall coating.

Rev 1/00 MGM