# StoMachine Technology Product Reference

# Equipment for Mixing and Spraying Sto Products

The following chart provides general guidance for selection of spraying equipment to be used with Sto products.  Because all spray application projects are different, we cannot recommend a specific orifice size or pressure setting for each material.  Test areas are always recommended to be sure of desired results.

|  | Mixing and Spraying Equipment |
| --- | --- |
| Product | Airless Sprayer | Hopper Sprayer | Bottom-Feed Pistol | Pressure Pot | Sto M-8 | S-25 Mixer | StoSilo Combo |
| CONDITIONERS |  |  |  |  |  |  |  |
| Sto Plex W | Yes | NR | Yes | Yes | Yes, w/Power Roller | NR | NR |
| Sto Leveler | NR | Yes | NR | NR | NR | Yes | Recommended |
| Sto Primer | Requires Filter Removal | Yes | Yes | NR | Recommended | NR | Yes w/Hopper Attachment |
| Sto Primer Smooth | Yes | Yes | Yes | Yes | Recommended | NR | Yes w/Hopper Attachment |
| ADHESIVES |  |  |  |  |  |  |  |
| Sto BTS Silo | NR | Yes | NR | NR | Yes | Recommended | Recommended |
| Sto BTS-Plus | NR | Yes | NR | NR | Yes | Recommended | NR |
| Sto Primer/Adhesive-B | NR | Yes | NR | NR | Yes | Recommended | NR |
| Sto Primer Adhesive | NR | Yes | NR | NR | Yes | NR | NR |
| Sto BTS-FastSet | NR | NR | NR | NR | NR | Yes | NR |
| Sto Flexyl | NR | Yes | Yes | Yes | Recommended | NR | Yes |
| BASE COATS |  |  |  |  |  |  |  |
| Sto BTS Silo | NR | Yes | NR | NR | Yes | Recommended | Recommended |
| Sto BTS-Plus | NR | Yes | NR | NR | Yes | Recommended | NR |
| Sto Primer/Adhesive-B | NR | Yes | NR | NR | Yes | Recommended | NR |
| Sto Primer Adhesive | NR | Yes | NR | NR | Yes | NR | NR |
| Sto BTS-FastSet | NR | Yes | NR | NR | NR | Yes | NR |
| Sto RFP | NR | Yes | NR | NR | Recommended | NR | Yes w/ Hopper Attachment |
| FINISHES |  |  |  |  |  |  |  |
| Sto Finishes (all) | NR | Yes | Limited by Aggregate Size | NR | Recommended | NR | Yes w/Hopper Attachment |

# StoMachine Technology Product Reference

# Equipment for Mixing and Spraying Sto Products									Page 2 of 3

|  | Mixing and Spraying Equipment |
| --- | --- |
| Product | Airless Sprayer | Hopper Sprayer | Bottom-Feed Pistol | Pressure Pot | Sto M-8 | S-25 Mixer | StoSilo Combo |
| COATINGS |  |  |  |  |  |  |  |
| Sto Décor Tex | NR | Yes | Yes | NR | Recommended | NR | Yes w/Hopper Attachment |
| Sto Maxicryl | Yes | Yes | Yes | Yes | Recommended | NR | Yes w/Hopper Attachment |
| StoSilco Shield | Yes | Yes | Yes | Yes | Recommended | NR | Yes w/Hopper Attachment |
| Stolastic | Yes | Yes | Yes | Yes | Recommended | NR | Yes w/Hopper Attachment |
| Sto Silco Lastic | Yes | Yes | Yes | Yes | Recommended | NR | Yes w/Hopper Attachment |
| Sto Decocoat | NR | Yes | NR | NR | Recommended | NR | NR |
| Sto Granitex | NR | Recommended | NR | NR | NR | NR | NR |
| Sto Protective Concrete Coating | Yes | Yes | Yes | Yes | Recommended | NR | Yes w/Hopper Attachment |
| Sto Textured Deck Finish | NR | Yes | Limited by Aggregate Size | NR | Recommended | NR | Yes w/Hopper Attachment |
| Sto Textured Concrete Coating Medium | NR | Yes | Limited by Aggregate Size | NR | Recommended | NR | Yes w/Hopper Attachment |
| AIR/MOISTURE BARRIERS |  |  |  |  |  |  |  |
| Sto Gold Coat | NR | Yes | Yes | NR | Recommended | NR | Yes w/Hopper Attachment |
| Sto Gold Fill | NR | NR | NR | NR | Recommended | NR | Yes w/Hopper Attachment |

# StoMachine Technology Product Reference

# Equipment for Mixing and Spraying Sto Products									Page 3 of 3

|  | Mixing and Spraying Equipment |
| --- | --- |
| Product | Airless Sprayer | Hopper Sprayer | Bottom-Feed Pistol | Pressure Pot | Sto M-8 | S-25 Mixer | StoSilo Combo |
| CONCRETE FAÇADE & EXTERIOR REPAIR |  |  |  |  |  |  |  |
| Sto Bonding and Anti-corrosion agent | NR | Recommended | NR | NR | NR | NR | NR |
| Sto Clear Coat Sealer | Yes | NR | Yes | Yes | Yes, w/Power Roller | NR | NR |
| Sto Penetrating Sealer | Yes | NR | Yes | Yes | Yes, w/Power Roller | NR | NR |
| Sto Full Depth Repair Mortar CI | NR | NR | NR | NR | NR | Recommended | NR |
| Sto Flowable Mortar | NR | Yes | NR | NR | NR | Recommended | NR |
| Sto High-Strength Shotcrete | NR | NR | NR | NR | NR | NR | NR |
| StoPatch Repair Mortar | NR | NR | NR | NR | NR | NR | NR |
| Sto Thin-Coat Mortar | NR | NR | NR | NR | NR | NR | NR |
| Sto Trowel Grade Mortar | NR | NR | NR | NR | NR | NR | NR |
| Sto Skim Coat | NR | Yes | NR | NR | NR | Yes | Recommended |
| Sto Texture Coat | NR | Yes | NR | NR | Recommended | NR | Yes w/Hopper Attachment |
| *Sto Watertight Coat | NR | Yes | Yes | Yes | Recommended | NR | Yes |

* Call the StoMachine Technology HelpLine at (888) 522-0184 for special instructions on spraying Sto Watertight Coat

Notes: 	1)    If the Sto product that interests you does not appear above, it is not currently recommended for mixing or spraying applications.

- “Yes” – mixing and/or spraying the subject product with this type of equipment is possible.  “Recommended” - this equipment is the best choice for mixing and/or spraying the product.  “NR” – this equipment is not recommended for mixing and/or spraying this product.

- We cannot recommend specific orifice sizes and pressure settings because they will vary with the equipment being used and the desired finished appearance.  We suggest preparing a test area for review using the equipment, materials and methods proposed for the job.

- Specific questions about use of the Sto M-8 Spray Pump, the Sto S-25 Continuous Mixer and the StoSilo Combo should be directed to the StoMachine Technology group at (888) 522-0184.

D:\Winword\MISC_DOC\SMT Equipment - Sto Product Matrix.doc