PVC Waterstops: Ribbed Center Bulb with Hog Rings

Ribbed Center Bulb: Ribbed Center Bulb waterstops are used in expansion joints where movement between members is anticipated. They are generally used above grade, but since it is a universal design, they can be used below grade as well. The size of the joint and shear movement determines the size of the waterstop.

# Flat Ribbed

Flat Ribbed waterstops are used in construction joints where little or no movement is anticipated. They are generally used below grade in footings, walls and slabs.

| ## Typical Properties (.075" Slab) | ## Nominal Value | ### Nominal Value |
| --- | --- | --- |
| Water Absorption | 0.15% | D-570 |
| Tear Resistance | 350/lb.in. | D-624 |
| Specific Gravity, (+/-0.02) | 1.33 | D-792 |
| Hardness, Shore A (+/-3, 10 sec. delay) | 74 | D-2240 |
| Tensile, psi | 2000 | D-638, Type IV |
| Elongation, % | 375 | D-638, Type IV |
| 100% Modulus, psi | 725 | D-638, Type IV |
| Brittle Point (Tb), F | -35 (Passed) | D-746 |
| Stiffness in Flexure, psi | 1440 | D-747 |
| Ozone Resistance | No Failure | D1149 |
| Accelerated Extraction, CRD-C572 |  |  |
| Tensile, psi | 2000 | D-638, Type IV |
| Elongation, % | 390 | D-638, Type IV |
| Effect of Alkali, CRD-C572 |  |  |
| Weight Change, % | +0.12 | -------- |
| Change in Hardness, Shore A | -3 | D-2240 |

INSTALLATION INSTRUCTIONS FOR PVC WATERSTOPS

PREPARATION:  During progress of work all waterstop shall be protected from damage and should be free of oil, dirt and concrete spatter.  Waterstop coils should be uncoiled several days before installation to insure ease of installation and fabrication.  Be sure steel reinforcing bars do not interfere with proper positioning of waterstop.

PLACEMENT:  The location and embedment of the waterstop shall be as shown on the drawings, with approximately one-half of the width of the waterstop embedded in the concrete on each side of the joint.  All waterstops shall be sufficiently held in place to insure that they are correctly positioned to form a continuous watertight diaphragm in the joint unless otherwise shown.  The method used to fasten the waterstop may be as follows:

- extending through a slot in the keyway

- held in place by split bulkheads

- hog ring and wire tie to reinforcing bars every 12 inches.  Always secure hog ring or wire between the last rib and the end of the waterstop.

- Hog ring shall not penetrate the waterstop. BoMetals, Inc can provide hog rings 12” on center upon request.

Care should be taken during concrete placement on horizontal sections to prevent excessive movement of the waterstop to insure against displacement.  Always thoroughly and systematically vibrate concrete around the waterstop to avoid air entrapment and to provide a positive contact between the waterstop and the concrete.  On the second pour, sweep horizontal joints to insure there is no foreign matter to interfere with positive contact between the waterstop and the concrete.  When using split-ribbed waterstops, the split leg of the waterstop is opened and nailed to the bulkhead between the last rib and the edge.  Upon stripping the forms, the split legs are joined together by using a rubber-based contact cement and placing hog rings every 12 inches and wire-tied to the rebar.

IMPORTANT:  The technical data herein is believed to be accurate.  It is offered for your consideration, investigation and verification.  Buyer assumes all risk of use, storage and handling of the product.  NO WARRANTY, EXPRESS OR IMPLIED, IS MADE INCLUDING, BUT NOT LIMITED TO, IMPLIED WARRANTIES OF MERCHANTABILITY AND FITNESS FOR A PARTICULAR PURPOSE.  Nothing contained herein shall be construed as a license to operate under or recommendation to infringe any patents.