NOTE** This Section is based on systems of

NOTE** Butterfield Color®

NOTE** 625 West Illinois Avenue

NOTE** Aurora, Illinois 60506

NOTE** Telephone: 1-800-282-3388

NOTE** Fax: 630-906-1982

NOTE** www.butterfieldcolor.com

NOTE** This guide specification is intended to be used by a qualified construction specifier. It should not be used without appropriate modifications.

NOTE** Notes for review by specifier begin with “NOTE**.” Optional text requiring a selection is enclosed within brackets, e.g., “Color shall be [gray] [white].” Items requiring specifier input are indicated by a blank line enclosed within brackets, e.g., “Color: [_______].” Delete specifier notes and non-applicable optional text in final specification.

NOTE** Specification Section numbers and Section titles are according to The Construction Specifications Institute MasterFormat™ 1995 edition and indicated within brackets for MasterFormat™ 2004 edition.

GUIDE SPECIFICATION

NOTE ** Retain one Section number below and revise footer Section number to match.

SECTION 02753 [32 13 19]

CONCRETE PAVING TOP SURFACE RETARDERS

GENERAL

SUMMARY

Section Includes:  Top surface retarders for concrete surfaces.

SUBMITTALS

Submit according to Conditions of the Contract and Division 1 Specification Sections.

Product Data: For each product indicated.

Qualification Data: For Applicator and manufacturer specified in Quality Assurance Article, including names and addresses of completed projects, architects, and owners.

QUALITY ASSURANCE

Applicator Qualifications: [Two] [________] year's experience with projects of similar scope and quality.

NOTE ** Delete paragraph above or below.

Applicator Qualifications: Trained or approved by manufacturer of top surface retarder.

Manufacturer's Qualifications: Three year's experience manufacturing products required.

Source Limitations: Obtain products from same source throughout Project.

Mockup: Prepare mockups of top surface retarder to set quality standards for workmanship and application. Locate at site and obtain approval before start of final work. Mockup shall be minimum [25 sq. ft. (2.3 sq. m)] [_______].

Use materials, tools, and techniques that will be utilized for work to determine coverage rate, dwell time, substrate compatibility, and removal method.

Verify adequate dry and wet slip resistance of sealed concrete surfaces.

Approved mockups set quality standards for comparison with remaining work.

[Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.]

NOTE ** Delete paragraph below if preinstallation conference is not required.

Preinstallation Conference: Conduct conference at site to comply with requirements of Division 1 Section “Project Meetings.”

DELIVERY, STORAGE AND HANDLING

Deliver materials in original packaging with labels intact.

Store in clean, dry and protected location, according to manufacturer's requirements.

PROJECT CONDITIONS

Environmental Requirements: Comply with top-surface-retarder manufacturer's instructions.

Do not apply top surface retarder if air temperature and concrete substrate temperature are not between 55 to 90 deg F (10 to 32 deg C) before and during application.

In hot weather, apply top surface retarder in early morning or when surfaces are shaded.

Protect top surface retarders from rain until dry.

PRODUCTS

CONCRETE

Refer to Division 3 [03] Sections for concrete receiving top surface retarders.

TOP SURFACE RETARDERS

Top Surface Retarders: Manufacturer's standard water-based, biodegradable, low-odor, top-surface-retarder formulation for chemically delaying the set of surface mortar, while allowing underlying concrete to harden normally.

Product: Butterfield Color® SufEtch™.

CURING AND SEALING COMPOUNDS

Solvent-Borne Curing and Sealing Compound: Butterfield Color® Clear Guard Cure and Seal.

NOTE ** Delete subparagraph above or below. Use Clear Guard® Cure and Seal for exterior applications or interiors if a strong odor is not objectionable. Clear Guard® H2O Cure and Seal is a water-based system for interior and exterior applications.

Water-Borne Curing and Sealing Compound: Butterfield Color® Clear Guard H2O Cure and Seal.

ACCESSORY MATERIALS

Plastic Sheeting: Polyethylene film, ASTM D 4397, minimum 4-mils thick, clear.

Masking Tape: Nonstaining, nonabsorbent masking tape, compatible with indicated substrates, that removes easily, including adhesive.

Miscellaneous Products: Select materials and methods based on the following, and approved on mockups:

Effectiveness in performing work indicated.

Tools, General: Chemical-resistant type.

Application Tools: Airless sprayer, brush, or roller for vertical surfaces only, as recommended by top-surface-retarder manufacturer.

Removal Tools: Brooms and garden hoses, or pressure washers, as recommended by top-surface-retarder manufacturer, that do not damage concrete surfaces, including adjacent substrates not in contract.

MIXING

Mixing Top Surface Retarder: Mix top surface retarder according to manufacturer's instructions.

EXECUTION

PROTECTION

Protect personnel, vehicles, surrounding surfaces, plastic, rubber, site, plants, and adjacent surfaces from top surface retarder.

Adjacent Existing Concrete Surfaces: Install protective plastic sheeting over adjacent existing concrete surfaces, and secure by double taping, or spray-apply top surface retarder on adjacent existing concrete surfaces, and allow to completely dry before applying top surface retarder on new concrete surfaces.

Clean up spills immediately. Clean application tools with clean water immediately after use.

TOP SURFACE RETARDER APPLICATION

Apply top surface retarder according to manufacturer's instructions.

Apply an even layer of top surface retarder to entire concrete surface, at manufacturer’s recommended coverage rate, to achieve a masking, consistent blue color over concrete surface.

DWELL TIME

Allow top surface retarder to remain on concrete surfaces for period established by mockup.

Do not float or trowel concrete surfaces after applying top surface retarder.

Divert downspouts or other sources of substantial water exposure from flowing directly onto concrete surfaces after applying top surface retarder.

Do not apply curing compound over top surface retarder.

TOP SURFACE RETARDER REMOVAL

Top Surface Retarder Removal: Expose aggregate by washing top surface retarder within 6 to 24 hours after application.

Using a garden hose or pressure washer, work top surface retarder with new, clean brooms. Work a small area to determine depth of etching. If depth of etching is too deep, stop removing top surface retarder and allow concrete surfaces to further cure.

Achieve uniform depth of concrete-surface etching by working concrete surfaces at the same dwell time after initial application of top surface retarder.

Clean removal tools with clean water immediately after use.

Dispose of residue according to requirements of authorities having jurisdiction.

CURING AND SEALING

Apply curing and sealing compound by pump-up sprayer or short-nap roller in multiple light coats over etched surfaces according to manufacturer's instructions.

Apply curing and sealing compound to dry surfaces, with no visible moisture or dampness, not sooner than 12 to 24 hours after concrete placement.

Do not allow curing and sealing compounds to puddle on surfaces or in joints.

NOTE ** Delete two paragraphs below if slip-resistive additive is not required.

Slip-Resistive Additive: Thoroughly mix slip-resistive additive into curing and sealing compound before application, according to manufacturer's instructions. Stir curing and sealing compound often to maintain even distribution of slip-resistive additive.

Verify adequacy of slip resistance before opening up surfaces to traffic.

CLEANING

Clean spillage and residue from adjacent construction according to manufacturer's instructions.

PROTECTION

Protect etched concrete from damage or deterioration until date of Substantial Completion.

END OF SECTION

Copyright © 2009 Butterfield Color®. All Rights Reserved.

A copyright license to reproduce this specification is granted to specifying architects and engineers.