NOTE** This Section is based on systems of

NOTE** Butterfield Color®

NOTE** 625 West Illinois Avenue

NOTE** Aurora, Illinois 60506

NOTE** Telephone: 1-800-282-3388

NOTE** Fax: 630-906-1982

NOTE** www.butterfieldcolor.com

NOTE** This guide specification is intended to be used by a qualified construction specifier. It should not be used without appropriate modifications.

NOTE** Notes for review by specifier begin with “NOTE**.” Optional text requiring a selection is enclosed within brackets, e.g., “Color shall be [gray] [white].” Items requiring specifier input are indicated by a blank line enclosed within brackets, e.g., “Color: [_______].” Delete specifier notes and non-applicable optional text in final specification.

NOTE** Specification Section numbers and Section titles are according to The Construction Specifications Institute MasterFormat™ 1995 edition and indicated within brackets for MasterFormat™ 2004 edition.

GUIDE SPECIFICATION

NOTE ** Retain one Section number below and revise footer Section number to match.

SECTION 02753 [32 13 19]

CONCRETE PAVING TOP SURFACE RETARDERS

- GENERAL

  - SUMMARY

    - Section Includes:  Top surface retarders for concrete surfaces.

  - SUBMITTALS

    - Submit according to Conditions of the Contract and Division 1 Specification Sections.

    - Product Data: For each product indicated.

    - Qualification Data: For Applicator and manufacturer specified in Quality Assurance Article, including names and addresses of completed projects, architects, and owners.

  - QUALITY ASSURANCE

    - Applicator Qualifications: [Two] [________] year's experience with projects of similar scope and quality.

NOTE ** Delete paragraph above or below.

    - Applicator Qualifications: Trained or approved by manufacturer of top surface retarder.

    - Manufacturer's Qualifications: Three year's experience manufacturing products required.

    - Source Limitations: Obtain products from same source throughout Project.

    - Mockup: Prepare mockups of top surface retarder to set quality standards for workmanship and application. Locate at site and obtain approval before start of final work. Mockup shall be minimum [25 sq. ft. (2.3 sq. m)] [_______].

      - Use materials, tools, and techniques that will be utilized for work to determine coverage rate, dwell time, substrate compatibility, and removal method.

      - Verify adequate dry and wet slip resistance of sealed concrete surfaces.

      - Approved mockups set quality standards for comparison with remaining work.

      - [Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.]

NOTE ** Delete paragraph below if preinstallation conference is not required.

    - Preinstallation Conference: Conduct conference at site to comply with requirements of Division 1 Section “Project Meetings.”

  - DELIVERY, STORAGE AND HANDLING

    - Deliver materials in original packaging with labels intact.

    - Store in clean, dry and protected location, according to manufacturer's requirements.

  - PROJECT CONDITIONS

    - Environmental Requirements: Comply with top-surface-retarder manufacturer's instructions.

      - Do not apply top surface retarder if air temperature and concrete substrate temperature are not between 55 to 90 deg F (10 to 32 deg C) before and during application.

      - In hot weather, apply top surface retarder in early morning or when surfaces are shaded.

      - Protect top surface retarders from rain until dry.

- PRODUCTS

  - CONCRETE

    - Refer to Division 3 [03] Sections for concrete receiving top surface retarders.

  - TOP SURFACE RETARDERS

    - Top Surface Retarders: Manufacturer's standard water-based, biodegradable, low-odor, top-surface-retarder formulation for chemically delaying the set of surface mortar, while allowing underlying concrete to harden normally.

      - Product: Butterfield Color® SufEtch™.

    - CURING AND SEALING COMPOUNDS

      - Solvent-Borne Curing and Sealing Compound: Butterfield Color® Clear Guard Cure and Seal.

NOTE ** Delete subparagraph above or below. Use Clear Guard® Cure and Seal for exterior applications or interiors if a strong odor is not objectionable. Clear Guard® H2O Cure and Seal is a water-based system for interior and exterior applications.

      - Water-Borne Curing and Sealing Compound: Butterfield Color® Clear Guard H2O Cure and Seal.

    - ACCESSORY MATERIALS

      - Plastic Sheeting: Polyethylene film, ASTM D 4397, minimum 4-mils thick, clear.

      - Masking Tape: Nonstaining, nonabsorbent masking tape, compatible with indicated substrates, that removes easily, including adhesive.

    - Miscellaneous Products: Select materials and methods based on the following, and approved on mockups:

      - Effectiveness in performing work indicated.

      - Tools, General: Chemical-resistant type.

      - Application Tools: Airless sprayer, brush, or roller for vertical surfaces only, as recommended by top-surface-retarder manufacturer.

      - Removal Tools: Brooms and garden hoses, or pressure washers, as recommended by top-surface-retarder manufacturer, that do not damage concrete surfaces, including adjacent substrates not in contract.

  - MIXING

    - Mixing Top Surface Retarder: Mix top surface retarder according to manufacturer's instructions.

- EXECUTION

  - PROTECTION

    - Protect personnel, vehicles, surrounding surfaces, plastic, rubber, site, plants, and adjacent surfaces from top surface retarder.

      - Adjacent Existing Concrete Surfaces: Install protective plastic sheeting over adjacent existing concrete surfaces, and secure by double taping, or spray-apply top surface retarder on adjacent existing concrete surfaces, and allow to completely dry before applying top surface retarder on new concrete surfaces.

    - Clean up spills immediately. Clean application tools with clean water immediately after use.

  - TOP SURFACE RETARDER APPLICATION

    - Apply top surface retarder according to manufacturer's instructions.

    - Apply an even layer of top surface retarder to entire concrete surface, at manufacturer’s recommended coverage rate, to achieve a masking, consistent blue color over concrete surface.

  - DWELL TIME

    - Allow top surface retarder to remain on concrete surfaces for period established by mockup.

      - Do not float or trowel concrete surfaces after applying top surface retarder.

      - Divert downspouts or other sources of substantial water exposure from flowing directly onto concrete surfaces after applying top surface retarder.

      - Do not apply curing compound over top surface retarder.

  - TOP SURFACE RETARDER REMOVAL

    - Top Surface Retarder Removal: Expose aggregate by washing top surface retarder within 6 to 24 hours after application.

      - Using a garden hose or pressure washer, work top surface retarder with new, clean brooms. Work a small area to determine depth of etching. If depth of etching is too deep, stop removing top surface retarder and allow concrete surfaces to further cure.

      - Achieve uniform depth of concrete-surface etching by working concrete surfaces at the same dwell time after initial application of top surface retarder.

    - Clean removal tools with clean water immediately after use.

    - Dispose of residue according to requirements of authorities having jurisdiction.

  - CURING AND SEALING

    - Apply curing and sealing compound by pump-up sprayer or short-nap roller in multiple light coats over etched surfaces according to manufacturer's instructions.

      - Apply curing and sealing compound to dry surfaces, with no visible moisture or dampness, not sooner than 12 to 24 hours after concrete placement.

      - Do not allow curing and sealing compounds to puddle on surfaces or in joints.

NOTE ** Delete two paragraphs below if slip-resistive additive is not required.

    - Slip-Resistive Additive: Thoroughly mix slip-resistive additive into curing and sealing compound before application, according to manufacturer's instructions. Stir curing and sealing compound often to maintain even distribution of slip-resistive additive.

    - Verify adequacy of slip resistance before opening up surfaces to traffic.

  - CLEANING

    - Clean spillage and residue from adjacent construction according to manufacturer's instructions.

  - PROTECTION

    - Protect etched concrete from damage or deterioration until date of Substantial Completion.

END OF SECTION

Copyright © 2009 Butterfield Color®. All Rights Reserved.

A copyright license to reproduce this specification is granted to specifying architects and engineers.