NOTE** This Section is based on systems of

NOTE** Butterfield Color®

NOTE** 625 West Illinois Avenue

NOTE** Aurora, Illinois 60506

NOTE** Telephone: 1-800-282-3388

NOTE** Fax: 630-906-1982

NOTE** www.butterfieldcolor.com

NOTE** This guide specification is intended to be used by a qualified construction specifier. It should not be used without appropriate modifications.

NOTE** Notes for review by specifier begin with “NOTE**.” Optional text requiring a selection is enclosed within brackets, e.g., “Color shall be [gray] [white].” Items requiring specifier input are indicated by a blank line enclosed within brackets, e.g., “Color: [_______].” Delete specifier notes and non-applicable optional text in final specification.

NOTE** Specification Section numbers and Section titles are according to The Construction Specifications Institute MasterFormat™ 1995 edition and indicated within brackets for MasterFormat™ 2004 edition.

GUIDE SPECIFICATION

NOTE ** Retain one Section number and title below and revise footer Section number and title to match.

SECTION 02980 [32 01 26]

CEMENT CONCRETE BONDED OVERLAYS [RIGID PAVING REHABILITATION]

SECTION 03920 [03 01 50]

CONCRETE RESURFACING [RESUFACING OF CONCRETE]

SECTION 09980 [09 97 23]

CONCRETE COATINGS [CONCRETE COATINGS]

- GENERAL

  - SUMMARY

    - Section Includes:

NOTE** Delete overlay cementitious topping system subparagraphs below that are not required. Delete optional text below for exterior concrete pavement or interior concrete floor that is not required.

      - Overlay cementitious toppings for resurfacing concrete [pavement] [floor].

    - Related Sections:

NOTE** Delete subparagraphs below that are not required; add others as required.

      - [Division 2 Section “Cement Concrete Pavement”] [Division 32 Section “Concrete Paving”] for cast-in-place concrete pavement with overlay cementitious toppings.

      - Division 3 Section “Cast-in-Place Concrete” for interior concrete with overlay cementitious toppings.

  - SUBMITTALS

    - Submit according to Conditions of the Contract and Division 1 Specification Sections.

    - Product Data: For each product indicated.

    - Sample Panels: [2 by 2 feet (610 by 610 mm)] [_______], to demonstrate finish of overlay cementitious topping.

    - Qualification Data: For Installer and manufacturer specified in Quality Assurance Article, including names and addresses of completed projects, architects, and owners.

  - QUALITY ASSURANCE

    - Installer Qualifications: Two year's experience with projects of similar scope and quality.

NOTE ** Delete paragraph above or below.

    - Installer Qualifications: Trained or approved by Manufacturer of overlay cementitious topping systems.

    - Manufacturer's Qualifications: Three year's experience manufacturing products required.

    - Source Limitations: Obtain products from same source throughout Project.

    - Field Samples: Locate at site and obtain approval before start of final work. Field samples shall be minimum [4 by 4 feet (1.2 by 1.2 m)] [_______].

      - Demonstrate range of finishes and workmanship, including curing procedures.

      - Approved field samples set quality standards for comparison with remaining work.

      - [Remove field samples when directed.] [Approved field samples may become part of the completed Work if undisturbed at completion of Project.]

NOTE ** Delete paragraph below if preinstallation conference is not required.

    - Preinstallation Conference: Conduct conference at site to comply with requirements of Division 1 Section “Project Meetings.”

  - DELIVERY, STORAGE AND HANDLING

    - Deliver materials in original packaging with labels intact.

    - Store in clean, dry and protected location, according to manufacturer's requirements.

  - PROJECT CONDITIONS

    - Environmental Requirements: Comply with overlay cementitious topping manufacturer's instructions.

      - Do not apply overlay cementitious topping if air temperature and concrete substrate temperature are not between 45 to 85 deg F before and during installation.

      - In hot weather, install overlay cementitious topping in early morning or when surfaces are shaded.

      - Keep bagged products out of sunlight. Use cool water; do not use water from hot watering hoses.

      - Protect overlay cementitious topping from rain for 24 hours.

      - In windy weather, protect adjacent construction from over-spray during application of sealers.

- PRODUCTS

  - OVERLAY CEMENTITIOUS TOPPING MATERIALS

    - Overlay Cementitious Topping: Polymer-modified cementitious topping designed for resurfacing stable, non-moving concrete [floors] [pavements].

      - Product: Butterfield Color® T1000™ Fine Overlay.

NOTE ** Retain Paragraph article below if primer is required for added durability.

    - Primer: Butterfield Color® T1000™ Primer.

    - Water: Potable.

  - SEALING MATERIALS

    - Clear, Solvent-Borne, Membrane-Forming Sealing Compound: ASTM C 309, non-yellowing, VOC-compliant, high-gloss, clear liquid.

      - Product: Butterfield Color® Clear-Guard™ Cure & Seal.

NOTE ** Delete paragraph below if matte finish for sealer is not required.

    - Flatten Paste: Manufacturer's standard product designed to reduce sealer gloss finish to matte finish.

      - Product: Butterfield Color® Flatten Paste.

NOTE ** Delete paragraph below if slip-resistive additive is not required for interior concrete.

    - Slip-Resistive Additive: Finely graded aggregate or polymer additive designed to add to sealer for slip-resistant surface.

  - MIXING

    - Mixing Overlay Cementitious Topping: Mix thoroughly according to manufacturer's instructions.

      - Bulk Mixing: For machine mixing of overlay cementitious topping, use a paddle mortar mixer.

- EXECUTION

  - EXAMINATION

    - Examine substrate for compliance with requirements.

    - Do not proceed with overlay cementitious topping installation until unacceptable conditions are corrected.

  - SUBSTRATE PREPARATION

    - Map out locations of existing control joints before installation of overlay cementitious topping.

    - Thoroughly clean substrate using high-pressure water or trisodium phosphate (TSP) and water with a scrub brush, then rinse thoroughly. Remove potential bond breakers, such as grease, oil, silicone, paint, sealant, curing and sealing compound, drywall taping compound, etc.

    - For painted, sealed, or overly slick hard-troweled concrete substrates, mechanically abrade surfaces by sanding, scarifying, or shot blasting to allow for proper bonding.

    - Remove weak, delaminated, or unsound concrete substrates.

NOTE** Delete paragraph below if concrete does not require patching.

    - Patching: Fill chips, pits, and cracks prior to application of overlay cementitious topping with a slurry of Butterfield Color® T1000™ Fine Overlay and water in lifts up to 3/16 inch. Fill depths not exceeding one inch with a slurry of Butterfield Color® T1000™ Fine Overlay, water, and clean pea gravel or small aggregate.

    - Allow surfaces to dry thoroughly prior to application of overlay cementitious topping.

NOTE** Delete Article below if priming substrate for added durability is not required.

  - PRIMING SUBSTRATES

    - Apply an even coat of concrete primer from two directions, free of holidays, to prepared substrates using a paint roller or stiff bristle brush. Protect adjacent surfaces from overspray or splash.

    - Allow concrete primer to dry tack free prior to application of overlay cementitious topping.  If primed substrates become wet, reapply primer.

    - Prevent contamination of primed surfaces by moisture, dirt or other deleterious materials or conditions.

    - Apply overlay cementitious topping within 24 hours of concrete primer application.

  - TROWEL-APPLIED OVERLAY CEMENTITIOUS TOPPING PLACEMENT

    - Trowel Application: Distribute overlay cementitious topping by trowel or squeegee to a uniform thickness of 1/16 to 3/16 inch.

    - Clean tools frequently to avoid build up of topping materials.

    - Do not add water to surface once placing has begun. Do not retemper overlay cementitious topping.

NOTE** Delete Article below if overlay cementitious topping is indoor or not required.

  - BROOM FINISH

    - Apply fine broom finish to overlay cementitious topping immediately following initial troweling of material. Clean broom by hand after each pass.

NOTE** Delete Article below if trowel finish overlay cementitious topping is not required. Hard trowel finish is not recommended for exterior overlay cementitious topping.

  - TROWEL FINISH

    - Trowel Finish: Finish as required to achieve desired surface.

  - JOINTS

    - Recut existing control joints before cracking occurs, generally within 8 to 24 hours after placement at 70 deg F.

  - SEALING

    - Sealer Application: Apply uniformly in continuous operation by sprayer or short nap roller according to manufacturer's instructions. After initial application is dry and tack free, apply a second coat.

      - Do not over apply or apply in a single heavy coat.

NOTE ** Delete subparagraph below if flatten paste not required for reducing sealer gloss finish to matte finish.

      - Thoroughly mix flatten paste in sealer according to manufacturer's instructions. Stir occasionally to maintain uniform distribution of paste.

NOTE ** Delete subparagraphs below for interior concrete. For interior applications subject to wetting, consider slip-resistant floor wax over sealer.

      - Thoroughly mix slip-resistant additive in sealer according to manufacturer's instructions. Stir occasionally to maintain uniform distribution of additive.

      - Verify adequacy of slip resistance before opening up surfaces to traffic.

  - REPAIRS AND PROTECTION

    - Repair damaged overlay cementitious topping according to manufacturer's instructions.

    - Clean spillage and soiling from adjacent construction according to manufacturer's instructions.

    - Protect overlay cementitious topping from damage or deterioration until date of Substantial Completion.

END OF SECTION

Copyright © 2006 Butterfield Color®. All Rights Reserved.

A copyright license to reproduce this specification is granted to specifying architects and engineers.