(Specifier Note:  The purpose of this guide specification is to assist the specifier in correctly specifying gypsum board products and installation.  The specifier needs to edit the guide specifications to fit the needs of specific projects.  Contact a CertainTeed Product Representative to assist in making the appropriate product selections.  Throughout the guide specification, there are Specifier notes to assist in the editing of the file.  The term Architect is used throughout these guide specifications, as a guide and may be edited to read “Design Professional”, “Engineer”, “Owner” or other appropriate designation as required for specific project.

References have been made within the text of the specification to MasterFormat 2004 Section numbers and titles, specifier need to coordinate this numbers and titles with sections included for the specific project.  Brackets [ ]; “AND/OR”; and “OR” have been used to indicate when a selection is required.)

SECTION 09 29 00

GYPSUM BOARD

- GENERAL

      - SECTION INCLUDES

        - Gypsum board wall panels

        - Gypsum Board soffit and ceiling panels

        - Accessories and Trim

      - REFERENCES

        - ASTM C473 – Standard Test Methods for Physical Testing of Gypsum Panel Products

        - ASTM C475/C475M – Standard Specification for Joint Compound and Joint Tape for Finishing Gypsum Board

        - ASTM C514 – Standard Specifications for Nails for the Application of Gypsum Board

        - ASTM C665 – Standard Specification for Mineral-Fiber Blanket Thermal Insulation for Light Frame Construction and Manufactured Housing

        - ASTM C840 – Standard Specification for Application and Finishing of Gypsum Board

        - ASTM C954 – Standard Specification for Steel Drill Screws for the Application of Gypsum Panel Products or Metal Plaster Bases to Steel Studs From 0.033 in. to 0.112 in. in Thickness

        - ASTM C1002 – Standard Specification for Steel Self-Piercing Tapping Screws for the Application of Gypsum Panel Products or Metal Plaster Bases to Wood Studs or Steel Studs

        - ASTM C1047 – Standard Specification for Accessories For Gypsum Wallboard and Gypsum Veneer Base

        - ASTM C1396/C1396M – Standard Specification for Gypsum Board

        - ASTM C1629/C1629M – Standard Classification for Abuse-Resistant Nondecorated Interior Gypsum Panel Products and Fiber-Reinforced Cement Panels

        - ASTMC1766 – Standard Specification for Factory-Laminated Gypsum Panel Products

        - ASTM D3273 – Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber

        - ASTM E84 – Test Method for Surface Burning Characteristics of Building Materials

        - ASTM E119 – Standard Test Methods for Fire Tests of Building Construction and Materials

        - ASTM G21 – Standard Practice for Determining Resistance of Synthetic Polymeric Materials to Fungi

        - California Department of Public Health CDPH/EHLB/Standard Method Version 1.1, 2010

        - CAN/ULC-S101 – Fire Endurance Tests of Building Construction and Materials

        - CAN/ULC-S102 – Surface Burning Characteristics of Building Materials and Assemblies

        - CAN/ULC-A82-20 Series – Methods of Testing Gypsum and Gypsum Products

        - CAN/ULC-A82.27 – Gypsum Board

        - CAN/ULC-A82-31 – Gypsum Board Application

        - GA-214 - Recommended Levels of Gypsum Board Finish

        - GA-216 - Application and Finishing of Gypsum Board

        - GA-231 - Assessing Water Damage to Gypsum Board

        - GA-238 - Guidelines for the Prevention of Mold Growth on Gypsum Board

        - Health Product Declaration Standard v2.0 – hpdcollaborative.org

        - ISO 14024 – Environmental Labels and Declarations – Type I Environmental Labeling – Principles and Procedures

        - ISO 14025 – Environmental Labels and Declarations – Type III Environmental Declarations – Principles and Procedures

        - ISO 16000-23 – Performance Test for Evaluating Reduction of Formaldehyde Concentrations by Sorptive Building Materials

      - SUBMITTALS

        - Refer to Section [01 33 00 Submittal Procedures] [insert section number and title].

        - Product Data:  Submit manufacturer current technical literature for each component.

        - Samples:

          - Board: Submit sample of each panel product specified, [6 inches (150 mm) square] [insert size].

          - Trim:  Submit sample of each type of trim specified, [12 inches (305 mm) long] [insert size].

          - Texture:  Submit sample [12 inches (305 mm) square] [insert size] of textured coated gypsum board.

        - Quality Assurance Submittals

- (Specifier Note:  DELETE Design Data, Test Report submittal requirements when propriety specification is used and can be held.  MAINTAIN Design Data, Test Report submittal requirement when other products may be submitted as substitution.)

          - Provide products manufactured in North America only.

          - Design Data, Test Reports:  Provide manufacturer test reports indicating product compliance with indicated requirements.

          - Manufacturer Instructions:  Provide manufacturer’s written installation instructions

        - Closeout Submittals

          - Refer to Section [01 78 00 Closeout Submittals] [insert section number and title].

      - QUALITY ASSURANCE

        - Qualifications:  Installer shall have experience with installation of gypsum board under similar conditions.

        - Mock-ups:

          - Install mock-up using approved gypsum products, including fasteners and related accessories per manufacturer’s current printed instructions and recommendations.

            - Mock-up size: [10 feet by 10 feet (3050 x 3050 mm)] [insert size].

            - Mockup for [[each] [designated] level of exposed gypsum board finish] AND/OR [[each] [designated] texture finish indicated]

            - Mock-up Substrate: Match wall assembly construction.

            - Mock-up may [not] remain as part of the work.

      - DELIVERY, STORAGE AND HANDLING

        - Deliver materials in manufacturer’s original packages, indicating manufacturer and product name.

        - Store gypsum in accordance with GA-238 and manufacturer recommendations.

      - PROJECT CONDITIONS

        - In accordance with ASTM C840.

- PRODUCTS

- (Specifier Note: Product Information is proprietary to CertainTeed Gypsum, Inc. products.)

      - MANUFACTURER

        - Basis of Design: CertainTeed Gypsum, Inc.; 20 Moores Road, Malvern, PA  19355; 1-800-233-8990; www.certainteed.com

        - Equivalent Design:  Manufacturer with products of equivalent design may include, but are not limited to:

          - National Gypsum Company

          - USG Corporation

      - GYPSUM BOARD WALL PANELS

        - Standard Gypsum Board Products

          - Regular Gypsum Board: Gypsum core panel solid set core enclosed in paper.  Complying with ASTM C1396/C1396M.

            - Basis of Design:  CertainTeed Easi-Lite™, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/2 inch (12.7 mm)

            - Width: [48 inches (1220 mm)] [54 inches (1370 mm)] [48 inches or 54 inches (1220 or 1370 mm)]

            - Length: [8 feet (2440 mm)] [9 feet (2740 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges: [Square] [Rounded] [Tapered]

            - GREENGUARD Gold Certification

          - Fire Rated Gypsum Board: Gypsum core panel with a specially formulated core for use in fire-resistive Type X designs.  Complying with ASTM C1396/C1396M, Type X.

            - Basis of Design:  CertainTeed Type X, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 5/8 inch (15.9 mm)

            - Width: [48 inches (1220 mm)] [54 inches (1370 mm)] [48 inches or 54 inches (1220 or 1370 mm)]

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  [Tapered]

            - GREENGUARD Gold Certification

          - Fire Rated Gypsum Board: Gypsum core panel with a solid set, fire-resistive core for use in fire-resistive Type C (Enhanced Type X) designs.  Complying with and ASTM C1396/C1396M, Type X.

            - Basis of Design:  CertainTeed Type C, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: [1/2 inch (12.7 mm)] [5/8 inch (15.9 mm)]

            - Width: 48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  Tapered

            - GREENGUARD Gold Certification

          - 30 Minute Fire Rated Gypsum Board: Gypsum core panel with a specially formulated core for use in 30 minute fire-resistive designs.  Complying with ASTM C1396/C1396M.

            - Basis of Design:  CertainTeed Easi-Lite™ 30, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 5/8 inch (15.9 mm)

            - Width: 48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  [Tapered]

            - GREENGUARD Gold Certification

        - Moisture and Mold Resistant Products

          - Moisture and Mold Resistant Gypsum Board: Gypsum core panel with enhanced core formulated for resistance to moisture and mold; surfaced with moisture/mold resistant paper on front, back, and long edges. Complying with ASTM C1396/C1396M.

            - Basis of Design: CertainTeed M2Tech® Gypsum Board, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/2 inch (12.7 mm)

            - Width: [48 (1220 mm)] [54 (1370 mm)] inches

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)]

            - Edges: Tapered

            - GREENGUARD Gold Certification

            - Mold Resistance: Panel score of 10 (highest rating available) when tested in accordance with ASTM D3273

          - Fire Rated Moisture and Mold Resistant Gypsum Board: Gypsum core panel with enhanced core formulated for resistance to moisture and mold; for use in fire-resistant Type X designs. Surfaced with moisture/ mold resistant paper on front, back, and long edges. Complying with ASTM C1396/C1396M, Type X.

            - Basis of Design: CertainTeed M2Tech® Type X Gypsum Board by CertainTeed Gypsum, Inc.

            - Thickness: 5/8 inch (15.9 mm)

            - Width: [48 )1220 mm)] [54 (1370 mm)] inches

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] feet

            - Edges: Tapered

            - GREENGUARD Gold Certification

            - Mold Resistance: Panel score of 10 (highest rating available) when tested in accordance with ASTM D3273

          - Moisture and Mold Resistant Fire-Rated Gypsum Shaft Liner Board: Gypsum core shaftwall panel with enhanced fire resistant core, surfaced with moisture and mold resistant paper on front/back/ long edges. Complying with ASTM C 1396/C1396M, Type X.

            - Basis of Design: CertainTeed M2Tech® Shaftliner Type X, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1 inch (25.4 mm)

            - Width: 24 inches (610 mm)

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  Double-Beveled

            - GREENGUARD Gold Certification

            - Mold Resistance:  Panel score of 10 (highest rating available) when tested in accordance with ASTM D3273.

        - VOC Reducing Products

          - VOC Reducing Gypsum Board: Gypsum core panel formulated to capture, contain convert Formaldehyde to inert compounds. Tested as an Indoor Passive Panel Technology (IPPT) in accordance with ISO 16000-23.  Complying with ASTM C1396/C1396M.

            - Basis of Design:  CertainTeed AirRenew® Essential Indoor Air Quality (IAQ) Gypsum Board, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/2 inch (12.7 mm)

            - Width: [48 (1220 mm)] [54 (1370 mm)]  inches

            - Length: [8 feet (2440 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  Tapered

            - GREENGUARD Gold Certification

- f.	Surface Paper: 100% recycled paper on face, back and long edges.

          - VOC Reducing Moisture and Mold Resistant Gypsum Board: Gypsum core panel formulated to capture, contain, convert Formaldehyde to inert compounds. Gypsum core panel with enhanced core formulated for resistance to moisture and mold. Tested as an Indoor Passive Panel Technology (IPPT) in accordance with ISO 16000-23.  Complying with ASTM C1396/C1396M.

            - Basis of Design:  CertainTeed AirRenew® M2Tech® Indoor Air Quality (IAQ) Gypsum Board, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: Type X, 5/8 inch (15.9 mm) thick where indicated and as otherwise required to meet fire rating for specific element

- [1/2 inch (12.7 mm) elsewhere]

            - Width: 48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  Tapered

            - GREENGUARD Gold Certification

            - Mold Resistance Rating:

- 1. Score of 10 (best possible) tested in accordance with ASTM D3273

- 2. Rating of 0 (best possible) tested in accordance with ASTM G21

            - Surface Paper: 100% recycled moisture and mold resistant paper on face,

- back and long edges.

        - Specialty Products

          - Abuse-Resistant Moisture and Mold Resistant Gypsum Board: Gypsum core panel formulated with enhanced core for abuse resistance; moisture and mold resistance; for use in fire-resistant Type X designs. Surfaced with abuse resistant moisture/mold resistant paper on front and long edges and moisture/mold resistant paper on back.  Complying with ASTM C1396/C1396M, Type X and ASTM C1629/C1629M.

- NOTE: Installation of Abuse-Resistant Gypsum Board requires steel studs complying with ASTM C645 and shall be not less than 0.0312 inch (0.792 mm) design thickness and shall be in accordance with sections 4.3 and 8.1 of ASTM C645.

- a.	Basis of Design:  CertainTeed Extreme Abuse Resistant Gypsum Board, manufactured by CertainTeed Gypsum, Inc.

- b.  Thickness: Type X, 5/8 inch (15.9 mm) thick where indicated and as otherwise required to meet fire rating for specific element

- c.	Width: 48 inches (1220 mm)

- d.   Length:  [8 feet (2440 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

- e.   Edges: Tapered

- f.	GREENGUARD Gold Certification.

- g.	Mold Resistance Rating:

- 1. Score of 10 (best possible) tested in accordance with ASTM D3273

- 2. Rating of 0 (best possible) tested in accordance with ASTM G21

- h.	Surface Paper: 100% recycled moisture and mold resistant paper on face,

- back and long edges.

            - ASTM 1629/C1629M Classification Levels:

- 1. Surface Abrasion:   	Level 3

- 2. Surface Indention:  	Level 1

- 3. Soft Body Impact: 	Level 2

- 4. Hard Body Impact: 	Level 1

          - Impact-Resistant Moisture and Mold Resistant Gypsum Board: Gypsum core panel formulated with enhanced core for impact resistance; moisture and mold resistance; for use in fire-resistant Type X designs. Surfaced with abuse resistant moisture/mold resistant paper on front and long edges and moisture/mold resistant paper on back.   Complying with ASTM C1396/C1396M, Type X and ASTM C1629/C1629M.

- NOTE: Installation of Impact-Resistant Gypsum Board requires steel studs complying with ASTM C645 and shall be not less than 0.0312 inch (0.792 mm) design thickness and shall be in accordance with sections 4.3 and 8.1 of ASTM C645.

- a.	Basis of Design:  CertainTeed Extreme Impact Resistant Gypsum Board, manufactured by CertainTeed Gypsum, Inc.

- b.  Thickness: Type X, 5/8 inch (15.9 mm) thick where indicated and as otherwise required to meet fire rating for specific element

- c.	Width: 48 inches (1220 mm)

- d.    Length:  [8 feet (2440 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

- e.    Edges: Tapered

- f.	GREENGUARD Gold Certification.

- g.	Mold Resistance Rating:

- 1. Score of 10 (best possible) tested in accordance with ASTM D 3273

- 2. Rating of 0 (best possible) tested in accordance with ASTM G 21

- h.	Surface Paper: 100% recycled moisture and mold resistant paper on face,

- back and long edges.

            - ASTM 1629/C1629M Classification Levels:

- 1. Surface Abrasion:   	Level 3

- 2. Surface Indention:  	Level 1

- 3. Soft Body Impact: 	Level 3

- 4. Hard Body Impact: 	Level 3

          - Flexible Gypsum Board: Gypsum core panel with enhanced core to allow for flexibility; Complying with ASTM C1396/C1396M.

            - Basis of Design:  CertainTeed 1/4” Flex, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/4 inch (6.4 mm)

            - Width: 48 inches (1220 mm)

            - Length: [8 feet (2440 mm)]  [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges:  Tapered

          - Noise-Reducing Gypsum Board

            - Basis of Design: CertainTeed SilentFX® QuickCut™ Gypsum Board, manufactured by CertainTeed Gypsum, Inc.

- 1. Factory-Laminated noise-reducing gypsum board consisting of two layers of dense gypsum board encased in smooth, moisture and mold resistant paper facings laminated together with sound damping viscoelastic polymer.  Board incorporates Score and Snap technology.  Complying with ASTM C1766, ASTM C1396/C1396M and ASTM C1629/C1629M.

- b.   Thickness: Type X, 5/8 inch (15.9 mm) thick where indicated and as otherwise required to meet fire rating for specific element

- [1/2 inch (12.7 mm) elsewhere]

- c.	Width: 48 inches (1220 mm)

- d. 	Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

- e. 	Edges: Tapered

- f. 	Surface Paper: 100% recycled moisture and mold resistant paper on face, back and long edges

- g.	Mold resistance Rating: score of 10 (best possible) tested in accordance with ASTM D3273

- h.	GREENGUARD Gold Certification.

- i.	ASTM 1629/C1629M Classification Levels:

- 1. Surface Abrasion:   	Level 2

- 2. Soft Body Impact: 	Level 1

        - Plaster Base Products

          - Regular Veneer Plaster Base:  Gypsum core lathing panel with face paper for use under veneer plaster finishes.  Complying with ASTM C1396/C1396M.

            - Basis of Design: CertainTeed Easi-Lite™ Veneer Plaster Base, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/2 inch (12.7 mm)

            - Width:  48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges: [Tapered]

            - GREENGUARD Gold Certification

          - Fire Rated Veneer Plaster Base:  Gypsum core lathing panel with enhanced fire resistant core for use under veneer plaster finishes in Type X Designs.  Complying with ASTM C1396/C1396M, Type X.

            - Basis of Design: CertainTeed Veneer Plaster Base Type X, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 5/8 inch (15.9 mm)

            - Width:  48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [9 feet (1370 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [Use longest length available to avoid joints]

            - Edges: [Tapered]

            - GREENGUARD Gold Certification

      - GYPSUM BOARD CEILING AND SOFFIT PANELS

        - Exterior Soffit Board

          - Fire Rated Exterior Soffit Board:  Gypsum core soffit panel with enhanced fire and sag resistant core for use in fire resistive Type X designs. Complying with ASTM C1396C1396M, Type X.

            - Basis of Design: CertainTeed Exterior Soffit Board Type X, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 5/8 inch (15.9 mm)

            - Width:  48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [12 feet (3660 mm)]  [Use longest length available to avoid joints]

            - Edges: Tapered

            - GREENGUARD Gold Certification

        - Interior Ceiling Board

          - Gypsum Ceiling Board:  Lightweight Gypsum Core panel with enhanced sag resistant core.  Complying with ASTM C1396/C1396M.

            - Basis of Design: CertainTeed Easi-Lite™ Interior Ceiling Board, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/2 inch (12.7 mm)

            - Width:  48 inches (1220 mm)

            - Length: [8 feet (2440 mm)] [10 feet (3050 mm)] [12 feet (3660 mm)] [14 feet (4270 mm)] [Use longest length available to avoid joints]

            - Edges: Tapered

            - GREENGUARD Gold Certification

          - Regular Gypsum Ceiling Board:  Gypsum Core panel with enhanced sag resistant core.  Complying with ASTM C1396/C1396M.

            - Basis of Design: CertainTeed Interior Ceiling Board, manufactured by CertainTeed Gypsum, Inc.

            - Thickness: 1/2 inch (12.7 mm)

            - Width:  48 inches (1220 mm)

            - Length: [10 feet (3050 mm)] [12 feet (3660 mm)] [14 feet (4270 mm)] [16 feet (4880 mm)]  [Use longest length available to avoid joints]

            - Edges: Tapered

            - GREENGUARD Gold Certification

      - INDEPENDENT ENVIRONMENTAL CERTIFICATIONS

        - VOC Content

          - Third-Party certification of compliance per California Department of Public Health CDPH/EHLB/Standard Method Version 1.1, 2010

          - GREENGUARD Certification per UL Standard 2818

        - Recycled Content

          - Third-party validated Type I Environmental Label per ISO 14024 Environmental Labels and Declarations - Type I Environmental labeling – Principles and Procedures

        - Environmental Product Declarations

          - Third-party verified Type III Environmental Product Declaration per ISO 14025 – Environmental Labels and Declarations – Type III Environmental Declarations – Principles and Procedures

        - Health Product Declarations

          - Per Health Product Declaration Standard v2.0

            - Hpdcollaborative.org

      - ACCESSORIES

        - Interior Trim:  Complying with ASTM C1047.

          - Corner Bead:

            - Basis-of-Design:  Subject to compliance with requirements provide;

- [NO-COAT Structural Laminate Drywall Corner Trim] [AQUABEAD Water-Activated Drywall Corners] [LEVELLINE Corner Trim] [ZOOMA-FLEX Corner Trim] [other corner trim], manufactured by CertainTeed Gypsum, Inc.

          - Casing Beads: [LC-Bead] [L-Bead] [U-Bead]

          - Control Joint

        - Fasteners:

          - Screws: [ASTM C954] [ASTM C1002] as recommended by panel manufacturer.

          - Nails: ASTM C514 with heads, lengths, configurations, and finish as recommended by panel manufacturer.

          - Adhesive:  Recommended by panel manufacturer.

        - Joint Treatment

          - Tape: ASTM C475/C475M

          - Joint Compound:  Comply with ASTM C475/C475

        - Texture Finishes

          - Primer

          - Wall Texture: [Fine] [Medium] [Coarse]

          - Ceiling Texture: [Fine] [Medium] [Coarse]

        - Sealant

- (Specifier Note:  Sealants may be specified in this section or may be specified elsewhere in Division 07.  EDIT paragraphs below dependent upon location of sealant specification.)

          - Refer to Section [07 92 00 Joint Sealants]  [insert section number and title].

- OR

          - Acoustical Sealant: Nondrying, non-hardening, non-skinning, non-staining, non-bleeding, gunnable type as recommended by panel manufacturer.

            - Basis of Design:  Green Glue Noiseproofing Sealant, manufactured by Saint-Gobain.

        - Insulation

- (Specifier Note:  Insulation may be specified in this section or may be specified in Division 09.  EDIT paragraphs below dependent upon location of acoustical insulation specification.)

          - Refer to Section [09 81 00 Acoustic Insulation] [insert section number and title].

- OR

          - Insulation: ASTM C665, Type I, glass fiber insulation blankets without membrane facing.

            - Basis of Design:  CertainTeed Thermal & Acoustical Fiber Glass Insulation, manufactured by CertainTeed Corporation.

- EXECUTION

      - EXAMINATION

        - Examine gypsum board panels for damage and existence of mold.  Install undamaged panels

        - Examine gypsum board in accordance with GA-231 for water damage.

      - INSTALLATION

        - Comply with [ASTM C840] [GA216]

      - FINISHING

        - General:  Comply with [ASTM C840]  [GA214 and GA216]

          - Level 1: Plenums, service corridors; above ceilings

          - Level 2: Areas of water resistant gypsum backing board under tile; exposed areas where appearance is not critical.

          - Level 3: Areas to receive heavy or medium textured coatings; heavy-grade wallcoverings.

          - Level 4: Areas to receive flat sheen paint finish; light textured coatings; lightweight wallcoverings.

          - Level 5:  Areas to receive gloss, semi-gloss sheen paints; critical lighting conditions.

      - PROTECTION

        - Protect installed products from damage during remainder of the construction period.

        - Remove and replace panels that are damaged.

END OF SECTION