SECTIONS 07 21 00 and 07 26 00

FIBER GLASS BUILDING INSULATION and VAPOR RETARDERS

Display hidden notes to specifier. (Don't know how? Click Here)

** NOTE TO SPECIFIER ** CertainTeed Corp., Insulation Group; Building Insulation products.
 .
 This section is based on the products of CertainTeed Corp., Insulation Group, which is located at:
750 E. Swedesford Rd. P. O. Box 860 
Valley Forge, PA 19482-0860
Toll Free Tel: 800-233-8990
Fax: 610-341-7940
Email: request info
Web: certainteed.com/CertainTeed/Pro/Design+Professional/Insulation 
[ Click Here ] for additional information.
 
 CertainTeed is one of America's leading producers of fiber glass insulation used in Residential, Commercial and Mechanical/HVAC markets for both new or existing buildings. Our product line includes fiber glass batts, blankets, blowing products, fiber glass insulation for HVAC duct systems and MemBrain™ - The Smart Vapor Retarder. Our insulation products have achieved GREENGARD™ Certification for superior indoor air quality (IAQ) performance.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER **  Delete items below not required for project.

    - Batt and Roll Insulation.

    - Blanket Insulation.

    - Vapor Retarder.

  - RELATED SECTIONS

** NOTE TO SPECIFIER **  Delete any sections below not relevant to this project; add others as required.

    - Section 07100 -  Dampproofing and Waterproofing: Insulation installed with waterproofing systems.

    - Section 07260 - Vapor Retarders: Vapor retarder materials to adjacent insulation.

    - Section 07270 - Air Barriers: Air seal materials to adjacent insulation.

    - Section 07480 - Exterior Wall Assemblies: Exterior Insulated Finish Systems EIFS.

    - Section 07810 -  Fire and Smoke Protection: Insulation installed in conjunction with firestopping or smoke containment systems.

    - Section 09200 -  Plaster and Gypsum Board: Insulation installed in conjunction with interior wall and ceiling finish systems.

    - Section 15810 -  Ducts: Insulation to surround HVAC ductwork.

  - REFERENCES

** NOTE TO SPECIFIER **  Delete references from the list below that are not actually required by the text of the edited section.

    - ASTM C 423 - Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

    - ASTM C 518 - Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus.

    - ASTM C 553 - Standard Specification for Mineral Fiber Blanket Thermal Insulation for Commercial and Industrial Applications.

    - ASTM C 612 - Standard Specification for Mineral Fiber Block and Board Thermal Insulation.

    - ASTM C 665 - Standard Specification for Mineral-Fiber Blanket Thermal Insulation for Light Frame Construction and Manufactured Housing.

    - ASTM C 764 - Standard. Specification for Mineral Fiber. Loose-Fill Thermal Insulation.

    - ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

    - ASTM E 96 - Standard Test Methods for Water Vapor Transmission of Materials.

    - ASTM E 119 - Standard Test Methods for Fire Tests of Building Construction and Materials.

    - ASTM E 136 - Standard Test Method for Behavior of Materials in a Vertical Tube Furnace at 750 Degrees C.

    - ASTM E 814 - Standard Test Method for Fire Tests of Through-Penetration Fire Stops.

    - Federal Specification HH-I-521F: Insulation Blankets, Thermal (Mineral Fiber, For Ambient Temperatures).

    - Federal Specification HH-I-558B: Insulation, Blocks, Blankets, Felts, Sleeving (Pipe and Tube Covering), and Pipe fitting Covering, Thermal (Mineral Fiber, Industrial Type)

    - National Fire Protection Association (NFPA) Life Safety Code

    - Underwriters Laboratories (UL) - UL 2079 Standard test method for fire resistance of Building Joint Systems.

  - SUBMITTALS

    - Submit under provisions of Section 01300.

    - Product Data:  Manufacturer's data sheets on each product to be used, including:

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Installation methods.

    - Manufacturer's Certificates: Certify products meet or exceed specified requirements.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Manufacturer with a minimum of ten years experience manufacturing products in this section shall provide all products listed.

    - Installer Qualifications: Products listed in this section shall be installed by a single organization with at least five years’ experience successfully installing insulation on projects of similar type and scope as specified in this section.

** NOTE TO SPECIFIER **  Include a mock-up if the project size and/or quality warrant taking such a precaution.  The following is one example of how a mock-up on a large project might be specified.  When deciding on the extent of the mock-up, consider all the major different types of work on the project.

    - Mock-Up:  Provide a mock-up for evaluation of surface preparation techniques and application workmanship.

      - Finish areas designated by Architect.

      - Do not proceed with remaining work until workmanship is approved by Architect.

      - Refinish mock-up area as required to produce acceptable work.

  - DELIVERY, STORAGE, AND HANDLING

    - Deliver and store products in manufacturer's unopened packaging bearing the brand name and manufacturer's identification until ready for installation.

    - Storage: Store materials in dry locations with adequate ventilation, free from water, and in such a manner to permit easy access for inspection and handling.

    - Handling: Handle materials to avoid damage.

  - SEQUENCING

    - Coordinate with the installation of vapor retarders and air seal materials specified is Section 07260 and Section 07270.

    - Ensure that products of this section are supplied to affected trades in time to prevent interruption of construction progress.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: CertainTeed Corp., Insulation Group, which is located at: 20 Moores Road, Malvern, PA 19355; Toll Free Tel: 800-233-8990; Email: request info; Web: certainteed.com/CertainTeed/Pro/Design+Professional/Insulation

** NOTE TO SPECIFIER **  Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions:	Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01600.

  - APPLICATIONS

** NOTE TO SPECIFIER ** The following is an example of how to specify different types of insulation for different applications. If the insulation types, R-values, and/or thicknesses are clearly indicated on the Drawings, this series of paragraphs is not required. 
 
 If used, determine which applications are necessary and add any other applications needed that are not identified. Where applicable, specify product thicknesses and width dimensions so insulation completely fills wall cavities to meet thermal and acoustical performance specifications. Specify type of vapor retarder facing to meet water vapor transmission and fire rating required.
 
 Review the insulation types specified and determine which type(s) should be used for each application. If required, add the names of the types specified to the applications specified below. Insert R-values if thicknesses are not indicated on the Drawings.

    - Exterior Stud Walls: Batt type.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs.

      - Thickness: As indicated on the Drawings.

      - Thickness: _____.

      - R-Value: ______.

** NOTE TO SPECIFIER ** Delete two of the following three paragraphs.

      - Vapor Retarder: Separate.

    - Above Soffits: Batt type.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs.

      - Thickness: As indicated on the Drawings.

      - Thickness: _____.

      - R-Value: ______.

    - Interior Partitions Indicated with STC Rating: Batt type.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs.

      - Thickness: As indicated on the Drawings.

      - Thickness: _____.

    - Above Interior Ceilings: Batt type.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs.

      - Thickness: As indicated on the Drawings.

      - Thickness: _____.

** NOTE TO SPECIFIER **  The following major paragraphs contain various insulation types including Batt and Roll Insulation, Blowing Insulation, Board Insulation, Blanket Insulation and Vapor Retarders. These products are intended for use in either residential or commercial construction. Select the products required from the following paragraphs and delete those not required. Coordinate with the Drawings and/or the applications paragraph above.

  - BATT AND ROLL INSULATION (SECTION 07 21 00)

** NOTE TO SPECIFIER ** Certainteed High-Density Fiber Glass Building Insulation is intended for use in walls, ceilings, floors and attics where maximum thermal performance is desired and limited space is available.

** NOTE TO SPECIFIER ** Certainteed Fiber Glass Building Insulation is intended for use in either residential or commercial construction as thermal and acoustical insulation in ceilings, walls and floors. Available unfaced or kraft-faced and is designed for use in standard wood stud and steel frame assemblies.

    - Thermal Batt Insulation: CertainTeed Fiber Glass Building Insulation and High Density Fiber Glass Building Insulation. Fiber glass building insulation for walls, ceilings, attics and floors. Complies with ASTM C 665; preformed glass fiber batt insulation:

* NOTE TO SPECIFIER **  Select one or both of the following two paragraphs for faced and unfaced batt insulation as required and delete those not required.

      - Facing: ASTM C 665 Type I Unfaced.

        - Fire Hazard Classification: ASTM E 84:

          - Maximum Flame Spread Index; 25.

          - Maximum Smoke Developed Index; 50.

        - Noncombustibility: ASTM E 136, passes.

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for thermal resistance and facing as required and delete those not required.

        - Thermal Resistance: R of 5.8 (RSI 1.0).

          - Thickness: 1-1/2 inches (38 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 11 (RSI 1.9).

          - Thickness: 3-1/2 inches (89 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 11-1/4 inches (286 mm).

          - Width: 15 inches (381 mm).

          - Width: 15-1/4 inches (387 mm).

          - Width: 19-1/4 inches (489 mm).

          - Width: 23 inches (584 mm).

          - Width: 23-1/4 inches (591 mm).

          - Width: 48 inches (1219 mm).

          - Width: 84 inches (2134 mm).

        - Thermal Resistance: R of 13 (RSI 2.3).

          - Thickness: 3-1/2 inches (89 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15-1/4 inches (387 mm).

          - Width: 16 inches (406 mm).

          - Width:  19-1/4 inches (489 mm).

          - Width: 23-1/4 inches (591 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 15 (RSI 2.6).

          - Thickness: 3-1/2 inches (89 mm).

          - Width:  11-1/4 inches (286 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15-1/4 inches (387 mm).

          - Width:  16 inches (406 mm).

          - Width: 23-1/4 inches (591 mm).

          - Width:  24 inches (610 mm).

        - Thermal Resistance: R of 19 (RSI 3.3).

          - Thickness: 6-1/4 inches (159 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 11-1/4 inches (286 mm).

          - Width: 15 inches (381 mm).

          - Width: 15-1/4 inches (387 mm).

          - Width: 16 inches (406 mm).

          - Width: 19-1/4 inches (489 mm).

          - Width: 23 inches (584 mm).

          - Width: 23-1/4 inches (591 mm).

          - Width: 24 inches (610 mm).

          - Width: 30 inches (762 mm).

          - Width: 48 inches (1219 mm).

          - Width: 60 inches (555 mm).

          - Width: 72 inches (1829 mm).

        - Thermal Resistance:  R of 20 (RSI 3.5)

          - Thickness: 5-1/2 inches (140 mm) & 6 inches (152 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15 inches (381 mm).

          - Width: 15-1/4 inches (387 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 21 (RSI 3.7).

          - Thickness: 5-1/2 inches (140 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15-1/4 inches (387 mm).

          - Width:  16 inches (406 mm).

          - Width: 23-1/4 inches (591 mm).

          - Width:  24 inches (610 mm).

        - Thermal Resistance:  R of 22 (RSI 3.8)

          - Thickness: 6-1/4 inches (159 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15 inches (381 mm).

          - Width: 16 inches (406 mm).

          - Width: 19-1/4 inches (489 mm).

          - Width: 23 inches (584 mm).

        - Thermal Resistance: R of 25 (RSI 4.4).

          - Thickness: 8 inches (203 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15 inches (381 mm).

          - Width: 16 inches (406 mm).

          - Width: 23 inches (584 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 30 (RSI 5.3).

          - Thickness: 10 inches (254 mm) and 9-1/2 inches (241 mm).

          - Width:  12 inches (305 mm).

          - Width:  15 inches (381 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 16 inches (406 mm).

          - Width: 19-1/4 inches (489 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 30C (RSI 5.3). Cathedral Ceiling Batt.

          - Thickness: 8-1/4 inches (210 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15-1/4 inches (387 mm).

          - Width:  16 inches (406 mm).

          - Width: 23-1/4 inches (591 mm).

        - Thermal Resistance: R of 38 (RSI 6.7).

          - Thickness: 12 inches (305 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 16 inches (406 mm).

          - Width:  19-1/4 inches (489 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 38C (RSI 6.7). Cathedral Ceiling Batt.

          - Thickness: 10-1/4 inches (260 mm).

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

          - Width: 15-1/4 inches (387 mm).

          - Width:  16 inches (406 mm)

          - Width:  19-1/4 inches (489 mm).

          - Width: 23-1/4 inches (591 mm).

** NOTE TO SPECIFIER ** Certainteed SpeedyR™ Tabless Batts are intended for use in either residential or commercial construction as thermal and acoustical insulation in walls. These batts are designed for use in standard width wood framed construction where a vapor retarder is needed. The batts have kraft-paper facing without flanges and can be friction-fit between wall studs for non-exposed applications.

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for width required and delete those not required.

** NOTE TO SPECIFIER ** Certainteed Basement Wall and Masonry Wall Building Insulation. Basement Wall is designed for use in semi-finished or unfinished residential and commercial basement areas. The product is available either with a white reinforced polypropylene facing or a reinforced foil facing, both of which can be left exposed and are perforated. Masonry Wall Insulation is designed as unfaced fiber glass insulation for use behind paneling or in masonry type construction where cavity depth is limited. No stapling is required because the batts fit tightly between furring strips.

    - Acoustical/Thermal Insulation, Unfaced: Certainteed Sound Attenuation NoiseReducer Batts. Fiber glass building insulation for friction fit between steel studs. Complies with ASTM C 665; preformed glass fiber batt insulation. Fire Hazard Classification ASTM E84, Maximum Flame Spread Index of 25, Maximum Smoke Developed Index of 50, Noncombustable ASTM E 136, passes:

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for thermal resistance as required and delete those not required.

      - Facing: ASTM C 665, Type 1, Unfaced.

        - Thermal Resistance: R of 8 (RSI 1.4).

          - Thickness: 2-12 inches (64 mm).

          - Width: 16 inches (406 mm).

        - Thermal Resistance: R of 8 (RSI 1.4).

          - Thickness: 2-12 inches (64 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 11 (RSI 1.9).

          - Thickness: 3-12 inches (89 mm).

          - Width: 16 inches (406 mm).

        - Thermal Resistance: R of 11 (RSI 1.9).

          - Thickness: 3-12 inches (89 mm).

          - Width: 24 inches (610 mm).

** NOTE TO SPECIFIER ** Certainteed NoiseReducer™ Acoustical Ceiling Batts is intended for use in either residential or commercial construction to effectively reduce transmission of airborne sound and provide thermal insulation. Acoustic ceiling batts are available unfaced and faced for installation on suspended ceilings.

    - Acoustical/Thermal Insulation: Certainteed Acoustical Ceiling NoiseReducer Batts. Fiber glass acoustical insulation for ceilings. Complies with ASTM C 665; preformed glass fiber batt insulation:

      - Facing: ASTM C 665, Type 1, Unfaced.

        - Fire Hazard Classification: ASTM E 84:

          - Maximum Flame Spread Index; 25.

          - Maximum Smoke Developed Index; 50.

        - Noncombustibility: ASTM E 136, passes.

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for thermal resistance as required and delete those not required.

        - Thermal Resistance: R of 11 (RSI 1.9).

          - Thickness: 3-12 inches (89 mm).

          - Width: 24 inches (610 mm).

        - Thermal Resistance: R of 19 (RSI 3.3).

          - Thickness: 6-14 inches (159 mm).

          - Width: 24 inches (610 mm).

** NOTE TO SPECIFIER ** Certainteed NoiseReducer™ Sound Attenuation Batts are intended for use in either residential or commercial construction to effectively reduce transmission of airborne sound and provide thermal insulation. Faced batts are intended for friction fit between interior wood studs.

** NOTE TO SPECIFIER ** Certainteed CertaPro™ AcoustaTherm™ Batts are intended for use in commercial construction to enhance acoustical and thermal performance in exterior and interior walls and improve sound transmission loss over suspended ceilings.

    - Acoustical/Thermal Batt Insulation, Certainteed CertaPro Batts. Complies with ASTM C 665; preformed glass fiber batt insulation.

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for faced or unfaced as required and delete those not required.

      - Unfaced: ASTM C 665, Type 1,.

        - Fire Hazard Classification: ASTM E 84:

          - Maximum Flame Spread Index; 5.

          - Maximum Smoke Developed Index; 5.

        - Noncombustibility: ASTM E 136, passes.

        - Sizes:

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for thermal resistance as required and delete those not required.

          - Thermal Resistance: R of 8 (RSI 1.41).

            - Thickness: 2-12 inches (64 mm).

** NOTE TO SPECIFIER **  Select one of the following width paragraphs for size required and delete the one not required.

            - Width: 16 inches (406 mm).

            - Width: 24 inches (610 mm).

          - Thermal Resistance: R of 11 (RSI 1.94).

            - Thickness: 3-12 inches (89 mm).

** NOTE TO SPECIFIER **  Select one of the following width paragraphs for size required and delete the one not required.

            - Width: 16 inches (406 mm).

            - Width: 24 inches (610 mm).

          - Thermal Resistance: R of 19 (RSI 3.35).

            - Thickness: 6-1/4 inches (159 mm).

** NOTE TO SPECIFIER **  Select one of the following width paragraphs for size required and delete the one not required.

            - Width: 16 inches (406 mm).

            - Width: 24 inches (610 mm).

          - Thermal Resistance: R of 30 (RSI 5.28).

            - Thickness: 10 inches (254 mm).

            - Width: 24 inches (610 mm).

** NOTE TO SPECIFIER ** Certainteed CertaPro™ Partition Batts are intended for use in commercial construction to enhance acoustical and thermal performance in shaft and partition walls.

    - Acoustical/Thermal Unfaced Batt Insulation, Certainteed CertaPro Partition Batts. Complies with ASTM C 665; preformed glass fiber batt insulation.

      - Unfaced: ASTM C 665, Type 1,.

        - Fire Hazard Classification: ASTM E 84:

          - Maximum Flame Spread Index; 5.

          - Maximum Smoke Developed Index; 5.

        - Noncombustibility: ASTM E 136, passes.

        - Size:

          - Thermal Resistance: R of 5.8 (RSI 1.02).

            - Thickness: 1-1/2 inches (38 mm).

            - Width: 24 inches (610 mm).

** NOTE TO SPECIFIER ** Certainteed CertaPro™ Thermal Kraft Faced Batts are light density batts intended for use in commercial construction to enhance thermal and acoustical performance in exterior and interior walls and floor/ceiling assemblies where a vapor retarders are required..

** NOTE TO SPECIFIER ** Certainteed CertaPro™ Thermal Extended Flange Batts are intended for use in commercial construction for use in exposed wood framing, below panel deck roof systems and other special construction where a 25 Flame Spread Rating for exposed applications is required.

** NOTE TO SPECIFIER ** Certainteed CertaPro™ Thermal Foil Faced Batts are light density batts intended for use in commercial construction to enhance thermal performance in non-exposed exterior walls and floor/ceiling assemblies where a vapor retarder is  required.

** NOTE TO SPECIFIER ** Certainteed THERMAFIBER® Sound Attenuation Fire Blankets (SAFB) are intended for use in multi-family residential projects, hotels and motels, offices, retail businesses and other commercial construction. Thermofiber provides high acoustical performance with high fire ratings in walls and floor/ceiling assemblies.

** NOTE TO SPECIFIER ** Certainteed THERMAFIBER® Safing™ Insulation is intended for 
 Firestopping curtain wall fire and smoke containment systems, floor and wall penetrations, and head-of-wall construction joints in multi-family residential projects, hotels and motels, offices, retail businesses and other commercial construction.

** NOTE TO SPECIFIER **  Safing insulation is available in three densities. Select one or more of the following density paragraphs as required and delete those not required.

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for thermal blowing insulation as required and delete those not required.

  - BLANKET INSULATION

** NOTE TO SPECIFIER ** Certainteed Commercial Blanket Insulation is intended for use in commercial construction where wide rolls of unfaced insulation are required such as retrofitting a warehouse.

** NOTE TO SPECIFIER **  Select one of the following paragraphs as required and delete those not required.

** NOTE TO SPECIFIER **  Select one of the following paragraphs as required and delete those not required.

** NOTE TO SPECIFIER ** Certainteed Metal Building Insulation is intended for use in commercial construction for metal buildings. Metal Building Insulation is a flexible blanket insulation furnished in rolls and intended to be laminated on one side with a suitable vapor retarder. Metal Building Insulation may be used as an additional layer of insulation over laminated metal building insulation in systems or over the top of BUR or single ply roofs in metal reroof applications to achieve greater thermal performance.

    - Metal Building Insulation, Certainteed Metal Building Insulation. Complies with ASTM C 553, Type I and ASTM 665, Type I Plain. Composed of inorganic glass fibers bonded with a thermoset resin.

      - Fire Hazard Classification: ASTM E 84:

        - Maximum Flame Spread Index; 25.

        - Maximum Smoke Developed Index; 50.

** NOTE TO SPECIFIER **  Select one of the following paragraphs as required and delete those not required.

      - Size:

** NOTE TO SPECIFIER **  Select one of the following paragraphs as required and delete those not required.

        - Thickness: 3-3/8 inches (86 mm).

          - Thermal Resistance: R of 10 (RSI 1.8).

        - Thickness: 3-3/4 inches (94 mm).

          - Thermal Resistance: R of 11 (RSI 1.9).

        - Thickness: 4-3/8 inches (109 mm).

          - Thermal Resistance: R of 13 (RSI 2.3).

        - Thickness: 5-1/4 inches (133.35 mm).

          - Thermal Resistance: R of 16 (RSI 2.8).

        - Thickness: 6-3/8 inches (160 mm).

          - Thermal Resistance: R of 19 (RSI 3.3).

        - Thickness:  6-3/4 inches (152.4 mm).

          - Thermal Resistance:  R of 21 (RSI 3.7)

        - Thickness: 8 inches (203 mm).

          - Thermal Resistance: R of 25 (RSI 4.4).

        - Thickness: 9-1/4 inches (235 mm).

          - Thermal Resistance: R of 30 (RSI 5.3).

        - Width:

** NOTE TO SPECIFIER **  Select one of the following paragraphs as required and delete those not required.

          - 36 inches (914 mm).

          - 48 inches (1219 mm).

          - 60 inches (1524 mm.).

          - 72 inches (1829 mm.).

** NOTE TO SPECIFIER **  MemBrain™ The SMRT Vapor Retarder is for use with unfaced, vapor permeable, mass insulation (fiber glass and mineral wool) in wall and ceiling cavities. MemBrain™ Smart changes its permeability with the ambient humidity condition. This process allows closed building envelope systems to increase their drying potential with seasonal climatic changes.

  - VAPOR RETARDER; SECTION 07 26 00

** NOTE TO SPECIFIER **  Select one or more of the following paragraphs for thermal blowing insulation as required and delete those not required.

    - Sheet Retarder: Certainteed MemBrain, The SMART Vapor Retarder. Polyimide film vapor retarder for use with unfaced, vapor permeable glass fiber and mineral wool insulation in wall and ceiling cavities. Material has a permeance of 1 perm or less when tested to ASTM E 86, dry cup method and increases to greater than 10 perms using the wet cup method.

      - Water Vapor Permeance:

        - ASTM E 86, dry cup method: 1.0 perms (57ng/Pa*s*m2).

        - ASTM E 86, wet cup method: 10.0 perms (1144ng/Pa*s*m2).

      - Fire Hazard Classification: ASTM E 84:

        - Maximum Flame Spread Index; 20.

        - Maximum Smoke Developed Index; 55.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly prepared.

    - Verify that all exterior and interior wall, partition, and floor/ceiling assembly construction has been completed to the point where the insulation may correctly be installed.

    - Verify that mechanical and electrical services in ceilings, walls and floors have been installed and tested and, if appropriate, verify that adjacent materials are dry and ready to receive insulation.

    - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with manufacturer's instructions.

    - Install in exterior spaces without gaps or voids. Do not compress insulation.

    - Trim insulation neatly to fit spaces. Insulate miscellaneous gaps and voids.

    - Fit insulation tight in spaces and tight to exterior side of mechanical and electrical services within plane of insulation.

    - Install insulation with vapor barrier installed facing the warm side. Seal or tape joints as required.

  - PROTECTION

    - Protect installed products until completion of project.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION