Crane Composites, Inc.

23525 W. Eames Street

Channahon, IL 60410-3220

Phone: (888) DECOFRP

Phone: (815) 467-8600

Fax: (815) 467-8666

E-mail: decofrp@kemlite.com

www.frpdesignsolutions.com

This MANU-SPEC® utilizes the Construction Specifications Institute (CSI) Manual of Practice, including MasterFormat™, SectionFormat™ and PageFormat™. A MANU-SPEC is a manufacturer-specific proprietary product specification using the proprietary method of specifying applicable to project specifications and master guide specifications. Optional text is indicated by brackets [ ]; delete optional text in final copy of specification. Specifier Notes typically precede specification text; delete notes in final copy of specification. Trade/brand names with appropriate symbols typically are used in Specifier Notes; symbols are not used in specification text. Metric conversion, where used, is soft metric conversion.

This MANU-SPEC specifies Varietex™ fiberglass reinforced plastic (FRP) panels in sandstone, linen or cedar finish textures, in nine colors, for use as special wall finishes. These products are manufactured by Crane Composites, Inc. (formerly Kemlite Company, Inc.). Revise MANU-SPEC section number and title below to suit project requirements, specification practices and section content. Refer to CSI MasterFormat™ for other section numbers and titles.

SECTION 09 77 00

SPECIAL WALL SURFACING

GENERAL

SUMMARY

Specifier Note: Revise paragraphs below to suit project requirements.

Section Includes: Fiberglass reinforced plastic (FRP) panels with [Sandstone] [Linen] [And] [Cedar] surface texture.

Related Sections:

Section [06 20 00 - Finish Carpentry] [_____].

Section [09 29 00 - Gypsum Board] [_____].

Specifier Note: Article below may be omitted when specifying manufacturer’s proprietary products and recommended installation. Retain References Article when specifying products and installation by an industry reference standard. If retained, list standard(s) referenced in this section. Indicate issuing authority name, acronym, standard designation and title. Establish policy for indicating edition date of standard referenced. Conditions of the Contract or Division 01 References Section may establish the edition date of standards. This article does not require compliance with standard. It is a listing of all references used in this section.

REFERENCES

General: Standards listed by reference, including revisions by issuing authority, form a part of this specification section to the extent indicated. Standards listed are identified by issuing authority, authority abbreviation, designation number, title or other designation established by issuing authority. Standards subsequently referenced herein are referred to by issuing authority abbreviation and standard designation.

ASTM International:

ASTM D256 Standard Test Methods for Determining the Izod Pendulum Impact Resistance of Plastics.

ASTM D570 Standard Test Method for Water Absorption of Plastics.

ASTM D638 Standard Test Method for Tensile Properties of Plastics.

ASTM D696 Standard Test Method for Coefficient of Linear Thermal Expansion of Plastics Between -30 degrees C and 30 degrees C With a Vitreous Silica Dilatometer.

ASTM D790 Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials.

ASTM D2583 Standard Test Method for Indentation Hardness of Rigid Plastics by Means of a Barcol Impressor.

ASTM D5420 Standard Test Method for Impact Resistance of Flat, Rigid Plastic Specimen by Means of a Striker Impacted by a Falling Weight (Gardner Impact).

ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials.

Underwriters’ Laboratories of Canada (ULC):

ULC-S102 Test for Surface Burning Characteristics of Building Materials.

SYSTEM DESCRIPTION

Performance Requirements: Provide fiberglass reinforced plastic (FRP) panels, which have been manufactured and installed to maintain performance criteria stated by manufacturer without defects, damage or failure.

Specifier Note: Article below includes submittal of relevant data to be furnished by Contractor before, during or after construction. Coordinate this article with Architect’s and Contractor’s duties and responsibilities in Conditions of the Contract and Division 01 Submittal Procedures Section.

SUBMITTALS

General: Submit listed submittals in accordance with Conditions of the Contract and Division 01 Submittal Procedures Section.

Product Data: Submit manufacturer’s product data and installation instructions.

Shop Drawings: Submit shop drawings showing layout, profiles and product components, including anchorage, accessories, finish colors, patterns and textures. Indicate location and dimension of joints and fastener attachment.

Samples: Submit selection and verification samples for finishes, colors and textures. Submit 2 samples of each type of panel, trim and fastener.

Quality Assurance/Control Submittals: Submit the following:

Test Reports: Certified test reports showing compliance with specified performance characteristics and physical properties.

Certificates:

Submit manufacturer’s certificate that products meet or exceed specified requirements.

Submit certificate of installer’s qualifications.

Specifier Note: For more information on installation recommendations, visit manufacturer’s website at www.frpdesignsolutions.com.

Manufacturer’s Instructions: Manufacturer’s installation instructions.

Closeout Submittals: Submit the following:

Operations and Maintenance Data: Operation and maintenance data for installed products in accordance with Division 01 Closeout Submittals (Maintenance Data and Operation Data) Section. Include methods for maintaining installed products and precautions against cleaning materials and methods detrimental to finishes and performance.

Warranty documents specified herein.

Specifier Note: Article below should include prerequisites, standards, limitations and criteria that establish an overall level of quality for products and workmanship for this section. Coordinate article below with Division 01 Quality Assurance Section.

QUALITY ASSURANCE

Installer Qualifications: Utilize an installer having demonstrated experience on projects of similar size and complexity.

Specifier Note: Paragraph below should list obligations for compliance with specific code requirements particular to this section. General statements to comply with a particular code are typically addressed in Conditions of the Contract and Division 01 Regulatory Requirements Section. Repetitive statements should be avoided.

Regulatory Requirements and Approvals: [Specify applicable requirements of regulatory agencies.].

Specifier Note: Retain paragraph below if mock-up is required.

Mock-Ups: [Specify requirements for mock-up.].

Subject to acceptance by owner, mock-up may be retained as part of finish work.

If mock-up is not retained, remove and properly dispose of mock-up.

Specifier Note: Retain paragraph below if preinstallation meeting is required.

Preinstallation Meetings: [Specify requirements for meeting.].

Specifier Note: Article below should include special and unique requirements. Coordinate article below with Division 01 Product Requirements Section.

DELIVERY, STORAGE & HANDLING

General: Comply with Division 01 Product Requirements Section.

Lead Time: Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

Delivery: Deliver materials in manufacturer’s original, unopened, undamaged containers with identification labels intact.

Storage and Protection: Store materials protected from exposure to harmful environmental conditions and at temperature and humidity conditions recommended by the manufacturer.

Store panels indoors.

Lay panels flat. Do not stand panels on edge.

Protect panels from moisture.

Do not store panels in contact with the floor or against an outside wall.

Handling: Remove foreign matter from face of panel by using a soft bristle brush, avoiding abrasive action.

Specifier Note: In article below, state physical or environmental limitations or criteria for installation such as weather, temperature, humidity, ventilation or illumination required for proper installation or application.

PROJECT/SITE CONDITIONS

Environmental Requirements:

Installation shall not begin until building is enclosed, permanent heating and cooling equipment is in operation and residual moisture from plaster, concrete or terrazzo work has dissipated.

Install panels between 60 and 75 degrees F (15 and 24 degrees C) and relative humidity below 65%, ideally at the same conditions as the room’s normal operating temperatures after building is occupied.

Provide ventilation to disperse fumes during application of adhesive as recommended by adhesive manufacturer.

Field Measurements: Verify actual measurements/openings by field measurements before fabrication; show recorded measurements on shop drawings. Coordinate field measurements and fabrication schedule with construction progress to avoid construction delays.

Specifier Note: Coordinate article below with Conditions of the Contract and with Division 01 Closeout Submittals (Warranty) Section.

WARRANTY

Project Warranty: Refer to Conditions of the Contract for project warranty provisions.

Manufacturer’s Warranty: Submit, for Owner’s acceptance, manufacturer’s standard warranty document executed by authorized company official. Manufacturer’s warranty is in addition to, and not a limitation of, other rights Owner may have under Contract Documents.

Specifier Note: Coordinate paragraph below with manufacturer’s warranty requirements.

Warranty Period: [Specify term] years commencing on Date of Substantial Completion.

MAINTENANCE

Extra Materials: Provide [A recommended percentage of] [Specify percentage.] additional material for use by owner in building maintenance and repair.

PRODUCTS

Specifier Note: Retain article below for proprietary method specification. Add product attributes, performance characteristics, material standards and descriptions as applicable. Use of such phrases as “or equal” or “or approved equal” or similar phrases may cause ambiguity in specifications. Such phrases require verification (procedural, legal and regulatory) and assignment of responsibility for determining “or equal” products.

DECORATIVE LIGHTLY TEXTURED FIBERGLASS REINFORCED PLASTIC (FRP) PANELS

Specifier Note: Paragraph below is an addition to CSI SectionFormat and a supplement to MANU-SPEC. Retain or delete paragraph below per project requirements and specifier’s practice.

Manufacturer: Crane Composites, Inc. (formerly known as Kemlite Company, Inc.).

Contact: 23525 W. Eames Street, Channahon, IL 60410-3220; Telephone: (888) DECOFRP, (815) 467-8600; Fax: (815) 467-8666; E-mail: decofrp@kemlite.com; website: www.frpdesignsolutions.com.

Specifier Note: Paragraphs below list proprietary fiberglass reinforced plastic (FRP) panel products offered by Crane Composites, Inc. (formerly known as Kemlite Company, Inc.). Varietex panels are available in a variety of surface appearances, including sandstone, linen and cedar. Consult manufacturer regarding product options. Select and retain product characteristics required; delete characteristics not required. Refer to manufacturer’s product data or other publications for more information.

Proprietary Products/Systems: FRP panels, including the following:

VARIETEX CLASS A

Surface Texture: [Sandstone] [Linen] [Cedar].

Thickness: 0.09 inch (2.3 mm).

Weight: 0.73 psf (3.56 kg/m2).

Size: [4 feet × 8 feet (1.2 × 2.4 m)] [4 feet × 10 feet (1.2 × 3 m)].

Specifier Note: Sandstone and Linen texture panels are available in all 9 colors listed in subparagraph below. Cedar texture panels are available only in White Magnolia (488), Almond Breeze (866) and Fawn Brown (809).

Color: [White Magnolia (488)] [Almond Breeze (866)] [Fawn Brown (809)] [Cherry Blossom Pink (703)] [Yellow Sunrise (104)] [Sky Blue (306)] [Willow Green (205)] [Spring Lilac (708)] [Morning Mist Gray (636)].

Physical Properties:

Flexural Strength (ASTM D790): 14 × 103 psi (97 MPa).

Flexural Modulus (ASTM D790): 0.4 × 106 psi (2758 MPa).

Tensile Strength (ASTM D638): 7 × 103 psi (48 MPa).

Tensile Modulus (ASTM D638): 0.8 × 106 psi (5516 MPa).

Barcol Hardness (ASTM D2583): 45.

Izod Impact (ASTM D256): 4 ft lb/in2 (0.21 J/mm).

Gardner Impact (ASTM D5420): 25 in-lb (2.82 J).

Water Absorption (ASTM D570): 0.16% (24 hrs @ 77 degrees F (25 degrees C)), 0.16% (24 hrs @ 25 degrees F (-4 degrees C)).

Surface Burning Characteristics (ASTM E84): Class A.

Coefficient of Linear Thermal Expansion (ASTM D696): 2 × 10-5 in/in°F (36 μm/m °C).

Taber Abrasion Test: 0.036% maximum weight loss when subjected to 25 cycles with 1000g CS17 wheel.

VARIETEX CLASS C

Surface Texture: [Sandstone] [Linen] [Cedar].

Thickness: 0.09 inch (2.3 mm).

Weight: 0.73 psf (3.56 kg/m2).

Size: [4 feet × 8 feet (1.2 × 2.4 m)] [4 feet × 10 feet (1.2 × 3 m)].

Specifier Note: Sandstone and Linen texture panels are available in all 9 colors listed in subparagraph below. Cedar texture panels are available only in White Magnolia (488), Almond Breeze (866) and Fawn Brown (809).

Color: [White Magnolia (488)] [Almond Breeze (866)] [Fawn Brown (809)] [Cherry Blossom Pink (703)] [Yellow Sunrise (104)] [Sky Blue (306)] [Willow Green (205)] [Spring Lilac (708)] [Morning Mist Gray (636)].

Physical Properties:

Flexural Strength (ASTM D790): 10 × 103 psi (69 MPa).

Flexural Modulus (ASTM D790): 0.35 × 106 psi (2413 MPa).

Tensile Strength (ASTM D638): 5 × 103 psi (34 MPa).

Tensile Modulus (ASTM D638): 0.7 × 106 psi (4826 MPa).

Barcol Hardness (ASTM D2583): 45.

Izod Impact (ASTM D256): 4 ft lb/in2 (0.21 J/mm).

Gardner Impact (ASTM D5420): 25 in-lb (2.82 J).

Water Absorption (ASTM D570): 0.16% (24 hrs @ 77 degrees F (25 degrees C)), 0.16% (24 hrs @ 25 degrees F (-4 degrees C)).

Surface Burning Characteristics (ASTM E84): Class C.

Coefficient of Linear Thermal Expansion (ASTM D696): 2 × 10-5 in/in°F (36 μm/m °C).

Taber Abrasion Test: 0.015% maximum weight loss when subjected to 25 cycles with 1000g CS17 wheel.

VARIETEX FOR CANADA

Surface Texture: [Sandstone] [Linen] [Cedar].

Thickness: 0.09 inch (2.3 mm).

Weight: 0.73 psf (3.56 kg/m2).

Size: [4 feet × 8 feet (1.2 × 2.4 m)] [4 feet × 10 feet (1.2 × 3 m)].

Specifier Note: Sandstone and Linen texture panels are available in all 9 colors listed in subparagraph below. Cedar texture panels are available only in White Magnolia (488), Almond Breeze (866) and Fawn Brown (809).

Color: [White Magnolia (488)] [Almond Breeze (866)] [Fawn Brown (809)] [Cherry Blossom Pink (703)] [Yellow Sunrise (104)] [Sky Blue (306)] [Willow Green (205)] [Spring Lilac (708)] [Morning Mist Gray (636)].

Physical Properties:

Flexural Strength (ASTM D790): 14 × 103 psi (97 MPa).

Flexural Modulus (ASTM D790): 0.4 × 106 psi (2758 MPa).

Tensile Strength (ASTM D638): 6 × 103 psi (41 MPa).

Tensile Modulus (ASTM D638): 0.75 × 106 psi (5171 MPa).

Barcol Hardness (ASTM D2583): 45.

Izod Impact (ASTM D256): 4 ft lb/in2 (0.21 J/mm).

Gardner Impact (ASTM D5420): 35 in-lb (3.95 J).

Water Absorption (ASTM D570): 0.17% (24 hrs @ 77 degrees F (25 degrees C)), 0.17% (24 hrs @ 25 degrees F (-4 degrees C)).

Surface Burning Characteristics ([ASTM E84] [CAN/ULC S102]): Flamespread less than or equal to 150. Smoke developed less than or equal to 300.

Coefficient of Linear Thermal Expansion (ASTM D696): 2.2 × 10-5 in/in°F (40 μm/m °C).

Taber Abrasion Test: 0.015% maximum weight loss when subjected to 25 cycles with 1000g CS17 wheel.

Specifier Note: Edit Paragraph below to suit project requirements. If substitutions are permitted, edit text below. Add text to refer to Division 1 Project Requirements (Product Substitutions Procedures) Section.

PRODUCT SUBSTITUTIONS

Substitutions: No substitutions permitted.

Specifier Note: Specify subordinate or secondary items that aid and assist primary products specified above or are necessary for preparation or installation of those items. Specify method of joint seam treatment below under Installation.

ACCESSORIES

Panel Adhesive:

Provide [Adhesive recommended by panel manufacturer] [Insert adhesive.].

Specifier Note: Retain one or both of the 2 paragraphs, and related subparagraphs below to suit project requirements.

Trim Treatment:

Material Type: [Dual durometer with rigid PVC base and flexible PVC top] [Aluminum].

Manufacturer Designation: [Silhouette Trim] [Standard FRP Moldings].

Profile: [Division bar] [Inside corner] [Outside corner] [End cap].

Color: [Match panel.] [Insert color.].

Seam Treatment:

Material Type: Acrylic latex caulk with silicone.

Color: [Match panel.] [Insert color.].

EXECUTION

Specifier Note: Paragraph below is an addition to CSI SectionFormat and a supplement to MANU-SPEC. Revise article below to suit project requirements and specifier’s practice.

MANUFACTURER’S INSTRUCTIONS

Comply with the instructions and recommendations of the FRP panel manufacturer.

Specifier Note: Specify actions to physically determine that conditions are acceptable to receive primary products of the section.

EXAMINATION

Site Verification of Conditions: Verify that substrate conditions, which have been previously installed under other sections, are acceptable for product installation in accordance with manufacturer’s instructions.

Verify that site conditions are acceptable for installation of FRP panels.

Examine back-up surfaces to determine that corners are plumb and straight, surfaces are smooth, uniform, clean and free from foreign matter, nails are countersunk and joints and cracks are filled flush and smooth with the adjoining surface.

Do not proceed with installation of FRP panels until unacceptable conditions are corrected.

PREPARATION

General:

Prior to installing panels, remove packaging and allow panels to acclimate to room temperature and humidity for at least 48 hours.

Wall substrate must be dry and free from dirt, dust, grease and other contaminants.

Walls must be flat and even. Remove high spots and fill low spots with material acceptable to panel manufacturer.

Remove wallpaper, soluble or loose paint and other foreign matter that might interfere with proper adhesive bond.

Specifier Note: Coordinate article below with manufacturer’s recommended installation requirements.

INSTALLATION

Specifier Note: For more information on installation recommendations, visit manufacturer’s website at www.frpdesignsolutions.com.

General:

Immediately inspect panels for any defects. Do not install panels of unacceptable quality.

Do not install panels directly over stud framing or furring.

When cutting panels, position them so that the saw blade enters the finished HPL side first to avoid chipping or damage.

Protect decorative face of panel by covering work area.

Follow adhesive manufacturer’s recommendations for appropriate height of adhesive bead left by trowel, and do not allow adhesive to skin over.

Joint Seam Treatment: Install panels using the following method.

[Color-matched acrylic latex caulk].

[Silhouette trim].

Installation Using Molding:

Start in the corner. Mark plumb line 48 1/8 inches (1222 mm) from corner. Set first panel true with plumb line. Where several courses of panels are used on a high wall, use both vertical and horizontal lines to ensure alignment.

Install one piece of inside corner molding.

Apply adhesive directly to back of FRP panel with full adhesive coverage using crosshatch pattern. Extend adhesive to within 1/2 inch (12.7 mm) of all edges of panels that will receive moldings.

Slide panel into molding. [Withdraw 1/8 inch (3.2 mm) from vinyl molding to provide appropriate gap.] [Withdraw 1/16 inch (1.6 mm) from aluminum molding to provide appropriate gap.] [Install panel to contact Silhouette Trim and do not withdraw to provide gap.] Align with plumb line.

Begin in top corner nearest molding with laminate roller, rolling down and out toward the edge without molding.

Continue rolling down and out working across panel away from previously installed panel or initial molding. Remove all trapped air.

Install one-piece division bar and caps or next molding by sliding onto panel.

Repeat process, working in one direction around room.

Immediately remove all adhesive residue. To remove, clean with nonabrasive cotton cloth and warm water. If necessary, use a mild nonabrasive detergent. For cleanup with solvent based adhesives, use mineral spirits or acetone to remove residue.

Installation Using Caulk:

Install corner moldings as described in manufacturer’s molding instructions.

Plan panel layout so seams are not directly over seams of substrate.

Apply adhesive directly to back of FRP panel with full adhesive coverage using crosshatch pattern. Extend adhesive to all edges of panel.

Install panel. Place six-penny finishing nails against the installed panel about 2 feet (610 mm) on centers to hold panels in place while adhesive sets and to provide proper spacing for color caulk. Continue installing panels using this method, leaving nails in place during installation.

Remove nails after adhesive sets.

Place a narrow piece of masking tape along panel edge from top to bottom, exactly at joint edge. Firmly apply tape to both panels.

Fill 1/8 inch (3.2 mm) gap between the panels with caulk, making sure gap is completely filled.

Tilt caulk tube back from vertical so that tip of tube advances first in direction of travel.

Wet finger and smooth bead if necessary.

Remove masking tape before bead cures. Clean off excess adhesive with damp cloth.

Specifier Note: Specify the final actions required to clean installed equipment or other completed work to properly function or perform. Coordinate article below with Division 1 Execution Requirements (Cleaning) Section.

CLEANING

Clean panel surfaces in compliance with manufacturer’s recommendations.

Use a clean, damp, nonabrasive cotton cloth and a mild liquid detergent or household cleaner.

Rinse with clean water using a clean, nonabrasive cotton cloth.

Dry panels with a soft, clean nonabrasive cotton cloth.

Do not use cleaners containing acid, alkali or sodium hypochlorite.

Specifier Note: Specify provisions for protecting work after installation but prior to acceptance by the owner. Coordinate article below with Division 1 Execution Requirements Section.

PROTECTION

Protect installed work from damage due to subsequent construction activity on the site.

Specifier Note: Retain, edit or delete article below to suit project and specifier practice. If retained, indicate item, element, product or equipment and its location. Provide other coordinating data.

SCHEDULES

[Specify panel schedule.].

END OF SECTION