SECTION 03300

Concrete Floor Joint Filler, Crack and Joint Repair

# PART 1 - GENERAL

1.1       General Description of Work

- Provide all labor, products and equipment required to properly install semi-rigid filler in interior concrete floor slab joints and repair surface defects.

## 1.2	SUMMARY

### A.	Section Includes:

#### 1.	Joint filler.

#### 2.	Joint edge spall repair.

#### 3.	Crack Repair.

#### 4. 	Surface defect repair, including pop-outs, chips, spalls and pitting.

### B.	Related Sections include the following:

#### 1.	Division 3 Section "Cast-in-Place Concrete Floor Slab" for  new floor installations.

#### 2.	Division 3 Section "Concrete Shrinkage Control Joints and Fillers" for new floor installations.

#### 3.	Division 3 Section "Concrete Slab Patching And Repair" for minor concrete work in remodel projects.

1.3        APPLICABLE STANDARDS

- Products and installation shall be in compliance or exceed the joint filling criteria established in the latest ACI  302.1R Guide for Concrete Floor and Slab Repair.

## 1.4	DEFINITIONS

### A.	Floor Slab Joints: Joints deliberately created in regular, grid pattern intervals during construction.

#### 1.	Construction Joints and Closure Strip Joints:  Formed joints between adjacent slab panels, where panels are separate concrete pours.

#### 2.	Shrinkage Joints:  Also called control or contraction joints, are saw-cut after slab troweling to control slab breaks caused by concrete shrinkage, and keep cracks in straight lines under the saw-cuts.

### B.	Cracks in Floor Slab: Random, uncontrolled breaks in the floor slab.

#### 1.	Shrinkage Cracks: Cracks that are the result of overall concrete shrinking beyond the capacity of the construction joints to contain.

#### Slab Curl Cracks: Caused by concrete shrinking faster at the slab top than the bottom, with resulting curl at pour edges, breaking may be from wheeled vehicle impact.

### C. 	Slab Spalls: Locations where slab surface has delaminated, chipped or broken off, exposing aggregate in the mix.

## 1.5	CONTRACTOR QUALIFICATIONS

### Installer shall have a minimum of three (3) years experience in performing the types of work covered by this Section and shall be a Certified Applicator of the material manufacturer.

### Certified Applicator shall use tools and equipment specifically designed for the preparation and placement of industrial joint fillers and concrete crack and defect repair.

## 1.6	SUBMITTALS

- Joint Filler, Crack and Defect Repair Materials:  Comply with section 01330 – Submittal procedures.

- Product data: Submit manufacturer’s product data, including proper procedures and installation methods as required by the specified product manufacturers.

- Product data for all products and primary equipment used for repair of existing concrete slab defects.

## 1.7	DELIVERY, STORAGE, AND HANDLING

### A.	Deliver materials to project site in manufacturer's original and unopened containers, labeled with type and name of products and manufacturers.

### B.	Comply with manufacturer's written instructions for minimum and maximum temperature requirements and other conditions for storage.

# PART 2 - PRODUCTS

## 2.1	MATERIALS

### A.    Available Products:  Subject to compliance with requirements, utilize products distributed by  Curecrete Distribution, Inc., 1203 W. Spring Creek Place, Springville, UT 84663  800-998-5664

#### B.  Polyurea joint filler: “CreteFill Pro 85MI Control Joint Filler”

### Rapid setting two-component polyurea elastomer joint filler with the physical properties listed below.

    - Shore “A” hardness ASTM D-2240  		85-87 A

    - Viscosity (mixed) 				Self Leveling

    - Mix Ratio (by volume) 				1:1

    - Initial Cure 						15 minutes

    - Tack Free (thin film)@ 77°F 			  3 minutes

    - Final Cure						60 minutes

    - Tensile Strength, psi ASTM D-412  	             960 minimum

    - 100% Solids acceptable for use in USDA applications

    - Contains no VOC’s

C.   Surface defects, spall repair: “CreteFill Spall Repair” Low viscosity rigid Urethane with the physical properties listed below.

1.   Viscosity (Mixed)		250 cps

2.   Hardness, durometer (ASTM D2240)	57- 62

3.   Tensile Strength, PSI (ASTM D412)	4600

4.   Tear Strength (ASTM D624)	-lb/mil 489

5.    Elongation % (AST D412)	6% to 8%

6.    Compressive Strength (neat)	3900 psi

(ASTM C109)  (With Sand)	4950 psi

7.    Bond Strength (ASTM 882-99)	3450 psi

8.    Contains no VOC’s

- Crack Repair  “CreteFill Crack Repair EZ Shave”  Extremely low viscosity modified polymer repair material with the physical properties listed below.

- Viscosity (Mixed)		100-130 cps

- Hardness, durometer (ASTM D2240)	50 D

- Tensile Strength, PSI (ASTM D412)	4900

- Elongation % (AST D412)	10% to 12%

- Compressive Strength (neat)	4100 psi

(ASTM C109)  (With Sand)	3000 psi

- Bond Strength (ASTM 882-99)	4000 psi

- Low odor

- No joint filler or crack repair material substitutions are allowed unless substituted products meet the above referenced physical properties.

# PART 3 - EXECUTION

  - Project Conditions

- Work area should be free of obstructions and other trades.

- Surface and control joints must be clean and dry.

  - Examination of Joint Conditions

- The installer shall inspect the project and joint conditions and notify on-site management in writing of any deficiencies that might adversely affect the quality or durability of the work performed.

- Work shall commence upon acceptance of joint and project conditions.

  - Joint Preparation

A.   See manufacturer’s instructions for all joint preparation.

3.4 	Joint Filler/CRACK AND SPALL Installation

- Installation of CreteFill Pro 85MI Polyurea Joint Filler shall be per manufacturer’s instructions.

  - A.   Installation of CreteFill Spall Repair and CreteFill Crack Repair shall be per manufacturer’s

comprehensive installation instructions.

END OF SECTION 03300