DISCLAIMER: The manufacturer has reviewed the product information contained in this short form specification. The information is organized and presented to assist the specification writer working on a construction project to select the appropriate products and to save time in writing the project specification Section. The specification writer is responsible for product selection as well as the use and application of this information, and should contact the manufacturer to ensure that all options are available and that the associated specification information is valid and correct.

SPEC NOTE: Insert the required paragraphs into the Section under the noted Articles, and make any required selections. Where selection is indicated with an [OR] statement, select the appropriate paragraph and delete the inappropriate statement. Delete all SPEC NOTEs and [OR] statements prior to final printing.

*01 4100: CONTINUOUS ENVELOPE AIR SEALING*

*PART 1 GENERAL*

*1.01 SECTION INCLUDES*

*A. Administrative and procedural requirements to create an airtight building enclosure that controls infiltration / exfiltration of air.*

1. *The Prime Contractor shall ensure that the continuous air barrier around the building enclosure is achieved with the following characteristics:*
   1. *It must be continuous, with all joints, penetrations, and air paths sealed.*
   2. *It must be structurally supported.*
   3. *It must be connected and continuous between foundation & walls, walls & windows/doors, different wall systems, wall & roof.*

*1.02 RESPONSIBILITIES*

*A. Prime Contractor Responsibilities: Unless otherwise indicated, the Prime Contractor shall provide coordination of the trades, and the sequence of construction to ensure continuity of the air barrier system joints, junctures and transitions between materials and assemblies of materials and products, from substructure to walls to roof.*

*PART 2 – PRODUCTS – [not used]*

*PART 3 – EXECUTION – [not used]*

*END OF SECTION*

SECTION 07 2100

THERMAL INSULATION

PART 1 GENERAL

1.01 SECTION INCLUDES

A. Styrofoam™ Brand Extruded Polystyrene Board insulation.

1.02 REFERENCE STANDARDS

A. ASTM C272 - Standard Test Method for Water Absorption of Core Materials for Sandwich Constructions; 2018.

B. [ASTM C578](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C578) - Standard Specification for Rigid, Cellular Polystyrene Thermal Insulation; 2016.

C. [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84) - Standard Test Method for Surface Burning Characteristics of Building Materials; 2016.

1.03 SUBMITTALS

A. See Section 01 3000 - Administrative Requirements, for submittal procedures.

B. Product Data: Provide data on product characteristics, performance criteria, and product limitations.

C. Warranty: Provide Manufacturer's Limited Thermal Warranty for extruded polystyrene insulation.

1.04 QUALITY ASSURANCE

A. Source Limitations: Obtain exterior building insulation through one source from a single manufacturer.

1.05 FIELD CONDITIONS

A. Application Temperatures: Comply with Manufacturer's recommendations for product applications.

PART 2 PRODUCTS

2.01 APPLICATIONS

A. Insulation at Below Grade Walls: Extruded polystyrene board.

2.02 FOAM BOARD INSULATION MATERIALS

A. Extruded Polystyrene Board Insulation: Extruded polystyrene board; ASTM C578; with either natural skin or cut cell surfaces, and the following characteristics:

1. Basis of Design:
2. DuPont de Nemours Inc.; **DuPont™ Styrofoam™ Brand Square Edge Insulation\*** [OR] **DuPont™ Styrofoam™ Brand Scoreboard XPS Foam Insulation\***;  
   building.dupont.com
3. Type: [ASTM C578](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C578), Type IV - 25 PSI.
4. Flame Spread Index (FSI): Class A - 0 to 25, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
5. Smoke Developed Index (SDI): 450 or less, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
6. R-value (RSI-value); 1 inch (25 mm) of material at 72 degrees F (22 C): 5 (0.88), minimum.
7. Panel Size: [Thickness in inches] thick by 48" wide by 96" long.
8. Board Edges: Square.
9. Recycled Content: Average of 20% pre-consumer certified by UL Environment Inc.
10. Sustainability: Third party listed Environmental Product Declaration certificate.
11. Water Absorption: ASTM C272, 0.1% max, by volume.

**[OR]**

B. Extruded Polystyrene Board Insulation: Extruded polystyrene board; ASTM C578; with either natural skin or cut cell surfaces, and the following characteristics:

1. Basis of Design:
   1. DuPont de Nemours Inc.; **DuPont™ Styrofoam™ Brand Perimate™ Extruded Polystyrene Insulation\***: building.dupont.com
2. Type: [ASTM C578](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C578), Type IV - 25 PSI.
3. Flame Spread Index (FSI): Class A - 0 to 25, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
4. Smoke Developed Index (SDI): 450 or less, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
5. R-value (RSI-value); 1 inch (25 mm) of material at 72 degrees F (22 C): 5 (0.88), minimum.
6. Drainage Capacity: 3.0 gal/min/ft based on ASTM D4716 @ 1200 psf, gradient 0.19.
7. Panel Size: 1.063” **[OR]** 2.125” thick by 24" wide by 96" long.
8. Board Edges: Shiplap on long edges.
9. Drainage Channels: Dovetail shape channels running in long direction on one face of board.
10. Recycled Content: Average of 20% pre-consumer certified by UL Environment Inc.
11. Sustainability: Third party listed Environmental Product Declaration certificate.
12. Water Absorption: ASTM C272, 0.1% max, by volume.

**[OR]**

C. Extruded Polystyrene Board Insulation: Extruded polystyrene board; ASTM C578; with either natural skin or cut cell surfaces, and the following characteristics:

1. Basis of Design:
   1. DuPont de Nemours Inc.; **DuPont™ Styrofoam™ Brand Highload 40 Extruded Polystyrene Insulation\***; building.dupont.com
2. Type: [ASTM C578](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C578), Type VI - 40 PSI.
3. Flame Spread Index (FSI): Class A - 0 to 25, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
4. Smoke Developed Index (SDI): 450 or less, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
5. R-value (RSI-value); 1 inch (25 mm) of material at 72 degrees F (22 C): 5 (0.88), minimum.
6. Panel Size: [Thickness in inches] thick by 24" wide by 96" long.
7. Board Edges: Square.
8. Recycled Content: Average of 20% pre-consumer certified by UL Environment Inc.
9. Sustainability: Third party listed Environmental Product Declaration certificate.
10. Water Absorption: ASTM C272, 0.1% max, by volume.

**[OR]**

D. Extruded Polystyrene Board Insulation: Extruded polystyrene board; ASTM C578; with either natural skin or cut cell surfaces, and the following characteristics:

1. Basis of Design:
   1. DuPont de Nemours Inc.; **DuPont™ Styrofoam™ Brand Highload 60 Extruded Polystyrene Insulation\***; building.dupont.com
2. Type: [ASTM C578](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C578), Type VII - 60 PSI.
3. Flame Spread Index (FSI): Class A - 0 to 25, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
4. Smoke Developed Index (SDI): 450 or less, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
5. R-value (RSI-value); 1 inch (25 mm) of material at 72 degrees F (22 C): 5 (0.88), minimum.
6. Panel Size: [Thickness in inches] thick by 24" wide by 96" long.
7. Board Edges: Square.
8. Recycled Content: Average of 20% pre-consumer certified by UL Environment Inc.
9. Sustainability: Third party listed Environmental Product Declaration certificate.
10. Water Absorption: ASTM C272, 0.1% max, by volume.

**[OR]**

E. Extruded Polystyrene Board Insulation: Extruded polystyrene board; ASTM C578; with either natural skin or cut cell surfaces, and the following characteristics:

1. Basis of Design:
   1. DuPont de Nemours Inc.; **DuPont™ Styrofoam™ Brand Highload 100 Extruded Polystyrene Insulation\***; building.dupont.com
2. Type: [ASTM C578](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C578), Type V - 100 PSI.
3. Flame Spread Index (FSI): Class A - 0 to 25, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
4. Smoke Developed Index (SDI): 450 or less, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).
5. R-value (RSI-value); 1 inch (25 mm) of material at 72 degrees F (22 C): 5 (0.88), minimum.
6. Panel Size: [Thickness in inches] thick by 24" wide by 96" long.
7. Board Edges: Square.
8. Recycled Content: Average of 20% pre-consumer certified by UL Environment Inc.
9. Sustainability: Third party listed Environmental Product Declaration certificate.
10. Water Absorption: ASTM C272, 0.1% max, by volume.

2.03 ACCESSRIES

A. Board Insulation Bonding Adhesive: Provide product as recommended by insulation manufacturer that will not damage insulation or substrates.

PART 3 EXECUTION

3.01 EXAMINATION

A. Verify that substrate, adjacent materials, and insulation materials are dry and that substrates are ready to receive insulation.

3.02 BOARD INSTALLATION AT BELOW GRADE WALLS

A. Apply mastic adhesive in six 2” diameter equally spaced daubs on the smooth side of panels to adhere them to the cured waterproofing temporarily until backfill is in place. **[AND / OR]** Mechanically fasten insulation to substrate.

B. Install panels vertically, with long edge flush with a corner.

1. If shiplapped: Each shiplap of panel should overlap previous panel.
2. Cut and fit insulation tightly to protrusions or interruptions to the insulation plane.

C. When additional tiers are required, shiplap edges at both horizontal and vertical joints.

D. Seal off top edge of panels below grade to prevent soil from entry, using a J or Z channel, sheathing tape, or soil fabric.

E. Protect exposed panels above grade from physical damage and ultraviolet exposure with protection panel, flashing, or latex coating.

F. Before Backfilling, completely cover damp-proofed or waterproofed wall with insulation drainage panels.

3.03 FIELD QUALITY CONTROL

A. See Section 01 4000 - Quality Requirements, for additional requirements.

3.04 PROTECTION

A. Do not permit installed insulation to be damaged prior to its concealment.

END OF SECTION

**NOTICE**: No freedom from any patent owned by DuPont or others is to be inferred. Because use conditions and applicable laws may differ from one location to another and may change with time, Customer is responsible for determining whether products and the information in this document are appropriate for Customer’s use and for ensuring that Customer’s workplace and disposal practices are in compliance with applicable laws and other government enactments. The product shown in this literature may not be available for sale and/or available in all geographies where DuPont is represented. The claims made may not have been approved for use in all countries or regions. DuPont assumes no obligation or liability for the information in this document. References to “DuPont” or the “Company” mean the DuPont legal entity selling the products to Customer unless otherwise expressly noted. NO EXPRESS WARRANTIES ARE GIVEN EXCEPT FOR ANY APPLICABLE WRITTEN WARRANTIES SPECIFICALLY PROVIDED BY DUPONT. ALL IMPLIED WARRANTIES INCLUDING THOSE OF MERCHANTABILITY AND FITNESS FOR A PARTICULAR PURPOSE ARE EXPRESSLY EXCLUDED.

**DuPont™ Styrofoam™ Brand Spray Polyurethane Foam\*** contains isocyanate, hydrofluorocarbon blowing agent and polyol. Read the instructions and (Material) Safety Data Sheet ((M)SDS) carefully before use. Wear protective clothing (including long sleeves), gloves, goggles and proper respiratory protection. Supplied air or an approved air-purifying respirator equipped with an organic vapor sorbent and a P100 particulate filter is required to maintain exposure levels below ACGIH, OSHA, WEEL or other applicable limits. Provide adequate ventilation. Contents under pressure. Styrofoam™ Brand SPF should be installed by a trained SPF applicator.  
**CAUTION**: When cured, these products are combustible and will burn if exposed to open flame or sparks from high-energy sources. Do not expose to temperatures above 240ºF (116ºC). For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**DuPont™ Great Stuff Pro™ Polyurethane Foam Sealants and Adhesives\*** contain isocyanate and a flammable blowing agent. Read all instructions and (Material) Safety Data Sheet ((M)SDS), carefully before use. Eliminate all sources of ignition before use. Cover all skin. Wear long sleeves, gloves, and safety glasses or goggles. Not for use in aviation, or food/beverage contact, or as structural support in marine applications. Provide adequate ventilation or wear proper respiratory protection. Contents under pressure. Not to be used for filling closed cavities or voids such as behind walls and under tub surrounds.  
**CAUTION**: When cured, these products are combustible and will burn if exposed to open flame or sparks from high-energy sources. Do not expose to temperatures above 240ºF (116ºC). For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.   
  
**DuPont Polyurethane Foam Insulation and Sealant\***  
**CAUTION**: When cured, these products are combustible and will burn if exposed to open flame or sparks from high-energy sources. Do not expose to temperatures above 240ºF (116ºC). For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.  
**CAUTION**: This product is combustible and shall only be used as specified by the local building code with respect to flame spread classification and to the use of a suitable thermal barrier. For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**DuPont™ LiquidArmor™ Flashing and Sealant\***Read the instructions and (Material) Safety Data Sheets ((M)SDS) carefully before use. It is recommended that spray applicators and those working in the spray area wear eye protection. Contact with exposed skin may cause skin discoloration and dryness. Gloves are recommended for prolonged exposures. Ensure adequate ventilation during spray applications.

**DuPont™ ThermaxTM Brand Polyisocyanurate Insulation\*  
CAUTION**: This product is combustible and shall only be used as specified by the local building code with respect to flame spread classification and to the use of a suitable thermal barrier. For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583, or contact your local building inspector. In an emergency, call 1-989-636-4400.

**DuPont™ StyrofoamTM Extruded Polystyrene Foam Insulation\*  
CAUTION**: This product is combustible. Protect from high heat sources. A protective barrier or thermal barrier may be required as specified in the appropriate building code. For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**WARNING**: Rigid foam insulation does not constitute a working walkable surface or qualify as a fall protection product.

Building and/or construction practices unrelated to building materials could greatly affect moisture and the potential for mold formation. No material supplier including DuPont can give assurance that mold will not develop in any specific system.

\*A former product of The Dow Chemical Company

DuPont™, the DuPont Oval Logo, and all trademarks and service marks denoted with ™, ℠ or ® are owned by affiliates of DuPont de Nemours, Inc. unless otherwise noted. © 2019 DuPont. All rights reserved.

Form No. 43-D100398-enUS