DISCLAIMER: The manufacturer has reviewed the product information contained in this short form specification. The information is organized and presented to assist the specification writer working on a construction project to select the appropriate products and to save time in writing the project specification Section. The specification writer is responsible for product selection as well as the use and application of this information, and should contact the manufacturer to ensure that all options are available and that the associated specification information is valid and correct.

SPEC NOTE: Insert the required paragraphs into the Section under the noted Articles, and make any required selections. Where selection is indicated with an [OR] statement, select the appropriate paragraph and delete the inappropriate statement. Delete all SPEC NOTEs and [OR] statements prior to final printing.

SECTION 07 2100

THERMAL INSULATION

PART 1 GENERAL

1.01 SECTION INCLUDES

A. Thermax™ Brand Polyisocyanurate Board Insulation with FM 4880 Approval.

1.02 REFERENCE STANDARDS

A. [ASTM C1289](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C1289) - Standard Specification for Faced Rigid Cellular Polyisocyanurate Thermal Insulation Board; 2016.

B. [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84) - Standard Test Method for Surface Burning Characteristics of Building Materials; 2016.

C. FM 4880 – Factory Mutual Wall-Ceiling Construction/Roof Construction (25 feet); 2010.

D. UL 1715 or NFPA 286 – Standard Methods of Fire Tests for Evaluating Contribution of Wall and Ceiling Interior Finish to Room Fire Growth; 2015.

1.03 SUBMITTALS

A. See Section 01 3000 - Administrative Requirements, for submittal procedures.

B. Product Data: Provide data on product characteristics, performance criteria, and product limitations.

C. Warranty: Provide Manufacturer's Limited Thermal Warranty for polyisocyanurate insulation.

D. Factory Mutual Compliance: Submit current listing in Factory Mutual Approved Guide (FM 4880).

E. UL 1715 or NFPA 286 Compliance: Submit third party report showing compliance.

1.04 QUALITY ASSURANCE

A. Source Limitations: Obtain building insulation through one source from a single manufacturer.

1.05 FIELD CONDITIONS

A. Application Temperatures: Comply with Manufacturer's recommendations for product applications.

PART 2 PRODUCTS

2.01 APPLICATIONS

A. Insulation Exposed at Interior of Walls: Polyisocyanurate board.

2.02 FOAM BOARD INSULATION MATERIALS

A. Polyisocyanurate Board Insulation with Facers Both Sides: Rigid cellular foam, complying with [ASTM C1289](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C1289); Type I, aluminum foil both faces; Class 2, glass fiber-reinforced core.

1. Basis of Design:

a. DuPont de Nemours Inc.; **DuPont™ Thermax™ Heavy Duty Insulation\***: building.dupont.com/commercial.

2. Flame Spread Index (FSI): Class A - 0 to 25 for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

3. Smoke Developed Index (SDI): 450 or less for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

4. Front Facer: 4.0 mil white embossed aluminum.

5. Back Facer: 1.25 mil embossed aluminum.

6. Board Thickness: \_\_\_\_ inch (\_\_\_\_ mm).

7. Board Edges: Square.

8. Sustainability: Third party listed Environmental Product Declaration certificate.

 **[OR]**

B. Polyisocyanurate Board Insulation with Facers Both Sides: Rigid cellular foam, complying with [ASTM C1289](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C1289); Type I, aluminum foil both faces; Class 2, glass fiber-reinforced core.

1. Basis of Design:

a. DuPont de Nemours Inc.; **DuPont™ Thermax™ Light Duty Insulation\*,**: building.dupont.com/commercial.

2. Flame Spread Index (FSI): Class A - 0 to 25 for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

3. Smoke Developed Index (SDI): 450 or less for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

4. Front Facer: 1.25 mil white embossed aluminum.

5. Back Facer: 1.25 mil embossed aluminum.

6. Board Thickness: \_\_\_\_ inch (\_\_\_\_ mm).

7. Board Edges: Square.

8. Sustainability: Third party listed Environmental Product Declaration certificate.

 **[OR]**

C. Polyisocyanurate Board Insulation with Facers Both Sides: Rigid cellular foam, complying with [ASTM C1289](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C1289); Type I, aluminum foil both faces; Class 2, glass fiber-reinforced core.

1. Basis of Design:

a. DuPont de Nemours Inc.; **DuPont™** **Thermax**™ **Sheathing\***: building.dupont.com/commercial.

2. Flame Spread Index (FSI): Class A - 0 to 25 for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

3. Smoke Developed Index (SDI): 450 or less for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

4. Front Facer: 1.0 mil smooth aluminum.

5. Back Facer: 1.0 mil smooth aluminum.

6. Board Thickness: \_\_\_\_ inch (\_\_\_\_ mm).

7. Board Edges: Square.

8. Sustainability: Third party listed Environmental Product Declaration certificate.

 **[OR]**

D. Polyisocyanurate Board Insulation with Facers Both Sides: Rigid cellular foam, complying with [ASTM C1289](http://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20C1289); Type I, aluminum foil both faces; Class 2, glass fiber-reinforced core.

1. Basis of Design:

a. DuPont de Nemours Inc.; **DuPont™ Thermax**™ **Metal Building Board\***: building.dupont.com/commercial.

2. Flame Spread Index (FSI): Class A - 0 to 25 for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

3. Smoke Developed Index (SDI): 450 or less for both core AND finished product, when tested in accordance with [ASTM E84](https://global.ihs.com/doc_detail.cfm?rid=BSD&document_name=ASTM%20E84).

4. Front Facer: 1.25 mil embossed aluminum.

5. Back Facer: 1.25 mil embossed aluminum.

6. Board Thickness: \_\_\_\_ inch (\_\_\_\_ mm).

7. Board Edges: Square.

8. Sustainability: Third party listed Environmental Product Declaration certificate.

2.03 ACCESSORIES

A. Exposed Interior Insulation Joint Treatment for Factory Mutual 4880.

1. DuPont™ Thermax™ White Foil Tape\*;
**[OR]** DuPont™ Thermax™ Aluminum Foil Tape\*.

PART 3 EXECUTION

3.01 EXAMINATION

A. Verify that substrate, adjacent materials, and insulation materials are dry and that substrates are ready to receive insulation.

3.02 GENERAL INSTALLATION

A. Maintain continuity of air barrier by sealing the roof/wall juncture with Roof/Wall Juncture Sealing material.

3.03 BOARD INSTALLATION AT INTERIOR WALLS

A. Apply fasteners per current edition of Factory Mutual Approval Guide. Verify current edition prior to installing. As of May 2017:

1. Fastener with minimum 1 inch diameter plastic or metal washer every 1 sq ft of board.
E.g. 4ft x 8ft (1.2 M x 2.4 M) needs 32 fasteners or 4 rows of 8 fasteners per row.

2. If using on concrete wall or tilt up apply a bead of sealant as recommended by Manufacturer behind the top edge of board and bottom edge of board to prevent airflow getting behind board (optional).

3. Fasteners are to be minimum 1 inch longer than board thickness

B. Cut and fit insulation tightly to protrusions or interruptions to the insulation plane.

C. Install DuPont™ Thermax™ White Foil Tape **[OR]** DuPont™ Thermax™ Aluminum Foil Tape at seams. Be sure seams are clean and dry before applying tapes – wipe with dry cloth as necessary to remove dirt and dust

3.04 FIELD QUALITY CONTROL

A. See Section 01 4000 - Quality Requirements, for additional requirements.

3.05 PROTECTION

A. Do not permit installed insulation to be damaged prior to its concealment.

END OF SECTION

**NOTICE**: No freedom from any patent owned by DuPont or others is to be inferred. Because use conditions and applicable laws may differ from one location to another and may change with time, Customer is responsible for determining whether products and the information in this document are appropriate for Customer’s use and for ensuring that Customer’s workplace and disposal practices are in compliance with applicable laws and other government enactments. The product shown in this literature may not be available for sale and/or available in all geographies where DuPont is represented. The claims made may not have been approved for use in all countries or regions. DuPont assumes no obligation or liability for the information in this document. References to “DuPont” or the “Company” mean the DuPont legal entity selling the products to Customer unless otherwise expressly noted. NO EXPRESS WARRANTIES ARE GIVEN EXCEPT FOR ANY APPLICABLE WRITTEN WARRANTIES SPECIFICALLY PROVIDED BY DUPONT. ALL IMPLIED WARRANTIES INCLUDING THOSE OF MERCHANTABILITY AND FITNESS FOR A PARTICULAR PURPOSE ARE EXPRESSLY EXCLUDED.

**DuPont™ Styrofoam™ Brand Spray Polyurethane Foam\*** contains isocyanate, hydrofluorocarbon blowing agent and polyol. Read the instructions and (Material) Safety Data Sheet ((M)SDS) carefully before use. Wear protective clothing (including long sleeves), gloves, goggles and proper respiratory protection. Supplied air or an approved air-purifying respirator equipped with an organic vapor sorbent and a P100 particulate filter is required to maintain exposure levels below ACGIH, OSHA, WEEL or other applicable limits. Provide adequate ventilation. Contents under pressure. Styrofoam™ Brand SPF should be installed by a trained SPF applicator.
**CAUTION**: When cured, these products are combustible and will burn if exposed to open flame or sparks from high-energy sources. Do not expose to temperatures above 240ºF (116ºC). For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**DuPont™ Great Stuff Pro™ Polyurethane Foam Sealants and Adhesives\*** contain isocyanate and a flammable blowing agent. Read all instructions and (Material) Safety Data Sheet ((M)SDS), carefully before use. Eliminate all sources of ignition before use. Cover all skin. Wear long sleeves, gloves, and safety glasses or goggles. Not for use in aviation, or food/beverage contact, or as structural support in marine applications. Provide adequate ventilation or wear proper respiratory protection. Contents under pressure. Not to be used for filling closed cavities or voids such as behind walls and under tub surrounds.
**CAUTION**: When cured, these products are combustible and will burn if exposed to open flame or sparks from high-energy sources. Do not expose to temperatures above 240ºF (116ºC). For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**DuPont Polyurethane Foam Insulation and Sealant\***
**CAUTION**: When cured, these products are combustible and will burn if exposed to open flame or sparks from high-energy sources. Do not expose to temperatures above 240ºF (116ºC). For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.
**CAUTION**: This product is combustible and shall only be used as specified by the local building code with respect to flame spread classification and to the use of a suitable thermal barrier. For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**DuPont™ LiquidArmor™ Flashing and Sealant\***Read the instructions and (Material) Safety Data Sheets ((M)SDS) carefully before use. It is recommended that spray applicators and those working in the spray area wear eye protection. Contact with exposed skin may cause skin discoloration and dryness. Gloves are recommended for prolonged exposures. Ensure adequate ventilation during spray applications.

**DuPont™ ThermaxTM Brand Polyisocyanurate Insulation\*
CAUTION**: This product is combustible and shall only be used as specified by the local building code with respect to flame spread classification and to the use of a suitable thermal barrier. For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583, or contact your local building inspector. In an emergency, call 1-989-636-4400.

**DuPont™ StyrofoamTM Extruded Polystyrene Foam Insulation\*
CAUTION**: This product is combustible. Protect from high heat sources. A protective barrier or thermal barrier may be required as specified in the appropriate building code. For more information, consult (Material) Safety Data Sheet ((M)SDS), call DuPont at 1-866-583-2583 or contact your local building inspector. In an emergency, call 1-989-636-4400 in the U.S. or 1-519-339-3711 in Canada.

**WARNING**: Rigid foam insulation does not constitute a working walkable surface or qualify as a fall protection product.

Building and/or construction practices unrelated to building materials could greatly affect moisture and the potential for mold formation. No material supplier including DuPont can give assurance that mold will not develop in any specific system.

\*A former product of The Dow Chemical Company

DuPont™, the DuPont Oval Logo, and all trademarks and service marks denoted with ™, ℠ or ® are owned by affiliates of DuPont de Nemours, Inc. unless otherwise noted. © 2019 DuPont. All rights reserved.

Form No. 43-D100408-enNA-0619