***25V by EMSEAL  GUIDE SPECIFICATION***

Application:	For Watertight Exterior Wall Joints

Basis of Design:	 25V Expanding Foam Sealant by EMSEAL Joint Systems

USA & INTERNATIONAL:  EMSEAL JOINT SYSTEMS, LTD, 23 Bridle Lane, Suite 3, Westborough, MA 01581-2603, Toll Free: 800-526-8365 or PH: 508-836-0280, FX: 508-836-0281, www.emseal.com.

CANADA:  EMSEAL CORPORATION, 120 Carrier Drive, Toronto, Ontario, Canada, M9W 5R1 Toll Free: 800-526-8365 or PH: 416-740-2090, FX: 416-740-0233, www.emseal.com.

Basis of Design: 25V expanding foam sealant by EMSEAL Joint Systems for primary exterior joint system in vertical-plane walls (above-grade).  Typical locations include, but are not limited to the following: applications in window perimeters, other façade penetrations such as doors, store fronts, vents, HVAC units etc, panel to panel joints, curtain walls, control joints, between dissimilar materials, structural expansion joints, and new-to-existing connections.

Foam shall be open cell polyurethane foam impregnated with an acrylic polymer-modified, water-based asphalt emulsion. Alternates containing wax or wax compounds shall not be permitted. Impregnation agent to have proven non-migratory characteristics.  Compression when expanded in joint shall be at approximately 25% of its uncompressed dimension (4x compression).

Material to be supplied in sticks or rolls, precompressed to less than joint size at mean temperature for ease of installation.  Material will contain pressure-sensitive mounting adhesive on one side of the material to aide installation.

***END OF GUIDE SPECIFICATION***