DURALPREP A.C.

Water-Based Epoxy Bonding Agent and Anti-Corrosion Coating

DURALPREP A.C. is a three-component bonding agent and anti-corrosion coating for reinforcing steel. It is a pre-proportioned kit that contains a water-based epoxy, combined with portland cement that can be used as a bonding agent for placing fresh concrete and repair mortars to existing concrete substrates. DURALPREP A.C. contains a corrosion inhibitor which protects reinforcement when used as an anti-corrosion coating for steel. DURALPREP A.C. has a long open time, is non-flammable, VOC compliant, and does not form a water vapor barrier after cure.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings. In no case shall these Guide Specifications be considered to be Contract Documents or serve as installation instructions for the product being discussed. In any cases of discrepancy the manufacturer's most recently published data sheet shall take precedent. }

PART 2:	PRODUCT

{Note to Specifier: Duralprep A.C. is suitable for use as an anti-corrosion coating for reinforcing steel and as the bonding agent for subsequent repair mortar or concrete. Do not use this product as a bonding agent for horizontal toppings less than 3.5 inches thick. Place fresh repair mortar or concrete within the open time of Duralprep A.C.}

2.__	BONDING AGENT AND ANTI-CORROSION COATING

- Extended Open Time Bonding Agent: Three component, pre-proportioned, VOC compliant, water-based portland cement modified epoxy bonding agent, that does not form a vapor barrier and contains a corrosion inhibitor for use on concrete and steel. Bonding agent shall provide 24 hours of open time at 75 °F. Product shall conform to: ASTM C 882.

- Bond Strength of 2,000 psi (with 24 hour open time) at 7 days in accordance with ASTM C882

- Pull-Off Strength (Concrete) 418 psi @ 14 days in accordance with ASTM C1583

- ASTM E96 Water Vapor Permeance

  - 20 mils: 0.371 perms

  - 40 mils: 0.209 perms

- ASTM G109 Coulomb Reading

  - 1 coat: 4.4 coulombs

  - Uncoated control: 372 coulombs

- ASTM G109 Top Rebar Corrosion

  - 1 Coat: 0 percent

  - Uncoated control: 35 percent

6.	Basis of Design Product:

- Euclid Chemical Company (The); Duralprep A.C. www.euclidchemical.com

2.__	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all products shall be from the same manufacturer.

PART 3:	EXECUTION

3.__ 	EXAMINATION

A. 	Examine concrete surfaces to receive epoxy bonding agent. Notify Engineer if surfaces are not acceptable. Do not begin surface preparation or application until unacceptable conditions are corrected.

3.__	SURFACE PREPARATION

A.	Concrete Removal: Remove all loose and unsound concrete per ICRI Guideline 310.1R “Guide for Surface Preparation”.

1.	Unsound concrete surface areas shall have the perimeter boundaries saw cut to a minimum depth of 1/2 inch or less if such depth will cause saw to come in contact with embedded reinforcing steel. All saw cuts shall be made perpendicular to the concrete surface and all concrete removal boundaries shall be straight and aligned parallel to opposite boundary edges resulting in repair areas that are rectangular in shape.

2.	All concrete shall be removed from within the repair boundary to minimum depth of 1/2 inch. Provide a surface with suitable profile for bond as defined in repair mortar manufacturer’s written recommendations. If delaminations, cracking, or unsound materials exist beyond the minimum removal depth, then removal shall continue until all unsound, delaminated, and cracked concrete has been removed from the cavity.

3.    	Provide concrete surface profile CSP stated on manufacturer’s literature per ICRI Guideline 310.2R “Selecting and Specifying Concrete Surface Preparation for Sealers, Coatings, and Polymer Overlays”.

B.      	Preparing Reinforcing Steel: Clean and prepare embedded reinforcing steel per ICRI Guideline 310.1R.

1.	Where 1/2 or more of the diameter of the reinforcement steel is exposed either by existing conditions or concrete removal, the bond between the concrete and the reinforcing steel is broken, or corrosion is present the concrete shall be removed to provide a minimum 3/4 inch clearance around the entire perimeter of the steel and along the entire exposed length.

2. 	Clean all exposed reinforcing steel to bright steel, (SSPC SP10) prior to installation of repair mortar.

- If section loss of a reinforcing bar is more than 25% or 20% in two or more adjacent bars contact Engineer.

C.       	Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, paint, oil, efflorescence, laitance, and other contaminants, and shall have a Concrete Surface Profile (CSP) equal to that recommended by the repair mortar manufacturer per ICRI Guideline 310.2R.

D.	Clean surface using un-oiled compressed air or vacuum clean.

3.__	APPLICATION

A.	Mix and place epoxy adhesive in accordance with manufacturer’s written instructions.

B.	Place concrete or repair mortar over epoxy adhesive within the maximum allowable time.

C.	As a Bonding Agent:

Mix bonding agent and apply to SSD concrete substrate per manufacturer’s recommendations. Allow minimum 30 minutes to 24 hours cure time at 75 deg F before placement of repair mortar.

{Note to specifier. A second coat of DURALPREP AC may be applied for added corrosion protection. Insert language below if desired.}

D.	As an Anti-Corrosion Coating:

Mix bonding agent and apply 20 mil coat to properly prepared steel in accordance with manufacturer’s recommendations. [Where multiple coats are specified, allow 3 to 6 hours between coats] Allow minimum 30 minutes to 24 hours cure time at 75 °F before placement of repair mortar.

END OF GUIDE SPEC