EUCON VANDEX AM-10

Integral Crystalline Waterproofing Admixture

{Note to Specifier: The paragraphs below are meant to be incorporated into Part 2 of a standard CSI 3 Part Format specification (normally 03 30 00), the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 2:	PRODUCTS

{PRODUCT}

2.__	ADMIXTURES

A.	Crystalline Waterproofing Admixture: Integral crystalline admixture specifically formulated to interact with capillary pore structures to provide a waterproofing system that is a permanent part of the concrete matrix. Admixture shall provide the following properties:

Water Penetration per DIN 1048				40% Reduction at 72 psi.

Water Permeability per CRD C48-92			>70% Reduction at 200 psi

Capillary Absorption per ASTM C-1585			>40% Reduction

Compressive Strength per ASTM C-39			Equal to and up to 8% increase

Resistance to Chloride Penetration per ASTM C-1202	10% improvement

Length Change per ASTM C-157			Up to 20% Reduction

1.	Product:

a)	Euclid Chemical Company (The); Vandex AM-10, www.euclidchemical.com

{ISO AND SINGLE SOURCE}

2.__	MANUFACTURER

A.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all admixtures shall be from the same manufacturer.