TUF-STRAND MAXTEN

Structural Synthetic Macro Fiber for Slabs-on-Grade and Toppings

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification (normally 03 30 00), the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 2:	PRODUCTS

2._	STRUCTURAL SYNTHETIC MACRO FIBER REINFORCEMENT

- A.	Structural Synthetic Macro Fiber Reinforcement: 100% virgin blended copolymer complying with ASTM C 1116, .75 or 1.5 inches (13 or 38 mm) length, and maximum aspect ratio 100.

- 1.	Product:

- Euclid Chemical Company (The); Tuf-Strand MaxTen; www.euclidchemical.com

- Fiber manufacturer shall have ISO 9001 certification.

2._	CONCRETE  MIXES

- A.	Use Structural Synthetic Macro Fiber Reinforcement for slabs-on-grade and toppings at rate of [Insert dosage provided to specifier by fiber manufacturer] pounds per cubic yard of concrete.

PART 3:	EXECUTION

3._	STRUCTURAL SYNTHETIC MACRO FIBER REINFORCEMENT

- Structural Synthetic Macro Fibers:  Add to concrete and mix for 3 – 5 minutes to provide uniform distribution.

- For broomed surfaces, broom once in one direction only.