## Proper installation of GRACE ICE & WATER SHIELD®

### The Conventional Method

- Cut the membrane into 3-5 m (10-15 ft.) lengths and re-roll loosely. Peel back 300-600 mm (1-2 ft.) of release liner, align membrane.

- Peel the release liner from the membrane. Press the membrane in place with heavy hand pressure.

- Minimum overlap guidelines are set by the manufacturer. GCP requires side laps to be a minimum of 90 mm (3.5 in.) and end laps a minimum of 150 mm (6 in.).

### The Back-Roll Method

Some contractors prefer the back-roll method. The back-roll technique can go quicker than the conventional method since you can lay down the membrane in just a few minutes!

- Start by unrolling a 3-5 m (10-15 ft.) piece of membrane, leaving the release liner in place. Align the membrane and roll in the intended direction of the membrane application.

- Carefully cut the release liner on top of the roll in the cross direction, being careful not to cut the membrane.

- Peel back about 150 mm (6 in.) of the release liner in the opposite direction of the intended membrane application, exposing the black adhesive.

- Hold the release liner with one hand and pull the roll along the deck with the release liner, leaving the applied membrane behind.

- Stop frequently to press the membrane in place with heavy hand pressure, smoothing the membrane toward the outer edge.

- When finished with the roll, go back and remove the remaining release liner.

- Smooth to the edge.