Heckmann Building Products Inc.
1501 N. 31st Avenue

Melrose Park, IL 60160-2911

800-621-4140 or 708-865-2403

Fax: 708-865-2640

Flashing Specifications

SECTION 04085

MASONRY ANCHORS AND ACCESSORIES

PART 1 GENERAL

1.1 SECTION INCLUDES

********************************************
NOTE: Delete items below not required for project.
*********************************************

A. Masonry veneer anchors and ties.

B. Stone veneer anchors and ties.

C. Masonry accessories.

1.2 RELATED SECTIONS

A. Section 04810 - Unit Masonry Assemblies.

B. Section 04851 - Cut Stone Veneer.

C. Section 04852 - Stone Masonry Veneer.

1.3 REFERENCES

*********************************************
NOTE: Delete references from the list below that are not actually required by the text of the edited section.
**********************************************

A. ASCE/ACI 530.1 – Specifications for Masonry Structures; 1995.

B. ASTM A 153/A 153M - Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware; 1998.

C. ASTM A 167 - Standard Specification for Stainless and Heat-Resisting Chromium-Nickel Steel Plate, Sheet, and Strip; 1996.

D. ASTM A 240/A 240M - Standard Specification for Heat-Resisting Chromium and Chromium-Nickel Stainless Steel Plate, Sheet, and Strip for Pressure Vessels; 1998b.

E. ASTM A 276 - Standard Specification for Stainless Steel Bars and Shapes; 1998b.

F. ASTM A 479/A 479M - Standard Specification for Stainless and Heat-Resisting Steel Bars and Shapes for Use in Boilers and Other Pressure Vessels; 1997a.

G. ASTM A 580/A 580M - Standard Specification for Stainless Steel Wire; 1998.

H. ASTM A 653/A 653M - Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process; 1998.

I. ASTM B 633 – Standard Specification for Electrodeposited Coatings of Zinc on Iron and Steel; (Reapproved 1994).

1.4 SUBMITTALS

A. Submit under provisions of Section 01300.

B. Product Data: Manufacturer's data on each type of product furnished.

PART 2 PRODUCTS

2.1 MANUFACTURERS

Acceptable Manufacturer:  Heckmann Building Products Inc.,

1501 N. 31st Avenue, Melrose Park, IL 60160

800-621-4140 or 708-865-2403 FAX: 708-865-2640
Email: Heckmann@worldnet.att.net.
Website: www.heckmannbuildingprods.com.

*********************************************
NOTE: Delete paragraph below; coordinate with Division 1 requirements.
**********************************************

B. Requests for substitutions will be considered in accordance with provisions of Section 01600.

C. Substitutions: Not permitted.

2.2 APPLICATIONS

A. Provide anchoring systems that comply with ACI 530.1/ASCE 6/TMS 602.

2.3 MATERIALS

A. Stainless Steel: Type 304.

1. Sheet Metal: ASTM A 167 or ASTM A 240/A 240M.

B. Mill Galvanized Steel:

1. Sheet Metal: ASTM A 653/A 653M, G60 coating.

2. Wire: ASTM A 641, regular coating; minimum 3/16 inch (4.76 mm) diameter.

C. Copper: ASTM B 370 Soft Temper; 16 oz and 20 oz.

D: Steel Sheet Metal Flashings:

1005 L-FLASHING
[Leg dimension] x [Leg dimension] x [length]

1008 L-FLASHING WITH DRIP
[Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1009 U-FLASHING
[Leg dimension] x [Leg dimension] x [Leg dimension] x [length]

1010 Z-FLASHING WITH DRIP
[Leg dimension] x [Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1011 ACUTE BEND FLASHING
[Leg dimension] x [Leg dimension] x [length]

1012 OBTUSE FLASHING
[Leg dimension] x [Leg dimension] x [length]

1017 HOOK-ON FLASHING W/DRIP
[Hook Dimension] x [Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1020 HOOK-ON Z-FLASHING W/DRIP
[Hook Dimension] x [Leg dimension] x [Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1022 Z-FLASHING W/DRIP
[Leg dimension] x [Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1024 HOOK-ON Z-FLASHING W/DRIP
[Hook Dimension] x [Leg dimension] x [Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1052 ANGLED FLASHING
[Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1053 CRIMPED U-FLASHING
[Hook Dimension] x [Leg dimension] x [Leg dimension] x [Leg dimension] x [length]

1054 L-FLASHING W/DRIP
[Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1055 SPECIAL FLASHING
[Leg dimension] x [Leg dimension] x [Leg dimension] x [Leg dimension] x [drip dimension] x [length]

1056 SPECIAL FLASHING
[Leg dimension] x [Leg dimension] x [Leg dimension] x [length]

Termination Bar

T-BAR
1/8 inch (3.175 mm) thick x 1-1/4 inch (32 mm) wide x [length] with [diameter] holes [length] on center.

PART 3 EXECUTION

3.1 INSTALLATION

A. Install as specified in applicable masonry section(s) and in accordance with manufacturer's instructions.

END OF SECTION