SECTION 04085

MASONRY ANCHORS AND ACCESSORIES

PART 1	GENERAL

1.1	SECTION INCLUDES

*****************************************************************

NOTE: Delete items below not required for project.

*****************************************************************

A.	Masonry veneer anchors and ties.

B.	Stone veneer anchors and ties.

C.	Masonry accessories.

1.2	RELATED SECTIONS

A.	Section 04810 - Unit Masonry Assemblies.

B.	Section 04851 - Cut Stone Veneer.

C.	Section 04852 - Stone Masonry Veneer.

1.3	REFERENCES

*****************************************************************

NOTE: Delete references from the list below that are not actually required by the text of the edited section.

*****************************************************************

A.  ASCE/ACI 530.1 – Specifications for Masonry Structures;    		1995.

B.	ASTM A 153/A 153M - Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware; 1998.

C.	ASTM A 167 - Standard Specification for Stainless and Heat-Resisting Chromium-Nickel Steel Plate, Sheet, and Strip; 1996.

D.	ASTM A 240/A 240M - Standard Specification for Heat-Resisting Chromium and Chromium-Nickel Stainless Steel Plate, Sheet, and Strip for Pressure Vessels; 1998b.

E.	ASTM A 276 - Standard Specification for Stainless Steel Bars and Shapes; 1998b.

F.	ASTM A 479/A 479M - Standard Specification for Stainless and Heat-Resisting Steel Bars and Shapes for Use in Boilers and Other Pressure Vessels; 1997a.

G.	ASTM A 580/A 580M - Standard Specification for Stainless Steel Wire; 1998.

H.	ASTM A 653/A 653M - Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process; 1998.

- ASTM B 633 – Standard Specification for Electrodepositied Coatings of Zinc on Iron and Steel; (Reapproved 1994).

1.4	SUBMITTALS

A.	Submit under provisions of Section 01300.

B.	Product Data:  Manufacturer's data on each type of product furnished.

PART 2	PRODUCTS

2.1	MANUFACTURERS

Acceptable Manufacturer:  Heckmann Building Products Inc., 1501 N. 31st Avenue, Melrose Park, IL 60160

800-621-4140 or 708-865-2403 FAX: 708-865-2640

Email: Heckmann@worldnet.att.net.

Website:  www.heckmannbuildingprods.com.

*****************************************************************

NOTE: Delete paragraph below; coordinate with Division 1 requirements.

*****************************************************************

A.	Requests for substitutions will be considered in accordance with provisions of Section 01600.

B.	Substitutions:  Not permitted.

2.2	APPLICATIONS

A.  Provide anchoring systems that comply with ACI 530.1/ASCE 6/TMS 602.

*****************************************************************

Note: Select one of the following 3 combinations of materials: all stainless steel, all hot-dip galvanized, or hot-dip galvanized except for items completely embedded in mortar.  Delete the inappropriate choices.

*****************************************************************

F.	Material for Anchors and Ties in Exterior Walls:  Stainless steel.

G.	Material for Anchors and Ties in Exterior Walls:  Hot-dip galvanized.

H.	Material for Anchors and Ties Exposed to Air in Exterior Walls:  Hot-dip galvanized.

I.	Material for Ties Completely Embedded in Mortar Joints:  Mill galvanized.

2.3	MATERIALS

A. Steel Types

1. Stainless Steel:  Type 304.

A. Sheet Metal:  ASTM A 167 or ASTM A 240/A 240M.

B. Wire:  ASTM A 580/A 580M.

C. Bars:  ASTM A 479/A 479M, annealed and ground.

D. Plates, Bars, and Shapes:  ASTM A 167 or ASTM A 276.

2. Hot-Dip Galvanized Steel:  Hot-dip galvanized after fabrication in accordance with ASTM A 153/A 153M, Class B-2.

B. Products

1.	Masonry Wall Stabilizing Anchors:  Anchoring top of wall to structure while allowing vertical deflection.

1.	Type:  No. 419 Pin Type 12 gage (2.6 mm) plate with 3/8 inch (10 mm) diameter pin; plate anchored to structure overhead, pin sliding in No. 421 Plastic Tube embedded in mortar at top of wall.

A. Material:  Hot-dip galvanized.

B. Material:  Stainless steel.

2.	Type:  No. 420 Cap 12 gage (2.6 mm) channel cap; attached to structure overhead.

A. Material:  Hot-dip galvanized.

B. Material:  Stainless steel.

3. Type: No. 138-R Channel Slot Threaded Rod Anchor used with a [#130 Welded Channel Slot][#133 Continuous Welded Channel Slot] on a Structural Beam. Channel Slot Anchor 12 gage (2.6 mm) with a welded 3/8 inch (10 mm) threaded rod [length] from channel, pin sliding in No. 421 Plastic Tube embedded in mortar at top of wall.

A. Material:  Hot-dip galvanized.

B. Material:  Stainless steel.

4. Type: No. 138 Channel Slot Flat Anchor used with a [#130 Welded Channel Slot][#133 Continuous Welded Channel Slot] on a Structural Beam. Channel Slot Anchor 12 gage (2.6 mm) x 1-1/4 inch ( mm) wide x[length] from channel, sliding in No. 422 Plastic Rectangle Tube embedded in mortar at top of wall.

A. Material:  Hot-dip galvanized.

B. Material:  Stainless steel.

5. Type: No. 121 Dovetail Threaded Rod Anchor used with a

No. 100 Dovetail Slot built in to Top Slab. Dovetail

Anchor 12 gage (2.6 mm) with a welded 3/8 inch (10 mm) threaded rod [length] from face of Top Slab, pin sliding in No. 421 Plastic Tube embedded in mortar at top of wall.

A. Material:  Hot-dip galvanized.

B. Material:  Stainless steel.

6. Type: No. 109 Dovetail Flat Anchor used with a

No. 100 Dovetail Slot built in to Top Slab. Dovetail

Anchor 12 gage (2.6 mm) x 1 inch (25 mm) wide x  [length] from face of Top Slab, sliding in No. 422 Plastic Rectangle Tube embedded in mortar at top of wall.

A. Material:  Hot-dip galvanized.

B. Material:  Stainless steel.

PART 3	EXECUTION

3.1	INSTALLATION

A.	Install as specified in applicable masonry section(s) and in accordance with manufacturer's instructions.

END OF SECTION