SECTION 04085

MASONRY ANCHORS AND ACCESSORIES

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Masonry veneer anchors and ties.

1.2	RELATED SECTIONS

A.	Section 04810 - Unit Masonry Assemblies.

1.3	REFERENCES

*****************************************************************

NOTE:Delete references from the list below that are not actually required by the text of the edited section.

*****************************************************************

A.  ASCE/ACI 530.1 – Specifications for Masonry Structures;    		1995.

B.	ASTM A 153/A 153M - Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware; 1998.

G.	ASTM A 580/A 580M - Standard Specification for Stainless Steel Wire; 1998.

1.4	SUBMITTALS

A.	Submit under provisions of Section 01300.

B.	Product Data:  Manufacturer's data on each type of product furnished.

PART 2	PRODUCTS

2.1	MANUFACTURER

Acceptable Manufacturer:  Heckmann Building Products Inc., 1501 N. 31st Avenue, Melrose Park, IL 60160

800-621-4140 or 708-865-2403 FAX: 708-865-2640

Email: Heckmann@worldnet.att.net.

Website:  www.heckmannbuildingprods.com.

*****************************************************************

NOTE: Delete paragraph below; coordinate with Division 1 requirements.

*****************************************************************

A.	Requests for substitutions will be considered in accordance with provisions of Section 01600.

B.	Substitutions:  Not permitted.

2.2	APPLICATIONS

A.  Provide anchoring systems that comply with ACI 530.1/ASCE 6/TMS 602.

- Masonry Anchors:

1.	Anchors to Concrete: No. 75: Heckmann "Pos-I-Tie®" Tapcon® Screw.

2.	Anchors to Masonry Backup: No. 75: Heckmann "Pos-I-Tie®" Tapcon® Screw.

3.	Anchors to Metal Stud Backup: No. 75: Heckmann "Pos-I-Tie®" Self-Drilling Screw.

4.	Anchors to Structural Steel: No. 75: Heckmann "Pos-I-Tie®" Dril-It® Screw.

5.  Anchors to Wood Stud Backup: No. 75: Heckmann "Pos-I-Tie®" Tapcon® Screw.

C.	Masonry Ties:

1.Masonry Veneer Ties:  Provide minimum 2 inches (50 mm) embedment in mortar.

A. Wire 3/16 inch (4.75 mm) diameter x [Length]

*****************************************************************

Note: ** Delete all of the following types that are not required.

*****************************************************************

- No. 75 Pos-I-Tie® Triangle Wire Tie

- No. 75 Pos-I-Tie® Single Wire Tie

Other Applications: Where details or installation conditions require, provide ties fabricated of shape and size to suit conditions and provide adequate anchorage.

2. Masonry Veneer Seismic Ties: Continuous wire in mortar joint, anchored to Pos-I-Tie® Triangle Tie with welded No. 370 Seismic clip.

*****************************************************************

Note: Select one of the following 3 combinations of materials: for wire ties.

*****************************************************************

D.	Material for Ties in Exterior Walls:  Stainless steel.

E.	Material for Ties in Exterior Walls:  Hot-dip galvanized.

F.	Material for Ties Exposed to Air in Exterior Walls:  Hot-dip galvanized.

G.	Material for Ties Completely Embedded in Mortar Joints:  Mill galvanized.

2.3	MATERIALS

1. Barrel Materials

Heckmann "No. 75 Pos-I-Tie®":  One-Piece Screw consisting of a 92% Zamac 2 Zinc barrel, washer, flanged head and eye to receive Pos-I-Tie® wire tie; designed to seat barrel directly on structural portion of backup, with flanged head covering fastener hole.

1.	Provide barrel shaft length [5/8 inch] [1 inch] [1-1/2 inch] [2 inch] [2-1/2 inch] [3 inch] 3-1/2 inch]and screws to suit substrate.

1. Wire Tie Materials

A.	Stainless Steel:  Type 304.

1.	Wire: 3/16 inch (4.76 mm) diameter ASTM A 580/A 580M.

B.	Hot-Dip Galvanized Steel:  Hot-dip galvanized after fabrication in accordance with ASTM A 153/A 153M, Class B-2.

1.	Wire: 3/16 inch (4.76 mm) diameter.

C.	Mill Galvanized Steel:

1.	Wire:  ASTM A 641, regular coating; 3/16 inch (4.76 mm) diameter.

PART 3	EXECUTION

3.1	INSTALLATION

A.	Pos-I-Tie® Screws

- Self-Drilling Screw: Use a standard drill with a variable clutch adjustment and a Pos-I-Tie® Chuck Adapter. Place the barrel end of the screw in the chuck adapter, drill through the gypsum baord and into the metal stud.

- Tapcon® Screw: Use a standard hammer drill and a Pos-I-Tie® Sleeve Tool with a Pos-I-Tie Chuck Adapter on the end. Set Drill to Hammer, slide off the chuck adapter sleeve and drill a 2" deep hole into the backup with a 3/16" (4.76 mm) masonry drillbit. Replace the sleeve/chuck adapter, switch the hammer mode off, and place the barrel end of the screw in the chuck adapter. Drill the screw into the hole.

- Dril-It® Screw: Use a standard drill with a variable clutch adjustment and a Pos-I-Tie® Chuck Adapter. Place the barrel end of the screw in the chuck adapter, and drill the screw into the structural member. (Some structural steel may require pre-drilling a pilot hole)

- Pos-I-Tie® Wires

- Configure ties to prevent flow of water to anchor and to transfer lateral loads without excess mechanical play or deformation.

END OF SECTION