*********************************************************************************************

SPEC NOTE: Henry® Pro-Grade® 988 Silicone Roof Coating for Existing Modified Bitumen (MB) Roofs.  This specification is ideally suited for the protection and maintenance of existing coated and non-coated granulated or smooth surfaced MB roofs to extend the life of the roofing assembly.

SPEC NOTE: This document includes Henry notes to assist the architect/specification writer. A Henry “SPEC NOTE” immediately precedes the text to which it is referring. The section is a guideline; modify to meet specific project requirements. Delete spec notes in the final copy of the specification.

SPEC NOTE: Contact Henry technical services at (800) 486-1278 for previously coated roofs.

SPEC NOTE: Pro-Grade 988 Silicone Roof Coating discussed in this specification is not recommended for use on cold storage or cryogenic structures due to constant high water vapor drive causing long-term accumulation of moisture in the insulation. Consult Henry for vapor retardant systems to use on refrigerated structures.

SPEC NOTE: Use extreme caution when applying and walking on coated surfaces. Coated surfaces are extremely slippery and can create a fall hazard resulting in injury or death.

SPEC NOTE: Coverage rates indicated in guide specifications do not include material calculations for waste.

SPEC NOTE: Contact Henry sales representative for a list of required documents and procedures prior to material purchase. Warranties submitted without required documents and procedures completed may result in delay or rejection of warranty request.

*********************************************************************************************

SECTION 07 01 50

MAINTENANCE OF MEMBRANE ROOFING

- GENERAL

  - SUMMARY

    - This Section Includes

Silicone roof coating over existing granulated or smooth surfaced modified bitumen (MB) roofs

    - Related Requirements

      - Section 07 01 60 – Maintenance of Flashing and Sheet Metal

      - Section 07 01 90 – Maintenance of Joint Protection

  - REFERENCES

    - Reference Standards

      - American Society for Testing and Materials (ASTM):

        - ASTM D1549 – Standard Test Method for Determination of Solar Reflectance Near Ambient Temperature Using a Portable Solar Reflectometer

        - ASTM D7281 – Standard Test Method for Determining Water Migration Resistance Through Roof Membranes

        - ASTM E108 - Standard Test Methods for Fire Tests of Roof Coverings

        - ASTM G154 – Standard Practice for Operating Fluorescent Ultraviolet (UV) Lamp Apparatus for Exposure of Nonmetallic Materials

      - Factory Mutual (FM):

        - FM Approvals 4470 – Single-Ply, Polymer-Modified Bitumen Sheet, Built-Up Roof (BUR) and Liquid Applied Roof Assemblies for Use in Class 1 and Noncombustible Roof Deck Construction

      - Miami-Dade County Product Control

        - Miami-Dade County Approved; Notice of Acceptance (NOA)

      - Dirt Pick-Up Resistance

        - MOT P-14 – Dirt Pickup Resistance

      - National Sanitation Foundation (NSF):

        - Protocol P151 Health Effects from Rainwater Catchment System Components

      - Underwriters Laboratories (UL):

        - UL 790 – Standard Test Methods for Fire Tests of Roof Coverings

  - ADMINISTRATIVE REQUIREMENTS

    - Coordination

      - Do not allow access to installation areas by other trades during roof coating installation.

    - Pre-bid Meeting

      - Manufacturer representative interested in submitting a bid are required to attend a pre-bid conference 10 days prior to bid opening.

      - Substitution limitations

        - Submit a Roof Coating Manufacturer certification letter during the pre-bid meeting, signed by an officer of the manufacturer, stating alternative material is equivalent to the specified product.

        - Submit independent laboratory testing information verifying physical properties meet the specified performance criteria.

        - Products accepted as equal to the specified product will be considered an alternate and presented as a bid addendum 5 days prior to bid opening.

        - No changes or substitutions to the specified product will be accepted after bid opening.

    - Pre-installation Meetings

      - Review installation and coordination requirements for warranty eligibility prior to pre-applied roof coating installation.

  - SUBMITTALS

    - Provide submittals in accordance with Section 01 33 00 Submittal Procedures.

    - Action Submittals

      - Product data

        - Guide specification

        - Safety data sheets

        - Standard details

        - Technical data sheets

      - Certificates

        - Certification stating assembly components are supplied and warranted by single source Manufacturer.

        - Certification stating Roof Coating Manufacturer meets the following standards:

          - Part of a single source manufacturer for roof coatings, Spray Polyurethane Foam (SPF), and EPDM, TPO, PVC roofing systems.

          - Incorporates a national manufacturing and production capabilities program including supply chain procurement teams and logistics management.

          - Each manufacturing facility must implement a full-time quality control and oversight operating system.

          - Participates in the Global Environmental, Social, and Governance (ESG) program to achieve Net Zero greenhouse gas emissions across the entire value chain by 2050.

        - Sarbanes-Oxley Act (SOX) compliant with public access to published annual report.

        - Statement stating Installer is authorized by Roof Coating Manufacturer to complete Work as specified.

  - QUALITY ASSURANCE

    - Qualifications

      - Manufacturer qualifications:

        - Minimum of 20 years of experience in production and sales of roof coatings.

        - Part of a single source manufacturer for roof coatings, Spray Polyurethane Foam (SPF), and EPDM, TPO, PVC roofing systems.

        - Incorporates a national manufacturing and production capabilities program including supply chain procurement teams and logistics management.

        - Each manufacturing facility must implement a full-time quality control and oversight operating system.

        - Participates in the Global Environmental, Social, and Governance (ESG) program to achieve Net Zero greenhouse gas emissions across the entire value chain by 2050.

        - Sarbanes-Oxley Act (SOX) compliant with public access to published annual report.

      - Installer qualifications

        - Authorized by Roof Coating Manufacturer to complete Work as specified.

        - 5 years minimum of experience in Work as described in this section.

  - DELIVERY, STORAGE, AND HANDLING

    - Delivery and Acceptance Requirements

      - Deliver materials in original, factory-sealed, unopened containers with intact and legible product label and manufacturer name.

    - Storage and Handling

      - Store materials as recommended by the Roof Coating Manufacturer in a protected area and out of direct sunlight. Protect materials from rain and physical damage.

  - SITE CONDITIONS

    - Ambient Conditions

      - Do not perform Work during rain or inclement weather.

      - Do not perform Work on surfaces covered in frost, snow, or wet to touch.

      - Do not perform Work over saturated insulation or saturated substrates.

      - Do not perform Work when temperatures exceed product specific limitations. Refer to product specific technical data sheet for minimum application temperature.

- *********************************************************************************************

SPEC NOTE: Henry offers two warranty configurations. Select one of the following warranty terms. Delete sections not applicable to project specific conditions.

- *********************************************************************************************

  - WARRANTY

    - Manufacturer Warranty

      - Material Plus Warranty:

        - Warrants product against product defect; provides material only for a period of [10] [15] [20] years from date of purchase.

      - Gold Seal Warranty:

        - Warrants system and installation; provides material and labor costs for repair for a period of [10] [15] [20] years from the date of installation completion as a result of any of the following:

          - Manufacturing product defect

          - Faulty Installer’s workmanship

- PRODUCTS

  - ASSEMBLIES

    - Manufacturers

      - Manufacturer list

        - Henry® a Carlisle Company

336 Cold Stream Rd.

Kimberton, PA 19442

(800) 486-1278

www.henry.com

    - Performance Criteria

      - Energy performance:

        - Initial solar reflectance (ASTM C1549): 88%

        - Solar reflective index (SRI): 111

        - Thermal emittance (ASTM C1371): 0.90

        - Meets California Energy Commission (CEC) Title Section 118(i)3

      - FM approved (Class number 4470): Max Roof Slope: 5:12

      - Florida product approval: Miami-Dade County, Florida NOA

      - Tested fire response characteristics (ASTM E 108 or UL 790): Class A

      - NSF Protocol P151: Tested and certified - system does not contaminate water

      - Ponding water resistant

      - Water leakage resistance (ASTM D7281): Pass (≥22 dry mils)

      - Resistant to fungi, mold, and mildew

      - Dirt pick-up resistance (MOT P-14): Pass

      - Rain safe in 15 minutes

      - Tack-free time: Approximately 1-2 hours

      - Does not contain hydrocarbon solvents

      - Does not contain calcium carbonate

      - Does not require hazardous cleaners or solvents

      - Volatile Organic Content (VOC): 10g/l max.

- *********************************************************************************************

SPEC NOTE: Contact Henry for additional roof coating color options. Custom color typical properties may vary.

- *********************************************************************************************

    - Materials

      - Roof coating

        - Top coat

          - Solvent free one-component moisture curing silicone rubber roof coating, having the following typical properties:

            - Basis of design: Pro-Grade® 988 Silicone Roof Coating

            - Color: Bright White

            - Energy performance:

              - Initial solar reflectance (ASTM C1549): 88%

              - Solar reflective index (SRI): 111

              - Thermal emittance (ASTM C1371): 0.90

              - Meets California Energy Commission (CEC) Title Section 118(i)3

            - FM approved (Class number 4470): Max Roof Slope: 5:12

            - Florida product approval: Miami-Dade County, Florida NOA

            - Tested fire response characteristics (ASTM E 108 or UL 790): Class A

            - NSF Protocol P151: Tested and certified - system does not contaminate water

            - Ponding water resistant

            - Water leakage resistance (ASTM D7281): Pass (≥22 dry mils)

            - Resistant to fungi, mold, and mildew

            - Dirt pick-up resistance (MOT P-14): Pass

            - Rain safe in 15 minutes

            - Tack-free time: Approximately 1-2 hours

            - Does not contain hydrocarbon solvents

            - Does not contain calcium carbonate

            - Does not require hazardous cleaners or solvents

            - Volatile Organic Content (VOC): 10g/l max.

        - Base coat

          - Solvent free one-component moisture curing silicone rubber roof coating:

            - Basis of design: Pro-Grade 988 Silicone Roof Coating

            - Color: Bright White, Tan, or Gray

      - Stain blocking primer

        - Water based acrylic latex elastomeric roof coating:

          - Basis of design: Pro-Grade 294 Base Coat and Sealer

      - Reinforcement

        - Stich bonded, high performance fabric reinforcement sheet:

          - Basis of design:  Henry 195 Polyester Fabric

      - Sealant

        - Butter grade, one-part moisture cure sealant consisting of silicone rubber:

          - Basis of design: Pro-Grade 923 Butter Grade Silicone Roof Sealer

        - Standard grade, one- part moisture cure sealant consisting of silicone rubber:

          - Basis of design: Pro-Grade 920 Silicone Roof Sealant

        - Fibered grade, one-part moisture cure sealant consisting of silicone rubber:

          - Basis of design: Pro-Grade 957 Silicone Fibered Roof Sealer

      - Roof granules:

        - Roof granules supplied by Henry a Carlisle Company

  - ACCESSORIES

    - Rust inhibitor

      - Contact Henry for a list of recommended products.

- EXECUTION

  - EXAMINATION

    - Verification of Conditions

      - Verify substrates are in accordance with Roof Coating Manufacturer requirements and as specified in this Section prior to roof coating installation. Commencement of Work indicates installer acceptance of the substrate.

        - Verify surfaces are sound, dry, clean, and free of oil, grease, dirt, excess mortar, frost, laitance, loose and flaking particles, or other contaminants.

        - Verify substrates are continuous and secured.

        - Verify metal flashings, skylights, scuppers, gutters, penetrations, and structures located within area of Work are leak free and in good working condition.

        - Verify insulation is intact not previously saturated with water.

        - Do not install roof coating over rusted substrates.

      - Previously coated areas

        - Contact Roof Coating Manufacturer for previously coated examination procedures.

    - Preinstallation Testing

      - Moisture detection survey

        - Visual inspection

        - Moisture analysis, choose from the following:

          - Infrared Thermography

          - Nuclear Scan

          - Electric Capacitance / Impedance Testing

          - Roof core cut samples

      - Adhesion test

        - Granulated substrates:

          - Not required

        - Smooth substrates:

          - Complete an adhesion test over all substrates prior to installation of roof coating.

            - Submit passing adhesion test results to Roof Coating Manufacturer during warranty application process.

          - Refer to Roof Coating Manufacturer’s application guide for adhesion test procedures.

          - Allow roof coating to cure a minimum of 72 hours prior to conducting adhesion test.

    - Evaluation and assessment

      - Verify roof areas promote positive drainage. Contact Roof Coating Manufacturer for ponding area repair procedures.

  - PREPARATION

    - Protection of In-Place Conditions

      - Protect areas and surfaces not included in scope of Work against damage or soiling.

      - Secure protective coverings against wind and vent area if used in conjunction with applications preventing collection and moisture.

      - Post signs noting potential overspray hazard within 400 feet (120 meters) of applications.

      - Turn off air-intake ventilation equipment to prevent fumes from entering building.

      - Post “No Smoking” signs near roof coating installation until vapors dissipate.

    - Surface Preparation

      - Surface cleaning

        - Remove oil and other contaminates that may inhibit adhesion.

        - Confirm local ordinances and jurisdiction cleaning method restrictions.

        - Do not to inject water into roofing substrate.

        - Acceptable cleaning methods

          - Pressure washer with greater than 2000psi.

          - Algae, mildew, or fungus:

            - Treat with a tri-sodium phosphate (TSP) or equivalent non-filming detergent and water solution.

            - Clear water rinse until complete cleaning residue removal.

    - Membrane Repairs

      - Use a stiff bristled brush or sealant knife to apply sealant.

      - Damaged insulation and roofing membrane

        - Remove damaged insulation and roofing membrane.

        - Replace roofing system with matching materials to create a continuous, flush, and secure substrate.

        - Seal repaired membrane seams using one of the following methods:

          - Sealant

            - Install butter grade or fibered grade sealant at 125 wet mils [1/8-inch (3 millimeters)], extending 3 inches (75 millimeters) each side of seam.

          - Reinforced roof coating

            - Install roof coating at 32 wet mils [2 gallons per square (7.5 liters per 9.3 square meters)], extending 4 inches (100 millimeters) each side of seam.

            - Center 6 inch (150 millimeter) wide strip of reinforcement fabric over seam and fully embed into wet roof coating.

            - Apply roof coating over cured reinforced seam at 16 wet mils [1 gallon per square (3.75 liters per 9.3 square meters)], extending 4 inches (100 millimeters) each side of seam.

      - Loose or torn seams

        - Repair membrane using one of the following methods:

          - Sealant

            - Apply sealant under loose or torn or membrane and firmly press membrane into place.

            - Verify membrane is fully bonded with no gaps or loose material.

            - Coat repaired area with sealant to create a smooth, continuous, and watertight finish.

          - Reinforced roof coating

            - Install roof coating at 32 wet mils [2 gallons per square (7.5 liters per 9.3 square meters)] extending 4 inches (100 millimeters) each side of seam.

            - Center 6 inch (150 millimeter) wide strip of reinforcement fabric over seam and fully embed into wet roof coating.

            - Apply roof coating over cured reinforced seam at 16 wet mils [1 gallon per square (3.75 liters per 9.3 square meters)], extending 4 inches (100 millimeters) each side of seam.

      - Membrane defects

        - Repair splits, cracks, blisters, deteriorated flashings, and cracked metal edging using one of the following methods:

          - Sealant

            - Install butter grade or fibered grade sealant at 125 wet mils [1/8-inch (3 millimeters)], extending 3 inches (75 millimeters) each side of defect.

          - Reinforced roof coating

            - Install roof coating at 32 wet mils [2 gallons per square (7.5 liters per 9.3 square meters)], extending 4 inches (100 millimeters) each side of defect.

            - Center 6 inch (150 millimeter) wide strip of reinforcement fabric over defect and fully embed into wet roof coating.

            - Apply roof coating over cured reinforced defect at 16 wet mils [1 gallon per square (3.75 liters per 9.3 square meters)], extending 4 inches (100 millimeters) each side of defect.

  - INSTALLATION

    - Roof coating may settle during storage. Mix roof coating prior to use with drill and mixer blade until consistent viscosity is achieved.

    - Stain Blocking Primer

      - Install primer in accordance with Roof Coating Manufacturer's application guide.

      - Allow primer to dry prior to subsequent installations.

    - Detailing and Flashing

      - Install detailing and flashings per Roof Coating Manufacturer’s details and application guide.

      - Refer to Roof Coating Manufacturer’s application guide for pretreatment of secure and intact seams, curbs, parapets, pipe penetrations, fastener heads, and drains.

      - Roof valleys and waterways:

        - Install roof coating at 16 wet mils [1 gallon per square (3.75 liters per 9.3 square meters)], extending 12 inches (300 millimeters) each side of valley.

        - Center 18 inch (450 millimeter) wide strip of reinforcement fabric over valley and fully embed into wet roof coating.

        - Brush reinforcement fabric with soft bristled broom or paint roller to remove voids and air gaps.

        - Coat reinforcement fabric side and end laps with roof coating. Overlap of dry fabric is not acceptable.

        - Overlap reinforcement fabric 4 inches (100 millimeters) minimum.

        - Apply roof coating over cured reinforced seam at 16 wet mils [1 gallon per square (3.75 liters per 9.3 square meters)], extending 4 inches (100 millimeters) each side of seam.

    - Roof Marking

      - Measure and mark area prior to roof coating installation.

      - Contact Roof Coating Manufacturer for roof marking instructions.

        - Coverage rates are theoretical and do not account for material loss due to spraying, surface texture, and waste.

        - Install a test patch to verify coating achieves millage requirements.

        - Adjust application rates based on test patch results to meet specified requirements.

    - Roof Coating

      - Apply roof coating per Roof Coating Manufacturer minimum application rates.

        - Refer to Roof Coating Manufacturer warranty chart for coverage rate options.

        - Application rates apply to both Material Plus and Gold Seal Warranties.

    - Walkways

      - Install roof coating at 16 wet mils [1 gallon per square (3.75 liters per 9.3 square meters)] at traffic areas.

      - Apply roof granules into wet roof coating at 20-30 pounds per square (9-13.5 kilograms per square meter).

      - Remove loose particles after roof coating is fully cured.

  - SITE QUALITY CONTROL

    - Site Tests and Inspections

      - Observe roof coating installation during the following phases:

        - Substrate verification

        - Roof coating installation start

        - Final inspection of roof coating installation

  - CLEANING

    - Waste Management

      - As the Work proceeds, and upon completion, promptly clean up and remove from the premises all rubbish and surplus materials resulting from the foregoing Work.

      - Clean soiled surfaces, spatters, and damage caused by Work of this Section.

      - Dispose of roof coating per local code ordinances.

  - PROTECTION

    - Protect roof coating from damage by other trades.

    - Limit traffic on roof coated surfaces for a minimum of 2 days.

END OF SECTION