SECTION 07 46 46

FIBER CEMENT SIDING – HARDIE PANEL, ARCHITECTURAL PANEL, SOFFIT, AND TRIM

PART 1 – GENERAL

1.1	SECTION INCLUDES

- Fiber Cement Panel Siding.

- Fiber Cement Architectural Panel Siding.

- Trim, Fascia, Molding, and Accessories.

1.2	RELATED REQUIREMENTS

- Section 05 12 00, Structural Steel Framing.

- Section 05 40 00 – Cold-Formed Metal Framing.

- Section 06 10 00 – Rough Carpentry.

- Section 07 21 00 – Thermal Insulation.

- Section 07 25 00 – Weather Barriers.

- Section 07 92 00 – Joint Sealants.

- Section 09 21 16 – Gypsum Board Assemblies.

- Section 09 91 13 – Exterior Painting.

Editor Note:

Other References you may want to include based on location of project.

- CAL-FIRE, Fire Engineering Division Building Materials Listing - Wildland Urban Interface (WUI) Listed Product.

- City of Los Angeles, Research Report No. 24862.

- Miami Dade County, -Notice of Acceptance -24-0221.07

- US Department of Housing and Urban Development Materials Release -1263h.

- Florida State Produ.ct Approval - FL 13223 and FL 13265.

- Texas Department of Insurance Product Evaluation EC-23.

1.3	REFERENCE STANDARDS

- ASCE 7, Minimum Design Loads for Buildings and Other Structures, Current Edition.

- ASTM C1185, Standard Test Methods for Sampling and Testing Fiber-Cement  Flat Sheet, Roofing and siding Shingles, and Clapboards; 2023.

- ASTM C1186., Standard Specification for Flat Fiber-Cement Sheets; 2022, with 2023 Editorial Revision.

- ASTM D3359, Standard Test Methods for Rating Adhesion by Tape Test; 2023.

- ASTM E84, Standard Test Method for Surface Burning Characteristics of Building Materials; 2020.

- ASTM E119, Standard Test Methods for Fire Tests of Building Construction and Materials; 2024.

- ASTM E136, Standard Test Method for Assessing Combustibility of Materials Using a Vertical Tube Furnace at 750 Degrees C; 2022.

- ASTM E330/E330M, Standard Test Method for Structural Performance of Exterior Windows, Doors, Skylights and Curtain Walls by Uniform Static Air Pressure Difference; 2021.

- ICC-ES Evaluation Reports ESR-1844, ESR-2290 and ESR-2273 (IBC, IRC, CBC, CRC); Current Editions.

- [_________________]

- [_________________]

1.4	ADMINISTRATIVE REQUIREMENTS

- Pre-Installation Conference:

  - A minimum of 2-weeks prior to the commencement of the Work of this section, conduct a preliminary pre-installation conference at project site.

  - Meet with Owner, Architect, and Installer, and Subcontractors completing related work.

  - Review the Following:

    - Methods and procedures to complete the Work.

    - Substrate and installation requirements.

    - Temporary protection requirements.

    - Repair procedures.

    - Schedule.

    - Other pertinent topics.

  - Provide record of discussion with meeting minutes distributed to all attendees.

1.5	SUBMITTALS

- See Section 01 30 00, Administrative Requirements.

- Product Data:

  - Manufacturer’s product data sheets.

  - Manufacturer’s storage and handling requirements.

  - Manufacturer’s preparation instructions.

  - Manufacturer’s installation instructions.

  - Manufacturer’s operation and maintenance instructions.

- Shop Drawings:

  - Provide detailed drawings showing dimensions, layout, joints, construction details, and attachments.

  - Indicate atypical non-standard applications outside of manufacturer’s standard details and specifications.

- Selection Samples:

  - Provide two complete sets of color ships representing manufacturer’s full range of available colors and patterns for each finish product specified.

- Verification Samples:

  - Provide two samples, minimum 4-inch x 6-inch (100 mm x 150 mm) representing selected product, color, texture, and patterns for each finish product specified.

- Installers qualification statement.

- Warranty:

  - Manufacturer’s sample warranty.

  - Manufacturer’s executed written warranty, completed in Owner’s name and registered with manufacturer.

1.6	QUALITY ASSURANCE

- Installer Qualifications: Company specializing in work specified in this section with a minimum of [__]-years of experience with installation of products of this type.

- Mock-up:

  - Mock-Up: Build mock-up for evaluation of surface preparation techniques, installation workmanship, and to verify selections made from sample submittals to demonstrate aesthetic effects and set quality standards for fabrication and installation.

    - Minimum 48-inches wide x 60-inches high or similar area as fits the layout of the building exterior.

    - Include outside corner on one end of mockup and inside corner on the other end.

    - Finish areas designated by Architect.

    - Approval of mock-up does not constitute approval of deviations from the Contract Documents unless approved in writing.

    - Approved mock-up [may, may not] remain as a part of the completed work.

  - Provide a minimum of [___]-days notification to Architect, Installer, and Manufacturer’s Representative prior to application of mock-up for review.

  - Obtain approval of mock-up from Architect prior to commencement of Work.

1.7	DELIVERY, STORAGE, AND HANDLING

- Deliver and store products in manufacturer's unopened packaging with labels intact until ready for installation.

- Store siding flat on a smooth level surface and carry on its side.

- Protect edges and corners from chipping.

- Store materials under dry, waterproof, well-ventilated cover, elevated above grade, and kept dry prior to installation.

- Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of the Authorities Having Jurisdiction.

- Protect materials from damage, dust, or other detrimental conditions.

1.8	FIELD CONDITIONS

- Maintain environmental conditions including temperature, humidity, and ventilation in accordance with the limits indicated in the manufacturer’s written instructions.

- Do not install products in conditions outside of the manufacturer’s stated limits.

1.9	WARRANTY

- Manufacturer’s Limited, Non Pro-rated Product Warranty:

  - Plank, Soffit, and Trim: 30-year Warranty.

  - Color-Plus Finish: 15-year Warranty.

  - When installed and maintained in accordance with manufacturer’s written requirements, warranty for 15-years from date of purchase covering peeling, cracking, and chipping.

- Installers Warranty:

  - Provide [___]-year installers warranty covering workmanship for work of this Section.

PART 2 – PRODUCTS

2.1	MANUFACTURERS

- Basis-of-Design: James Hardie Building Products, Inc.; Hardie Panel and Hardie Architectural Panel; www.jameshardie.com.

- Substitutions: In accordance with the requirements of Division 01, General Requirements.

2.2	FIBER CEMENT – VERTICAL PANEL SIDING

- Fiber Cement Panel Siding:

  - Type A, Grade II, ASTM C1186..

  - Non-combustible Material, ASTM E136.

  - Flame Spread Index: 0, ASTM E84.

  - Smoke Developed Index: <5, ASTM E84.

- Vertical Siding Panel - Type:

  - Smooth:

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 9-feet (2743 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

  - Cedarmill:

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 9-feet (2743 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

  - Stucco:

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 9-feet (2743 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

  - Sierra, 8-inch (203 mm):

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 9-feet (2743 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

- Color:

  - [__________].

  - As selected by Architect from manufacturer’s standard range.

- Product:

  - Basis-of-Design: Hardie Panel Siding; www.jameshardie.com.

  - Substitutions: In accordance with the requirements of Division 01, General Requirements.

2.3	FIBER CEMENT – ARCHITECTURAL PANEL SIDING

- Fiber Cement Panel Siding:

  - Type A, Grade II, ASTM C1186.

  - Non-combustible Material, ASTM E136.

  - Flame Spread Index: 0, ASTM E84.

  - Smoke Developed Index: 0, ASTM E84.

- Vertical Siding Panel – Architectural Collection - Type:

  - Thickness: 0.3125 inches.

  - Fine Sand:

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

    - 4-feet (1219 mm) x 12-feet (3658 mm).

  - Fine Sand – Grooved:

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

    - 4-feet (1219 mm) x 12-feet (3658 mm).

  - Mounded Sand:

    - 4-feet (1219 mm) x 8-feet (2438 mm).

    - 4-feet (1219 mm) x 10-feet (3048 mm).

    - 4-feet (1219 mm) x 12-feet (3658 mm).

  - Sea Grass:

  - 4-feet (1219 mm) x 8-feet (2438 mm).

  - 4-feet (1219 mm) x 10-feet (3048 mm).

  - 4-feet (1219 mm) x 12-feet (3658 mm).

- Color:

  - [__________].

  - As selected by Architect from manufacturer’s standard range.

- Product:

  - Basis-of-Design: Hardie Architectural Panel Siding; www.jameshardie.com.

  - Substitutions: In accordance with the requirements of Division 01, General Requirements.

2.4	FIBER CEMENT NON-VENTED SOFFIT PANELS

- Type A, Grade II, ASTM C1186.

- Non-combustible Material, ASTM E136.

- Flame Spread Index: 0, ASTM E84.

- Smoke Developed Index: <5, ASTM E84.

- Thickness: 1/4-inch (6 mm).

- Type:

  - Smooth:

    - 12-inches (305 mm) x 12-feet (3658 mm).

    - 16-inches (406 mm) x 12-feet (3658 mm.

    - 24-inches (610 mm) x 8-feet (2438 mm).

- Color:

  - [__________].

  - As selected by Architect from manufacturer’s standard range.

- Product:

  - Basis-of-Design: HardiePlank; www.jameshardie.com.

  - Substitutions: In accordance with the requirements of Division 01, General Requirements.

2.5	FIBER CEMENT VENTED SOFFIT PANELS

- Type A, Grade II, ASTM C1186.

- Non-combustible Material, ASTM E136.

- Flame Spread Index: 0, ASTM E84.

- Smoke Developed Index: <5, ASTM E84.

- Net Free Ventilation: 5-square inches per linear foot (10583 sq. mm per linear meter).

- Thickness: 1/4-inch (6 mm).

- Type:

  - Smooth:

    - 12-inches (305 mm) x 12-feet (3658 mm).

    - 16-inches (406 mm) x 12-feet (3658 mm),

    - 24-inches (610 mm) x 8-feet (2438 mm).

  - Textured Cedarmill:

    - 12-inches (305 mm) x 12-feet (3658 mm).

    - 16-inches (406 mm) x 12-feet (3658 mm).

    - 24-inches (610 mm) x 8-feet (2438 mm).

- Color:

  - [__________].

  - As selected by Architect from manufacturer’s standard range.

- Product:

  - Basis-of-Design: HardiePlank; www.jameshardie.com.

  - Substitutions: In accordance with the requirements of Division 01, General Requirements.

2.6	FIBER CEMENT VENTED PLUS SOFFIT PANELS

- Type A, Grade II, ASTM C1186.

- Non-combustible Material, ASTM E136.

- Flame Spread Index: 0, ASTM E84.

- Smoke Developed Index: 5, ASTM E84.

- Net Free Ventilation: 12.6-square inches per linear foot (26670 sq. mm per linear meter).

- Thickness: 1/4-inch (6 mm).

- Type:

  - Smooth, Vented:

    - 12-inches (305 mm) x 12-feet (3658 mm).

    - 16-inches (406 mm) x 12-feet (3658 mm).

    - 24-inches (610 mm) x 8-feet (2438 mm).

  - Textured Cedarmill:

    - 12-inches (305 mm) x 12-feet (3658 mm).

    - 16-inches (406 mm) x 12-feet (3658 mm).

    - 24-inches (610 mm) x 8-feet (2438 mm).

- Color:

  - [__________].

  - As selected by Architect from manufacturer’s standard range.

- Product:

  - Basis-of-Design: HardieSoffit VentedPlus Panels; www.jameshardie.com.

  - Substitutions: In accordance with the requirements of Division 01, General Requirements.

2.7	ACCESSORIES

- HardieTrim Trim Boards; www.jameshardie.com.

  - Type A, Grade I, ASTM C1186..

  - Flame Spread Index: 0, ASTM E84.

  - Smoke Developed Index: <5, ASTM E84.

  - Batten Board: 2-1/2 inch (63 mm) width.

  - 4/4 Boards:

    - 3-1/2 inch (89 mm) width.

    - 5-1/2 inch (140 mm) width.

    - 7-1/4 inch (184 mm) width.

    - 9-1/4 inch (235 mm) width.

    - 11-1/4 inch (286 mm) width.

  - 5/4 Boards:

    - 3-1/2 inch (89 mm) width.

    - 5-1/2 inch (140 mm) width.

    - 7-1/4 inch (184 mm) width.

    - 9-1/4 inch (235 mm) width.

    - 11-1/4 inch (286 mm) width.

  - Color:

    - [__________].

    - As selected by Architect from manufacturer’s standard range.

  - Texture:

    - Smooth.

    - Rustic.

    - Wood Grained.

  - Length: 12-feet (3658 mm).

  - Thickness:

    - 3/4-inch (19 mm).

    - 1-inch.

- Seam Tape: HardieWrap; www.jameshardie.com.

- Flashing:

  - HardieWrap Flashing Tape; www.jameshardie.com.

  - HardieWrap Flex Flashing Tape; www.jameshardie.com.

- Fasteners:

  - Wood Framing Fasteners:

    - 4d common corrosion resistant nails.

    - 6d common corrosion resistant nails.

    - 8d box ring common corrosion resistant nails.

    - 0.089-inch (2.2 mm) shank x 0.221-inch (5.6 mm) head x 2-inches (51 mm) corrosion resistant siding nails.

    - 0.093-inch (2.4 mm) shank x 0.222-inch (5.6 mm) head x 2-inches (51 mm) corrosion resistant siding nails.

    - 0.093-inch (2.4 mm) shank x 0.222-inch (5.6 mm) head x 2-1/2 inches (64 mm) corrosion resistant siding nails.

    - 0.091-inch (2.3 mm) shank x 0.221-inch (5.6 mm) head x 1-1/2 inches (38 mm) corrosion resistant siding nails.

    - 0.091-inch (2.3 mm) shank x 0.225-inch (5.7 mm) head x 1-1/2-inches (38 mm) corrosion resistant siding nails.

    - 0.121-inch (3 mm) shank x 0.371-inch (9.4 mm) head x 1-1/4 inches (32 mm) corrosion resistant roofing nails.

    - No. 11 gauge 1-1/4 inches (32 mm) corrosion resistant roofing nails.

    - No. 11 gauge 1-1/2 inches (38 mm) corrosion resistant roofing nails.

    - No. 11 gauge 1-3/4 inches (44 mm) corrosion resistant roofing nails.

    - 16 gauge 1-1/2 inches (38 mm) stainless finish nails.

  - Metal Framing Fasteners:

    - 1-1/4 inches (32 mm) No. 8-18 x 0.375-inch (9.5 mm) head self- drilling, corrosion resistant S-12 ribbed buglehead screws.

    - 1-5/8 inches (41 mm) No. 8-18 x 0.323-inch (8.2 mm) head self- drilling, corrosion resistant S-12 ribbed buglehead screws.

    - 1-inch (25 mm) No. 8-18 x 0.323-inch (8.2 mm) head self-drilling, corrosion resistant ribbed buglehead screws.

    - 1-inch (25 mm) No. 8-18 x 0.311-inch (7.9 mm) head self-drilling, corrosion resistant S-12 ribbed buglehead screws.

    - 1.5-inch (38 mm) [AGS-100] .100-inches x 25-inches (2540 mm x 635 mm) ETandF Pin or equivalent pneumatic fastener.

  - Masonry Walls:

    - Aerico Stud Nail, ET&F ASM No.-144-125, 0.14-inch (3.6 mm) shank x 0.30-inch (7.6 mm) head by 2-inches (51 mm) long corrosion resistant nails.

2.8	FINISHES

- Factory Primer: Provide factory applied universal primer.

  - Primer: Factory primed by manufacturer.

  - Topcoat: Reference Section 09 90 00, Painting and Coating and project Finish Schedule.

- Factory Finish: Reference project Finish Schedule.

  - As supplied by manufacturer.

  - Factory applied finish is finish applied by the same company and in the same facility that manufactures the siding substrate.

  - Require factory applied finish by fiber cement manufacturer applied in controlled environment within manufacturer's facility utilizing multi-coat, heat cured finish within one manufacturing process.

  - Each finish color to have documented color match to Delta E of 0.5 or better between product lines, manufacturing lots, or production runs as measured by photospectrometer and verified by third party.

  - Provide factory applied finish protection prior to transit to site. Remove finish protection after installation.

  - Accessories: Provide complete finishing system including pre-packaged touch-up kit provided by manufacturer.

  - Provide quantities as recommended by manufacturer.

PART 3 – EXECUTION

3.1	EXAMINATION

- Do not begin installation until substrates have been properly prepared.

- Examine substrate, clean and repair to eliminate conditions detrimental to installation.

- Do not commence with the Work until unacceptable conditions are remedied.

- Verify that weather barrier is installed over substrate and ready to receive the Work.

- If framing preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation prior to commencement of Work.

3.2	PREPARATION

- Clean surfaces thoroughly prior to installation.

- Prepare surfaces using methods recommended by manufacturer’s written requirements.

- Protect surrounding work areas and surface during installation.

- Repair punctures or tears in weather barrier prior to installation of siding.

3.3	WEATHER BARRIER

- See Section 07 25 00, Weather Barriers.

- Ensure weather barrier is installed with penetration and junction flashing in accordance with manufacturer’s written requirements and the Authorities Having Jurisdiction.

3.4	INSTALLATION – PANEL SIDING

- Install in strict accordance with manufacturer's written installation instructions at locations shown on Drawings.

- General:

  - Protect siding from Work of other trades.

  - Surfaces to be dry prior to installation of weather barriers and siding.

  - Reference trim details on Drawings.

  - Touch-up cut edges prior to installation.

- Flashing:

  - Install above door and window trim and casings.

  - Install above horizontal trim in field of siding.

  - [______________].

  - [______________].

3.5	INSTALLATION OF SOFFIT AND VENTED PANELS

- Install in strict accordance with manufacturer's written installation instructions at locations shown on Drawings.

- Panels may be installed as soffit or ceiling over wood or steel framing.

- 20-gauge (33 mil) minimum to 16-gauge (54 mil) in compliance with the Authorities Having Jurisdiction.

- Additional framing may be necessary to ensure proper fastening of siding.

3.6	INSTALLATION OF TRIM BOARDS

- Install in strict accordance with manufacturer's written installation instructions at locations shown on Drawings.

- Install flashing around all wall openings.

3.7	FINISHING

- Finish in accordance with paint manufacturer’s written application instructions.

- Finish unprimed siding with a minimum of one coat of manufacturer approved primer and one coat of 100 percent [acrylic];[latex] exterior grade topcoat or two coats of manufacturer approved high quality alkali resistant 100 percent [acrylic; latex] exterior grade topcoat within 90-days of installation.

- Finish factory primed siding with a minimum of one coat of manufacturer approved high quality 100 percent [acrylic][latex] exterior grade paint within 180-days of installation.

3.8	CLEANING

- See Section 01 70 00, Execution and Closeout Requirements.

- Clean siding in accordance with manufacturer’s written instructions using materials and methods acceptable to manufacturer.

3.9	PROTECTION

- Protect installed products until date of Substantial Completion.

- Touch-up, repair or replace damaged areas prior to date of Substantial Completion.

END OF SECTION