Guide Specification

STRUCTODEK® HD WITH PRIMED RED COATING Fiberboard - Roof Insulation Cover Board

Revision Date:  September 3, 2020

Section 07 22 16 – Roof Insulation

Specifier Notes: This guide specification is written according to the Construction Specifications Institute (CSI) MasterFormat 2010. The section must be carefully reviewed and edited by the Architect or Engineer to meet the requirements of the project. Coordinate this section with other specification sections and the drawings.

Specifier Notes:  STRUCTODEK HD with Primed Red Coating can be used as an insulation board, cover board, or re-roof/recover board.  The product is a high-density roofing board designed for low-slope single-ply, as well as traditional roof system applications.

STRUCTODEK HD is an integral roofing system component; it makes roofing easier with physical properties that generate rigidity and insulation (both thermal and sound) value. The proprietary, patented, non-asphaltic Primed Red Coating integrated on the surface of STRUCTODEK HD possesses unique bonding characteristics that ultimately result in superior adhesion capabilities with the current membrane and adhesive technology on the market today. The non-asphaltic Primed Red Coating is compatible with all single-ply membranes including PVC, TPO, EPDM, and CSPE without concern of premature membrane degradation that is often associated with asphalt emulsion coated fiberboard products. Additionally the Primed Red Coating, unlike asphalt emulsion coated products, has proven to be compatible with traditional, low VOC and water-based adhesives as well as many foam adhesives.

While STRUCTODEK HD with Primed Red Coating was designed with the single-ply application in mind it contains many of the same great attributes as STRUCTODEK HD with the traditional non-asphaltic black coating. Accordingly, it also works well with asphaltic based systems (BUR), coal tar, and cold-process adhesive products. Additionally, STRUCTODEK HD with Primed Red Coating has also been successful in peel-and-stick applications without the typical need for an additional primer in many instances. The rigid and strong, yet lightweight nature of STRUCTODEK HD with Primed Red Coating is better than heavier alternatives and will keep the roof load below the specified maximum weight.

PART 1	 GENERAL

1.1	SECTION INCLUDES

Specifier Notes:  In all, use of STRUCTODEK High Density Fiberboard Roof Insulation must be approved by the specific roof membrane manufacturer.  Install membrane and membrane fastening system according to the membrane manufacturer’s application instructions.

- Furnishings and installation of high density fiberboard roof insulation for roofs and roof systems.

1.2	REFERENCES

A.	ASTM C 208 - Standard Specifications for Cellulosic Fiber Insulating Board. 				Type II, Grade 1 and Grade 2

B.	ASTM C 209 - Standard Test Methods for Cellulosic Fiber Insulating Board.

C.	Canadian Construction Materials Centre, Evaluation Listing CCMC #13186-L.

D.	CAN/ULC-S706-09: Standard for Wood Fibre Insulating Boards for Buildings, Type II, 			Class 1 and Class 2.

E.	Factory Mutual Class I Approval per FMRC Standard 4450/4470 subject to the conditions 	of approval as roof insulation when installed as described in the FMRC Approval Guide.

F.	Miami-Dade County, Florida, NOA No. 18-0523.03, Expiration Date: 09/18/23.

G.	Underwriters Laboratories, Inc. Classified as “Roof Covering Materials” for use in 				construction of Class A roof covers. UL certification reference TGFU.R20803 and 			TGFU7.R20803 Canadian Standard CAN/ULC-S107 and United States Standard UL790.

1.3	SUBMITTALS

A.	Comply with Section 01 33 00 - Submittal Procedures.

B.	Submit manufacturer's product data and installation instructions.

1.	All materials shall be manufactured by BLUE RIDGE FIBERBOARD unless specified otherwise.

2.	Refer to the roof membrane manufacturer for full roof system installation guides

and precautions, including fastening patterns for fastening down materials.

C.	Quality Assurance/Control Submittals.

1.	Refer to safety data sheet, technical data sheet and product brochure.

1.4	QUALITY ASSURANCE

A.	Manufacturer’s Qualifications.

1.	Over 50 years experience in producing wood fiber roof insulation boards.

1.5	DELIVERY, STORAGE, AND HANDLING

A.	Deliver materials in manufacturer’s original packages or bundles bearing the brand name 			of the product.

1.	Inspect the materials upon delivery to assure that specified products have been 				received.

2.	Report damaged material immediately to the delivering carrier and note such 				damage on the carrier’s freight bill of lading.

B.	Store materials inside on a dry, level surface under cover.

C.	Keep dry, protect from weather and damage from construction operations and other 			causes.

D.	Store at a location where humidity and temperature duplicates those during installation 			and occupancy in order to stabilize the material.

1.6	PRECAUTIONS

A.	Fiberboard  products must not be used in close proximity to chimneys, heater units, 			fireplaces, steam pipes or other surfaces which could provide long term exposure 			to excessive heat (maximum 212° F) without adequate thermal protection.

B.	Consult the appropriate heating appliance manufacturer’s instructions before installation.

PART 2  PRODUCTS

2.1	MANUFACTURER

A.	Acceptable Manufacturer: BLUE RIDGE FIBERBOARD, INC., 250 Celotex Dr., Danville, VA  24541

B.	Requests for substitutions will be considered in accordance with provisions of Section 01 			25 00 – Substitution Procedures.

C.	Provide all roof insulation boards from a single manufacturer.

2.2	MATERIALS

Specifier Notes:  Consult roofing manufacturer for specific recommendations of tested assembly and construction.  Select insulation board and accessories based on specific project requirements.

- High Density Fiberboard Roof Insulation Boards: STRUCTODEK High Density with primed  red coating physical properties as follows:

1.	Thickness, Thermal Values, Flute Span and Board Dimensions

| NOMINAL PRODUCT THICKNESS (INCHES) | THERMAL VALUES R-VALUES(1) | MAXIMUM FLUTE SPAN | BOARD DIMENSIONS | WEIGHT PER SQUARE FOOT (lb/ft2) |
| --- | --- | --- | --- | --- |
| ½” (12.75 mm) | 1.3 | 1 5/8” (40 mm) | 4’x4’, 4’x8’ | 0.700 |

2.	Typical Physical Properties

| PROPERTY | TEST METHOD | VALUE |
| --- | --- | --- |
| Water Absorption | ASTM C209 | 7% Volume Max. |
| Linear Expansion | ASTM C209 | 0.5% Max. |
| Compressive Strength @ 10% Deformation | ASTM C165 | 22 psi |
| Compressive Strength @ 20% Deformation | ASTM C165 | 45 psi |

2.3	ACCESSORIES

- TAPERED EDGE where applicable for proper roof drainage and slope to prevent water standing on the roof.

B.	CANT STRIP where applicable for 90 degree angle where roof will meet the parapet wall.

PART 3  EXECUTION

3.1	EXAMINATION

A.	Examine substrates upon which work will be installed.

B.	Verify substrates comply with roof manufacturer’s requirements.

C.	Verify environmental conditions are, and will continue to be, maintained in accordance 			with manufacturer’s recommendations.

D.	Coordinate with responsible entity to perform corrective work on unsatisfactory substrates 		or conditions.

E.	Starting work by installer is acceptance of substrate and environmental conditions.

3.2	 PREPARATION

A.	Follow manufacturer’s instructions. Store in a well ventilated area. Material must be kept 			dry before installation.

1.	Insulation panels must be installed in a clean, dry condition.

2.	Ensure panels are thoroughly dry prior to closing in the structure.

3.	Provide proper ventilation and use of respiratory protection as required by the 				manufacturer.

4.	Avoid dust inhalation.

5.	Use caution when creating large amounts of dust because of potential

explosion hazard.

6.	Refer to manufacturer’s SDS data for these and other precautions.

3.3	INSTALLATION

- Contact the roof membrane manufacturer for full roof system installation guides and

Precautions, including fastening patterns for fastening down materials.

B.	Ensure that the proper thickness of fiberboard is used in conjunction with the proper flute 			span when installing over a steel deck.

- When installing insulation board over an existing roof, ensure that the roof is free of all loose gravel and debris, and conduct a moisture survey to ensure the roof is dry.

D.	Replace wet material in any areas where leaks are present.

E.	Do not install more insulation that can be covered by the roof membrane in a day.

END OF SECTION