SECTION 3395/03050/003366

Floor Polish

PART 1			GENERAL

1.1				SCOPE OF WORK

The contractor shall provide all labor, material, equipment and accessories necessary to complete the work. This section includes the following.

A.		Application of floor polish in accordance with manufacturer’s instructions.

1.2				SECTION INCLUDES

A.		High gloss synthetic polymer floor polish.

1.3				RELATED SECTIONS

A.		Section 03300 - Cast-In-Place Concrete.

**NOTE: PLEASE LIST ANY OTHER SECTIONS WITH WORK DIRECTLY RELATED TO THIS SECTION AS REQUIRED FOR THIS PROJECT.**

1.4				REFERENCES

A.		American Society for Testing Materials (ASTM)

1.		ASTM D 2047 – Static Coefficient of Friction

1.5				SUBMITTALS

A.	Submittal Procedures: Submit in accordance with procedures specified in Section 01330.

B.	Product Data: Submit manufacturer’s Product Data Sheet, to include all surface preparation and application instructions.

1.6				QUALITY ASSURANCE

A.		Installer Qualifications: An installer with a minimum of 3 years experience in the installation of surface treatments.

1.7				DELIVERY AND STORAGE

A.		Delivery: Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.	Storage: Store materials in a clean, dry area in accordance with manufacturer’s instructions. Promptly and tightly reseal all unused open containers. Product should be stored in a dry environment. Prevent product from freezing.

PART 2				PRODUCT

2.1				MANUFACTURER

A.		Nox-Crete Products Group, 1444 S. 20th St., Omaha, NE.

Toll Free: (800) 669-2738; Phone: (402) 341-1976;

Fax: (402) 341-9752; Website: www.nox-crete.com

B.		Substitutions not permitted.

2.2				MATERIALS

A.		Floor Polish: Duro-Polish - High gloss, metal cross linked, concentrated, synthetic polymer floor polish:

1.	Deep penetrating, high gloss durable floor polish

2.	Increased slip resistance and stain protection

3.		Meets all federal and state VOC requirements

- Will not flake or peel

5.		Low odor

6.		ASTM D 2047 – Static Coefficient of Friction…..>0.5

**SPECIFIER NOTE: DURO-POLISH IS A UNIQUE PRODUCT THAT NOT ONLY PROVIDES A VERY HARD AND IMMEDIATE HIGH GLOSS, BUT ALSO MEETS ASTM D-2047 FOR SLIP RESISTANCE.  ANY SUBSTITUTIONS SHOULD BE REQUIRED TO MEET THE APPEARANCE AND MINIMUM STATIC COEFFICIENT OF FRICTION REQUIREMENTS OF 0.5.**

PART 3			EXECUTION

3.1			EXAMINATION

A.	Examine concrete floors to receive the floor polish. Do not proceed with application until conditions are acceptable.

3.2			SURFACE PREPARATION

A.		Prepare floor in accordance with manufacturer’s instructions.

B.	Floor should be free of laitance, debris, oil, grease, paint, and/or other material(s) which may interfere with the application of the floor polish.

C.	If necessary floors should be cleaned with Nox-Crete’s biodegradable floor cleaner, Bio-Clean.

3.3			APPLICATION

A.	Apply floor polish to concrete floors in accordance with manufacturer’s instructions.

B.	A representative test application must be conducted in advance of full scale installation to determine required dilution rate, rate of application and desired appearance.

C.	Do not apply at air or substrate temperatures below 40º F (4º C) or over 100º F (38º C).

END OF SECTION

Nox-Crete Products Group

1444 S. 20th St., Omaha, NE 68108

(402) 341-1976 / (800) 669-2738

www.nox-crete.com