Section 07200

Exterior Wall Thermal

Insulation

Part 1	General

1.01 	Summary

A.	Provide glass fiber thermal insulation for exterior walls as indicated in building plans.

1.02	Materials Provided in Other Sections

These sections are typically cross referenced.  Delete section(s) not included in project manual.

A.	Section 03400- Precast Concrete

B.	Section 04200- Unit Masonry

C.	Section 04235- Preassembled Masonry Panels

D.	Section 04400- Stone

E.	Section 07240- Exterior Insulation and Finish Systems

F.	Section 07410- Preformed Roof and Wall Panels

G.	Section 07420- Composite Building Panels

H.	Section 07920- Sealants, Caulking and Seals

I.	Section 08400- Entrances and Storefronts

J.	Section 08500- Metal Windows

K.	Section 08810- Glass

L.	Section 08900- Glazed Curtain Walls

M.	Section 09300- Tile

1.03	References

A.	American Society for Testing and Materials (ASTM).

1.	E 84 Test Method for Surface Burning

Characteristics of Building Materials

2.	E 96 Test Method for Water Vapor Transmission of Materials

3.	E 136 Test Method for Behavior of Materials in a Vertical

Tube Furnace  at 750(C.

4.	C 177 Test Method for Steady-State Thermal Transmission

Properties by  means of the Guarded Hot Plate

5.	C 423 Test Method for Sound Absorption and the Sound

Absorption Coefficient by the Reverberation Room Method

6.	C 518 Test Method for Steady-State Thermal Transmission

Properties by  Means of the Heat Flow Meter

7.	C 553 Standard Specification for Mineral Fiber Blanket and

Felt Insulations

8.	C 612 Standard Specification for Mineral Fiber Block and

Board Thermal Insulation

9.	C 665 Specification for Mineral Fiber Blanket Thermal

Insulation for Light Frame Construction and Manufactured

Housing.

1.04 	Submittals

A.	Product Data: Submit Owens-Corning product literature, samples

and installation instructions for specified insulation.

1.05 	Delivery

A.	Protect insulation from physical damage and from becoming wet,

soiled, or  covered with ice or snow. Comply with manufacturer's

recommendations for handling, storage and protection during installation.

B.	Label insulation packages to include material name, production

date and/or product code.

Delete paragraph below if section 01600 or 01620 are not included in project manual.

C.	Deliver and store materials under provision of Section (01600) (01620).

1.06 	Limitations

A.	Do not use unfaced insulation in exposed applications where there

is potential for skin contact and irritation.

B.	Kraft and standard foil facings will burn and must not be left

exposed. The facing must be installed in substantial contact with

an approved exterior wall construction material. Protect facing

from any open flame or heat source.

Part 2 	Products

2.01 	Manufacturer

A.	Owens-Corning.

2.02 	Curtainwall CW225 Insulation

A.	Type: Unfaced or FRK-faced glass fiber thermal insulation

complying with ASTM C 612, Type 1A and 1B.

B.	Size:  R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness		   Width			Length	    	R-value

1"		25mm		24"  609mm		48"  1219mm	       4.3

1½" 	38mm		24"  609mm     	    	48"  1219mm	       6.5

2"		51mm		24"  609mm		48"  1219mm	       8.7

2½" 	64mm		24"  609mm     	    	48"  1219mm	      10.9

3"		76mm		24"  609mm		48"  1219mm	      13.0

3½" 	89mm		24"  609mm     	    	48"  1219mm	      15.2

4"		102mm		24"  609mm		48"  1219mm	      17.4

C.	Vapor Retarder Perm Rating:

FRK-facing Perms Maximum 0.10

When tested in accordance with ASTM E 96.

D.	Surface Burning Characteristics:

1.	Unfaced Insulation

Maximum flame spread: 20

Maximum smoke developed: 20

2.	FRK-faced Insulation

Maximum flame spread: 25

Maximum smoke developed: 50

When tested in accordance with ASTM E 84.

E.	Noise Reduction Coefficient:

1.	Unfaced 2" NRC 1.00

2.	FRK-faced 2" NRC 0.80

When tested in accordance with ASTM C 423

on a Type E-405 mounting.

F.	Dimensional Stability:

Linear shrinkage less than 0.1%

2.03 	700 Series Insulation

A.	Type: 701 Unfaced glass fiber thermal insulation

complying with ASTM C 553, Type III and ASTM C 665, Type I.

B.	Type: 711 Unfaced glass fiber thermal insulation

complying with ASTM C 553, Type III and ASTM C 665, Type I.

C.	Type: 703 Unfaced, FRK-faced and ASJ-faced glass fiber

thermal insulation complying with ASTM C 612, Type 1A and 1B.

D.	Type: 705 Unfaced, FRK-faced and ASJ-faced glass fiber

thermal insulation complying with ASTM C 612, Type 1A and 1B.

E.	Size:        R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness		   Width		      Length	    R-value

1"		25mm		24"  609mm	    48"  1219mm+       4.2

1½" 	38mm		24"  609mm     	    48"  1219mm	       6.3

Type2"		51mm		24"  609mm	    48"  1219mm	       8.3

701	2½" 	64mm		24"  609mm     	    48"  1219mm	      10.4

3"		76mm		24"  609mm	    48"  1219mm	      12.5

3½" 	89mm		24"  609mm     	    48"  1219mm	      14.6

4"		102mm		24"  609mm	    48"  1219mm	      16.7

1"		25mm		24"  609mm	    48"  1219mm+       4.0

1½" 	38mm		24"  609mm     	    48"  1219mm	       6.0

Type2"		51mm		24"  609mm	    48"  1219mm	       8.0

711	2½" 	64mm		24"  609mm     	    48"  1219mm	      10.0

3"		76mm		24"  609mm	    48"  1219mm	      12.0

4"		102mm		24"  609mm	    48"  1219mm	      16.0

1"		25mm		24"  609mm	    48"  1219mm+       4.3

Type1½" 	38mm		24"  609mm     	    48"  1219mm	       6.5

703	2"		51mm		24"  609mm	    48"  1219mm	       8.7

2½" 	64mm		24"  609mm     	    48"  1219mm	      10.9

Type3"		76mm		24"  609mm	    48"  1219mm	      13.0

705	3½" 	89mm		24"  609mm     	    48"  1219mm	      15.2

4"		102mm		24"  609mm	    48"  1219mm	      17.4

F.	Vapor Retarder Perm Rating:

1.	FRK-facing Perms Maximum 0.02

2.	ASJ-facing Perms Maximum 0.02

When tested in accordance with ASTM C 1136.

G.	Surface Burning Characteristics:

Maximum flame spread: ____

Maximum smoke developed: ____

When tested in accordance with ASTM E 84.

Flame            Smoke

Spread	     Developed

701 Unfaced		20		20

711 Unfaced		20		20

703 Unfaced		15		0

703 ASJ-faced	25		50

703 FRK-faced	25		50

705 Unfaced		15		0

705 ASJ-faced	25		50

705 FRK-faced	25		50

H.	Noise Reduction Coefficient: 	NRC ____

When tested in accordance with ASTM C 423 on a Type A mounting.

NRC

Type					1"	25mm			0.70

701/711 Unfaced			2"	51mm			0.90

3"	76mm			1.15

Type					1"	25mm			0.70

703 Unfaced			2"	51mm			1.00

3"	76mm			1.10

Type					1"	25mm			0.65

705 Unfaced			2"	51mm			0.95

3"	76mm			1.10

Type					1"	25mm			0.65

703 FRK-faced			2"	51mm			0.75

Type					1"	25mm			0.55

705 FRK-faced			2"	51mm			0.60

Type					1"	25mm			0.65

703 ASJ-faced			2"	51mm			0.75

Type					1"	25mm			0.50

705 ASJ-faced			2"	51mm			0.65

I.	Dimensional Stability

Linear shrinkage less than 0.1%

2.04 	Flame Spread 25 Insulation

A.	Type: FRK-faced glass fiber thermal insulation complying

with ASTM C 665, Type III, Class A.

B.	Size:

Metal Frame Insulation

R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness		   	Width				Length	    	   R-value

3½"    89mm		16"  406mm  	24"  609mm	       96"  2438mm	       11.0

3½"    89mm		16"  406mm  	24"  609mm	       96"  2438mm	       13.0

6¼"    159mm		16"  406mm  	24"  609mm	       96"  2438mm	       19.0

Wood Frame Insulation

R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness			   Width				Length	    	    R-value

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       11.0

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       13.0

6¼"    159mm		15"  381mm  	23"  584mm	       93"  2362mm	       19.0

Special Application Insulation

R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness		     	    Width		        	         Length	        R-value

9½"    241mm		16"  406mm  	24"  609mm	       48"  1219mm	30.0

6¼"    159mm		48"  1219mm			       40'   12.19m	  	19.0

3½"    89mm		48"  1219mm			       72'   21.95m	     	11.0

C.	Vapor Retarder Perm Rating:

FRK-facing Perms Maximum 0.10

When tested in accordance with ASTM E 96.

D.	Surface Burning Characteristics:

Maximum flame spread: 25

Maximum smoke developed: 50

When tested in accordance with ASTM E 84.

E.	Combustion Characteristics:

Classified non-combustible by model building codes.

F.	Dimensional Stability:

Linear shrinkage less than 0.1%

2.05 	Thermal Batt Insulation

A.	Type: Unfaced glass fiber thermal insulation complying with

ASTM C 665, Type I and ASTM E 136.

B.	Type: Kraft-faced glass fiber insulation complying with

ASTM C 665, Type II, Class C.

C.	Type: Foil-faced glass fiber thermal insulation complying with

ASTM C 665, Type III, Class B and C.

D.	Size:

Metal Frame Insulation

R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness			   Width				Length	    	   R-value

3½"    89mm		16"  406mm  	24"  609mm	       96"  2438mm	       11.0

3½"    89mm		16"  406mm  	24"  609mm	       96"  2438mm	       13.0

6¼"    159mm		16"  406mm  	24"  609mm	       96"  2438mm	       19.0

Wood Frame Insulation

R-value ____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness			   Width				Length	    	   R-value

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       11.0

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       13.0

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       15.0

6¼"    159mm		15"  381mm  	23"  584mm	       93"  2362mm	       19.0

5½"    139mm		15"  381mm  	23"  584mm	       93"  2362mm	       21.0

E.	Vapor Retarder Perm Rating:

1.	Foil-facing Perms Maximum 0.50

2.	Kraft-facing Perms Maximum 1.00

When tested in accordance with ASTM E 96.

F.	Surface Burning Characteristics:

1.	Unfaced Insulation

Maximum flame spread: 10

Maximum smoke developed: 10

2.	Foil-Faced Insulation

Maximum flame spread: 75

Maximum smoke developed: 150

When tested in accordance with ASTM E 84.

Kraft and standard foil facings on this insulation will burn and

must not be left exposed. The facing must be installed in substantial

contact with an approved exterior wall construction material.

Protect facing from any open flame or heat source.

G. 	Combustion Characteristics:

Unfaced insulation passes ASTM E 136 test.

H. 	Dimensional Stability:

Linear shrinkage less than 0.1%

2.06 	Other Materials

Provide materials, not specifically described but required for

a complete and proper installation of the work in this section.

Part 3 	Execution

3.01 	Inspection and Preparation

A.	Examine the areas and conditions under which work of this section

will be installed. Verify that adjacent materials are dry and ready

to receive insulation. Verify mechanical and electrical services within

walls have been tested.

B.	Provide written report listing conditions detrimental to performance

of work in this section. Do not proceed with installation until

unsatisfactory conditions have been corrected.

3.02 Installation - General

A.	Comply with manufacturer's instruction for particular conditions

of installation in each case.

B. 	Mechanical Fasteners

Curtainwall, 700 Series, Flame Spread 25 and Thermal Batts Insulation

Apply insulation directly to the interior surface of the exterior wall with

appropriate spindle or prong-type anchors.

- Fasten anchors to wall by welding the pin to metal and then impale the insulation, or by using pre-attached heads and welding them through the insulation.

- Fasten anchors to wall with adhesive. Follow manufacturer's recommendations for surface preparation and adhesive pattern.

- Impale insulation on anchor and secure with washer. Select pin lengths to ensure tight fit. Protect pin tips where subject to human contact. See manufacturer's diagram for impaling pin pattern.

C. 	Adhesive Fasteners

Curtainwall and 700 Series Insulation

Apply insulation with adhesives. Follow adhesive manufacturer's

recommendations for surface preparation and adhesive pattern.

D.	Furring Strips

Thermal Batts, Flame Spread 25 and 700 Series Insulation

- Install insulation between furring strips, hat channels, or Z-shaped furring in areas where finish surface will be applied.

- Contact the furring strip manufacturer for recommendations on the appropriate fastener system to use.

E. 	Between Metal Studs

Thermal Batts and Flame Spread 25 Insulation

Friction-fit insulation between studs after cover material has been installed

on one side of the cavity. Use wire or metal straps to hold insulation in place

in applications without a cover material or where the stud depth is larger

than the insulation thickness. When faced insulation is used, the attachment

flanges may be taped to the face of the metal stud prior to applying the interior finish.

- Provide supplementary support to hold the product in place until finish surface is applied when insulation is installed in heights over 8 feet.

F. Between Wood Studs

Thermal Batts and Flame Spread 25 Insulation

Friction-fit unfaced insulation between studs after cover material has been installed on one side of the cavity. Use wire or metal straps to hold insulation in place in applications without a cover material. When faced insulation is used staple attachment flanges to face or side of stud every 8 to 12 inches to prevent gaps along the edge of the vapor retarder.

3.03 	Installation - Vapor Retarders

The architect or specifier should evaluate the requirements of each project before making decisions about the use and placement of vapor retarders.

Maintain vapor retarder integrity by tightly abutting adjacent insulation.

Repair punctures or tears in vapor retarder facing by taping. Follow tape

manufacturer's application recommendations.

3.04 	Material Storage and Protection

Protect insulation from damage and from becoming wet before, during and after installation.