Owens-Corning

Commercial Insulation

ProSpec

Welcome to Owens-Corning's digitized Commercial Insulation Specifications.  ProSpec provides editable insulation specifications for a wide range of interior partition, exterior wall and roof/ceiling assembly applications.

ProSpec includes directions for the specification writer and product data that can be easily selected for insertion in your project specifications.

Directions for the specification writer and product data boxes are eliminated by turning the toggle off. (Tools, Option, Hidden Text) Turning the toggle on restores the on screen directions and product data.

To add product data from these product data boxes, choose text and insert in the specification text.

If you have questions regarding our products, applications or installation please call us at 1-800-GET-PINK.

# Section 07200

# Roof/Ceiling Thermal

# Insulation

Part 1 	General

# 1.01 	Summary

- Provide glass fiber thermal insulation for (roof) (ceiling) assembly

as indicated in building plans.

# 1.02 	Materials Provided in Other Sections

# These sections are typically cross referenced. Delete section(s) not included in project manual.

A.	Section 03500-Cementitious Decks

B.	Section 05300-Metal Decking

C.	Section 07410-Preformed Roof and Wall Panels

D.	Section 07500-Membrane Roofing

E.	Section 07610-Metal Roofing

F.	Section 09120-Ceiling Suspension Systems

G.	Section 09500-Acoustical Treatment

H.	Section 09545-Special Ceiling Finish Panels

# 1.03 	References

A. American Society for Testing and Materials (ASTM).

1.	E 84 Test Method for Surface Burning Characteristics of Building Materials.

2.	E 96 Test Method for Water Vapor Transmission of Materials

3.	E 136 Test Method for Behavior of Materials in a Vertical Tube Furnace at 750(C.

4.	C 177 Test Method for Steady-State Thermal

Transmission Properties by means of the Guarded Hot Plate

5.	C 423 Test Method for Sound Absorption and the Sound Absorption Coefficient by the Reverberation Room Method

6.	C 518 Test Method for Steady-State Thermal

Transmission Properties by Means of the Heat Flow Meter

7.	C 553 Standard Specification for Mineral Fiber Blanket and Felt Insulations

8.	C 612 Standard Specification for Mineral Fiber Block and Board Thermal Insulation

9.	C 665 Specification for Mineral Fiber Blanket Thermal Insulation for Light Frame Construction and Manufactured Housing.

# 1.04 	Submittals

A.	Product Data: Submit Owens-Corning product literature, samples and

installation instructions for specified insulation.

# 1.05 	Delivery

A.	Protect insulation from physical damage and from becoming wet,

soiled, or covered with ice or snow. Comply with manufacturer's

recommendations for handling, storage and protection during

installation.

B.	Label insulation packages to include material name, production

date and/or  product code.

# Delete paragraph below if section 01600 or 01620 are not included in project manual.

C.	Deliver and store materials under provision of Section (01600) (01620).

# 1.06 	Limitations

A.	Do not use unfaced insulation in exposed applications where there

is potential for skin contact and irritation.

B.	Kraft and standard foil facings will burn and must not be left

exposed. The facing must be installed in substantial contact with

the unexposed surface of the ceiling finish material. Protect facing from

any open flame or heat source.

Part 2 	Products

# 2.01 	Manufacturer

A.	Owens-Corning.

# 2.02 	700 Series Insulation

A.	Type: 701 Unfaced glass fiber thermal insulation complying

with ASTM C 553, Type III and ASTM C 665, Type I.

B.	Type: 711 Unfaced glass fiber thermal insulation complying

with ASTM C 553, Type III and ASTM C 665, Type I.

C.	Type: 703 Unfaced, FRK (foil) faced or ASJ (white) faced glass fiber

thermal insulation complying with ASTM C 612, Type 1A and 1B.

D.	Type: 705 Unfaced, FRK (foil) faced or ASJ (white) faced glass fiber

thermal insulation complying with ASTM C 612, Type 1A and 1B.

E.	Size:  R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length____

Thickness		   Width		        Length	    R-value

1"		25mm		24"  609mm	    48"  1219mm+       4.2

1½" 	38mm		24"  609mm     	    48"  1219mm	       6.3

Type	2"		51mm		24"  609mm	    48"  1219mm	       8.3

701		2½" 	64mm		24"  609mm     	    48"  1219mm	      10.4

3"		76mm		24"  609mm	    48"  1219mm	      12.5

3½" 	89mm		24"  609mm     	    48"  1219mm	      14.6

4"		102mm		24"  609mm	    48"  1219mm	      16.7

1"		25mm		24"  609mm	    48"  1219mm+       4.0

1½" 	38mm		24"  609mm     	    48"  1219mm	       6.0

Type	2"		51mm		24"  609mm	    48"  1219mm	       8.0

711		2½" 	64mm		24"  609mm     	    48"  1219mm	      10.0

3"		76mm		24"  609mm	    48"  1219mm	      12.0

4"		102mm		24"  609mm	    48"  1219mm	      16.0

1"		25mm		24"  609mm	    48"  1219mm+       4.3

Type	1½" 	38mm		24"  609mm     	    48"  1219mm	       6.5

703		2"		51mm		24"  609mm	    48"  1219mm	       8.7

2½" 	64mm		24"  609mm     	    48"  1219mm	      10.9

Type	3"		76mm		24"  609mm	    48"  1219mm	      13.0

705		3½" 	89mm		24"  609mm     	    48"  1219mm	      15.2

4"		102mm		24"  609mm	    48"  1219mm	      17.4

F.	Vapor Retarder Perm Rating:

1.	FRK (foil) facing Perms Maximum 0.02

2.	ASJ (white) facing Perms Maximum 0.02

When tested in accordance with ASTM C 1136.

G.	Surface Burning Characteristics:

Maximum flame spread:  25

Maximum smoke developed:  50

When tested in accordance with ASTM E 84.

Flame	      Smoke

Spread	     Developed

701 Unfaced			20		20

711 Unfaced			20		20

703 Unfaced			15		0

703 ASJ-faced		25		50

703 FRK-faced		25		50

705 Unfaced			15		0

705 ASJ-faced		25		50

705 FRK-faced		25		50

H.	Noise Reduction Coefficient: 	NRC___

When tested in accordance with ASTM C 423 on a Type A mounting.

NRC

Type					1"	25mm			0.70

701/711 Unfaced			2"	51mm			0.90

3"	76mm			1.15

Type					1"	25mm			0.70

703 Unfaced			2"	51mm			1.00

3"	76mm			1.10

Type					1"	25mm			0.65

705 Unfaced			2"	51mm			0.95

3"	76mm			1.10

Type					1"	25mm			0.65

703 FRK-faced			2"	51mm			0.75

Type					1"	25mm			0.55

705 FRK-faced			2"	51mm			0.60

Type					1"	25mm			0.65

703 ASJ-faced			2"	51mm			0.75

Type					1"	25mm			0.50

705 ASJ-faced			2"	51mm			0.65

I.	Dimensional Stability:

Linear shrinkage less than 0.1%

# 2.03 	Flame Spread 25 Insulation

A.	Type: FRK (foil) or PSK (white) faced glass fiber thermal insulation complying with

ASTM C 665,  Type III, Class A.

B.	Size:

# Metal Frame Insulation

# R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length____

Thickness			   Width				Length	   	   R-value

3½"    89mm		16"  406mm  	24"  609mm	       96"  2438mm	       11.0

3½"    89mm		16"  406mm  	24"  609mm	       96"  2438mm	       13.0

6¼"    159mm		16"  406mm  	24"  609mm	       96"  2438mm	       19.0

# Wood Frame Insulation

# R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length____

Thickness			   Width				Length	 	   R-value

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       11.0

3½"    89mm		15"  381mm  	23"  584mm	       93"  2362mm	       13.0

6¼"    159mm		15"  381mm  	23"  584mm	       93"  2362mm	       19.0

# Special Application Insulation

# R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length____

Thickness		     	    Width			Length	    	R-value

9½"    241mm		16"  406mm  	24"  609mm	48"  1219mm	       30.0

6¼"    159mm		48"  1219mm		      	40'   12.19m	       19.0

3½"    89mm		48"  1219mm		      	72'   21.95m	       11.0

C.	Vapor Retarder Perm Rating:

FRK (foil) facing Perms Maximum 0.10

PSK (white) facing Perms Maximum 0.10

When tested in accordance with ASTM E 96.

D. Surface Burning Characteristics:

Maximum flame spread: 25

Maximum smoke developed: 50

When tested in accordance with ASTM E 84.

E. 	Combustion Characteristics:

Classified non-combustible by model building codes.

Not required to be covered.  May be left exposed.

F. 	Dimensional Stability:

Linear shrinkage less than 0.1%

# 2.04 	Sonobatts® Insulation

A.	Type: Unfaced glass fiber insulation complying with

ASTM C 665, Type I.

B.	Type: Kraft faced glass fiber insulation complying with

ASTM C 665, Type II, Class C.

C.	Size: R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length____

Thickness		    Width		     Length			R-value

3½"    89mm		24"   609mm	       	48"  1219mm       	11.0

6¼"    159mm		24"   609mm		48"  1219mm		19.0

9½"    241mm		24"   609mm		48"  1219mm		30.0

12"     305mm		24"   609mm		48"  1219mm	 	38.0

D.	Vapor Retarder Perm Rating:

Kraft-facing Perms Maximum 1.00

When tested in accordance with ASTM E 96.

E.	Surface Burning Characteristics:

1. 	Unfaced Insulation

Maximum flame spread: 10

Maximum smoke developed: 10

- Kraft Faced Insulation

Maximum flame spread:  Not Rated

Maximum smoke developed:  Not Rated

When tested in accordance with ASTM E 84.

Kraft facings on this insulation will burn and must not be left exposed. The facing must be installed in substantial contact with the unexposed surface of the ceiling finish material. Protect facing from any open flame or heat source.

F. 	Combustion Characteristics:

Unfaced insulation passes ASTM E 136.

G. Dimensional Stability:

Linear shrinkage less than 0.1%

# 2.05 	Thermal Batt Insulation

A.	Type: Unfaced glass fiber thermal insulation complying with

ASTM C 665, Type I.

B.	Type: Kraft-faced glass fiber insulation complying with

ASTM C 665, Type II, Class C.

C.	Type: Foil-faced glass fiber thermal insulation complying with

ASTM C 665, Type III, Class B and C.

D.	Size:

# Metal Frame Insulation

# R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness			   Width			Length	    	R-value

6¼"    159mm		16"  406mm  	24"  609mm	96"  2438mm	       19.0

# Wood Frame Insulation

# R-Value____

When tested in accordance with ASTM C 518.

Thickness____ Width____ Length ____

Thickness			   Width			Length	   	 R-value

6¼"    159mm		15"   381mm   23"  584mm      93"  2362mm	      19.0

9½"    241mm		16"   406mm   24"  609mm      48"  1219mm	      30.0

12"     305mm		16"   406mm   24"  609mm      48"  1219mm	      38.0C

8¼"    209mm		15½" 394mm  23¾" 603mm     48"  1219mm	      30.0C			10¼"   260mm	15½" 394mm  23¾"  603mm      48"  1219mm	      38.0C

E. 	Vapor Retarder Perm Rating:

1.	Foil-facing Perms Maximum 0.50

2.	Kraft-facing Perms Maximum 1.00

When tested in accordance with ASTM E 96.

F. 	Surface Burning Characteristics:

1.	Unfaced Insulation

Maximum flame spread: 10

Maximum smoke developed: 10

2.	Foil-Faced Insulation

Maximum flame spread: 75

Maximum smoke developed: 150

When tested in accordance with ASTM E 84.

- Kraft Faced Insulation

Maximum flame spread:  Not Rated

Maximum smoke developed:  Not Rated

Kraft and standard foil facings on this insulation will burn and must not be left exposed. The facing must be installed in substantial contact with an approved roof/ceiling construction material. Protect facing from any open flame or heat source.

G. 	Combustion Characteristics:

Unfaced Insulation Passes ASTM E 136.

H. 	Dimensional Stability:

Linear shrinkage less than 0.1%

# 2.06	Quiet Zone Acoustic Batts

A.	Type: Kraft faced glass fiber acoustical insulation complying with

ASTM C 665,  Type II, Class C.

B.	Size:

Thickness___ Width___ Length___

Thickness		        Width		  Length

3½"    89mm	   16"  406mm     24"  609mm    	 96"  2438mm

2½"    64mm	   16"  406mm     24"  609mm     	 96"  2438mm

C.	Surface Burning Characteristics:

1.	Maximum flame spread:  Not Rated

2.	Maximum smoke developed:  Not Rated

When tested in accordance with ASTM E 84.

# Kraft facing on this insulation will burn and

must not be left exposed. The facing must be installed in substantial

contact with the unexposed surface of the ceiling finish material.

# Protect facing from any open flame or heat source.

D.	Sound Transmission Class:  STC___

# Select STC from Wall System Chart included in the ProSpec Introduction & Instruction Package.

E.	Dimensional Stability:

Linear Shrinkage less than 0.1%

# 2.07 	Other Materials

Provide materials, not specifically described but required for a

complete and proper installation of the work in this section.

Part 3 	Execution

# 3.01 	Inspection and Preparation

A.	Examine the areas and conditions under which work of this section

will be installed. Verify that adjacent materials are dry and ready to

receive insulation. Verify mechanical and electrical services within

the above ceiling space have been tested and inspected.

B.	Provide written report listing conditions detrimental to performance

of work in this section. Do not proceed with installation until

unsatisfactory conditions have been corrected.

3.02 	Installation - General

A.	Comply with manufacturer's instructions for particular conditions

of installation in each case.

B.	Under Roof Decks

# 700 Series and Flame Spread 25

Apply insulation directly to the interior surface of the underside of roof deck with appropriate spindle or prong-type anchors.

- Fasten anchors to deck by welding the pin to metal and then impale the insulation, or by using pre-attached heads and welding them through the insulation.

- Fasten anchors to deck with adhesive. Follow manufacturer's recommendations for surface preparation and adhesive pattern.

- Impale insulation on anchor and secure with washer. Select pin lengths to ensure tight fit. Protect pin tips where subject to human contact. See manufacturer's diagram for impaling pin pattern.

C. Between Open Web Bar Joists

Flame Spread 25 Insulation

Wire up insulation under roof decks by running 16 or 18 gauge wire diagonally or perpendicular to the insulation every 18 to 24 inches.

D.	Between Wood Roof Rafters

Flame Spread 25 Insulation

Staple insulation to the bottom face of the roof rafter at 8 to 12 inch intervals.

Flame Spread 25 Insulation with Extended Flanges

Staple the first flange on inside face of roof rafter. Staple every 6-8" apart

with a staple within 1" of each end of the batt. Position batt in cavity and

staple the other flange to the adjoining rafter.

E.	Over Suspended Ceilings

# Sonobatts® Insulation

# Install insulation over ceiling panels. Butt insulation together tightly to

# prevent thermal leaks.

# 3.03 	Installation - Vapor Retarders

The architect or specifier should evaluate the requirements of each project before making decisions about the use and placement of vapor retarders.

Maintain vapor retarder integrity by tightly abutting adjacent insulation.

Repair punctures or tears in vapor retarder facing by taping. Follow tape

manufacturer's application recommendations.

# 3.04 	Material Storage and Protection

Protect insulation from damage and from becoming wet before, during and after installation.

# END OF SECTION