Product Information Sheet

TRUMBULL

BUILT-UP ROOFING ASPHALT

Description

Trumbull's Built-Up Roofing Asphalt products are manufactured from selected petroleum based materials and processed to various softening points and penetrations, meeting required specifications.   It is supplied in tank vehicles and cartons.

Typical Physical Properties

| Property | Range |
| --- | --- |
|  | Type I | Type II | Type III | Type IV |
| Color | - - - - - - - -Dark Brown to Black - - - - - - - |
| Softening Point ASTM D-36 | 135-151oF | 158-176oF | 185-205oF | 210-225oF |
| ASTM D-5 Penetration @ 77oF 100 grams, 5 sec. | 18-60 dmm | 18-40 dmm | 15-35 dmm | 12 - 25 dmm |
| ASTM D-5 Penetration @ 115oF 50 grams, 5 sec. | 90-180 dmm | 100 dmm max. | 90 dmm max. | 75 dmm max. |
| Flash Point (COC) ASTM D-92 | - - - - - - - - - - 500oF minimum - - - - - - - - - - |
| Solubility in trichloroethylene (%) | - - - - - - - - - - 99.0 minimum - - - - - - - - - - |

1/99

Asphalt Technology Lab - 7800 West 59th Street - Summit, IL 60501 - 708.594.6971