Section 09820

SelectSound Acoustic Blanket

Part 1	General

1.1	Section Includes

A. 	Acoustical Blanket Material -''SelectSound Acoustic blanket"

1.2	Related Sections

A.	Section 03000 - Cast-in-place Concrete: Surface attachment to concrete walls or deck for improved sound absorption.

B.	Section 04200 - Masonry Units: Surface attachment to masonry wall for improved sound absorption.

C.	Section 05300 - Metal Decking: Surface attachment to underside of metal deck for improved sound absorption.

D.	Section 09500 - Acoustical Metal Ceilings: Sound-absorptive core material for perforated metal suspended ceiling systems.

E.	Section 09260 - Gypsum Board Assemblies: Surface attachment to gypsum board partitions for improved sound absorption.

1.3	References

A.	ASTM C423 - Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

B.	UL 723 - Test for Surface Burning Characteristics of Building Materials.

C.	ASTM C553, Type I - Specification for Mineral Fiber Blanket Thermal Insulation for Commercial and Industrial Applications.

D.	ASTM C1104 - Test Method for Determining the Water Vapor Sorption of Unfaced Mineral Fiber Insulation.

E.	ASTM C1338 - Standard Test Method for Determining Fungi Resistance of Insulation Materials and Facings.

F.	ASTM C665 - Standard Specification for Mineral-Fiber Blanket Thermal Insulation for Light Frame Construction and Manufactured Housing.

1.4	Product Description

A.	SelectSound Acoustic Blanket is a lightweight and resilient insulation material with a black mat faced finish that can be used for eliminating sound and light reflections or for preventing insulation from showing through most surface treatments.

- SelectSound Acoustic Blanket is excellent for multiplex theaters and other cinematic spaces, yet can also be used for Performance Spaces, Churches, Museums, Amusement Parks, Sports Complexes, Sound Studios and any other project where a non-reflective finished surface and good acoustical performance is required.

  - Performance Requirements

A.	Product shall be available in standard thickness of 1" and 2", and in standard densities of 1.5 pcf (Type 150) and 2.0 pcf. (Type 200). Special orders for 1.5", Type 150 are also available.

B.	Blankets shall be available in rolls of 48" standard width, and in lengths of 100' for 1 " thickness and 50' for 2" thickness.

C.	Product shall be dimensionally stable with no capability for shrinking or warping.

D.	Product shall have a resilient composition with good resistance to damage from job-site impact.

E.	Product shall be composed of inorganic glass fibers.

F.	Product's mat face shall be able to be cleaned by vacuuming.

G.	Product shall not be susceptible to rot or mildew contamination.

H.	Product shall not cause corrosion greater than caused by sterile cotton to steel and aluminum, when tested in accordance with ASTM C665.

I.	Acoustical Performance (Tested to ASTM C423, Type A mounting).

| Product | Density | Thickness | Octave Band Center Frequencies, Hz |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | pcf (kg/m3) | in (mm) | 125 | 250 | 500 | 1000 | 2000 | 4000 | NRC |
| SelectSound 150 | 1.5 (24) | - (25) - (51) | 0.15 0.20 | 0.25 0.53 | 0.45 0.79 | 0.68 0.94 | 0.79 0.95 | 0.81 0.97 | 0.55 0.80 |
| SelectSound 200 | 2.0 (32) | 1.0 (25) 2.0 (51) | 0.11 0.20 | 0.28 0.55 | 0.49 0.87 | 0.70 1.00 | 0.81 0.95 | 0.86 0.95 | 0.55 0.85 |

- Surface Burning of Core Material (tested to UL 723, or CANIULC-S102-M):

- Flame spread 25, smoke developed 50 (Class A).

- Water vapor sorption - by weight (Tested to ASTM C1104):

- <3% at 120°F (49°C) at 95% relative humidity.

- Fungi resistance

1.	Meets all requirements of ASTM C1338.

1.6	Submittals

A.	Product Data: Submit to requirements of Section 01XXX.

B.	Product Data: Manufacturer's descriptive literature for SelectSound Acoustic Blanket, including component item data, physical sizes, material densities, fastening and attachment methods.

C.	Samples:

- Submit to requirements of Section 01XXX.

- Submit two samples, 125mm x 250mm (6" x 10"), of each specified type of Acoustic Blanket.

D.	Manufacturer's Certificate: Provide to requirements of Section 01XXX that products meet or exceed specified requirements.

1. 	Certify system acoustical and fire resistance performance.

2. 	Certify that installers have been trained and are qualified to install the system.

- Manufacturer's Installation Instructions: Provide to requirements of Section 01XXX.

1.7	Quality Assurance

A. 	Installer: Experienced in the installation of building insulation and acoustical materials.

B. 	Test Reports: Submit tests reports from a NVLAP accredited testing laboratory indicating that the system has passed all noted fire resistance requirements and acoustical requirements.

1.8	Regulatory Requirements

A. 	Conform to applicable code for fire rated panel construction and combustibility requirements for materials.

1.9	Delivery, Storage And Handling

A.	Inspect material upon arrival to the site. Immediately log damaged materials with the shipping company and report to the manufacturer. Report flaws or defects in the material to the manufacturer within 24 hours of delivery.

B.	Store material in a secure, dry, clean, and dust free environment away from high traffic areas. Store material in such a manner to prevent damage to insulation core or mat faced finish. (Do not pile material on top of other components.)

C.	Keep material in its original packaging until installation.

# Part 2    Products

2.1	Manufacturer

A. 	SelectSound Acoustic Blanket, by Owens Corning, One Owens Corning Parkway, Toledo, Ohio 43659, Tel: 1-800-GET-PINK, www.owenscorning.com

B.	Substitutions: Not accepted.

## Part 3    Execution

  - Examination

A.	Verify that adjacent materials and surfaces are dry, in a dust free environment, free of obstructions, and ready to receive Acoustic Blanket installation.

B.	Verify painting, finish woodwork, wiring runs, and flooring is complete prior to Acoustic Blanket installation.

C.	Verify that special standouts and furring for wall trim details or additional wall support items are installed.

D.	Verify wall penetrations have been sealed, where applicable.

3.2	Preparation

A. 	Provide written report listing conditions detrimental to performance of work in this section. Do not proceed with installation until unsatisfactory or unsafe conditions have been corrected.

B. 	Confirm to the manufacturer that the site has been properly prepared prior to installation.

3.3	Installation

A.	Install SelectSound Acoustic Blanket to drywall, concrete block, precast concrete or other manufacturer-approved surfaces using impaling pins or construction adhesives.

B.	When installing with adhesive, follow adhesive manufacturer’s recommendations for surface preparation and pattern prior to installation.

C.	When installing with impaling pins, follow pin manufacturer's recommendations for surface preparation, location and spacing of pins. Pin length shall be selected to ensure tight fit. Where subject to contact, protect pin tips.

3.4	Cleaning

- Clean finish surfaces of Blanket. Remove foreign objects from material.

3-IN-44100-C   Copyright © 2002 OWENS CORNING