Product Information Sheet

TRUMBULL

WATERPROOFING ASPHALTS

ASTM D-449-94

Uses

Trumbull  Waterproofing products are suitaable for use as a mopping coat in damproofing, or as a plying or mopping cement in the construction of membrane waterproofing systems and with felts and glass mats

Description

Trumbull Waterproofing producst are manufactured from selected petroleum based materials, processed to various softening points and penetrations, meeting required specifications.

Typical Physical Properties

| Property |  |  |  |
| --- | --- | --- | --- |
| Grade Code Number | Below Grade Type I #3201 | Above or Below Grade Type II #3200 | Above Grade Type III #3203 |
| Color | ............Dark Brown to Black............ |  |  |
| Softening Point, ASTM D-36 | 115oF - 140oF | 145oF - 170oF | 180oF - 200oF |
| Penetration @ 77oF, 100 grams, 5 sec. ASTM D-5 | 50 - 100 | 25 -50 | 20 - 40 |
| Penetration @ 32oF, 200 grams, 60 sec. ASTM D-5 | 5 min. | 10 min. | 10 min. |
| Penetration @ 115oF, 50 grams, 5 sec. ASTM D-5 | 100 min. | 130 min. | 100. max. |
| Ductility @ 77oF, (centimeters) ASTM D-113 | 30 min. | 10 min. | 2 min. |
| Flash Point (COC), ASTM D-92 | 450 oF min. | 450 oF min. | 450 oF min. |
| Solubility in Trichloroethylene, ASTM D-2042 | 99.0% min. | 99.0% min. | 99.0% min. |

September 1997

Asphalt Technology Lab - Summit, IL 60501 - 708.594.6970