Copyright 2019 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to PABCO Gypsum ("Licensee").

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact PABCO Gypsum, 37851 Cherry St., Newark, CA 94560; Phone: (800) 797-8159; Website: www.PABCOgypsum.com; Email: info@PABCOgypsum.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 092900 - GYPSUM BOARD

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Access Product MasterSpec Sections:

<Double click here to view the list of manufacturer Sections available at ProductMasterSpec.com.>

Access BIM Content on BIMsmith Market:

<Double click here to view products on BIMsmith Market.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Interior gypsum board.

          - Exterior gypsum board for ceilings and soffits.

Tile backing panels in first subparagraph below may be specified in this Section or in Section 093013 "Ceramic Tiling."

          - Tile backing panels.

          - Texture finishes.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 061600 "Sheathing" for gypsum sheathing for exterior walls.

          - Section 079219 "Acoustical Joint Sealants" for acoustical joint sealants installed in gypsum board assemblies.

          - Section 092116.23 "Gypsum Board Shaft Wall Assemblies" for metal shaft-wall framing, gypsum shaft liners, and other components of shaft-wall assemblies.

Add Section 092116.33 "Gypsum Board Area Separation Wall Assemblies" if your Firm Master library of sections includes this section.

          - Section 092216 "Non-Structural Metal Framing" for non-structural steel framing and suspension systems that support gypsum board panels.

          - Section 092613 "Gypsum Veneer Plastering" for gypsum base for veneer plaster and for other components of gypsum-veneer-plaster finishes.

Retain subparagraph below if tile backing panels are not specified in this Section.

          - Section 093013 "Ceramic Tiling" for cementitious backer units installed as substrates for ceramic tile.

      - ACTION SUBMITTALS

        - Product Data: For the following:

          - Gypsum wallboard.

          - Gypsum board, Type X.

          - Flexible gypsum board.

          - Gypsum ceiling board.

          - Foil-backed gypsum board.

          - Abuse-resistant gypsum board.

          - Impact-resistant gypsum board.

          - Mold-resistant gypsum board.

          - Gypsum board, Type C.

          - Glass-mat interior gypsum board.

          - Acoustically enhanced gypsum board.

          - Skim-coated gypsum board.

          - Exterior gypsum soffit board.

          - Glass-mat gypsum sheathing board.

          - Glass-mat, water-resistant backing board.

          - Cementitious backer units.

          - Water-resistant gypsum backing board.

          - Interior trim.

          - Exterior trim.

          - Aluminum trim.

          - Joint treatment materials.

          - Laminating adhesive.

          - Sound-attenuation blankets.

          - Acoustical sealant.

          - Textured finishes.

For PABCO's sustainability documentation, see www.pabcogypsum.com/document-library.

        - Sustainable Design Submittals:

Retain "Product Data" Subparagraph below to require minimum recycled content for LEED 2009, MRc 2, "Recycled Content."

          - Product Data: For recycled content, indicating postconsumer and preconsumer recycled content and cost.

First "Product Certificates" Subparagraph below applies to LEED 2009, MRc 5, "Regional Materials."

          - Product Certificates: For regional materials, indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include distance to Project and cost for each regional material.

First "Product Certificates" Subparagraph below applies to LEED v4, MRc "Building Product Disclosure and Optimization - Environmental Product Declarations, Option 2."

          - Product Certificates: For materials manufactured within 100 miles (160 km) of Project, indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include distance to Project and cost for each raw material.

"Product Certificates" Subparagraph below applies to IgCC, which requires that a minimum of 55 percent of building materials or products be extracted, harvested, manufactured, or recovered within 500 miles (800 km) of Project. See IgCC-2012, 505.2.5.

          - Product Certificates: For indigenous materials, indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include distance to Project, means of transportation, and cost for each indigenous material.

"Product Data" Subparagraph below applies to LEED 2009 NC, CI, and CS; LEED v4; IgCC; and Green Globes. Coordinate with requirements for adhesives and sealants.

          - Product Data: For adhesives and sealants, indicating VOC content.

First "Laboratory Test Reports" Subparagraph below applies to LEED 2009 for Schools, LEED v4, IgCC, and Green Globes. Coordinate with requirements for adhesives and sealants.

          - Laboratory Test Reports: For adhesives and sealants, indicating compliance with requirements for low-emitting materials.

"Laboratory Test Reports" Subparagraph below applies to LEED 2009 for Schools, IEQc 4.6.

          - Laboratory Test Reports: For ceiling and wall materials, indicating compliance with requirements for low-emitting materials.

Retain "Samples" Paragraph below for single-stage Samples. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For the following products:

Retain "Trim Accessories" Subparagraph below if special trim types and profiles are required. Delete if only standard-type trims are required.

          - Trim Accessories: Full-size Sample in 12-inch- (300-mm-) long length for each trim accessory indicated.

          - Textured Finishes: [Manufacturer's standard size] <Insert size> for each textured finish indicated and on same backing indicated for Work.

Retain "trim accessory" option in "Samples for Initial Selection" Paragraph below if special trim types and profiles are required. Delete if only standard-type trims are required.

        - Samples for Initial Selection: For each type of [trim accessory] [and] [textured finish] indicated.

        - Samples for Verification: For the following products:

Retain "Trim Accessories" Subparagraph below if special trim types and profiles are required. Delete if only standard-type trims are required.

          - Trim Accessories: Full-size Sample in 12-inch- (300-mm-) long length for each trim accessory indicated.

          - Textured Finishes: [Manufacturer's standard size] <Insert size> for each textured finish indicated and on same backing indicated for Work.

      - QUALITY ASSURANCE

        - Mockups: Build mockups of at least 100 sq. ft. (9 sq. m) in surface area to demonstrate aesthetic effects and to set quality standards for materials and execution.

          - Build mockups for the following:

            - Each level of gypsum board finish indicated for use in exposed locations.

            - Each texture finish indicated.

          - Apply or install final decoration indicated, including painting and wallcoverings, on exposed surfaces for review of mockups.

          - Simulate finished lighting conditions for review of mockups.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE AND HANDLING

For PABCO's product handling and storage recommendations, see www.pabcogypsum.com/sites/default/files/GA-801-2017.pdf.

        - Deliver, store, and handle in accordance with manufacturer's written instructions.

          - Store materials inside under cover and keep them dry and protected against weather, condensation, direct sunlight, construction traffic, and other potential causes of damage.

          - Store within temperature limits.

          - Stack panels flat and supported on risers on a flat platform to prevent sagging.

      - FIELD CONDITIONS

        - Environmental Limitations: Comply with ASTM C840 requirements or gypsum board manufacturer's written instructions, whichever are more stringent.

        - Do not install paper-faced gypsum panels until installation areas are enclosed and conditioned.

        - Do not install panels that are wet, moisture damaged, and mold damaged.

          - Indications that panels are wet or moisture damaged include, but are not limited to, discoloration, sagging, or irregular shape.

          - Indications that panels are mold damaged include, but are not limited to, fuzzy or splotchy surface contamination and discoloration.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - PERFORMANCE REQUIREMENTS

Retain "Fire-Resistance-Rated Assemblies" Paragraph below where gypsum board is part of fire-resistance-rated assemblies. Indicate design designations of specific assemblies on Drawings.

        - Fire-Resistance-Rated Assemblies: For fire-resistance-rated assemblies, provide materials and construction identical to those tested in assembly indicated in accordance with ASTM E119 by an independent testing agency.

Retain "STC-Rated Assemblies" Paragraph below where gypsum board is part of STC-rated assemblies. Indicate design designations of specific assemblies on Drawings.

        - STC-Rated Assemblies: For STC-rated assemblies, provide materials and construction identical to those tested in assembly indicated in accordance with ASTM E90 and classified in accordance with ASTM E413 by an independent testing agency.

First paragraph below applies to LEED 2009 for Schools, IEQc 4.6.

        - Ceiling and wall materials shall comply with the requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First paragraph below applies to LEED v4.

        - Ceiling and wall materials shall comply with the requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Paragraph below applies to IgCC.

        - Ceiling and wall materials shall comply with the requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." Formaldehyde emissions shall not exceed 16.5 mcg/cu. m or 13.5 ppb, whichever is less.

      - GYPSUM BOARD, GENERAL

Retain "Recycled Content" Paragraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

        - Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

First "Regional Materials" Paragraph below applies to LEED 2009 NC, CS, and LEED 2009 for Schools, MRc 5, and to LEED 2009 CI, MRc 5, Option 2; before retaining, verify availability of materials that comply.

        - Regional Materials: Products shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

First "Regional Materials" Paragraph below applies to LEED 2009 CI, MRc 5, Option 1.

        - Regional Materials: Products shall be manufactured within 500 miles (800 km) of Project site.

"Regional Materials" Paragraph below applies to LEED v4.

        - Regional Materials: Products shall be manufactured within 100 miles (160 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 100 miles (160 km) of Project site.

"Indigenous Materials" Paragraph below applies to IgCC; before retaining, verify availability of materials that comply.

        - Indigenous Materials: Products shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site. If materials are transported by rail or water, the distance transported by rail or water shall be multiplied by 0.25 to determine the distance to Project site.

        - Size: Provide maximum lengths and widths available that will minimize joints in each area and that correspond with support system indicated.

      - INTERIOR GYPSUM BOARD

        - Gypsum Wallboard: ASTM C1396/C1396M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO [LITECORE] [Regular] or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Retain first, second, or third option in "Thickness" Subparagraph below for "PABCO Regular"; retain third option for "PABCO LITECORE."Thickness: [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)].

          - Long Edges: [Tapered] [Tapered and featured (rounded or beveled) for prefilling].

        - Gypsum Board, Type X: ASTM C1396/C1396M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO FLAME CURB Type X or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Thickness: [5/8 inch (15.9 mm)] [3/4 inch (19 mm)].

          - Long Edges: [Tapered] [Tapered and featured (rounded or beveled) for prefilling].

        - Flexible Gypsum Board: ASTM C1396/C1396M. Manufactured to bend to fit radii and to be more flexible than standard regular-type gypsum board of same thickness.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO FLEX or comparable product by one of the following:

PABCO's 3/8-inch- (9.5-mm-) thick "PABCO FLEX" board does not currently have a true or comparable equal; contact PABCO for equivalents.

            - <Insert manufacturer's name>.

          - Thickness: 3/8 inch (9.5 mm).

          - Long Edges: Tapered.

        - Gypsum Ceiling Board: ASTM C1396/C1396M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO [Interior Ceiling] [LITECORE] [SOUND CURB] or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

Retain first option in "Thickness" Subparagraph below for "PABCO Interior Ceiling" or "PABCO LITECORE"; retain second option for "PABCO SOUND CURB."

          - Thickness: [1/2 inch (12.7 mm)] [3/4 inch (19 mm)].

          - Long Edges: [Round] [Tapered].

The foil backing on gypsum board in "Foil-Backed Gypsum Board" Paragraph below creates a vapor barrier. Verify limitations and proper uses with manufacturers.

        - Foil-Backed Gypsum Board: ASTM C1396/C1396M.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - CertainTeed Gypsum.

            - Continental Building Products, LLC.

            - Georgia-Pacific Gypsum LLC.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [As indicated on Drawings] [3/8 inch (9.5 mm), regular type] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X] [Type C as required by fire-resistance-rated assembly indicated on Drawings].

          - Long Edges: [Tapered] [Tapered and featured (rounded or beveled) for prefilling].

"Abuse-Resistant Gypsum Board" Paragraph below describes products tested in accordance with ASTM C1629/C1629M for resistance to abrasion, indentation, and soft-body impact. See "Abuse- and Impact-Resistant Gypsum Board" Article in the Evaluations for additional information. Verify availability with manufacturers.

        - Abuse-Resistant Gypsum Board: ASTM C1396/C1396M gypsum board, tested in accordance with ASTM C1629/C1629M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO ABUSE CURB or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: 5/8 inch (15.9 mm), Type X.

          - Surface Abrasion: ASTM C1629/C1629M, meets or exceeds Level 2 requirements.

          - Indentation: ASTM C1629/C1629M, meets or exceeds Level 1 requirements.

          - Soft-Body Impact: ASTM C1629/C1629M, meets or exceeds Level 1 requirements.

          - Long Edges: Tapered.

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

"Impact-Resistant Gypsum Board" Paragraph below describes products tested in accordance with ASTM C1629/C1629M for resistance to abrasion, indentation, and soft- and hard-body impact. See "Abuse- and Impact-Resistant Gypsum Board" Article in the Evaluations for additional information. Verify availability with manufacturers.

        - Impact-Resistant Gypsum Board: ASTM C1396/C1396M gypsum board, tested in accordance with ASTM C1629/C1629M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO Impact Resistant or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: 5/8 inch (15.9 mm), Type X.

          - Surface Abrasion: ASTM C1629/C1629M, meets or exceeds Level 2 requirements.

          - Indentation: ASTM C1629/C1629M, meets or exceeds Level 1 requirements.

          - Soft-Body Impact: ASTM C1629/C1629M, meets or exceeds Level 3 requirements.

          - Hard-Body Impact: ASTM C1629/C1629M, meets or exceeds Level 3 requirements in accordance with test in Annex A1.

          - Long Edges: Tapered.

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

        - Mold-Resistant Gypsum Board: ASTM C1396/C1396M. With moisture- and mold-resistant core and paper surfaces.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

For acoustically enhanced mold-resistant gypsum board, see PABCO's "QuietRock ES MR" at 2.4, C.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO MOLD CURB Plus or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [As indicated] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

          - Long Edges: Tapered.

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

      - SPECIALTY GYPSUM BOARD

Type C gypsum board has fire-resistive capability greater than that of Type X. Design designations of independent testing agencies indicated on Drawings generally determine product requirements for Type C gypsum board. Type C gypsum board from different manufacturers cannot be intermixed because the ratings apply only to assemblies identical in materials and construction to those tested.

        - Gypsum Board, Type C: ASTM C1396/C1396M. Manufactured to have increased fire-resistive capability.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO FLAME CURB [Super C] [Type C] or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Thickness: [1/2 inch (12.7 mm), Super C] [5/8 inch (15.9 mm), Type C].

          - Long Edges: Tapered.

        - Glass-Mat Interior Gypsum Board: ASTM C1658/C1658M. With fiberglass mat laminated to both sides. Specifically designed for interior use.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO GLASS INTERIOR or comparable product by one of the following:

            - Georgia-Pacific Gypsum LLC.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

          - Long Edges: Tapered.

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

Retain first option in "Acoustically Enhanced Gypsum Board" Paragraph below for "QuietRock 510" and "QuietRock ES"; retain second option for "QuietRock 545."

        - Acoustically Enhanced Gypsum Board: ASTM C1396/C1396M. Multilayer products constructed of [two] [multiple] layers of gypsum boards sandwiching a viscoelastic sound-absorbing polymer core tested in accordance with ASTM C1629/C1629M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; [QuietRock 510] [QuietRock 545] [QuietRock ES] or comparable product by one of the following:

PABCO's "QuietRock 545" acoustically enhanced gypsum board does not currently have a true or comparable equal; contact PABCO for equivalents.

            - CertainTeed Gypsum.

            - National Gypsum Company.

            - <Insert manufacturer's name>.

Retain first option in "Core" Subparagraph below for PABCO's "QuietRock 510"; retain second option for "QuietRock ES"; retain third option for "QuietRock 545."

          - Core: [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X] [3/4 inch (19 mm), Type X] [1-3/8 inch (35 mm), regular type] [As indicated].

          - Long Edges: Tapered.

        - Acoustically Enhanced and Impact-Resistant Gypsum Board: ASTM C1396/C1396M. Multilayer products constructed of two layers of gypsum board sandwiching a viscoelastic sound-absorbing polymer core tested in accordance with ASTM C1629/C1629M.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; QuietRock 530 or comparable product by one of the following:

PABCO's "QuietRock 530" acoustically enhanced and impact-resistant gypsum board does not currently have a true or comparable equal; contact PABCO for equivalents.

            - <Insert manufacturer's name>.

          - Core: 5/8 inch (15.9 mm), Type X.

          - Long Edges: Tapered.

          - Impact Resistance: ASTM C1629/C1629M.

        - Acoustically Enhanced Mold-Resistant Gypsum Board: ASTM C1396/C1396M. Multilayer products constructed of two layers of gypsum board sandwiching a viscoelastic sound-absorbing polymer core with moisture- and mold-resistant core and paper surfaces.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; QuietRock ES MR or comparable product by one of the following:

            - CertainTeed Gypsum.

            - National Gypsum Company.

            - <Insert manufacturer's name>.

          - Core: 5/8 inch (15.9 mm), Type X.

          - Long Edges: Tapered.

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

        - Radio Frequency and Noise Shielding Gypsum Board: ASTM C1396/C1396M. Multilayer products constructed of two layers of gypsum board sandwiching a viscoelastic sound-absorbing polymer core with radio frequency shielding.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; QuietRock 530 RF or comparable product by one of the following:

PABCO's "QuietRock 530 RF" radio frequency and noise shielding gypsum board does not currently have a true or comparable equal; contact PABCO for equivalents.

            - <Insert manufacturer's name>.

          - Core: 5/8 inch (15.9 mm), Type X.

          - Long Edges: Tapered.

          - Radio-Frequency (RF) Shielding Effectiveness: Average field magnitude of RF ranges in accordance with IEEE-299.

            - 30 dB at 20 to 200 MHz.

            - 40 dB at 200 MHz to 1 GHz.

            - 40 dB at 2 to 10 GHz.

        - Skim-Coated Gypsum Board: ASTM C1396/C1396M. Manufactured with a factory-applied skim coat.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by the following:

            - Continental Building Products, LLC.

            - <Insert manufacturer's name>.

          - Core: [As indicated] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

          - Long Edges: Tapered.

      - EXTERIOR GYPSUM BOARD FOR CEILINGS AND SOFFITS

        - Exterior Gypsum Soffit Board: ASTM C1396/C1396M, with manufacturer's standard edges.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO Exterior Soffit or comparable product by one of the following:

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [As indicated] [1/2 inch (12.7 mm), regular type] [1/2 inch (12.7 mm), Super C] [5/8 inch (15.9 mm), Type C] [5/8 inch (15.9 mm), Type X].

          - Long Edges: Tapered.

        - Glass-Mat Gypsum Sheathing Board: ASTM C1177/C1177M, with fiberglass mat laminated to both sides and with manufacturer's standard edges.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO GLASS Sheathing or comparable product by one of the following:

            - Georgia-Pacific Gypsum LLC.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [As indicated] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

      - TILE BACKING PANELS

Tile backing panels may be specified in this Section or in Section 093013 "Ceramic Tiling."

        - Glass-Mat, Water-Resistant Backing Board: ASTM C1178/C1178M, with manufacturer's standard edges.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For "PABCO GLASS INTERIOR" glass-mat, mold- and moisture-resistant backing board submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO GLASS INTERIOR or comparable product by one of the following:

            - Georgia-Pacific Gypsum LLC.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

          - Long Edges: Tapered.

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

        - Cementitious Backer Units: ANSI A118.9 and ASTM C1288 or ASTM C1325, with manufacturer's standard edges.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - C-Cure.

            - CertainTeed Gypsum.

            - Custom Building Products.

            - FinPan, Inc.

            - James Hardie Building Products, Inc.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Thickness: [1/4 inch (6.4 mm)] [1/2 inch (12.7 mm)] [5/8 inch (15.9 mm)] [As indicated].

          - Mold Resistance: ASTM D3273, score of 10 as rated in accordance with ASTM D3274.

In accordance with the International Building Code, water-resistant gypsum backing board is not permitted for use as a backing board for tile in tub and shower areas or as wall board or ceiling panels in shower areas.

        - Water-Resistant Gypsum Backing Board: ASTM C1396/C1396M, with manufacturer's standard edges.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; PABCO MOLD CURB Plus or comparable product by one of the following:

            - Georgia-Pacific Gypsum LLC.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Core: [As indicated on Drawings] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

      - TRIM ACCESSORIES

        - Interior Trim: ASTM C1047.

          - Material: [Galvanized or aluminum-coated steel sheet, rolled zinc, plastic, or paper-faced galvanized-steel sheet] [Galvanized or aluminum-coated steel sheet or rolled zinc] [Plastic] [Paper-faced galvanized-steel sheet].

          - Shapes:

            - Cornerbead.

            - Bullnose bead.

            - LC-Bead: J-shaped; exposed long flange receives joint compound.

            - L-Bead: L-shaped; exposed long flange receives joint compound.

            - U-Bead: J-shaped; exposed short flange does not receive joint compound.

            - Expansion (control) joint.

            - Curved-Edge Cornerbead: With notched or flexible flanges.

Retain "Base-of-Wall Galvanized Moisture Barrier Trim" or "Base-of-Wall PVC Moisture Barrier Trim" Subparagraph below, if required. Verify acceptance of product if used in fire-rated assemblies. PVC product does not have tested assemblies but has an independent engineering judgment letter for 1/2-inch- (12.7-mm-) high material. When this Section was updated, VersaDry was the only manufacturer that manufactured base-of-wall galvanized moisture barrier trim; Waterguard was the only manufacturer that manufactured base-of-wall PVC moisture barrier trim.

            - Base-of-Wall Galvanized Moisture Barrier Trim: Galvanized-steel sheet, 2 inches (50 mm) high.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

              - Manufacturers: Subject to compliance with requirements, provide products by the following:

                - VersaDry, LLC.

                - <Insert manufacturer's name>.

            - Base-of-Wall PVC Moisture Barrier Trim: Extruded PVC, [1/2 inch (12.7 mm)] [1-3/4 inch (44 mm)] [3-1/2 inch (89 mm)] high.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

              - Manufacturers: Subject to compliance with requirements, provide products by the following:

                - Waterguard.

                - <Insert manufacturer's name>.

        - Exterior Trim: ASTM C1047.

          - Material: [Hot-dip galvanized-steel sheet, plastic, or rolled zinc] <Insert material>.

          - Shapes:

            - Cornerbead.

            - LC-Bead: J-shaped; exposed long flange receives joint compound.

            - Expansion (Control) Joint: One-piece, rolled zinc with V-shaped slot and removable strip covering slot opening.

Indicate dimensions and profiles of aluminum trim on Drawings.

        - Aluminum Trim: Extruded accessories of profiles and dimensions indicated.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Flannery, Inc.

            - Fry Reglet Corporation.

            - Gordon, Inc.

            - Pittcon Industries.

            - Tamlyn.

            - <Insert manufacturer's name>.

          - Aluminum: Alloy and temper with not less than the strength and durability properties of ASTM B221 (ASTM B221M), Alloy 6063-T5.

          - Finish: [Corrosion-resistant primer compatible with joint compound and finish materials specified] <Insert requirements for Class II anodic finishes and factory-painted, baked-enamel finishes>.

      - JOINT TREATMENT MATERIALS

        - General: Comply with ASTM C475/C475M.

        - Joint Tape:

          - Interior Gypsum Board: Paper.

          - Exterior Gypsum Soffit Board: Paper.

          - Glass-Mat Gypsum Sheathing Board: 10-by-10 glass mesh.

          - Tile Backing Panels: As recommended by panel manufacturer.

        - Joint Compound for Interior Gypsum Board: For each coat, use formulation that is compatible with other compounds applied on previous or for successive coats.

          - Prefilling: At open joints[, rounded or beveled panel edges,] and damaged surface areas, use setting-type taping compound.

          - Embedding and First Coat: For embedding tape and first coat on joints, fasteners, and trim flanges, use [setting-type taping] [drying-type, all-purpose] compound.

            - Use setting-type compound for installing paper-faced metal trim accessories.

          - Fill Coat: For second coat, use [setting-type, sandable topping] [drying-type, all-purpose] compound.

          - Finish Coat: For third coat, use [setting-type, sandable topping] [drying-type, all-purpose] compound.

          - Skim Coat: For final coat of Level 5 finish, use [setting-type, sandable topping compound] [drying-type, all-purpose compound] [high-build interior coating product designed for application by airless sprayer and to be used instead of skim coat to produce Level 5 finish].

        - Joint Compound for Exterior Applications:

          - Exterior Gypsum Soffit Board: Use setting-type taping compound and setting-type, sandable topping compound.

          - Glass-Mat Gypsum Sheathing Board: As recommended by sheathing board manufacturer.

        - Joint Compound for Tile Backing Panels:

          - Glass-Mat, Water-Resistant Backing Panel: As recommended by backing panel manufacturer.

          - Cementitious Backer Units: As recommended by backer unit manufacturer.

          - Water-Resistant Gypsum Backing Board: Use setting-type taping compound and setting-type, sandable topping compound.

If required, insert joint treatment products designed for use with mold-resistant gypsum board products such as "ProForm XP" by National Gypsum Company.

          - <Insert products>.

      - AUXILIARY MATERIALS

        - Provide auxiliary materials that comply with referenced installation standards and manufacturer's written instructions.

        - Laminating Adhesive: Adhesive or joint compound recommended for directly adhering gypsum panels to continuous substrate.

First subparagraph below applies to LEED 2009 NC, CI, and CS; LEED v4; IgCC; and Green Globes. VOC content limit is that for gypsum board and panel adhesives.

          - Adhesives shall have a VOC content of [50] <Insert value> g/L or less.

First subparagraph below applies to LEED 2009 for Schools, IEQc 4.1.

          - Adhesive shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First subparagraph below applies to LEED v4.

          - Adhesive shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First subparagraph below applies to IgCC.

          - Adhesive shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." Formaldehyde emissions shall not exceed 9 mcg/cu. m or 7 ppb, whichever is less.

Subparagraph below applies to Green Globes.

          - Adhesive shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." The building concentration of formaldehyde shall not exceed half of the indoor recommended exposure limit or 33 mcg/cu. m and that of acetaldehyde shall not exceed 9 mcg/cu. m.

        - Steel Drill Screws: ASTM C1002 unless otherwise indicated.

Retain first subparagraph below if panels are attached to cold-formed metal framing specified in Section 054000 "Cold-Formed Metal Framing."

          - Use screws complying with ASTM C954 for fastening panels to steel members from 0.033 to 0.112 inch (0.84 to 2.84 mm) thick.

Retain subparagraph below for cementitious backer units.

          - For fastening cementitious backer units, use screws of type and size recommended by panel manufacturer.

        - Sound-Attenuation Blankets: ASTM C665, Type I (blankets without membrane facing) produced by combining thermosetting resins with mineral fibers manufactured from glass, slag wool, or rock wool.

          - Fire-Resistance-Rated Assemblies: Comply with mineral-fiber requirements of assembly.

Retain "Recycled Content" Subparagraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

          - Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

        - Acoustical Sealant: Manufacturer's standard nonsag, paintable, nonstaining latex sealant complying with ASTM C834. Product effectively reduces airborne sound transmission through perimeter joints and openings in building construction as demonstrated by testing representative assemblies in accordance with ASTM E90.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

For PABCO's product submittal literature, see www.pabcogypsum.com/sites/default/files/PABCO_Gypsum_Submittal_Book.pdf.

          - Basis-of-Design Product: Subject to compliance with requirements, provide PABCO Gypsum; QuietSeal Pro or comparable product by one of the following:

            - CertainTeed Gypsum.

            - USG Corporation.

            - <Insert manufacturer's name>.

First subparagraph below applies to LEED 2009 NC, CI, and CS; LEED v4; IgCC; and Green Globes.

PABCO's "QuietSeal Pro" has VOC content of 2 g/L or less.

          - Sealant shall have a VOC content of 250 g/L or less.

First subparagraph below applies to LEED 2009 for Schools, IEQc 4.1.

          - Sealant shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First subparagraph below applies to LEED v4.

          - Sealant shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First subparagraph below applies to IgCC.

          - Sealant shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." Formaldehyde emissions shall not exceed 9 mcg/cu. m or 7 ppb, whichever is less.

Subparagraph below applies to Green Globes.

          - Sealant shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." The building concentration of formaldehyde shall not exceed half of the indoor recommended exposure limit, or 33 mcg/cu. m, and that of acetaldehyde shall not exceed 9 mcg/cu. m.

        - Thermal Insulation: As specified in Section 072100 "Thermal Insulation."

        - Vapor Retarder: As specified in Section 072600 "Vapor Retarders."

      - TEXTURE FINISHES

        - Primer: As recommended by textured finish manufacturer.

        - Polystyrene Aggregate Ceiling Finish: Water-based, job-mixed, polystyrene aggregate finish with flame-spread and smoke-developed indexes of not more than 25 when tested in accordance with ASTM E84.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Georgia-Pacific Gypsum LLC.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Texture: [Fine] [Medium] [Coarse].

        - Aggregate Finish: Water-based, job-mixed, aggregated, drying-type texture finish for spray application.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - CertainTeed Gypsum.

            - Georgia-Pacific Gypsum LLC.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

Coordinate texture requirements with products retained or inserted above. Georgia-Pacific product is not available in spatter knock-down finish.

          - Texture: [Light spatter] [Spatter knock-down] <Insert texture>.

        - Non-Aggregate Finish: Premixed, vinyl texture finish for spray application.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - CertainTeed Gypsum.

            - National Gypsum Company.

            - USG Corporation.

            - <Insert manufacturer's name>.

Coordinate texture requirements with products retained or inserted above.

          - Texture: [Orange peel] [Spatter] [Spatter knock-down] <Insert texture>.

        - Acoustical Finish: Water-based, chemical-setting or drying-type, job-mixed texture finish for spray application.

Retain "Manufacturers" Subparagraph below and list of manufacturers to require products from manufacturers listed or a comparable product from other manufacturers.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - International Cellulose Corp.

            - Monoglass Incorporated.

            - USG Corporation.

            - <Insert manufacturer's name>.

          - Application Thickness: [1/2 inch (12.7 mm)] <Insert dimension>.

          - Surface-Burning Characteristics: As determined by testing identical products in accordance with ASTM E84 by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

            - Flame-Spread Index: [25] <Insert value> or less.

            - Smoke-Developed Index: [50] [450] <Insert value> or less.

          - NRC: [0.55] <Insert NRC> in accordance with ASTM C423.

- EXECUTION

      - EXAMINATION

        - Examine areas and substrates including welded hollow-metal frames and support framing, with Installer present, for compliance with requirements and other conditions affecting performance of the Work.

        - Examine panels before installation. Reject panels that are wet, moisture damaged, and mold damaged.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - INSTALLATION AND FINISHING OF PANELS, GENERAL

        - Comply with ASTM C840.

        - Install ceiling panels across framing to minimize the number of abutting end joints and to avoid abutting end joints in central area of each ceiling. Stagger abutting end joints of adjacent panels not less than one framing member.

        - Install panels with face side out. Butt panels together for a light contact at edges and ends with not more than 1/16 inch (1.5 mm) of open space between panels. Do not force into place.

        - Locate edge and end joints over supports, except in ceiling applications where intermediate supports or gypsum board back-blocking is provided behind end joints. Do not place tapered edges against cut edges or ends. Stagger vertical joints on opposite sides of partitions. Do not make joints other than control joints at corners of framed openings.

        - Form control and expansion joints with space between edges of adjoining gypsum panels.

        - Cover both faces of support framing with gypsum panels in concealed spaces (above ceilings, etc.), except in chases braced internally.

          - Unless concealed application is indicated or required for sound, fire, air, or smoke ratings, coverage may be accomplished with scraps of not less than 8 sq. ft. (0.7 sq. m) in area.

          - Fit gypsum panels around ducts, pipes, and conduits.

          - Where partitions intersect structural members projecting below underside of floor/roof slabs and decks, cut gypsum panels to fit profile formed by structural members; allow 1/4- to 3/8-inch- (6.4- to 9.5-mm-) wide joints to install sealant.

Indicate perimeter isolation on Drawings. See "Crack Control" Article in the Evaluations.

        - Isolate perimeter of gypsum board applied to non-load-bearing partitions at structural abutments. Provide 1/4- to 1/2-inch- (6.4- to 12.7-mm-) wide spaces at these locations and trim edges with edge trim where edges of panels are exposed. Seal joints between edges and abutting structural surfaces with acoustical sealant.

        - Attachment to Steel Framing: Attach panels so leading edge or end of each panel is attached to open (unsupported) edges of stud flanges first.

Retain "Wood Framing" Paragraph below for wood framing where fire ratings are not required.

        - Wood Framing: Install gypsum panels over wood framing, with floating internal corner construction. Do not attach gypsum panels across the flat grain of wide-dimension lumber, including floor joists and headers. Float gypsum panels over these members or provide control joints to counteract wood shrinkage.

        - STC-Rated Assemblies: Seal construction at perimeters, behind control joints, and at openings and penetrations with a continuous bead of acoustical sealant. Install acoustical sealant at both faces of partitions at perimeters and through penetrations. Comply with ASTM C919 and with manufacturer's written instructions for locating edge trim and closing off sound-flanking paths around or through assemblies, including sealing partitions above acoustical ceilings.

        - Install sound attenuation blankets before installing gypsum panels unless blankets are readily installed after panels have been installed on one side.

      - INSTALLATION OF INTERIOR GYPSUM BOARD

        - Install interior gypsum board in the following locations:

          - Wallboard Type: [As indicated on Drawings] [Vertical surfaces unless otherwise indicated].

          - Type X: [As indicated on Drawings] [Where required for fire-resistance-rated assembly] [Vertical surfaces unless otherwise indicated] <Insert requirements>.

          - Flexible Type: [As indicated on Drawings] [Apply in double layer at curved assemblies].

          - Ceiling Type: [As indicated on Drawings] [Ceiling surfaces].

          - Foil-Backed Type: [As indicated on Drawings] <Insert requirements>.

          - Abuse-Resistant Type: [As indicated on Drawings] <Insert requirements>.

          - Impact-Resistant Type: [As indicated on Drawings] <Insert requirements>.

          - Mold-Resistant Type: [As indicated on Drawings] <Insert requirements>.

          - Type C: [As indicated on Drawings] [Where required for specific fire-resistance-rated assembly indicated].

          - Glass-Mat Interior Type: [As indicated on Drawings] <Insert requirements>.

          - Acoustically Enhanced Type: [As indicated on Drawings] <Insert requirements>.

          - Skim-Coated Type: [As indicated on Drawings] <Insert requirements>.

        - Single-Layer Application:

          - On ceilings, apply gypsum panels before wall/partition board application to greatest extent possible and at right angles to framing unless otherwise indicated.

          - On partitions/walls, apply gypsum panels [vertically (parallel to framing)] [horizontally (perpendicular to framing)] unless otherwise indicated or required by fire-resistance-rated assembly, and minimize end joints.

            - Stagger abutting end joints not less than one framing member in alternate courses of panels.

Usually, retain first subparagraph below if vertical application of panels is specified.

            - At stairwells and other high walls, install panels horizontally unless otherwise indicated or required by fire-resistance-rated assembly.

          - On Z-shaped furring members, apply gypsum panels vertically (parallel to framing) with no end joints. Locate edge joints over furring members.

          - Fastening Methods: Apply gypsum panels to supports with steel drill screws.

        - Multilayer Application:

Retain first subparagraph below for multilayer gypsum board ceilings.

          - On ceilings, apply gypsum board indicated for base layers before applying base layers on walls/partitions; apply face layers in same sequence. Apply base layers at right angles to framing members and offset face-layer joints one framing member, 16 inches (400 mm) minimum, from parallel base-layer joints, unless otherwise indicated or required by fire-resistance-rated assembly.

Revise first two subparagraphs below if wall conditions permit economical use of horizontal application of base layer and face layers are laminated to base layers.

          - On partitions/walls, apply gypsum board indicated for base layers and face layers vertically (parallel to framing) with joints of base layers located over stud or furring member and face-layer joints offset at least one stud or furring member with base-layer joints unless otherwise indicated or required by fire-resistance-rated assembly. Stagger joints on opposite sides of partitions.

          - On Z-shaped furring members, apply base layer vertically (parallel to framing) and face layer either vertically (parallel to framing) or horizontally (perpendicular to framing) with vertical joints offset at least one furring member. Locate edge joints of base layer over furring members.

First option in "Fastening Methods" Subparagraph below is required for some fire-resistance-rated assemblies.

          - Fastening Methods: Fasten base layers [and face layers separately to supports with screws] [with screws; fasten face layers with adhesive and supplementary fasteners].

Insert specific requirements for particular substrate in "Laminating to Substrate" Paragraph below.

        - Laminating to Substrate: Where gypsum panels are indicated as directly adhered to a substrate (other than studs, joists, furring members, or base layer of gypsum board), comply with gypsum board manufacturer's written instructions and temporarily brace or fasten gypsum panels until fastening adhesive has set.

        - Curved Surfaces:

          - Install panels horizontally (perpendicular to supports) and unbroken, to extent possible, across curved surface plus 12-inch- (300-mm-) long straight sections at ends of curves and tangent to them.

          - For double-layer construction, fasten base layer to studs with screws 16 inches (400 mm) o.c. Center gypsum board face layer over joints in base layer, and fasten to studs with screws spaced 12 inches (300 mm) o.c.

      - INSTALLATION OF EXTERIOR GYPSUM PANELS FOR CEILINGS AND SOFFITS

        - Apply panels perpendicular to supports, with end joints staggered and located over supports.

Retain first subparagraph below unless perimeter relief is provided by trim. If retaining, indicate sealant in gap on Drawings to keep insects from entering above ceiling areas.

          - Install with 1/4-inch (6.4-mm) open space where panels abut other construction or structural penetrations.

          - Fasten with corrosion-resistant screws.

      - INSTALLATION OF TILE BACKING PANELS

        - Glass-Mat, Water-Resistant Backing Panels: Comply with manufacturer's written installation instructions and install at [showers, tubs, and where indicated] [locations indicated to receive tile]. Install with 1/4-inch (6.4-mm) gap where panels abut other construction or penetrations.

        - Cementitious Backer Units: ANSI A108.11, at [showers, tubs, and where indicated] [locations indicated to receive tile].

        - Water-Resistant Backing Board: Install where indicated with 1/4-inch (6.4-mm) gap where panels abut other construction or penetrations.

Retain paragraph below if tile backing panels abut thinner board in same plane, or vice versa, and detail these conditions on Drawings.

        - Where tile backing panels abut other types of panels in same plane, shim surfaces to produce a uniform plane across panel surfaces.

      - INSTALLATION OF TRIM ACCESSORIES

        - General: For trim with back flanges intended for fasteners, attach to framing with same fasteners used for panels. Otherwise, attach trim in accordance with manufacturer's written instructions.

Generally, retain first option in "Control Joints" Paragraph below and indicate joints on Drawings. See the Evaluations for discussion of control joints.

        - Control Joints: Install control joints [at locations indicated on Drawings] [in accordance with ASTM C840 and in specific locations approved by Architect for visual effect].

        - Interior Trim: Install in the following locations:

          - Cornerbead: Use at outside corners[ unless otherwise indicated].

          - Bullnose Bead: Use [at outside corners] [where indicated] <Insert requirements>.

          - LC-Bead: Use [at exposed panel edges] <Insert requirements>.

          - L-Bead: Use [where indicated] <Insert requirements>.

          - U-Bead: Use [at exposed panel edges] [where indicated] <Insert requirements>.

          - Curved-Edge Cornerbead: Use at curved openings.

        - Exterior Trim: Install in the following locations:

          - Cornerbead: Use at outside corners.

          - LC-Bead: Use [at exposed panel edges] <Insert requirements>.

        - Aluminum Trim: Install in locations [indicated on Drawings] <Insert requirements>.

      - FINISHING GYPSUM BOARD

        - General: Treat gypsum board joints, interior angles, edge trim, control joints, penetrations, fastener heads, surface defects, and elsewhere as required to prepare gypsum board surfaces for decoration. Promptly remove residual joint compound from adjacent surfaces.

        - Prefill open joints[, rounded or beveled edges,] and damaged surface areas.

        - Apply joint tape over gypsum board joints, except for trim products specifically indicated as not intended to receive tape.

See "Gypsum Board Finish Levels" Article in the Evaluations for a discussion of requirements of various levels.

        - Gypsum Board Finish Levels: Finish panels to levels indicated below and in accordance with ASTM C840:

Gypsum board finish levels are minimum requirements established by ASTM C840 without elaboration.

          - Level 1: Ceiling plenum areas, concealed areas, and where indicated.

          - Level 2: [Panels that are substrate for tile] [Panels that are substrate for acoustical tile] [Where indicated on Drawings] <Insert locations>.

Level 3 is suitable for surfaces receiving medium- or heavy-textured finishes before painting or heavy wallcoverings where lighting conditions are not critical.

          - Level 3: [Where indicated on Drawings] <Insert locations>.

Level 4 is suitable for surfaces receiving light-textured finishes, wallcoverings, and flat paints. It is generally the standard exposed finish. Gloss and semigloss enamel paints are not usually recommended over this level of finish. ASTM C840 requires application of "drywall primer" on surfaces before final decoration. Specify priming of gypsum board surfaces in Section 099123 "Interior Painting."

          - Level 4: [At panel surfaces that will be exposed to view unless otherwise indicated] <Insert locations>.

            - Primer and its application to surfaces are specified in Section 099123 "Interior Painting."

Level 5 is suitable for surfaces receiving gloss and semigloss enamels and other surfaces subject to severe lighting. It is considered a high-quality gypsum board finish.

          - Level 5: [Where indicated on Drawings] <Insert locations>.

            - Primer and its application to surfaces are specified in Section 099123 "Interior Painting."

        - Glass-Mat Gypsum Sheathing Board: Finish in accordance with manufacturer's written instructions for use as exposed soffit board.

        - Glass-Mat Faced Panels: Finish in accordance with manufacturer's written instructions.

        - Cementitious Backer Units: Finish in accordance with manufacturer's written instructions.

      - INSTALLATION OF TEXTURE FINISHES

        - Surface Preparation and Primer: Prepare and apply primer to gypsum panels and other surfaces receiving texture finishes. Apply primer to surfaces that are clean, dry, and smooth.

        - Texture Finish Application: Mix and apply finish using powered spray equipment, to produce a uniform texture[ matching approved mockup and] free of starved spots or other evidence of thin application or of application patterns.

        - Prevent texture finishes from coming into contact with surfaces not indicated to receive texture finish by covering them with masking agents, polyethylene film, or other means. If, despite these precautions, texture finishes contact these surfaces, immediately remove droppings and overspray to prevent damage in accordance with texture-finish manufacturer's written instructions.

      - PROTECTION

        - Protect adjacent surfaces from drywall compound and promptly remove from floors and other non-drywall surfaces. Repair surfaces stained, marred, or otherwise damaged during drywall application.

        - Protect installed products from damage from weather, condensation, direct sunlight, construction, and other causes during remainder of the construction period.

        - Remove and replace panels that are wet, moisture damaged, and mold damaged.

          - Indications that panels are wet or moisture damaged include, but are not limited to, discoloration, sagging, or irregular shape.

          - Indications that panels are mold damaged include, but are not limited to, fuzzy or splotchy surface contamination and discoloration.

END OF SECTION 092900