Sure Klean® 1260 Limestone & Marble Poultice Cleaning Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and SDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions.  Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® 1260 Limestone & Marble Poultice is an easy-to-use, low-odor paste poultice which draws deep-seated oil, dirt, harmful salts and other embedded stains out of sensitive masonry, including polished limestone and marble. Aided by special detergents and chelating agents, the moist poultice literally pulls contaminants out of the masonry pores and absorbs them into the paste. After a dwell time of 12-24 hours, the poultice and its captured contaminants are removed followed by a rinsing of the cleaned surface with fresh water to complete the restoration of the masonry to its intended appearance. Ready-to-use, non-acidic 1260 Limestone & Marble Poultice is suitable for interior and exterior cleaning of horizontal, vertical and overhead surfaces.

# Typical Technical Data

FORM: Grey paste, mild odor

SPECIFIC GRAVITY: 1.14 to 1.26

pH: 9.0

WEIGHT/GALLON: 9.5 to 10.5 pounds

TOTAL SOLIDS: 30 to 35 percent

FLASH POINT: not applicable

FREEZE POINT: 32 degrees F (0 degrees C)

VOC CONTENT: not applicable

SHELF LIFE: 1 year in tightly sealed, unopened container

# Limitations

- Cold temperatures will adversely affect the cleaning properties of 1260 Limestone & Marble Cleaner. Wet paste freezes.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for 1260 Limestone & Marble Poultice.  Do not dilute or alter; apply as packaged. Refer to test area results for the optimal dwell period.

- Apply 1260 Limestone & Marble Poultice to a dry surface one-eighth (1/8) to one-quarter inch (1/4) thick using a trowel or airless sprayer or other suitable applicator.

- Cover the poultice with Enviro Klean® OverCoat®. Press the OverCoat® protective paper against the poultice. It will cling to the surface. Tape/seal off the edges of the paper.

- Leave the covered poultice on the surface 12 to 24 hours.

- Remove OverCoat®. If the poultice is still wet, allow the poultice to dry 2 to 4 hours. The poultice surface develops cracks as it contracts and dries. A fully developed network of cracks indicates the poultice is completely dry.

- Remove the poultice and captured contaminants. Insert a corrosion-resistant spatula, trowel or other suitable scraping device under the paste and carefully lift from the surface. Remove as much residue as possible.

- Rinse the surface thoroughly with fresh water, using a sponge, soft cloth or low pressure/low volume water-rinsing equipment.

- Repeat application as needed.

# Cleanup

Clean tools and equipment using fresh water.