Sure Klean® 942 Limestone & Marble Cleaner Cleaning Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and SDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions.  Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® 942 Limestone & Marble Cleaner is a ready-to-use nonacidic cleaning gel designed to remove moderate-to-severe atmospheric staining on exterior or interior masonry surfaces. Safe for use on most polished or unpolished marble and limestone surfaces, 942 Limestone & Marble Cleaner removes surface and subsurface staining.  It dissolves damaging gypsum (calcium sulfate dihydrate) and related atmospheric staining, enabling removal in a safe, controlled manner with a simple water rinse.

# Technical Data

FORM: Clear amber gel

SPECIFIC GRAVITY: 1.040

TOTAL SOLIDS: N/A

pH: 8.3

WT./GAL.: 8.65 lbs.

FREEZE POINT: 25 degrees F (-4 degrees C) ASTM D 1177

FLASH POINT: > 200 degrees F (> 93 degrees)

# Limitations

- May damage highly polished limestone or marble surfaces.

- Not for use in subfreezing temperatures. Gel will freeze.

- Surface and air temperatures should be at least 50 degrees F (10 degrees C). Cold temperatures will adversely affect the cleaning properties of 942 Limestone & Marble Cleaner.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for 942 Limestone & Marble Cleaner.  Do not dilute. Refer to test area results for the optimal dwell period.

- Apply 942 Limestone & Marble Cleaner to the surface in a thick uniform coating using a brush or airless spray equipment.

- Let the cleaner stay on the surface for 2 to 24 hours. For long dwell periods, cover treated areas to prevent premature drying.

- Remove the gel and as much residue from the surface as possible. Rinse the surface thoroughly with fresh water using a sponge, soft cloth or low-pressure/low-volume water rinsing equipment.

- Repeat application where necessary.

Specifier Note: The appropriate dwell period for safe, effective cleaning should be determined through on-site testing, before full-scale cleaning operations.

Specifier Note: For longer dwell periods, it may be necessary to cover treated areas with polyethylene to prevent premature drying.

# Cleanup

Clean tools and equipment using fresh water.