Consolideck® ColorHard Specification (UV Stable – Suitable for Interior and Exterior Applications)

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of surface to confirm suitability and desired results. Use the manufacturer’s application instructions. Include representative imperfections in the test area to assess the impact on the color-hardened concrete floor. Let test area of protective treatment cure before inspection. Keep test panels available for comparison throughout the project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer:  PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Consolideck® ColorHard is a premeasured color concentrate formulated to mix with Consolideck® LS® or LS/CS® to color, harden and densify horizontal concrete in one step. When mixed with Consolideck® LS® or LS/CS®, ColorHard dustproofs and improves the abrasion-resistance of concrete floors and exterior pavements. ColorHard is available in 21 color hues which can be used alone or in combinations. All ColorHard colors are suitable for indoor use, and many are suitable for outdoor use, even in extreme climates. Supplied in concentrate form, ColorHard is a water-based, environmentally responsible product which minimizes freight, handling, storage and container disposal costs.

Typical Technical Data

FORM: 			Colored liquid concentrate

SPECIFIC GRAVITY:	1.2 to 2.10

pH:			6.5 to 9.5

WEIGHT/GALLON:	10 to 16.5 pounds

ACTIVE CONTENT:	50 to 70 percent

TOTAL SOLIDS:	50 to 70 percent

VOC CONTENT:	Less than 100 g/L as used

FLASH POINT:		no data

FREEZE POINT:	32 degrees Fahrenheit (0 degrees Celsius)

SHELF LIFE:		1 year in unopened, factory-sealed container

Limitations

- Floors treated with Consolideck® ColorHard require the application of a protective treatment.

- Consolideck® ColorHard is translucent. It will not hide or mask variations in the concrete.

- Not for use on surfaces exposed to continuous.

- Not for use on concrete floors polished higher than the equivalent of #200 grit resin bond diamonds.

- Some ColorHard colors are intended for interior use only.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet. Refer to the Product Data Sheet for additional information about application.

Dilution

Thoroughly mix color concentrate by shaking the 4-oz package well. Combine one shaken 4-oz package of Consolideck® ColorHard with up to one-gallon of Consolideck® LS® or LS/CS® before application to make one gallon of ready-to-use color hardener. Prepared ColorHard must be applied within 24-hours. To reduce color intensity, add more LS. To increase color intensity, apply two or more coats.

SPECIFIER NOTE: When environmental conditions cause rapid drying, mix ColorHard with LS/CS®.

SPECIFIER NOTE: For maximum densification, mix ColorHard with LS®.

SPECIFIER NOTE: Blend prepared ColorHard colors for unlimited colors and effects. Only blend prepared color hardener. Never blend color concentrates.

Color Application Instructions

SPECIFIER NOTE: Application practices using two people get best results; one spraying and one spreading.

SPECIFIER NOTE: Mask neighboring surfaces as needed to control color bleeding. Use shallow saw cuts to separate different colors. Use control joints, walls and other fixed objects as termination points. When practical, stop the day’s work at a termination point. Sequence application to lessen traffic on wet color-hardened floors.

SPECIFIER NOTE:  When spray applying, maintain a consistent flow rate and spray pattern. When triggering or releasing sprayer, direct spray tip into a container to minimize dripping.

- Using low-pressure spray and a conical spray tip, apply enough pre-mixed, ready-to-use ColorHard to wet the surface without producing puddles. Do not over apply. Do not atomize.

- Spread the product. Do not overwork or spread once drying begins. For a more mottled appearance, spray apply without spreading. 
On smooth surfaces, spread with a clean microfiber pad prewet with prepared ColorHard. Apply in a smooth, irregular pattern to minimize streaks. 
On textured surfaces, spread with a clean, soft-fibered push broom.

- Allow the floor to dry for at least one hour. Stay off wet surfaces.

- Repeat Steps 1-3 above for increased color intensity and surface hardening.

- When dry, burnish smooth surfaces using a high-speed burnishing fitted with a #800 grit (or higher) diamond-impregnated pad.

- Clean the floor with an auto-scrubbing machine and Consolideck® LSKlean. Collect ponded water. Allow surfaces to dry.

Cleanup

Remove all tape and plastic sheeting as soon as practical. Before product dries, clean tools and equipment with soap and water.