Sure Klean® Weather Seal Gloss ‘N Guard

Water Repellent Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and Safety Data Sheet for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 feet by 4 feet area on each type of masonry. Use the manufacturer’s application instructions. Let test area protective treatment cure before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Weather Seal Gloss ‘N Guard is a highly durable protective coating for tile, pavers, terrazzo and other polished and unpolished masonry. Gloss ‘N Guard dries to a high-gloss finish that enhances the natural beauty of treated surfaces.

# Limitations

- Not suitable for use around pools, fountains or showers.

- Not suitable for sale in states and districts with more restrictive AIM VOC regulations. Available in regulation-exempt small container sizes.

- Will not prevent water penetration through structural cracks, defects or open joints.

- Not recommended for below-grade application.

# Typical Technical Data

FORM: Clear, slight yellow liquid with mild petroleum odor

SPECIFIC GRAVITY: 0.825

pH: not applicable

WEIGHT PER GALLON: 6.86 pounds

ACTIVE CONTENT: 18 percent

TOTAL SOLIDS: 19 percent ASTM D 2369

FLASH POINT: 102 degrees Fahrenheit (39 degrees Celsius) ASTM D 3278

FREEZE POINT: less than -22 degrees Fahrenheit (less than -30 degrees Celsius)

VOC CONTENT: Manufactured and marketed in compliance with USEPA AIM VOC regulations (40 CFR 59.403). Not suitable for sale in states and districts with more restrictive AIM VOC regulations.

ASTM C 1028 Slip Resistance Test:

- 0.87 (DRY) static coefficient of friction

- 0.85 (WET) static coefficient of friction

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Gloss ‘N Guard.  Refer to the Product Data Sheet for additional information about application of Gloss ‘N Guard. Do not dilute or alter.

- Apply a thin, even coat of Gloss ‘N Guard with a natural-bristle brush or low-pressure sprayer.

- Two to four applications may be necessary for a uniform appearance on porous surfaces. Allow 1-3 hours between coats, or until surface is dry to the touch.

- Let treated surfaces dry thoroughly. Protect from rain for 24 hours after application.

# Cleanup

Clean tool and equipment immediately with mineral spirits or similar solvent. Container may contain residues. Keep from ignition sources. Do not reuse.