Sure Klean® Graffiti Remover Paint, Coating & Graffiti Removers Specification

Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and SDS for additional recommendations and for safety information.

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

# TEST AREA

Test a minimum 4 ft. by 4 ft. area on each type of surface, paint coating and graffiti stain to confirm suitability and desired results before beginning overall application. Test with the same equipment, recommended surface preparation and application procedures planned for general application. Let test dry thoroughly before inspection. Make the test panel available for comparison throughout cleaning project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# MANUFACTURER

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

# PRODUCT DESCRIPTION

Sure Klean® Graffiti Remover is a low-odor, water-rinseable product to remove a variety of graffiti media from most smooth masonry, split-faced concrete block, wood and metal surfaces. Graffiti Remover does not contain methanol, methylene chloride or other halogenated solvents. Graffiti Remover is fully compliant with all known VOC (volatile organic compound) regulations.

# TYPICAL TECHNICAL DATA

FORM: Clear, amber liquid with citrus odor

SPECIFIC GRAVITY: 1.03

pH: not applicable

WEIGHT/GALLON: 8.60 pounds

ACTIVE CONTENT: not applicable

TOTAL SOLIDS: not applicable

VOC CONTENT:  30 percent maximum

FLASH POINT: greater than 212 degrees F (greater than 100 degrees C) ASTM D3278

FREEZE POINT: not applicable

SHELF LIFE: 2 years in tightly sealed, unopened container

# Limitations

- Product efficiency is reduced during cold weather.

- May damage synthetic or reflective glass.

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation.

# APPLICATION

Before applying, read the Manufacturer’s Product Data Sheet for Graffiti Remover. Use as packaged. Do not dilute or alter.

# Application Instructions

- Apply with a brush or low-pressure spray to a dry surface.

- Allow to dwell for 3 to 20 minutes.

- Working from the bottom to the top, pressure water rinse. Hot water is preferable.

SPECIFIER NOTE: Periodic agitation with a stiff bristle brush improves penetration. Some coatings will need multiple applications/increased dwell time.

SPECIFIER NOTE: Removal results may be unsatisfactory if Graffiti Remover dries on the surface. If testing indicates long dwell periods are required, reapply to prevent drying or use PROSOCO’s Enviro Klean® SafStrip or SafStrip 8.

SPECIFIER NOTE: Heavy graffiti staining may require more than one application.

# Removing Sure klean® weather seal Sacrificial Coating SC-1

- Apply Graffiti Remover with a brush or low-pressure spray and allow to dwell for 3 to 20 minutes.

- Working from the bottom to the top, pressure water rinse. Hot water is preferable.

- Allow treated surfaces to dry completely.

- Reapply Sacrificial Coating SC-1 to restore graffiti protection according to manufacturer’s instructions.

# CLEANUP

Clean tools and equipment with fresh water. Dried residue may be cleaned with high-flash aromatic naphtha, mineral spirits or an equivalent cleaning solvent.