Sure Klean® Heavy Duty Restoration Cleaner Cleaning Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions.  Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer:  PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Heavy Duty Restoration Cleaner is a concentrated acidic cleaning compound for the removal of heavy atmospheric staining from unpolished masonry.

Used properly, Heavy Duty Restoration Cleaner dissolves heavy carbon and many other stains commonly found on masonry buildings in highly polluted areas. Dilute with water to produce a cost-effective, general-purpose restoration cleaner for brick, granite, sandstone, slate, terra cotta and many other masonry surfaces.

Technical Data

FORM: Clear liquid

SPECIFIC GRAVITY: 1.132

TOTAL SOLIDS: N/A

pH: 2.2 (@ 1:3 Dilution)

WT./GAL.: 9.42 lbs.

FLASH POINT: N/A

FREEZE POINT: N/D

Limitations

- Repeated application, or use when diluted with less than three parts fresh water, may damage some masonry surfaces. Use Sure Klean® Light Duty Restoration Cleaner or Sure Klean® Restoration Cleaner where possible.

- Not for interior use. Use Sure Klean® Light Duty Restoration Cleaner.

- Not suitable for polished stone and glazed surfaces. Use Sure Klean® Light Duty Restoration Cleaner.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Restoration Cleaner.  Dilute Heavy Duty Restoration Cleaner 3-6 parts water. Refer to Product Data Sheet for recommended dilution for intended use.

1. Prewet the surface with clean water.

2. Apply the cleaner using a brush or low-pressure spray.

3. Let the cleaning solution stay on the surface for 3 to 5 minutes. Reapply. Gently scrub heavily soiled areas.

4. Rinse with low-pressure flood rinse to remove initial acidic residue with minimum risk of wind drift.

5. Rinse thoroughly using high-pressure spray, from the bottom of the treated area to the top covering each section of the surface with a concentrated stream of water. The best combination of rinsing pressure and water volume is provided by masonry washing equipment generating 400-1000 psi with a water flow rate of 6-8 gallons per minute delivered through a 15-45 degree fan spray tip. Equipment should be adjustable to reduce water flow rate and rinsing pressure as required for controlled cleaning of more sensitive surfaces. See also “Equipment” section of the Product Data Sheet.

Note: Do not let cleaner dry on the surface. If drying occurs, lightly wet treated surfaces with fresh water and reapply in a gentle scrubbing manner. To avoid streaking, keep wall below wet and rinsed free of cleaner and residues.