Sure Klean® Heavy Duty Restoration Cleaner NE Cleaning Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions.  Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer:  PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Heavy Duty Restoration Cleaner NE is a concentrated acidic cleaner specifically made to attack and wipe out the heaviest atmospheric staining the Northeast U.S. urban and industrial environment can produce on brick, terra cotta, granite, sandstone and more.

Used carefully, this ultra-powerful formulation breaks loose and dissolves the decades of dirt, paint oxidation, carbon buildup and other atmospheric pollutants that can prove too difficult for other cleaners. A simple cold-water rinse then removes these unsightly, stubborn stains, revealing the masonry’s original beauty.

Technical Data

FORM: Clear liquid

SPECIFIC GRAVITY: 1.18

TOTAL SOLIDS: N/A

pH: 2.2 @ 1:3 dilution

WT./GAL.: 9.78 lbs.

FREEZE POINT: N/D

FLASH POINT: N/A

Limitations

- Repeated application, or dilutions with less than three parts fresh water, may damage some masonry surfaces. Use Sure Klean® Light Duty Restoration Cleaner or Sure Klean® Restoration Cleaner where possible.

- Not for interior use. Use Sure Klean® Light Duty Restoration Cleaner.

- Not suitable for polished stone and glazed surfaces. Use Sure Klean® Light Duty Restoration Cleaner.

- May etch glass.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Restoration Cleaner NE.  Dilute Heavy Duty Restoration Cleaner NE 3-6 parts water. Refer to Product Data Sheet for recommended dilution for intended use.

1. Prewet the surface with clean water.

2. Apply the cleaner using a brush or low-pressure spray.

3. Let the cleaning solution stay on the surface for 3 to 5 minutes. Reapply. Gently scrub heavily soiled areas.

4. Rinse with low-pressure flood rinse to remove initial acidic residue with minimum risk of wind drift.

5. Rinse thoroughly using high-pressure spray, from the bottom of the treated area to the top covering each section of the surface with a concentrated stream of water. The best combination of rinsing pressure and water volume is provided by masonry washing equipment generating 400-1000 psi with a water flow rate of 6-8 gallons per minute delivered through a 15-45 degree fan spray tip. Equipment should be adjustable to reduce water flow rate and rinsing pressure as required for controlled cleaning of more sensitive surfaces. See also “Equipment” section of the Product Data Sheet.

Note: Do not let cleaner dry on the surface. If drying occurs, lightly wet treated surfaces with fresh water and reapply in a gentle scrubbing manner. To avoid streaking, keep wall below wet and rinsed free of cleaner and residues.