Enviro Klean® SafStrip® Paint, Coating and Graffiti Remover Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and Safety Data Sheet for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of surface and coating for suitability and results before overall application. Include in the test area any previous repairs and patches, including aesthetic cementitious finishes. Different surface compositions may result in cleaning differences and/or appearance differences. Test using the following application instructions. Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Enviro Klean® SafStrip® quickly removes most paints, clear coats and graffiti from masonry, concrete, wood and metal – without use of methylene chloride or methanol.

Low-odor SafStrip® breaks the bond of high-strength paints and coatings including acrylics, alkyds, and clear sealers.  It dissolves common hard-to-remove graffiti media such as spray paints, marking pens and lacquers.  Its “thixotropic” gel consistency makes SafStrip® easy to apply and spill-resistant.  After cleaning, the spent paint stripper rinses off easily with cold or hot water.

# Typical Technical Data

FORM: Clear, colorless gel

SPECIFIC GRAVITY: 1.06

pH: 2.15

WEIGHT PER GALLON: 8.81 pounds

ACTIVE CONTENT: not applicable

TOTAL SOLIDS: not applicable

FLASH POINT: greater than 200 degrees Fahrenheit (greater than 93 degrees Celsius) ASTM D3278

FREEZE POINT: not applicable

SHELF LIFE:  1 year in tightly sealed, unopened container
VOC CONTENT:  30 percent, maximum

# Limitations

- Not for finely finished wood surfaces such as furniture.

- Not for removal of cementitious coatings.

- Not for use on polished surfaces

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet and for SafStrip. Do not dilute or alter.  Apply as packaged.

Application Instructions

Do not let stripper dry on the surface. Keep people away from stripper. Do not atomize or breathe product mists.

SPECIFIER NOTE: If tests indicate long dwell times, reapply to keep the previously applied material wet.

SPECIFIER NOTE: If the waste generated through paint stripping operations is classified as “hazardous,” contractors must consult and comply with current federal, state and local regulations regarding containment, transport and disposal of hazardous waste.

Exterior Applications

- Working from the bottom to the top, apply SafStrip® 1/8 to 1/4 inch thick to dry surface.

- Let the application dwell 15 to 60 minutes or until coating “lifts” or shows signs of dissolving. Periodic agitation with a stiff bristle brush improves penetration. Some coatings will need multiple applications/increased dwell time.

- Working from the bottom to the top, remove stripper and residue with pressure-water rinse.  Heated water may improve stripping efficiency.

SPECIFIER NOTE: The best combination of rinsing pressure and water volume is provided by masonry washing equipment generating 400-1000 psi with a water flow rate of 6-8 gallons per minute delivered through a 15-45 degree fan spray tip.  Equipment should be adjustable to reduce water flow rate and rinsing pressure as required for controlled cleaning of more sensitive surfaces.  See also “Equipment” section of the Product Data Sheet.

- Clean the stripped surface with the appropriate PROSOCO product. Call PROSOCO at 800-255-4255 for cleaning recommendations.

Interior Applications

- Follow steps 1 and 2 for exteriors.

- Using a low-pressure tank or pump-up sprayer, mist the treated surface with clean water. Water helps emulsify the old sealer and dilute the stripper so residues may be more easily picked up.

- Using a power-scrubber or buffer with an abrasive, nonmetallic scrubbing pad for floors, or stiff-bristled brush for walls, scrub the surface until coatings are gone. Add more water to aid scrubbing. Ventilate to prevent accumulation of combustible vapors.

- Use towels, mops or wet vacs to collect liquid residue. Locate wet vac motor outdoors well away from application site in a high area where vapors will not collect.

- Thoroughly brush or mop-and-bucket rinse with clean water. If needed, clean surface with appropriate PROSOCO product.

# Cleanup

Clean tools and equipment with water before product dries. Otherwise, use high-flash aromatic naphtha or similar solvent.