PROSOCO Saltguard® Water Repellent Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and SDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area dry thoroughly before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

PROSOCO Saltguard® is a general-purpose silane/siloxane water repellent and chloride screen for concrete and masonry, including concrete block, and clay and concrete brick surfaces. Saltguard® protects horizontal and vertical surfaces from moisture intrusion and chemical attack of chloride salts, reducing rebar corrosion and surface spalling.

Saltguard® may be used on horizontal surfaces such as sidewalks, tile and brick pavers. It also provides excellent protection for retaining walls, bridge pilings and other vertical areas. In coastal areas, Saltguard® protects against salt air by reducing chloride penetration. Saltguard® also prevents deep-seated staining by mud splashes and other waterborne contaminants.

# Typical Technical Data

FORM: Clear slightly yellow liquid with mild petroleum odor

SPECIFIC GRAVITY: 0.794

pH: not applicable

WEIGHT/GALLON.: 6.61 pounds

ACTIVE CONTENT: 11 percent

TOTAL SOLIDS: 9 percent

FLASH POINT: 127 degrees F (53 degrees C) ASTM D 3278

FREEZE POINT: no data

VOC CONTENT: greater than 600 g/Liter. Manufactured and marketed in compliance with USEPA AIM VOC regulations (40 CFR 59.403). Not suitable for sale in states and districts with more restrictive AIM VOC regulations.

# Limitations

- Not appropriate for use on limestone, marble, travertine or other calcareous stones. Always test other natural stone to ensure desired results.

- Not suitable for application to synthetic resin paints, gypsum, plaster or other non-masonry surfaces.

- May not be suitable for surfaces receiving paints or coatings. Always test.

- May cause slight darkening on some surfaces.

- May adhere to glass. Contact PROSOCO for removal recommendations.

- Not suitable for protecting surfaces subject to constant water spray.

- Will not compensate for structural or material defects.

- Not recommended for below-grade application.

- Not suitable for sale in states and districts with more restrictive AIM VOC regulations.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Saltguard®.  Refer to the Product Data Sheet for additional information about application of Saltguard®. Do not dilute or alter. Stir or mix well before use.

Vertical Spray Application Instructions

Apply with low-pressure (<50 psi) spray in a flooding application from the bottom up. Apply enough material for a rundown below the spray pattern. Brush out heavy runs and drips thoroughly so that the material completely penetrates the surface. When spray applying to fluted architectural block, spray in an “overlapping X pattern” for complete coverage of recessed surfaces.

Vertical Brush/Roller Application Instructions

SPECIFIER NOTE: Recommended for small scale application or when spray application is not appropriate. Contact PROSOCO for more information.

Saturate the surface to the point of rejection. Brush out heavy runs and drips thoroughly so that the material completely penetrates the surface.

Porous Surfaces Application Instructions

Porous surfaces will require a “wet-on-wet” application. Let the first application penetrate for 5 to 10 minutes and then reapply. Do not let any of the first application dry before making the second application. Less material will be required on the second application.

Horizontal Surfaces Application Instructions

Apply in a single, saturating application so that treated surfaces stay wet for a few minutes before penetrating. Broom out surface residues, pools and puddles until they completely penetrate the surface.

# Drying Time

Protect treated surface from rain and pedestrian traffic for 4–6 hours following application. Protect treated surfaces from vehicular traffic for 8–12 hours after treatment.

# Cleanup

Clean tools and equipment immediately with mineral spirits.