PROSOCO SingleStep® Cure-and-Seal Specification

Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area of each type of surface to confirm suitability, coverage rate and desired results before beginning overall application. Include in the test area any previous repairs and patches, including aesthetic cementitious finishes. Different surface compositions may result in absorption differences and/or appearance differences. Test with the same equipment, recommended surface preparation and application procedures planned for general application. Let the test area surface dry and cure thoroughly before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer: PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

# Product Description

PROSOCO® SingleStep® is an acrylic-silane blend for curing and weatherproofing new and existing concrete in one easy step. SingleStep® quickly penetrates concrete pores and forms a water repellent gel in the pores and a semi-glossy film on the surface. This film helps keep concrete moist until it reaches maximum hardness. The cured concrete resists damaging water penetration, salts, de-icer chemicals and acids. SingleStep® is quick curing and beads water after 24 hours. SingleStep® offers a fast, easy, effective alternative to curing compounds that require costly, time-consuming water curing and removal. SingleStep® is ideal for parking garages, athletic stadiums, engineered concrete structures, and sidewalks.

SingleStep® meets Type I, Class A requirements of ASTM C 1315 as they relate to physical characteristics including clarity, solids content, flash point and shelf life. SingleStep® also meets Type I, Class A requirements of ASTM C 1315 as they relate to product performance, including rapid drying, uniform defect-free coating and resistance to accelerated weathering.

# Typical Technical Data

FORM: clear, colorless liquid

SPECIFIC GRAVITY: 0.88

pH: not applicable

WEIGHT/GALLON: 7.32 pounds

ACTIVE CONTENT: 24 percent

TOTAL SOLIDS: 25 percent

FLASH POINT: greater than 100 degrees Fahrenheit (greater than 38 degrees Celsius)

FREEZE POINT: no data

SHELF LIFE: 2 years in tightly sealed, unopened container

VOC CONTENT: 700 g/L, maximum. Complies with USEPA AIM VOC regulations. May not be suitable for sale in states and districts with more restrictive regulations.

# Limitations

- May show rubber burns.

- Not gasoline resistant.

- Do not use on carbonated concrete.

- Not designed for application to asphaltic or painted surfaces. Always test.

- Not for surfaces set for coatings or bonded overlays.

- Not for use around pools or fountains.

- Will not prevent water penetration through structural cracks, defects or open joints.

- Not recommended for below-grade application.

- Not suitable for sale in districts and states with more restrictive AIM VOC regulations.

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for PROSOCO SingleStep®. Do not dilute or alter. Apply as packaged. Stir or mix well before use.

New Concrete

SPECIFIER NOTE: Wait at least 3 hours after freshly poured concrete has received final finishing, and until all surface water is gone before beginning application.

- Using a low pressure sprayer, apply a thin, uniform coat without producing puddles. Do not over apply.

- Allow product to dry tack free. If needed for film uniformity, apply a second coat 24-hours after the first.

SPECIFIER NOTE: Two light coats are preferable to one heavy coat.

SPECIFIER NOTE: Best practice is to apply SingleStep® to the vertical edges of sidewalks after the form work has been removed.

Existing Concrete

SPECIFIER NOTE: Application may begin as soon as surfaces are dry and free of ponded water. See Manufacturer’s Product Data Sheet for more preparation informant.

- Using a low pressure sprayer, apply a thin uniform coat without producing puddles. Do not over apply.

- Allow product to dry tack free. If needed for film uniformity, apply a second coat 24-hours after the first.

SPECIFIER NOTE: Two light coats are preferable to one heavy coat.

Drying Time: SingleStep® dries to the touch in 2 hours. Protect freshly treated concrete from foot traffic for 8 hours and from water and vehicular traffic for 24 hours. Treated surfaces develop their chemical resistance in seven days.

Cleanup: Clean tools and equipment with xylene or other appropriate solvent.