Sure Klean® White Scum Remover Cleaning Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions. Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer:  PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® White Scum Remover is a blend of inorganic and mild organic acids and special wetting agents and inhibitors, that safely and easily removes salt scum (carbonates and sulfates) from clay brick and tile surfaces without discoloring or altering the surface.

Technical Data

FORM: Clear liquid

SPECIFIC GRAVITY: 1.11

TOTAL SOLIDS: N/A

pH: 1.6 (@ 1:1 dilution)

WT./Gal.: 9.25 lbs

FLASH POINT: N/A

FREEZE POINT: N/A

Limitations

- Not for use on concrete, cementitious surfaces, stucco or natural stone. White Scum Remover is for use on clay brick and tile surfaces only.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for White Scum Remover.  Dilute White Scum Remover concentrate with 1 part concentrate to 1 part water or as test area results indicate.

1. Prewet the surface with clean water.

2. Apply diluted cleaning solution generously using low-pressure spray (40 psi), a densely filled masonry washing brush, or roller.

3. Leave diluted cleaning solution on surface for 2 to 3 minutes.

4. Reapply the cleaning solution and scrub the surface as required.

5. Rinse with low pressure to remove initial acidic residue. Then rinse the treated area thoroughly using high-pressure spray. The best combination of rinsing pressure and water volume is provided by masonry washing equipment generating 400-1000 psi with a water flow rate of 6-8 gallons per minute delivered through a 15-45 degree fan spray tip. Equipment should be adjustable to reduce water flow rate and rinsing pressure as required for controlled cleaning of more sensitive surfaces. See also “Equipment” section of the Product Data Sheet.