Propex Operating Company, LLC	July 2012

PO Box 22788

Chattanooga, Tennessee  37422

Phone	800-621-1273

Website	www.fibermesh.com

E-mail	fibermesh@propexglobal.com

Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format as described in The Project Resource Manual—CSI Manual of Practice.  The section must be carefully reviewed and edited by the Architect or Engineer to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” when editing this section.

Section numbers are from MasterFormat 1995 Edition, with numbers from MasterFormat 2004 Edition in parentheses.  Delete version not required.

SECTION 03240 (03 24 00)

STEEL FIBER REINFORCEMENT

Specifier Notes:  This section covers Propex Novocon® 1050 steel fibers for use as concrete primary, flexural, and/or secondary reinforcement.  Consult Propex for assistance in editing this section for the specific application.

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Steel fibers used as concrete primary, flexural, and/or secondary reinforcement.

1.2	RELATED SECTIONS

Specifier Notes:  Edit the following list of related sections as required for the project.  List other sections with work directly related to this section.

A.	Section 02750 (32 13 00) - Rigid Paving.

B.	Section 03210 (03 21 00) - Reinforcing Steel.

C.	Section 03300 (03 30 00) - Cast-in-Place Concrete.

D.	Section 03400 (03 40 00) - Precast Concrete.

E.	Section 03500 (03 50 00) - Cementitious Decks and Toppings.

1.3	REFERENCES

Specifier Notes:  List standards referenced in this section, complete with designations and titles.  This article does not require compliance with standards, but is merely a listing of those used.

A.	ASTM A 820/A 820M - Standard Specification for Steel Fibers for Fiber-Reinforced Concrete.

B.	ASTM C 94 - Standard Specification for Ready-Mixed Concrete.

C.	UL Report File No. R14701 (N).

1.4	SUBMITTALS

A.	Comply with Section 01330 (01 33 00) - Submittal Procedures.

B.	Product Data:  Submit manufacturer’s product data, including application rate and mixing instructions.

Specifier Notes:  Delete samples if not required.

C.	Samples:  Submit manufacturer’s sample of steel fiber reinforcement.

D.	Manufacturer’s Certification:

1.	Submit manufacturer’s certification that steel fiber reinforcement complies with specified requirements.

2.	Submit evidence of satisfactory performance history of steel fiber reinforcement.

1.5	QUALITY ASSURANCE

Specifier Notes:  In the section specifying the concrete, in the Quality Assurance article, Preconstruction Meeting paragraph, add text to review the addition of steel fiber reinforcement to the concrete mixture, including application rate and mixing instructions.  A representative from the steel fiber reinforcement manufacturer should attend this meeting.

A.	Manufacturer’s Qualifications:  Satisfactory performance history of specified steel fiber reinforcement.

1.6	DELIVERY, STORAGE, AND HANDLING

A.	Delivery:  Deliver steel fiber reinforcement in manufacturer’s original, unopened, undamaged containers and packaging, with labels clearly identifying product name, manufacturer, and weight of fibers.

B.	Storage:

1.	Store steel fiber reinforcement in clean, dry area indoors in accordance with manufacturer’s instructions.

2.	Keep packaging sealed until ready for use.

3.	Protect pallets against rain and snow.

4.	Do not stack pallets on top of each other.

C.	Handling:  Protect steel fiber reinforcement during handling to prevent contamination.

PART 2	PRODUCTS

2.1	MANUFACTURER

A.	Propex Operating Company, LLC.  PO Box 22788, Chattanooga, Tennessee  37422.

Toll Free 800-621-1273. Website www.fibermesh.com. E-mail fibermesh@propexglobal.com.

2.2	STEEL FIBER REINFORCEMENT

A.	Steel Fiber Reinforcement:  Novocon 1050.

1.	Material:  Cold-drawn steel wire, with deformed ends.

2.	Conformance:  ASTM A 820/A 820M, Type I.

3.	Fire Classification:  UL Report File No. R14701 (N).

4.	Tensile Strength:  Minimum 152,000 psi (1,050 MPa).

5.	Fiber Length:  2 inches (50 mm).

6.	Equivalent Diameter:  0.039 inch (1.0 mm).

7.	Aspect Ratio:  50.

8.	Appearance:  Bright and clean wire.

PART 3	EXECUTION

3.1	MIXING

A.	Add steel fiber reinforcement to concrete mixture in accordance with manufacturer’s instructions and ASTM C 94.

B.	Add steel fiber reinforcement into concrete mixer during or after batching other concrete materials.  Do not add fibers into concrete mixer as first material.

Specifier Notes:  Specify application rate of steel fiber reinforcement.  The fiber application rate will vary depending on the type of application, concrete mix design, and the performance/toughness requirements of the specific application.  Typically, fiber application rate will range from 25 to 75 pounds per cubic yard (15 to 45 kg/m3) of concrete.  Consult Propex for more information.

C.	Application Rate:  Add steel fiber reinforcement at application rate of _______ pounds per cubic yard ( _______ kg/m3) of concrete.

D.	Add steel fiber reinforcement to concrete and mix in concrete mixer for 75 rotations at full mixing speed to ensure uniform distribution and random orientation of fibers throughout concrete.

Specifier Notes:  Insert section number of the section specifying the concrete.

E.	Concrete shall be as specified in Section __________ .

3.2	PLACING AND FINISHING

Specifier Notes:  Insert section number of the section specifying the concrete.

A.	Placing and finishing concrete shall be as specified in Section __________ .

END OF SECTION