Sika Sarnafil

S327 RhinoBond

Roofing System

Introduction

Sarnafil S327 RhinoBond Roofing System	iii

Regional Offices	iv

Part 1 – General Conditions

1.01 Description	1

1.02 Quality Assurance	1

1.03 Submittals	1

1.04 Code Requirements	2

1.05 Product Delivery, Storage and Handling	2

1.06 Job Conditions	3

1.07 Bidding Requirements	4

1.08 Warranties	5

1.09 Warranty Durations	5

Part 2 - Products

2.01 General	5

2.02 Membrane	6

2.03 Flashing Materials	7

2.04 Insulation/Overlayment/Barrier Board	9

2.05 Attachment Components	10

2.06 Deck Primers	11

2.07 Walkway Protection	11

2.08 Vapor Barrier	11

2.09 Miscellaneous Accessories	12

2.10 Sealants and Pitch Pocket Fillers	12

2.11 Miscellaneous Fasteners and Anchors	13

2.12 Related Materials	13

Part 3 – Execution

3.01 Pre-Construction Conference	13

3.02 Substrate Condition	13

3.03 Substrate Preparation	14

3.04 Substrate Inspection	16

3.05 Vapor Barrier/Air Barrier Installation (As Required by Designer)	16

3.06 Wood Nailer Installation	18

3.07 Insulation Installation	18

3.08 Overlayment Board Installation	19

3.09 Installation of Sarnafil Membrane	20

3.10 RhinoBond Induction Welding	21

3.11 Hot-Air Welding of Seam Overlaps	21

3.12 Membrane Flashings	22

3.13 Metal Flashings	23

3.14 Sarnaclad Metal Base Flashings/Edge Metal	23

3.15 Edge-Tite Metal	23

3.16 Anchor-Tite Metal	24

3.17 Walkway Installation	24

3.18 Perimeter Warning Tape	25

3.19 Temporary Cut-Off	25

3.20 Completion	25

3.21 Details	25

INTRODUCTION TO

SIKA SARNAFIL S327 RHINOBOND ROOFING SYSTEM

The Sika Sarnafil RhinoBond Roofing Systems use the polyester reinforced Sarnafil S327 roof membrane.  The S327 membrane is welded directly to the 3 inch (76 mm) diameter polymer coated metal Sarnadisc .  The S327 RhinoBond Roofing System is described as follows:

S327 RhinoBond Metal Retrofit is a non penetrating system that uses 3 inch (76 mm) diameter, polymer coated metal discs.  Adjacent membrane panels are lapped and overlaps are heat-welded with a Sarnamatic hot-air welder.  The S327 membrane is then induction welded to the RhinoBond plate.

The advantages of the S327 RhinoBond Roofing System are speed at which a building can be “dried-in”, simplicity of design and minimizing sheet flutter.  The S327 RhinoBond System is a cost-effective, non-penetrating Roofing System using the Sarnafil S327 membrane.

S327 utilizes a high-strength polyester reinforcement that allows the system to exceed Factory Mutual requirements for wind uplift testing.  The manufacturing process imparts dimensional stability and minimizes water-wicking by the reinforcement. S327 is lacquer-coated on the weathering surface to reduce dirt pick up; a Sarnafil membrane exclusive feature.  It is available in EnergySmart® white and other colors.

S327 is marked at the factory with seam overlap lines with the 3 inch (76 mm) line used for aligning the sheets and creating the overlap.

The attached Guide Specification is generic in nature and should be amended as required to meet the project’s specific needs.  Prior to bid, submit amended Specifications with Detail Drawings to Sika Sarnafil’s Technical Department for review and comment with regards to Sika Sarnafil requirements.

We welcome you to review the following Guide Specification and Detail Drawings and we ask that you contact us if you have any questions or need any additional information.

Thank you for choosing Sika Sarnafil for your roofing and waterproofing needs.

Note to Specifier:

Notes to Specifier are designated by [ ].  Specifier is to select one of the options provided for project specific specifications.

REGIONAL OFFICES

| NEW ENGLAND REGION 225 Dan Road Canton, MA 02021 Phone:(781) 821-0865 Fax:(781) 821-9205 EASTERN REGION One Park Way 3rd Floor Upper Saddle River, NJ 07458 Phone:(201) 327-0479 Fax:(201) 327-4069 SOUTHERN REGION 3483 Satellite Boulevard Duluth, GA 30096 Phone:(770) 495-0025 Fax:(770) 495-0027 MIDWEST REGION 16614 W. 159th St., Suite 303 Lockport, IL 60441 Phone:(815) 838-3838 Fax:(815) 838-1722 | SOUTHWEST REGION 1213 West Loop, N, Suite 130 Houston, Texas 77055 Phone: (713) 812-0102 Fax: (713) 812-0107 NORTHWEST REGION 20412 87th Avenue South Kent, WA 98031 Phone:(253) 872-0258 Fax:(253) 872-0273 MOUNTAIN REGION 2881 South 900 West Salt Lake City, Utah 84119 Phone:(801) 575-8648 Fax:(801) 355-4407 WESTERN REGION 10701 Holder Street Cypress, CA 90630 Phone:(714) 821-9377 Fax:(714) 821-9356 |
| --- | --- |
| CANADA Sika Sarnafil 6820 Davand Drive Mississauga, ON L5T 1J5 Canada Phone:(800) 268-0479 Fax:(905) 670-5278 www.sika.ca |
| WEB ADDRESS: www.sikacorp.com | EMAIL ADDRESS: webmaster.sarnafil@us.sika.com |

SECTION 075419.13

RHINOBOND ATTACHED

THERMOPLASTIC MEMBRANE ROOFING

FEATURING SPECIAL COATED PLATES & SCREWS

# GENERAL CONDITIONS

## DESCRIPTION

### Scope

To install a complete RhinoBond attached Sika Sarnafil roofing system including membrane, flashings and other components.

### Related Work

The work includes but is not limited to the installation of:

#### Substrate Preparation

#### Roof Drains

#### Vapor Barrier

#### Wood Blocking

#### Insulation

#### Separation Layers

#### Roof Membrane

#### Fasteners

#### Adhesive for Flashings

#### Roof Membrane Flashings

#### Walkways

#### Metal Flashings

#### Sealants

### Upon successful completion of work the following warranties may be obtained:

#### Sika Sarnafil Warranty

#### Roofing Applicator Warranty

## QUALITY ASSURANCE

### This roofing system shall be applied only by a Roofing Applicator authorized by Sika Sarnafil prior to bid (Sika Sarnafil "Applicator").

### Upon completion of the installation and the delivery to Sika Sarnafil by the Applicator of certification that all work has been done in strict accordance with the contract specifications and Sika Sarnafil's requirements, a Sika Sarnafil Technical Service Representative will review the installed roof system wherever a Standard or System warranty has been specified.

### There shall be no deviation made from the Project Specification or the approved shop drawings without prior written approval by the Owner, the Owner's Representative and Sika Sarnafil.

### All work pertaining to the installation of Sarnafil membrane and flashings shall only be completed by Applicator personnel trained and authorized by Sika Sarnafil in those procedures.

## SUBMITTALS

At the time of bidding, the Applicator shall submit to the Owner (or Representative) the following:

### Copies of Specification.

### Samples of each primary component to be used in the roof system and the manufacturer's current literature for each component.

### Written approval by the insulation manufacturer (as applicable) for use and performance of the product in the proposed system.

### Sample copy of Sika Sarnafil's warranty.

### Sample copy of Applicator's warranty.

### Dimensioned shop drawings which shall include:

#### Outline of roof with roof size and elevations shown.

#### Profile details of flashing methods for penetrations.

#### Technical acceptance from Sika Sarnafil.

### Certifications by manufacturers of roofing and insulating materials that all materials supplied comply with all requirements of the identified ASTM and other industry standards or practices.

### Certification from the Applicator that the system specified meets all identified code and insurance requirements as required by the Specification.

### Material Safety Data Sheets (MSDS)

## CODE REQUIREMENTS

The Applicator shall submit evidence that the proposed roof system meets the requirements of the local building code and has been tested and approved or listed by the following test organizations.  These requirements are minimum standards and no roofing work shall commence without written documentation of the system's compliance, as required in the "Submittals" section of this specification.

[NOTE TO SPECIFIER:  IF REQUIRED, SELECT FROM A, or B 1-3 , and C 1-3 BELOW.]

### System shall be designed to meet a minimum wind design requirements of the most recent version of ASCE 7.

### Factory Mutual Research Corporation (FM) - Norwood, MA

#### Class 1-60 (required for most situations)

#### Class 1-75 (for increased wind exposure)

#### Class 1-90 (for high wind exposure)

### Underwriters Laboratories, Inc. - Northbrook, IL

#### Class A assembly

#### Class B assembly

#### Class C assembly

## PRODUCT DELIVERY, STORAGE AND HANDLING

[NOTE TO SPECIFIER:  IF REQUIRED, SELECT ITEM G BELOW.]

### All products delivered to the job site shall be in the original unopened containers or wrappings bearing all seals and approvals.

### Handle all materials to prevent damage.  Place all materials on pallets and fully protect from moisture.

### Membrane rolls shall be stored lying down on pallets and fully protected from the weather with clean canvas tarpaulins.  Unvented polyethylene tarpaulins are not accepted due to the accumulation of moisture beneath the tarpaulin in certain weather conditions that may affect the ease of membrane weldability.

### As a general rule all adhesives shall be stored at temperatures between 40 degree F (5 degree C) and 80 degree F (27 degree C).  Read instructions contained on adhesive canister for specific storage instructions.

### All flammable materials shall be stored in a cool, dry area away from sparks and open flames.  Follow precautions outlined on containers or supplied by material manufacturer/supplier.

### Any materials which the Owner’s representative or Sika Sarnafil determine to be damaged are to be removed from the job site and replaced at no cost to the Owner.

### The existing pvc roof membrane is to be recycled by the manufacturer of the replacement membrane.  Applicator is responsible for all costs associated with removing the membrane, preparing it and loading it for shipment, according to the manufacturer’s published procedures.

## JOB CONDITIONS

### Sarnafil materials may be installed under certain adverse weather conditions but only after consultation with Sika Sarnafil, as installation time and system integrity may be affected.

### Only as much of the new roofing as can be made weathertight each day, including all flashing and detail work, shall be installed.  All seams shall be cleaned and heat welded before leaving the job site that day.

### All work shall be scheduled and executed without exposing the interior building areas to the effects of inclement weather.  The existing building and its contents shall be protected against all risks.

### All surfaces to receive new insulation, membrane or flashings shall be dry.  Should surface moisture occur, the Applicator shall provide the necessary equipment to dry the surface prior to application.

### All new and temporary construction, including equipment and accessories, shall be secured in such a manner as to preclude wind blow-off and subsequent roof or equipment damage.

### Uninterrupted waterstops shall be installed at the end of each day's work and shall be completely removed before proceeding with the next day's work. Waterstops shall not emit dangerous or unsafe fumes and shall not remain in contact with the finished roof as the installation progresses.  Contaminated membrane shall be replaced at no cost to the Owner.

### The Applicator is cautioned that certain Sarnafil membranes are incompatible with asphalt, coal tar, heavy oils, roofing cements, creosote and some preservative materials.  Such materials shall not remain in contact with Sarnafil membranes.  The Applicator shall consult Sika Sarnafil regarding compatibility, precautions and recommendations.

### Arrange work sequence to avoid use of newly constructed roofing as a walking surface or for equipment movement and storage.  Where such access is absolutely required, the Applicator shall provide all necessary protection and barriers to segregate the work area and to prevent damage to adjacent areas.  A substantial protection layer consisting of plywood over Sarnafelt or plywood over insulation board shall be provided for all new and existing roof areas that receive rooftop traffic during construction.

### Prior to and during application, all dirt, debris and dust shall be removed from surfaces by vacuuming, sweeping, blowing with compressed air or similar methods.

### The Applicator shall follow all safety regulations as required by OSHA and any other applicable authority having jurisdiction.

### All roofing, insulation, flashings and metal work removed during construction shall be immediately taken off site to a legal dumping area authorized to receive such materials.  Hazardous materials, such as materials containing asbestos, are to be removed and disposed of in strict accordance with applicable City, State and Federal requirements.

### All new roofing waste material (i.e., scrap roof membrane, empty cans of adhesive) shall be immediately removed from the site by the Applicator and properly transported to a legal dumping area authorized to receive such material.

### The Applicator shall take precautions that storage and application of materials and equipment does not overload the roof deck or building structure.

### Installation of a Sarnafil membrane over coal tar pitch or a resaturated roof requires special consideration to protect the Sarnafil membrane from volatile fumes and materials.  Consult Sika Sarnafil for precautions prior to bid.

### Flammable adhesives and deck primers shall not be stored and not be used in the vicinity of open flames, sparks and excessive heat.

### All rooftop contamination that is anticipated or that is occurring shall be reported to Sika Sarnafil to determine the corrective steps to be taken.

### The Applicator shall verify that all roof drain lines are functioning correctly (not clogged or blocked) before starting work.  Applicator shall report any such blockages in writing (letter copy to Sika Sarnafil) to the Owner's Representative for corrective action prior to the installation of the Sika Sarnafil roof system.

### Applicator shall immediately stop work if any unusual or concealed condition is discovered and shall immediately notify Owner of such condition in writing for correction at the Owner's expense (letter copy to Sika Sarnafil).

### Site cleanup, including both interior and exterior building areas that have been affected by construction, shall be completed to the Owner's satisfaction.

### All landscaped areas damaged by construction activities shall be repaired at no cost to the Owner.

### The Applicator shall conduct fastener pullout tests in accordance with the latest version of the SPRI/ANSI Fastener Pullout Standard to verify condition of the deck/substrate and to confirm expected pullout values.

### The Sarnafil membrane shall not be installed under the following conditions without consulting Sika Sarnafil’s Technical Dept. for precautionary steps:

#### The roof assembly permits interior air to pressurize the membrane underside.

#### Any exterior wall has 10 percent or more of the surface area comprised of opening doors or windows.

#### The wall/deck intersection permits air entry into the wall flashing area.

### Precautions shall be taken when using Sarnacol adhesives at or near rooftop vents or air intakes.  Adhesive odors could enter the building.  Coordinate the operation of vents and air intakes in such a manner as to avoid the intake of adhesive odor while ventilating the building.  Keep lids on unused cans at all times.

### Protective wear shall be worn when using solvents or adhesives or as required by job conditions.

### Sarnafil membranes are slippery when wet or covered with snow, frost, or ice.  Working on surfaces under these conditions is hazardous.  Appropriate safety measures must be implemented prior to working on such surfaces.  Always follow OSHA and other relevant fall protection standards when working on roofs.

## BIDDING REQUIREMENTS

### Pre-Bid Meeting:

A pre-bid meeting shall be held with the Owner's Representative and involved trades to discuss all aspects of the project.  The Applicator's field representative or roofing foreman for the work shall be in attendance.  Procedures to avoid rooftop damage by other trades shall be determined.

### Site Visit:

Bidders shall visit the site and carefully examine the areas in question as to conditions that may affect proper execution of the work.  All dimensions and quantities shall be determined or verified by the Applicator.  No claims for extra costs will be allowed because of lack of full knowledge of the existing conditions unless agreed to in advance with the Owner or Owner's Representative.

## WARRANTIES

[NOTE TO SPECIFIER:  SELECT A, B, OR C.  D AND E SHOULD ALWAYS BE SPECIFIED.]

### Sika Sarnafil Membrane Warranty

Upon successful completion of the work to Sika Sarnafil's satisfaction and receipt of final payment, the Sika Sarnafil Membrane Warranty shall be issued.

### Sika Sarnafil Standard Warranty (only products purchased from Sika Sarnafil are covered under Standard Warranty)

Upon successful completion of the work to Sika Sarnafil's satisfaction and receipt of final payment, the Sika Sarnafil Standard Warranty shall be issued.

### Sika Sarnafil System Warranty (only products purchased from Sika Sarnafil are covered under System Warranty)

Upon successful completion of the work to Sika Sarnafil's satisfaction and receipt of final payment, the Sika Sarnafil System Warranty shall be issued.

### Applicator/Roofing Contractor Warranty

Applicator shall supply Owner with a separate workmanship warranty.  In the event any work related to roofing, flashing, or metal is found to be within the Applicator warranty term, defective or otherwise not in accordance with Contract Documents, the Applicator shall repair that defect at no cost to Owner.  Applicator's warranty obligation shall run directly to Owner, and a copy shall be sent to Sika Sarnafil.

### Owner Responsibility

Owner shall notify both Sika Sarnafil and the Applicator of any leaks as they occur during the time period when both warranties are in effect.

## WARRANTY DURATIONS

[NOTE TO SPECIFIER:  SPECIFY EITHER 5, 10, OR 15 YEAR DURATION BELOW FOR SIKA SARNAFIL WARRANTY]

### Sika Sarnafil’s warranty shall be in effect for a           year duration.

### Applicator’s/Roofing Contractor’s Warranty shall be in effect for a           year duration.

# PRODUCTS

##### GENERAL

### The components of the Sika Sarnafil RhinoBond-attached roof system are to be products of Sika Sarnafil as indicated on the Detail Drawings and specified in the Contract Documents.

### Components to be used that are other than those supplied or manufactured by Sika Sarnafil may be submitted for review and acceptance by Sika Sarnafil.  Sika Sarnafil’s acceptance of any other product is only for a determination of compatibility with Sika Sarnafil products and not for inclusion in the Sika Sarnafil warranty.  The specifications, installation instructions, limitations, and restrictions of the respective manufacturers must be reviewed by the Owner’s Representative for acceptability for the intended use with Sika Sarnafil products.

### Manufacturer to have a minimum of two years experience recycling their membranes at the end of their service life back into new membrane products.  Provide a minimum of five reference projects.

### Condensation or moisture migration into the roof system must be controlled so that it does not compromise the performance of the insulation and other components of the assembly.  Moisture vapor tends to migrate from warmer to cooler areas.  Air/vapor retarders are used to inhibit or block the flow of warm moist air into the roof system.  To determine if an air/vapor barrier is necessary, a design professional with experience with air handling and moisture control should be consulted.

Special consideration should be given to construction related moisture.  An example is the significant amount of moisture generated when concrete floor slabs are poured after the roof has been installed.  Sika Sarnafil is not responsible for damage to the insulation when exposed to construction related moisture.

##### MEMBRANE

### Sarnafil S327 polyester reinforced membrane with a lacquer coating.

### Membrane shall conform to ASTM D4434 (latest version), “Standard for Polyvinyl Chloride Sheet Roofing,” Classification:  Type III.

[NOTE TO SPECIFIER:  VARIOUS SARNAFIL S327 MEMBRANES ARE LISTED.  GENERALLY PHYSICAL PROPERTIES SUCH AS PUNCTURE RESISTANCE INCREASE AS MEMBRANE THICKNESS INCREASES.  SELECT APPROPRIATE PRODUCT.]

#### 10S327-12, 48 mil (1.2 mm), thermoplastic membrane with polyester reinforcement.

#### 10S327-15, 60 mil (1.5 mm), thermoplastic membrane with polyester reinforcement.

#### 10S327-18, 72 mil (1.8 mm), thermoplastic membrane with polyester reinforcement.

#### 10S327-20, 80 mil (2.0 mm), thermoplastic membrane with polyester reinforcement.

[NOTE TO SPECIFIER:  ADD ONE OF THE FOLLOWING WIDTHS TO THE ITEM SELECTED IN 2.02, B, 1-4: 10 FEET (3.0 M), 5 FEET (1.5 M), OR 6.56 FEET (2 M)]

### Certified Polymer Thickness

[(OPTIONAL) NOTE TO SPECIFIER: - TO CERTIFY POLYMER THICKNESS INCLUDE 2.02, C, 1.]

#### Membrane manufacturer is to certify that the polymer thickness is of the polymer thickness specified (see 2.02, B, 1-4).  Certification is to be signed by the membrane manufacturer’s quality control manager.  ASTM +/- tolerance for membrane thickness is not accepted.

### Color of Membrane

[NOTE TO SPECIFIER:  SARNAFIL’S ENERGYSMART ROOF MEMBRANE IS AN ENERGY STAR LISTED PRODUCT.  SPECIFY ENERGYSMART ROOF MEMBRANE UNLESS A SPECIAL COLOR IS REQUIRED.]

#### EnergySmart (white), initial reflectivity of 0.83, initial emissivity 0.90, solar reflective index (SRI) of >104.

#### Other

### Typical Physical Properties

[NOTE TO SPECIFIER:  LIST MIL THICKNESS OF MEMBRANE DESIRED – TOP ITEM SHOWN UNDER PHYSICAL PROPERTIES.]

| Parameters | ASTM Test Method | Minimum ASTM Requirement | Sarnafil Typical Physical Properties |
| --- | --- | --- | --- |
| Reinforcing Material | - |  | Polyester |
| Overall Thickness, min., inches (mm) | D751 | 0.045 (1.14) | [0.0__inches] |
| Breaking Strength, min., lbf/in. (KN/m) | D751 | 200 (35.0) | 230 (40.0) |
| Elongation at Break, min. | D751 | 15% | 20% |
| Seam strength*, min. (% of breaking strength) | D751 | 75 | 85 |
| Retention of Properties After Heat Aging | D3045 | - | - |
| Breaking Strength, min., (% of original) | D751 | 90 | 95 |
| Elongation, min., (% of original) | D751 | 90 | 90 |
| Tearing Strength, min., lbf (N) | D1004 | 45.0 (200) | 50 (220) |
| Low Temperature Bend, -40°F (-40°C) | D2136 | Pass | Pass |
| Accelerated Weathering Test (Florescent Light, UV exposure) | G154 | 5,000 Hours | Pass |
| Cracking (7x magnification) | - | None | None |
| Discoloration (by observation) | - | Negligible | Negligible |
| Crazing (7 x magnification) | - | None | None |
| Linear Dimensional Change | D1204 | 0.5% max. | 0.1% |
| Weight Change After Immersion in Water | D570 | + 3.0% max. | 2.5% |
| Static Puncture Resistance, 33 lbf (15 kg) | D5602 | Pass | Pass |
| Dynamic Puncture Resistance, 14.7 ft-lbf (20 J) | D5635 | Pass | Pass |
| Initial Solar Reflectance | E903 | - | 0.83 |
| Emissivity | E408, C1371, Other | - | 0.90 |
| Solar Reflective Index (SRI) | E1980 | - | 104 |
| Recycled Content (5 & 10 ft. sheets only) | Up to 12% Pre-Consumer / Up to 1% Post Consumer. |
| * Failure occurs through membrane rupture not seam failure. Physical Properties shown are prior to applying felt backing, if specified. |

##### FLASHING MATERIALS

### Wall/Curb Flashing

#### Sarnafil G410 Membrane

A fiberglass reinforced membrane adhered to approved substrate using Sarnacol adhesive.  Consult Product Data Sheets for adhesive options and additional information.

#### Sarnafil G459 Membrane

An asphalt-resistant, fiberglass reinforced membrane adhered to approved substrate using Sarnacol adhesive.  Consult Product Data Sheet for adhesive rates and additional information.

#### Sarnafil S327 Membrane

A polyester reinforced membrane used for mechanically-attached flashings to approved substrate using Sarnadisc or Sarnabar. Consult Product Data Sheet for additional information.

#### Sarnaclad

A PVC-coated, heat-weldable sheet metal capable of being formed into a variety of shapes and profiles.  Sarnaclad is a 24 gauge, G90 galvanized metal sheet with a 20 mil (0.5 mm) unsupported Sarnafil membrane laminated on one side.  The dimensions of Sarnaclad are 4 ft x 8 ft (1.2 m x 2.4 m) or 4 ft x 10 ft (1.2 m x 3.0 m).  Consult Product Data Sheet for additional information.

### Perimeter Edge Flashing

[NOTE TO SPECIFIER:  SELECT 1, 2, 3, OR 4 AND SPECIFY COLOR.]

#### Edge-Tite Flashing

A prefabricated perimeter edge attachment and fascia assembly provided by Sika Sarnafil.  Edge-Tite is made from three distinct parts.  The (base) rail is made of formed 0.050 inch (1.3 mm) thick, 5052-H32 mill-finish alloy aluminum in 12 foot (3.6 m) lengths, provided with predrilled fastening holes.  The spring clips are 6 inches (152 mm) wide and made from 0.020 inch (0.5 mm) stainless steel.  The snap-on fascia is made from 24 gauge (0.6 mm) G90 steel or from 0.040 inch (1.0 mm) aluminum in 12 foot (3.6 m) lengths.  Edge-Tite is available in a variety of fascia widths.  Color and fascia metal shall be                         .  Consult Product Data Sheet for additional information.

#### Anchor-Tite Flashing

A heavy-duty prefabricated perimeter edge attachment and fascia assembly provided by Sika Sarnafil.  Anchor-Tite is made of two distinct parts.  The anchor bar is extruded 0.125 inch (3.0 m) thick from 6063-T6 alloy aluminum in 12 foot (3.5 mm) lengths, provided with predrilled fastening holes.  Snap-on fascia covers are formed from either 24 gauge galvanized steel with Kynar or 0.40 inch (10 mm) aluminum with Kynar, anodized or mill finish.   Anchor-Tite is available in a variety of fascia widths.  Color and fascia metal type shall be                         .

#### Sarnaclad

A PVC-coated, heat-weldable sheet metal capable of being formed into a variety of shapes and profiles.  Sarnaclad is a 24 gauge, G90 galvanized metal sheet with a 20 mil (0.5 mm) unsupported Sarnafil membrane laminated on one side.  The dimensions of Sarnaclad are 4 ft x 8 ft (1.2 m x 2.4 m) or 4 ft x 10 ft (1.2 m x 3.0 m).  Consult Product Data Sheet for additional information.

#### Non-Typical Edge

Project-specific perimeter edge detail reviewed and accepted for one-time use by Sika Sarnafil's Technical Department.  Consult Regional Technical Manager prior to job start for review and consideration for acceptance.

### Miscellaneous Flashing

#### Sarnaflash

A prefabricated expansion joint cover made from Sarnafil membrane.  Sarnaflash is designed for securement to vertical or horizontal surfaces to span and accommodate the movement of expansion gaps from 1 inch to 4-1/2 inches (25 mm to 114 mm) across.  Available in 40 foot (12 m) rolls.  Consult Product Data Sheet for additional information.

#### Sarnareglet

A heavy-duty, extruded aluminum flashing termination reglet used at walls and large curbs.  Sarnareglet is produced from 6063-T5, 0.10 inch - 0.12 inch (2.5 mm - 3.0 mm) thick extruded aluminum.  Sarnareglet has a 2-1/4 inch (57 mm) deep profile, and is provided in 10 foot (3 m) lengths.  Use prefabricated Sarnareglet mitered inside and outside corners where walls intersect. Consult Product Data Sheet for additional information.

#### Sarnastack

A prefabricated vent pipe flashing made from 0.048 inch (48 mil/1.2 mm) thick Sarnafil G410 membrane.  Available in five different sizes.  Consult Product Data Sheet for sizes and additional information.

#### Sarnadrain-RAC

PVC-coated, heavy-duty aluminum roof drain insert that mechanically seals to the drainpipe interior.  Sarnadrain-RAC is made of 0.080 inch (2 mm) thick 6063 aluminum with a urethane seal installed at the end of the drainpipe.  The large 14 inch x 14 inch (0.36 m x 0.36 m) drain strainer is also made of 0.080 inch (2 mm) thick aluminum stock.  The flange dimensions of Sarnadrain-RAC are 18 inches x 18 inches (0.46 m x 0.46 m).  Consult Product Data Sheet for sizes and additional information.

#### Sarnacircle-"S"

Circular 0.048 inch (48 mil/1.2 mm) thick S327 membrane patch welded over T-joints formed by overlapping thick membranes.

#### Sarnacorners - Universal

Prefabricated outside and inside flashing corners made of 0.060 inch (60 mil/1.5 mm) thick membrane that are heat-welded to membrane or Sarnaclad base flashings.  Available in one size which accommodate both inside and outside corners.  Can be cut into one inside or one outside corner.  Consult Product Data Sheet for additional information.

#### Multi-Purpose Sealant

A proprietary sealant used at flashing terminations.  Consult Product Data Sheet for additional information.

#### Sarnacol 2165 Adhesive

A two-component urethane adhesive used for pitch pocket filler.  Cures with excellent elasticity and adhesion to various surfaces.  Consult Product Data Sheet for additional information.

#### Sarnacol 2170 Adhesive

A solvent-based reactivating-type adhesive used to attach membrane to flashing substrate. Consult Product Data Sheets for additional information.

#### S327 Coverstrip

8 inch (0.20 m) wide precut flashing made from Sarnafil S327 polyester reinforced membrane.  Used to coverstrip Sarnabar and Sarnadisc.

##### INSULATION/OVERLAYMENT/BARRIER BOARD

[NOTE TO SPECIFIER:]

Condensation or moisture migration into the roof system must be controlled so that it does not compromise the performance of the insulation and other components of the assembly.  Moisture vapor tends to migrate from warmer to cooler areas.  Air/vapor retarders are used to inhibit or block the flow of warm moist air into the roof system.  To determine if an air/vapor barrier is necessary, a design professional with experience with air handling and moisture control should be consulted.

Special consideration should be given to construction related moisture.  An example is the significant amount of moisture generated when concrete floor slabs are poured after the roof has been installed.  Sika Sarnafil is not responsible for damage to insulation when exposed to construction related moisture.

### Sarnatherm

A rigid isocyanurate foam insulation with black mat facers.  Available in 4 x 4 ft (1.2 x 1.2 m) or 4 x 8 ft (1.2 x 2.4 m) sizes and various thicknesses.  Consult Product Data Sheet for additional information.

### Sarnatherm EPS

### Expanded polystyrene closed-cell foam insulation.  Available in 4 ft x 4 ft (1.2 m x 1.2 m) or 4 ft x 8 ft (1.2 m x 2.4 m) sizes and various thicknesses.  A one inch minimum isocyanurate or gypsum based thermal barrier must be placed between styrene boards and Sarnafil membrane.  Sarnatherm EPS insulation is for use beneath the waterproofing layer.  Not allowed direct to steel deck for FM insured buildings, an approved thermal barrier must be installed between the EPS and deck.  Consult Product Data Sheets for additional information.

### Sarnatherm EXPS

Extruded polystyrene closed-cell foam insulation.  Available in 4 ft x 4 ft (1.2 m x 1.2 m) or 4 ft x 8 ft (1.2 m x 2.4 m) sizes and various thicknesses.  A one inch minimum isocyanurate or gypsum based thermal barrier must be placed between styrene boards and Sarnafil membrane.  Not allowed direct to steel deck for FM insured buildings, an approved thermal barrier must be installed between the EXPS and deck.  Consult Product Data Sheets for additional information.

[NOTE TO SPECIFIER:  SELECT ONLY ONE TYPE OF INSULATION TO SPECIFY.]

### DensDeck

A siliconized gypsum, fire-tested hardboard with glass-mat facers. DensDeck is provided in 4 ft x 4 ft (1.2 m x 1.2 m) or 4 ft x 8 ft (1.2 m x 2.4 m) board size and in thicknesses of 1/4 inch, 1/2 inch and 5/8 inch (13 mm, 13 mm or 16 mm).  Consult Product Data Sheet for size, thickness and additional information.

### Securock

A fire-tested, homogenous fiber reinforced gypsum roof board.  Securock is provided in 4 feet x 4 feet (1.2 m x 1.2 m) and 4 feet x 8 feet (1.2 m x 2.4 m) board sizes and in thicknesses of 1/4 inch (6.6 mm), 3/8 inch (9.5 mm), 1/2 inch (12.7 mm) and 5/8 inch (15.9 mm).  Consult Product Data Sheet for size, thickness and additional information.

##### ATTACHMENT COMPONENTS

### Sarnaplate

Used with various Sarnafasteners to attach insulation boards to the roof deck.  Sarnaplate is a 3 inch (75 mm) square or round, 26 gauge stamping of SAE 1010 steel with an AZ 55 Galvalume coating.  Consult Product Data Sheet for additional information.

### Sarnaplate-Preassembled

Combination of a 3 inch (75 mm) round plate and a #12 fastener used to attach insulation boards to steel roof decks. Sarnaplate-Preassembled consists of a 3 inch (75 mm) round, 26 gauge stamping of SAE 1010 steel with an AZ 55 Galvalume coating and Sarnafastener #12 with modified buttress thread.  The fastener shank diameter is approximately 0.168 inch (4 mm) and the thread diameter is approximately 0.214 inch (5 mm).  Consult Product Data Sheet for additional information.

### Sarnadisc RhinoBond

A high strength plate with a polymer coating used with various Sarnafasteners to attach insulation boards to the roof deck and as a substrate to induction weld the S327 membrane.  Sarnadisc is a 3 inch (75 mm) round, 22 gauge corrosion resistant steel plate.  Consult Product Data Sheet for additional information.

### Sarnafastener #12

A  #12 corrosion-resistant fastener used with Sarnaplates to attach insulation boards to steel roof decks. Sarnafastener #12 has a modified buttress thread, a shank diameter of approximately 0.168 inch (4 mm) and a thread diameter of approximately 0.214 inch (5 mm).  The driving head has a diameter of approximately 0.435 inch (11 mm) with a #3 Phillips recess for positive engagement.  Not to be used to fasten Sarnadisc RhinoBond plates.  Consult Product Data Sheet for additional information.

### Sarnafastener-XP

A #15, heavy-duty, corrosion-resistant fastener used with Sarnaplate to attach insulation or Sarnadisc, Sarnadisc-XPN and Sarnabar to attach Sarnafil S327 roof membrane to steel roof decks. Sarnafastener-XP has a shank diameter of approximately 0.21 inch (5.3 mm) and the thread diameter is approximately 0.26 inch (6.6 mm).  The driving head has a diameter of approximately 0.435 inch (11 mm) with a #3 Phillips recess for positive engagement.  Consult Product Data Sheet for additional information.

### Sarnafastener-MAXLoad

A specially designed, heavy-duty, corrosion-resistant fastener used with the Sarnarail polymeric batten strip to clamp Sarnafil S327 roof membrane to roof decks.   Sarnafastener-MAXLoad may also be used to secure Sarnadisc-MAXLoad and Sarnafil S327 roof membrane to roof decks.  Sarnafastener-MAXLoad has a shank diameter of approximately 0.26 inch (6.6 mm) and a thread diameter of approximately 0.33 inch (8.4 mm). The driving head has a diameter of approximately 0.66 inch (16.8 mm) with a #3 Phillips recess for positive engagement and simplicity of application. Consult Product Data Sheet for additional information.

##### DECK PRIMERS

### Sarnavap Self-Adhered Primer

A solvent-based primer designed for use with Sarnavap Self-Adhered vapor barrier to prime wood, concrete, lightweight concrete, gypsum boards and decks, and DensDeck boards prior to application of Sarnavap Self-Adhered vapor barrier.  Consult Product Data Sheet for additional information.

### Sarnavap Self-Adhered Primer WB

A water-based primer designed for use with Sarnavap Self-Adhered vapor barrier to promote adhesion to most substrates.  Particularly recommended when use of solvent-based primer is not advised or permitted, however the ambient temperature must be 41 degree F (5 degree C) and rising.  Consult Product Data Sheet for additional information.

##### WALKWAY PROTECTION

[NOTE TO SPECIFIER:  SELECT ONE TYPE OF WALKWAY.]

### Sarnatred

A polyester reinforced, 0.096 inch (96 mil/2.4 mm), weldable membrane with surface embossment.  Used as a protection layer from rooftop traffic.  Sarnatred is supplied in rolls of 39.3 inches (1.0 m) wide and 32.8 feet (10 m) long.  Consult Product Data Sheet for additional information.

### Crossgrip Walkway

A rolled-out walkway protection mat used to protect Sarnafil roofing membrane from mechanical abuse.  Crossgrip Walkway is 9/16 inch (14 mm) thick flexible pvc with a heavily textured surface.  Crossgrip Walkway is loose laid on top of completed Sika Sarnafil roof assemblies.  Where design windspeeds exceed 94 mph (150 km/h) the walkway must be secured with loops of Sarnafil membrane welded to the field sheet.  Consult Product Data Sheet for additional information.

### Sand-Coated Walkway

A fiberglass reinforced, 60 mil, weldable membrane with a thick sand-based coating on top.  Net dimensions are approximately 150 mil (4 mm) thick by 26 inches (0.6 m), 39 inches (1.0 m), 78 inches (2.0 m) wide with varying lengths.  The standard length is 32 feet (10 m).  Consult Product Data Sheet for additional information.

##### VAPOR BARRIER

### Sarnavap-10

A 10 mil (0.25 mm) thick polyethylene vapor barrier/air barrier. Sarnavap-10 is supplied in a folded panel that is rolled onto a core.  The core width is 5 feet (1.5 m).  When unrolled off the core and unfolded, the sheet dimensions are 20 feet (6.9 m) wide by 100 feet (33 m) long.  Consult Product Data Sheet for additional information.

### Sarnavap Self-Adhered

A 32 mil (0.8 mm) self-adhesive vapor barrier that can also serve as temporary roof protection.  Sarnavap Self-Adhered is available in rolls 44.9 inches x 133.8 feet (1.14 x 40.8 m).  Consult Product Data Sheet for additional information.

##### MISCELLANEOUS ACCESSORIES

### Aluminum Tape

A 2 inch (50 mm) wide pressure-sensitive aluminum tape used as a separation layer between small areas of asphalt contamination and the membrane and as a bond-breaker under the coverstrip at Sarnaclad joints.

### Sealing Tape Strip

Compressible foam with pressure-sensitive adhesive on one side.  Used with metal flashings as a preventive measure against air and wind blown moisture entry.

### Multi-Purpose Tape

A high performance sealant tape used with metal flashings as a preventive measure against air and wind blown moisture entry.

### RhinoBond Induction Welder

A 110 volt induction welding device that creates a radio frequency that allows the membrane to be welded to a specially coated plate.

### Sarnamatic 641mc or 661

220 volt, self-propelled, hot-air welding machine used to seal Sarnafil membrane seams.

### Sarnasolv

A high quality solvent cleaner used for the general cleaning of residual asphalt, scuff marks, etc., from the membrane surface.  Sarnasolv is also used daily to clean seam areas prior to hot-air welding in tear off or dirty conditions or if the membrane is not welded the same day it is unrolled. Consult Product Data Sheet for additional information.

### Perimeter Warning Tape

Designed for use on PVC membranes as a reflective, highly visible pressure sensitive tape used to draw attention to roof perimeters and potential hazardous areas.

The tape is available in 2 inch wide rolls by 30 feet long and comes on a release liner for easy application.  Perimeter Warning Tape exceeds reflectivity 3 requirements and Federal spec. L-S-300, Class 1.

##### SEALANTS AND PITCH POCKET FILLERS

### Sarnafil Multi-Purpose Sealant (for termination details).

### Sarnacol 2165 Adhesive (two-component urethane adhesive for pitch pocket toppings).

### Depending on substrates, the following sealants are options for temporary overnight tie-ins:

#### Type III hot asphalt conforming to ASTM D312 (latest version).

#### Sarnacol 2165 Adhesive.

#### Multiple layers of roofing cement and felt.

#### Spray-applied, water-resistant urethane foam.

#### Mechanical attachment with rigid bars and compressed sealant.

##### MISCELLANEOUS FASTENERS AND ANCHORS

### All fasteners, anchors, nails, straps, bars, etc. shall be post-galvanized steel, aluminum or stainless steel.  Mixing metal types and methods of contact shall be assembled in such a manner as to avoid galvanic corrosion.  Fasteners for attachment of metal to masonry shall be expansion type fasteners with stainless steel pins.  All concrete fasteners and anchors shall have a minimum embedment of 1-1/4 inch (32 mm) and shall be approved for such use by the fastener manufacturer.  All miscellaneous wood fasteners and anchors used for flashings shall have a minimum embedment of 1 inch (25 mm) and shall be approved for such use by the fastener manufacturer.

##### RELATED MATERIALS

### Wood Nailer

Treated wood nailers shall be installed into the structural purlins at the perimeter of the entire roof and around such other roof projections and penetrations as specified on Project Drawings.  Thickness of nailers must match the insulation thickness to achieve a smooth transition.  Wood nailers shall be treated for fire and rot resistance (wolmanized or osmose treated) and be #2 quality or better lumber.  Creosote or asphalt-treated wood is not acceptable.  Wood nailers shall conform to Factory Mutual Loss Prevention Data Sheet 1-49.  All wood shall have a maximum moisture content of 19 percent by weight on a dry-weight basis.

### Plywood

When bonding directly to plywood, a minimum 1/2 inch (12 mm) CDX (C side out), smooth-surfaced exterior grade plywood with exterior grade glue shall be used.  Rough-surfaced plywood or high fastener heads will require the use of Sarnafelt behind the flashing membrane.  Plywood shall have a maximum moisture content of 19 percent by weight on a dry weight basis.

# EXECUTION

###### PRE-CONSTRUCTION CONFERENCE

### The Applicator, Owner's Representative/Designer and Manufacturer(s) shall attend a pre-construction conference.

### The meeting shall discuss all aspects of the project including but not limited to:

#### Safety

#### Set up

#### Construction schedule

#### Contract conditions

#### Coordination of the work

###### SUBSTRATE CONDITION

### Applicator shall be responsible for acceptance or provision of proper substrate to receive new roofing materials.

### Applicator shall verify that the work done under related sections meets the following conditions:

#### Roof drains, gutters and scuppers have been reconditioned or replaced and installed properly.

#### Roof curbs, nailers, equipment supports, vents and other roof penetrations are properly secured and prepared to receive new roofing materials.

#### All surfaces are smooth and free of dirt, debris and incompatible materials.

#### All roof surfaces shall be free of water, ice and snow.

###### SUBSTRATE PREPERATION

The roof deck and existing roof construction must be structurally sound to provide support for the new roof system.  The Applicator shall load materials on the rooftop in such a manner as to eliminate risk of deck overload due to concentrated weight.  The Owner's Representative shall ensure that the roof deck is secured to the structural framing according to local building code and in such a manner as to resist all anticipated wind loads in that location.

### New Construction

#### Steel Deck:

                - FM approved steel deck - The roof deck shall be 22 gauge (minimum) grade E and shall conform and be installed to meet the latest revision of FM's Loss Prevention Data Sheet 1-28 and the local code's current requirements.

                - Non-FM approved steel deck - The roof deck shall be 24 gauge (minimum) grade D and shall conform and be installed to the local code's current requirements.

#### Wood Deck:

                - FM approved wood deck - The roof deck shall be minimum 2 inch (50 mm) thick lumber or 3/4 inch (19 mm) thick treated plywood.  The deck shall conform to FM requirements for Class 1 fire-retardant and rot-resistant wood decks.  Deck shall be installed according to FM and local code requirements.

                - Non-FM approved wood deck - The roof deck shall be minimum 1-1/2 inch (38 mm) thick lumber or 15/32 inch (12 mm) thick plywood.  Deck shall be installed according to local code requirements.  Contact Sika Sarnafil Technical for fastening patterns and methods.

#### Poured Lightweight (Cellular) Concrete Substrate:

The lightweight concrete shall be installed by a trained lightweight concrete Applicator in accordance with the lightweight concrete manufacturer's requirements and industry practice.  The surface shall be sealed with a water-based sealer accepted by the lightweight concrete manufacturer to create a surface free from dust and loose material.  The wet and dry densities shall be in accordance with the manufacturer's and FM’s (if applicable) requirements. Sharp ridges or other projections above the surface shall be removed before roofing. An insulation recover board is required as a substrate to adhere to.  Fastening shall be into the structural deck below the lightweight concrete (see steel/concrete deck requirements).

#### Poured Structural Concrete Deck:

The roof deck shall be installed and cured in accordance with industry standards.  The surface shall have a smooth and level finish and shall be free of dust, excess moisture, oil-based curing agents and loose debris.  Sharp ridges or other projections above the surface shall be removed before roofing.  An insulation recover board is required.

#### Insulating Fill Substrate:

The lightweight fill shall be installed by a trained lightweight fill Applicator in accordance with the lightweight fill manufacturer's requirements and industry practice.  The surface shall be free from dust and loose fragments, be smooth, level, and free from moisture.  Sharp ridges or other projections above the surface shall be removed before roofing.  Proper venting as recommended by the roof deck manufacturer shall be provided.  An insulation recover board is required as a substrate to adhere to.  Fastening shall be into the structural deck below the insulating fill (see steel/concrete deck requirements).

### Reroofing with Removal of Existing Bitumen Roofing

General Criteria

All existing roofing, base flashing, deteriorated wood blocking or deteriorated metal flashings shall be removed.  Remove only that amount of roofing and flashing which can be made weathertight with new materials during a one-day period or before the onset of inclement weather.

#### Steel Deck:

                - FM Approved Steel Deck - All rusted or deteriorated decking shall be brought to the attention of the Owner's Representative and FM to determine method of treatment or replacement.  Surface-only rusted metal shall be sanded and treated with rust-inhibiting paint.  Sections that have rusted deeper than the surface or are not structurally sound shall be removed and replaced.  The use and type of steel roof deck construction shall conform to FM's recommendations as outlined in FM Loss Prevention data Sheet I-28 and local requirements.

                - Non-FM Approved Steel Deck - All rusted or deteriorated decking shall be brought to the attention of the Owner's Representative to determine method of treatment or replacement.  Surface-only rusted metal shall be sanded and treated with rust-inhibiting paint.  Sections that have rusted deeper than the surface or are not structurally sound shall be removed and replaced.  Deck type shall match existing and the attachment shall conform to local code requirements.

#### Wood Deck:

                - FM Approved Wood Deck - All rotted or deteriorated wood shall be removed and replaced.  The deck thickness shall be 2 inch (50 mm) minimum lumber or 3/4 inch (19 mm) plywood.  The deck shall conform to FM's requirements for Class 1 wood decks.  Deck attachment shall conform to FM and local code requirements. Fastener heads shall be recessed into the wood surface.

                - Non-FM Approved Wood Deck - All rotted or deteriorated wood shall be removed and replaced.  The deck thickness shall be 1-1/2 inch (38 mm) lumber or 15/32 (12 mm) plywood or match existing deck if greater.  Deck type and attachment shall conform to local code requirements.  Fastener heads shall be recessed into the wood surface.

#### Poured Structural Concrete Deck:

The roof deck shall be smooth, even, free of dust, dirt, excess moisture or oil and be structurally sound.  Sharp ridges, other projections and accumulations of bitumen above the surface shall be removed to ensure a smooth surface before roofing.  Any deteriorated decking shall be repaired.

#### Poured Lightweight Concrete Substrate:

The roof deck shall be smooth, even, free of dust, dirt, excess moisture or oil and be structurally sound. Sharp ridges, other projections and accumulations of bitumen above the surface shall be removed to ensure a smooth surface before roofing.  Any deteriorated decking shall be repaired.

#### Insulating Fill Substrate:

All wet or deteriorated insulating fill shall be removed and replaced.  All accumulations of bitumen shall be removed and the surface of the deck shall be smooth, and free of ridges and depressions.  See steel/concrete requirements.

### Reroofing with Removal of Existing Single-Ply Roofing

[NOTE TO SPECIFIER:  SELECT C OR D.]

General Criteria:

The Owner's Representative and Applicator shall determine the condition of the roof deck and existing insulation.  Deteriorated decking or wet or deteriorated materials are to be removed and replaced.  After removal of single-ply roof, inspect insulation boards and reuse only if dry and in stable condition.  Add a Sika Sarnafil approved recover board or new insulation board.  Fasten recover board or top layer of insulation in accordance with Sika Sarnafil's requirements.

The existing pvc roof membrane is to be recycled by the manufacturer of the replacement membrane.  Applicator is responsible for all costs associated with removing the membrane, preparing it and loading it for shipment, according to the manufacturer’s published procedures.

### Reroofing Over Existing Single Ply Roofing

General Criteria:

The Owner's Representative and Applicator shall determine the condition of the roof deck and existing insulation.  Deteriorated decking or wet or deteriorated materials are to be removed and replaced.  Remove all debris from the existing single-ply roof and cut into 10 ft x 10 ft panels (3 m x 3 m).  Install a layer of Sika Sarnafil approved recover board or a new insulation board over the fastened 10 ft x 10 ft (3 m x 3 m) panels and then fasten the board according to Sika Sarnafil's requirements.

### Reroofing Over Existing Bitumen Roofing

General Criteria:

The Owner's Representative and Applicator shall determine the condition of the existing roof deck and old roof system.  Areas with deteriorated decking or wet materials are to be removed and replaced.

#### On graveled surfaces, all loose gravel and debris shall be removed by power brooming or vacuuming.  All blisters shall be removed and sealed or cut, fastened down and sealed.  Any accumulation of bitumen or other irregularities shall be scratched and removed so as to produce a smooth surface.

#### On smooth surfaced roofs, the surface must be clean and dry.  All blisters shall be removed and sealed or cut, fastened down and sealed. For Type III hot asphalt attachment of new insulation board, priming of the old roof surface after preparation is necessary.

#### Coal-tar pitch or heavily resaturated roofs may require removal.  Contact Sika Sarnafil Technical for coal-tar pitch or heavily resaturated reroof preparation requirements.

###### SUBSTRATE INSPECTION

### A dry, clean and smooth substrate shall be prepared to receive the Sika Sarnafil Sarnafast mechanically-attached roof system.

### The Applicator shall inspect the substrate for defects such as excessive surface roughness, contamination, structural inadequacy, or any other condition that will adversely affect the quality of work.

### The substrate shall be clean, smooth, dry, free of flaws, sharp edges, loose and foreign material, oil and grease.  Roofing shall not start until all defects have been corrected.

### All roof surfaces shall be free of water, ice and snow.

### E.	Sika Sarnafil shall be applied over compatible or acceptable substrates only.

###### VAPOR BARRIER/AIR BARRIER INSTALLATION (AS REQUIRED BY DESIGNER)

General Criteria:

Interior (inside temperature/relative humidity) or exterior conditions may create a need for a vapor barrier.  The design professional shall decide whether a vapor barrier is necessary.  It is the design professional's responsibility to determine the type and location of a vapor barrier.  If sealed properly, a vapor barrier can also act as an air barrier (positive pressure) for roofs intended over air-permeable decks (steel, wood, precast, etc.).

### Sarnavap-10

#### Steel Deck (New Construction or Reroofing with Removal of Existing Roofing):

Sarnavap-10 is loose-laid over suitable substrate.  Overlap all edges 4 inches (100 mm) and seal with butyl tape.  Extend Sarnavap-10 to perimeter and deck penetrations and seal to provide continuity of the building's air/vapor envelope.  Sarnavap-10 must be sealed on the vertical surface at roof penetrations also.

### Sarnavap Self-Adhered

      - Primer Application

The substrate must be clean, dry and free of dust, grease or other contaminants.  Shake well before using.  Apply to clean and dry surfaces with a paint brush, roller or sprayer.  Application rates will vary depending on substrate.  Sarnavap Self-Adhered vapor barrier must be installed on the same day as the primer application.  Acceptable substrates for primer application include wood, concrete, lightweight concrete, gypsum boards and decks, and DensDeck boards.  Drying time is typically 30 minutes to 3 hours.

Spraying equipment recommendations:

- Spray tip size: between 20 and 25 mils.

- Pressure: 1300 psi continuous

To Install:

- Apply primer to prepared substrate.

- Allow primer to dry completely.

- Install Sarnavap Self-Adhered vapor barrier.

Notes:

- Do not install when it is raining, snowing, or on wet/humid surfaces.

- Install Sarnavap Self-Adhered Primer at temperatures 32 degree F (0 degree C) and above.  Average coverage rate is 0.25 to 1.22 gallons per square (0.1 to 0.5 L per m²).

- Install Sarnavap Self-Adhered Primer WB at temperatures 41 degree F (5 degree C) and above.  Average coverage rate is 0.25 to 0.75 gallon per square (0.1 to 0.3 L per m²).  KEEP FROM FREEZING.

- Do not use Sarnavap Self-Adhered Primer WB to seal Sarnavap Self-Adhered vapor barrier membrane joints.

- Sarnavap Self-Adhered Primer WB is not suitable for plastic surfaces.

- Do not use Sarnavap Self-Adhered Primer WB on asphaltic boards.

      - Vapor Barrier Application Over Steel Deck (New Construction or Reroofing with Removal of Existing Roofing):

Install Sarnavap Self-Adhered over a clean and dry substrate.  Do not install when it is raining, snowing, or on wet/humid surfaces.  Install in temperatures 32 degree F (0 degree C) and above.  The use of a primer is required on the following substrates: wood, gypsum boards, and DensDeck boards.  On metal decks use a metal plate (6 x 42 inches - 15 x 106 cm) to support the membrane end lap between metal flutes ensuring a complete end lap seal.

- Begin application at the bottom of the slope.  Unroll Sarnavap Self-Adhered onto the substrate without adhering for alignment.  Overlap each preceding sheet by 3 inches (75 mm) lengthwise following the reference line and by 6 inches (150 mm) at each end.  Stagger end laps by at least 12 inches (300 mm).  Do not immediately remove the silicone release sheet.

- Once aligned, peel back a portion of the silicone release sheet and press the membrane onto the substrate for initial adherence.  Hold Sarnavap Self-Adhered tight and peel back the release sheet by pulling diagonally.

- Use a 75 lb. (34 kg) roller to press Sarnavap Self-Adhered down into the substrate including the laps.  Finish by aligning the edge of the roller with the lower end of the side laps and rolling up the membrane.  Do not cut the membrane to remove air bubbles trapped under the laps.  Squeeze out air bubbles by pushing the roller to the edge of the laps.

###### WOOD NAILER INSTALLATION

### Install wood nailers at the perimeter of the entire roof and around roof projections and penetrations as shown on the Detail Drawings.

### Nailers shall be anchored to the structural elements to resist a minimum force of 300 pounds per lineal foot (4,500 Newtons per lineal meter) in any direction.  Individual nailer lengths shall not be less than 3 feet (0.9 meter) long.  Nailer fastener spacing shall be no more than 12 inches (0.3 m) on center or at a distance to match the structural framing.  Fasteners shall be staggered 1/3 the nailer width and installed within 6 inches (0.15 m) of each end.  Two fasteners shall be installed at ends of nailer lengths.  Nailer attachment shall also meet the requirements of the current Factory Mutual Loss Prevention Data Sheet 1-49.

### Thickness shall be as required to match the total substrate and insulation height to allow a smooth transition.

### Any existing nailer woodwork which is to remain shall be firmly anchored in place to resist a minimum force of 300 pounds per lineal foot (4,500 Newtons per lineal meter) in any direction and shall be free of rot, excess moisture or deterioration.  Only woodwork shown to be reused in Detail Drawings shall be left in place.  All other nailer woodwork shall be removed.

### Stainless steel, corrosion resistant, fasteners are required when mechanically attaching any Sika Sarnafil product to wood nailers and wood products treated with ACQ (Alkaline copper Quaternary).  When ACQ treated wood is used on steel roof decks or with metal edge detailing, a separation layer must be placed between the metal and ACQ treated wood.

###### INSULATION INSTALLATION

General Criteria:

### For Factory Mutual insured buildings polystyrene insulation may not be applied direct to steel deck.

### Insulation shall be installed according to insulation manufacturer's instructions.

### Top layer of insulation shall be the membrane underlayment, with edges butted together having no gaps greater than 1/4 inch (6mm).

### Insulation shall be neatly cut to fit around penetrations and projections with gaps not exceeding 1/4 inch.

### F.	If applicable, install tapered insulation around drains creating a drain sump.

### G.	Do not install more insulation board than can be covered with Sarnafil membrane by the end of the day or the onset of inclement weather.

### H.	Use at least 2 layers of insulation when the total insulation thickness for the overlayment exceeds 2-1/2 inches (64 mm). Stagger joints at least 12 inches (0.3 m) between layers.

### I.	Mechanical Attachment

#### Insulation shall be mechanically fastened to the structural deck with approved Sarnafasteners and Sarnadisc RhinoBond according to the insulation manufacturer's and Sika Sarnafil's recommendations for fastening rates and patterns. The quantity and locations of the fasteners and plates shall also cause the insulation boards to rest evenly on the roof deck/substrate.  Each insulation board shall be installed tightly against the adjacent boards on all sides.

#### Fasten the insulation so the Sarnadisc RhinoBond and Sarnafastener XP or MAXLoad (depending on pullout value) in a 2 by 2 foot ( 0.6 by 0.6 m) or 2 by 3 foot (0.6 by 0.9 m) grid pattern according to Sika Sarnafil’s and the wind design requirements. Fasteners must be tight enough that the Sarnadisc does not turn, but not so tight as to deform the Sarnadisc.

#### Perimeter and Corner Areas

The perimeter and corner area will be determined by building height and width and other conditions according to ASCE 7 guidelines, Sika Sarnafil Technical or FM LPDS 1-29 if insured by Factory Mutual.  To meet the perimeter and corner uplift requirements, increase fastener density by decreasing the spacing between fastener points in one or both directions. The total tributary area to each fastener is no more than 60 percent for the perimeter and 40 percent for corners, based on the field of roof fastening density.  See Detail Drawings.

Notes:

                - Perimeter area is defined as the outer boundary of the roof.  If the roof is broken into different levels, each roof area shall be treated as an individual roof with its outer boundary being treated as a perimeter.  Typically, internal expansion joints and firewalls are not considered to be full perimeters.  Refer to Factory Mutual’s Data Sheet 1-28 for more information.

The ridge area is defined as the high point in the roof area formed by two intersecting planes.  When the sum of the slopes is a minimum of 4 inches in 12 inches (30 degrees), each side of the ridge shall be treated as a perimeter area.

#### Fasteners are to be installed consistently in accordance with fastener manufacturer's recommendations.  Fasteners are to have minimum penetration of 1 inch (25 mm) through the structural deck.

#### Use fastener tools with a depth locator and torque-limiting attachment as recommended or supplied by fastener manufacturer to ensure proper installation.

###### OVERLAYMENT BOARD INSTALLATION

[NOTE TO SPECIFIER:  ONLY NEEDED OVER NON-COMPATIBLE INSULATION OR SUBSTRATE, IN INSTANCES WHERE REPEATED FOOT TRAFFIC IS EXPECTED, OR AS AN ENHANCEMENT TO INCREASE LONGEVITY OF ROOF SYSTEM]

- General Criteria:

- Boards shall be installed according to manufacturer's instructions.

- Boards shall be neatly cut to fit around penetrations and projections.

- Do not install more boards than can be covered with Sarnafil membrane by end of day or onset of inclement weather.

- Boards shall be installed tightly against adjacent boards on all sides.

- Boards shall evenly on roof deck/substrate so that there are no significant and avoidable air spaces between boards and substrate.

- Mechanical Attachment of Overlayment Board

- Overlayment board shall be mechanically fastened to deck with approved fasteners and plates at a rate according to overlayment board manufacturer's, FM's and Sika Sarnafil's recommendations for fastening rates and patterns.

- Fasten overlayment board per layout indicated on detail drawing.  Fasteners must be tight enough so insulation plates do not turn, but not so tight as to deform them.

- Fasteners shall be installed consistently in accordance with fastener manufacturer's recommendations.  Fasteners shall have a minimum penetration of 1 inch (25 mm) through structural deck.

- Use fastener tools with a depth locator and torque-limiting attachment as recommended or supplied by fastener manufacturer to ensure proper installation.

- Perimeter and Corner Areas

Perimeter and corner areas will be determined by building height and width and other conditions according to ASCE 7 guidelines, Sika Sarnafil Technical, or FM LPDS 1-29 if insured by Factory Mutual.  To meet perimeter and corner uplift requirements, increase fastener density by decreasing spacing between fastener points in one or both directions.  Total tributary area to each fastener is no more than 60 percent for perimeter and 40 percent for corners, based on field of roof fastening density.  See Detail Drawings.

Notes:

                - Perimeter area is defined as the outer boundary of the roof.  If the roof is broken into different levels, each roof area shall be treated as an individual roof with its outer boundary being treated as a perimeter.  Typically, internal expansion joints and firewalls are not considered to be full perimeters.  Refer to Factory Mutual’s Data Sheet 1-28 for more information.

                - The ridge area is defined as the high point in the roof area formed by two intersecting planes.  When the sum of the slopes is a minimum of 4 inches in 12 inches (30 degrees), each side of the ridge shall be treated as a perimeter area.

###### INSTALLATION OF SARNAFIL MEMBRANE

### The surface of the insulation or substrate shall be inspected prior to installation of the Sarnafil roof membrane.  The substrate shall be clean, dry, free from debris and smooth with no surface roughness or contamination.  Broken, delaminated, wet or damaged insulation boards shall be removed and replaced.  Sarnafil S327 membrane shall be attached with Sarnafasteners and Sarnadisc RhinoBond according to Sika Sarnafil’s and wind uplift requirements per ASCE 7 or Factory Mutual.

[NOTE TO SPECIFIER:  SELECT ONE TYPE OF MEMBRANE INSTALLATION.]

### RhinoBond - Membrane Attachment to Structural Deck (Documented Pullout Tests Required)

#### General

                - Sarnafil S327 full width rolls shall be placed over the installed boards. Membrane overlaps shall be shingled with the flow of water where possible.  Seam overlaps may be placed over Sarnadisc RhinoBond plate.  Welding of the plate will not be affected.

Tack welding of the membrane for purposes of temporary restraint during installation is not permitted and may result in voiding of Sika Sarnafil warranty.  Consult Sika Sarnafil’s Technical Department for further information.

#### Field, Perimeter and Corner Areas

#### Over the properly prepared, installed and attached substrate surface following either the 2 by 2 foot (0.6 by 0.6 m) or 2 by 3 foot (0.6 by 0.9 m) grid pattern, S327 full-width rolls are to be installed so as to properly shed water. See Detail Drawings for fastener layouts. Refer to FM LPDS 1-29 for their requirements for perimeter and corner enhancements.

#### Securement Around Rooftop Penetrations

a)	Around all perimeters, at the base of walls, drains, curbs, vent pipes, or any other roof penetrations, Sarnafasteners and Sarnadisc RhinoBond, Sarnadiscs or Sarnabars shall be installed according to perimeter rate of attachment.  Fasteners shall be installed according to the manufacturer’s instructions.  Fasteners shall be installed using the fastener manufacturer’s recommended torque-sensitive fastening tools with depth locators.  If Sarnadisc RhinoBond is not used, the fasteners shall clamp the Sarnafil membrane tightly to the substrate.

  - Sarnafil membrane flashings shall extend 2-1/2 inches (63 mm) past Sarnadisc and be hot-air welded to the Sarnafil deck membrane.

###### RHINOBOND INDUCTION WELDING

### General

#### Welding equipment shall be provided by or approved by Sika Sarnafil.  All mechanics intending to use the equipment shall have successfully completed a training course provided by a Sika Sarnafil Technical Service Representative prior to welding.

#### All membrane to be welded shall be clean and dry.

### Induction Welding

#### Activate the weld between membrane and plate using approved portable induction device. The induction coil must be positioned over the center of the Sarnadisc RhinoBond, +/- 1 inch (25 mm)Portable induction device  must elevate the temperature of the Sarnadisc RhinoBond from ambient to 400 – 500 degree F (204 – 260 degree C). Cycle time will be affected by available power, use a heavy gauge power cord, at a minimum 12 gauge by 100 feet.

#### When the induction welding cycle is complete, immediately place a Cool & Clamp magnetic weight on the welded assembly. This device must be left in place for at least 60 seconds.

###### HOT-AIR WELDING OF SEAM OVERLAPS

### General

#### All seams shall be hot-air welded.  Seam overlaps should be 3 inches (76 mm) wide for the RhinoBond System and 4 inches (100 mm) wide when hand-welding, except for certain details.

#### Welding equipment shall be provided by or approved by Sika Sarnafil.  All mechanics intending to use the equipment shall have successfully completed a training course provided by a Sika Sarnafil Technical Service Representative prior to welding.

#### All membrane to be welded shall be clean and dry.

### Hand-Welding

Hand-welded seams shall be completed in two stages.  Hot-air welding equipment shall be allowed to warm up for at least one minute prior to welding.

#### The back edge of the seam shall be welded with a narrow but continuous weld to prevent loss of hot air during the final welding.

#### The nozzle shall be inserted into the seam at a 45 degree angle to the edge of the membrane.  Once the proper welding temperature has been reached and the membrane begins to "flow”, the hand roller is positioned perpendicular to the nozzle and rolled lightly.  For straight seams, the 1-1/2 inch (40 mm) wide nozzle is recommended for use.  For corners and compound connections, the 3/4 inch (20 mm) wide nozzle shall be used.

### Machine Welding

#### Machine welded seams are achieved by the use of Sika Sarnafil's automatic welding equipment.  When using this equipment, Sika Sarnafil's instructions shall be followed and local codes for electric supply, grounding and over current protection observed.  Dedicated circuit house power or a dedicated portable generator is recommended.  No other equipment shall be operated simultaneously off the generator.

#### Metal tracks may be used over the deck membrane and under the machine welder to minimize or eliminate wrinkles.

### Quality Control of Welded Seams

#### The Applicator shall check all welded seams for continuity using a rounded screwdriver.  Visible evidence that welding is proceeding correctly is smoke during the welding operation, shiny membrane surfaces, and an uninterrupted flow of dark grey material from the underside of the top membrane.  On-site evaluation of welded seams shall be made daily by the Applicator at locations as directed by the Owner's Representative or Sika Sarnafil's representative.  One inch (25 mm) wide cross-section samples of welded seams shall be taken at least three times a day.  Correct welds display failure from shearing of the membrane prior to separation of the weld.  Each test cut shall be patched by the Applicator at no extra cost to the Owner.

###### MEMBRANE FLASHINGS

All flashings shall be installed concurrently with the roof membrane as the job progresses.  No temporary flashings shall be allowed without the prior written approval of the Owner's Representative and Sika Sarnafil.  Approval shall only be for specific locations on specific dates.  If any water is allowed to enter under the newly completed roofing, the affected area shall be removed and replaced at the Applicator's expense.  Flashing shall be adhered to compatible, dry, smooth, and solvent-resistant surfaces.  Use caution to ensure adhesive fumes are not drawn into the building.

### Sarnacol Adhesive for Membrane Flashings

#### Over the properly installed and prepared flashing substrate, Sarnacol adhesive shall be applied according to instructions found on the Product Data Sheet.  The Sarnacol adhesive shall be applied in smooth, even coats with no gaps, globs or similar inconsistencies.  Only an area which can be completely covered in the same day's operations shall be flashed.  The bonded sheet shall be pressed firmly in place with a hand roller.

#### No adhesive shall be applied in seam areas that are to be welded.  All panels of membrane shall be applied in the same manner, overlapping the edges of the panels as required by welding techniques.

### Install Sarnabar/Sarnacord according to the Detail Drawings with approved fasteners into the structural deck at the base of parapets, walls and curbs.  Sarnabars may be required by Sika Sarnafil at the base of all tapered edge strips and at transitions, peaks, and valleys according to Sika Sarnafil’s details.

### Sika Sarnafil's requirements and recommendations and the specifications shall be followed.  All material submittals shall have been accepted by Sika Sarnafil prior to installation.

### All flashings shall extend a minimum of 8 inches (0.2 m) above roofing level unless otherwise accepted in writing by the Owner's Representative and the Sika Sarnafil Technical Department.

### All flashing membranes shall be consistently adhered to substrates.  All interior and exterior corners and miters shall be cut and hot-air welded into place.  No bitumen shall be in contact with the Sarnafil membrane.

### All flashing membranes shall be mechanically fastened along the counter-flashed top edge with Sarnastop at 6-8 inches (0.15-0.20 m) on center.

### Sarnafil flashings shall be terminated according to Sika Sarnafil recommended details.

### All adhered flashings that exceed 30 inches (0.75 m) in height shall receive additional securement.  Consult Sika Sarnafil Technical Department for securement methods.

### All mechanically-attached flashings that exceed 18 inches (0.46 m) in height shall receive additional securement.  Consult Sika Sarnafil Technical Department for securement methods.

###### METAL FLASHINGS

### Metal details, fabrication practices and installation methods shall conform to the applicable requirements of the following:

#### Factory Mutual Loss Prevention Data Sheet 1-49 (latest issue).

#### Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) - latest issue.

### Metal, other than that provided by Sika Sarnafil, is not covered under the Sika Sarnafil warranty.

### Complete all metal work in conjunction with roofing and flashings so that a watertight condition exists daily.

### Metal shall be installed to provide adequate resistance to bending to allow for normal thermal expansion and contraction.

### Metal joints shall be watertight.

### Metal flashings shall be securely fastened into solid wood blocking.  Fasteners shall penetrate the wood nailer a minimum of 1 inch (25 mm).

### Airtight and continuous metal hook strips are required behind metal fascias.  Hook strips are to be fastened 12 inches (0.3 m) on center into the wood nailer or masonry wall.

### Counter flashings shall overlap base flashings at least 4 inches (100 mm).

### Hook strips shall extend past wood nailers over wall surfaces by 1-1/2 inch (38 mm) minimum and shall be securely sealed from air entry.

###### SARNACLAD METAL BASE FLASHINGS/EDGE METAL

All flashings shall be installed concurrently with the roof membrane as the job progresses.  No temporary flashings shall be allowed without the prior written approval of the Owner's Representative and Sika Sarnafil.  Acceptance shall only be for specific locations on specific dates.  If any water is allowed to enter under the newly completed roofing due to incomplete flashings, the affected area shall be removed and replaced at the Applicator's expense.

### Sarnaclad metal flashings shall be formed and installed per the Detail Drawings.

#### All metal flashings shall be fastened into solid wood nailers with two rows of post galvanized flat head annular ring nails, 4 inches (100 mm) on center staggered.  Fasteners shall penetrate the nailer a minimum of 1 inch (25 mm).

#### Metal shall be installed to provide adequate resistance to bending and allow for normal thermal expansion and contraction.

### Adjacent sheets of Sarnaclad shall be spaced 1/4 inch (6 mm) apart.  The joint shall be covered with 2 inch (50 mm) wide aluminum tape.  A 4 inch minimum (100 mm) wide strip of Sarnafil flashing membrane shall be hot-air welded over the joint.  Exercise caution at perimeter of roof. Workers shall follow OSHA safety procedures.

###### EDGE-TITE METAL

### Position the Sarnafil membrane over the roof edge and down outside face of wall covering wood nailer(s) completely.  Allow 1/2 inch (13 mm) excess membrane.  Hot-air weld all seams making sure there are no voids in welds.

### Apply a 3/8 inch (10 mm) bead of Sarnafil sealant to the intersection of the right angle of the clean base rail.  Install base rail from right to left as seen from the rooftop, lapping joints 1 inch (25 mm).

### Fasten base rail into the side of the nailer 12 inches (0.3 m) on center using #12 x 1-5/8 inch corrosion-resistant fasteners provided with Edge-Tite.  Field cut sections as necessary.  A second row of fastening may be required based upon site conditions.  Exercise caution at perimeter of roof. Workers shall follow OSHA safety procedures.

### Position spring clips at 6 foot (1.8 m) centers on base rail.  Locate spring clips at fascia cover laps and at mid-span of fascia cover.

### Fascia covers are installed from right to left as seen from the rooftop.  Position fascia cover on top of base rail and overlap preceding panel by 1 inch (25 mm) at notches provided.  Snap covers into place.  Field cut where necessary.  Exercise caution at perimeter of roof. Workers shall follow OSHA safety procedures.

###### ANCHOR-TITE METAL

### Position the Sarnafil membrane over the roof edge and down outside face of wall covering wood nailer(s) completely, allowing 1/2 inch (13 mm) excess membrane.  Hot-air weld all seams making sure there are no voids in welds.

### Apply a 3/8 inch (10 mm) bead of Sarnafil sealant to the intersection of the right angle of the clean base rail.  Install base rail from right to left as seen from rooftop, lapping joints 1 inch (25 mm).

### Fasten base rail into the side of the nailer at 12 inches (0.3 m) on center using #12 x 1-5/8 inch corrosion-resistant fasteners provided with Anchor-Tite.  Field cut sections as necessary.  A second row of fastening may be required based upon site conditions.  Exercise caution at perimeter of roof.  Workers shall follow OSHA safety procedures.

### Fascia covers are installed from right to left as seen from rooftop.  Position fascia cover on top of base rail and overlap preceding panel by 1 inch (25 mm) at notches provided.  Snap covers into place.  Field cut where necessary.  Exercise caution at perimeter of roof.  Workers shall follow OSHA safety procedures.

###### WALKWAY INSTALLATION

### Sand Coated Walkway

Roofing membrane to receive Sand Coated Walkway shall be clean and dry.  Place chalk lines on deck sheet to indicate location of Walkway.  Clean the deck membrane in areas to be welded.  Walkway shall be unrolled and positioned within the chalk lines.  Hot-air weld the entire perimeter of the Walkway to the Sarnafil deck sheet.  Check all welds with a rounded screwdriver.  Re-weld any inconsistencies.  Important:  Check all existing deck membrane seams that are to be covered by Walkway with rounded screwdriver and reweld any inconsistencies before Walkway installation.

### Sarnatred Walkway

Roofing membrane to receive Sarnatred Walkway shall be clean and dry.  Place chalk lines on deck sheet to indicate location of Walkway.  Apply a continuous coat of Sarnacol 2170 adhesive to the deck sheet and the back of Walkway in accordance with Sika Sarnafil's technical requirements and press Walkway into place with a water-filled, foam-covered lawn roller.  Clean the deck membrane in areas to be welded.  Hot-air weld the entire perimeter of the Walkway to the Sika Sarnafil deck sheet.  Check all welds with a rounded screwdriver.  Re-weld any inconsistencies.  Important: Check all existing deck membrane seams that are to be covered by Walkway with rounded screwdriver and reweld any inconsistencies before Walkway installation.

### Crossgrip Walkway

Crossgrip Walkway is installed loose laid on top of completed Sarnafil roof assemblies.  Where design windspeeds exceed 94 mph (150 km/h) the walkway must be secured with loops of Sarnafil membrane welded to the field sheet.  Unroll and position Crossgrip Walkway within specified areas and cut to desired length.  Do not install Crossgrip Walkway directly over Sarnabars.  Connecting clips are available for butting two ends together.  Important: Check all existing deck membrane seams that are to be covered and reweld any inconsistencies before installation.

###### PERIMETER WARNING TAPE

Areas of membrane where tape is to be applied must be cleaned to a “like new” condition.  Failure to properly clean the membrane will result in less than satisfactory adhesion.  The membrane should be cleaned as follows:

1)	New membrane: Remove loose dirt and dust by wiping clean with water.  For areas where dirt is embedded, scrub the application area with a commercial cleaner such as Simple Green, 409 or other similar all purpose cleaner using a Scotch Brite scrubbing pad or similar product.  Wash away residual cleaning material with clean water.

2)	Weathered membrane: For older membranes or areas where there is excessive dirt buildup, use the above cleaning procedure followed by cleaning with a natural fiber rag wet with MEK, and wipe away all residual cleaning solution and remaining dirt until membrane has a “like new” appearance.

After surface is clean and dry, apply tape to surface taking care to avoid trapping air and creating blisters as tape is smoothed over with hand pressure.  If a chalk line is used be sure to keep chalk dust clear of application area.

Do not apply Perimeter Warning Tape to surfaces where the temperature is below 40 degrees Fahrenheit.

Perimeter Warning Tape may be slippery when wet.

###### TEMPORARY CUT-OFF

All flashings shall be installed concurrently with the roof membrane in order to maintain a watertight condition as the work progresses.  All temporary waterstops shall be constructed to provide a 100 percent watertight seal.  The stagger of the insulation joints shall be made even by installing partial panels of insulation.  The new membrane shall be carried into the waterstop.  Waterstop shall be sealed to the deck and substrate so that water will not be allowed to travel under the new or existing roofing.  The edge of the membrane shall be sealed in a continuous heavy application of sealant as described in Section 2.10.  When work resumes, the contaminated membrane shall be cut out. All sealant, contaminated membrane, insulation fillers, etc. shall be removed from the work area and properly disposed of off site. None of these materials shall be used in the new work.

If inclement weather occurs while a temporary waterstop is in place, the Applicator shall provide the labor necessary to monitor the situation to maintain a watertight condition.

If any water is allowed to enter under the newly-completed roofing, the affected area shall be removed and replaced at the Applicator's expense.

###### COMPLETION

Prior to demobilization from the site, the work shall be reviewed by the Owner's Representative and the Applicator.  All defects noted and non-compliances with the Specifications or the recommendations of Sika Sarnafil shall be itemized in a punch list.  These items must be corrected immediately by the Applicator to the satisfaction of the Owner's Representative and Sika Sarnafil prior to demobilization.

All Warranties referenced in this Specification shall have been submitted and have been accepted at time of contract award.

###### DETAILS

See accompanying Sika Sarnafil detail drawings.  Refer to the Sika Sarnafil Typical System Details section for additional details.

Sika Sarnafil has attempted to obtain information from the manufacturers of other products often used in conjunction with Sika Sarnafil products with respect to the characteristics of such products, as well as their compatibility with Sika Sarnafil's products.  In as much as these other products as supplied in the field are subject to possible variation in their productions, and in as much as their specifications and performance characteristics are subject to change without notification by the manufacturers, Sika Sarnafil expressly excludes from its warranty any responsibility for the performance or quality of the products of others used in conjunction with Sika Sarnafil products.  Sika Sarnafil provides this specification as a guide only in technical support to architects or roof designers/specifiers.  Sika Sarnafil assumes no liability for error in design of or for misuse of this guide specification.  The roof designer, engineer, architect or Applicator must verify suitability of the specification and details.

| S327 RHINOBOND ROOF SYSTEM DETAIL DRAWINGS |
| --- |
| DRAWING |  | FILE NAME |
| RB-ISO | RhinoBond Isometric | RB-ISO |
| RB-1A | Sarnadisc RhinoBond – 2x2 Insulation Fastening Grid | RB-1A |
| RB-1B | Sarnadisc RhinoBond – 2x3 Insulation Fastening Grid | RB-1B |