**Sikaplan®**

**Mechanically-Attached**

Sika Corporation - Roofing

100 Dan Road, Canton MA 02021

(800) 451-2504

usa.sarnafil.sika.com



[NOTE TO SPECIFIER: NOTES TO SPECIFIER ARE DESIGNATED BY [ ]. SPECIFIER IS TO SELECT ONE OF THE OPTIONS.]

# GENERAL CONDITIONS

## DESCRIPTION

##### Scope

To install a complete Sikaplan mechanically-attached system including membrane, flashings and other components.

##### Related Work

The work includes but is not limited to the installation of:

###### Removal of existing roofing and insulation

###### Substrate preparation

###### Roof drains

###### Vapor retarder

###### Insulation

###### Separation layers

###### Roof membrane

###### Fasteners

###### Adhesive for flashings

###### Roof membrane flashings

###### Walkways

###### Metal Flashings

###### Sealants

##### Upon successful completion of work the following warranties may be obtained:

###### Sika Corporation Warranty

###### Roofing Applicator Warranty

## QUALITY ASSURANCE

##### This roofing system shall be applied only by a roofing applicator authorized prior to bid by Sika Corporation (Sika Corporation "Applicator").

##### A Sika Corporation Technical Service Representative will review the installed roof system wherever a System Warranty has been requested.

##### All work pertaining to the installation of membrane, flashings, and accessories shall only be completed by Applicator authorized by Sika Corporation in those procedures.

##### Roofing membrane manufacturer must have a demonstrated performance history of producing PVC roof membranes no less, in duration of years, than the warranty duration specified.

##### Roofing membrane and membrane flashings to be manufactured by membrane supplier and not private labeled.

##### Manufacturer to have a minimum ten years of experience recycling their membranes at the end of their service life back into new membrane products. Provide a minimum of five reference projects completed with new membrane produced from recycled membrane.

##### Applicable code/insurance requirements shall be identified by the Owner or Owner’s representative.

## SUBMITTALS

##### At the time of bidding, the Applicator shall submit to the Owner (or Representative) the following:

###### Copies of Specification.

###### Samples of each primary components to be used in the roof system and the manufacturer’s current product data sheet for each component.

###### Written approval by the insulation manufacturer (as applicable) for use of the product in the proposed system.

###### Sample copy of Sika Corporation’s warranty.

###### Sample copy of Applicator’s warranty.

###### Safety Data Sheets (SDS)

## CODE REQUIREMENTS

The Applicator shall submit evidence that the proposed roof system meets the requirements of the local building code and has been tested and approved or listed by an approved, codified testing organization. These requirements are minimum standards and no roofing work shall commence without written documentation of the system's compliance.

[NOTE TO SPECIFIER: SELECT REQUIREMENT(S).]

##### System shall be designed to meet the minimum wind design requirements of the applicable version of ASCE 7.

##### Factory Mutual Research Corporation (FM) - Norwood, MA

System shall be designed to meet 4470 requirements and the most recent versions of FM Global LPDS 1-28 and 1-29.

##### Underwriters Laboratories, Inc. - Northbrook, IL

###### Class A assembly

###### Class B assembly

###### Class C assembly

## PRODUCT DELIVERY, STORAGE, AND HANDLING

[NOTE TO SPECIFIER: IF REQUIRED, SELECT ITEM H BELOW.]

##### All products delivered to the job site shall be in the original unopened containers or wrappings bearing all seals and approvals.

##### Handle all materials to prevent damage. Place all materials on pallets and fully protect from moisture.

##### Membrane rolls shall be stored lying down on pallets and fully protected from the weather with clean tarpaulins. Unvented tarpaulins are not accepted due to the potential accumulation of moisture beneath the tarpaulin which may affect the membrane weldability.

##### As a general rule all adhesives shall be stored at temperatures between 40°F (4°C) and 80°F (27°C). Read product data sheets and instructions contained on adhesive canisters for specific storage instructions.

##### All flammable materials shall be stored in a cool, dry area away from sparks and open flames. Follow precautions outlined on containers and read product Safety Data Sheets (SDS).

##### Any materials which the Owner’s representative or Sika Corporation determine to be damaged are to be removed from the job site and replaced at no cost to the Owner.

##### Safety Data Sheets (SDS) shall be available at the job site at all times.

##### The existing PVC roof membrane is to be recycled by the manufacturer of the replacement membrane. Applicator is responsible for all costs associated with removing the membrane, preparing it and loading it for shipment, according to the manufacturer’s published procedures.

## JOB CONDITIONS

##### Only as much of the new roofing as can be made weathertight each day, including all flashing and detail work, shall be installed. All seams shall be heat welded before leaving the job site that day.

##### Temporary overnight tie-ins shall be installed at the end of each day's work and shall be completely removed (including any contaminated materials) before proceeding with the next day's work.

##### The Applicator is cautioned that certain Sikaplan membranes are incompatible with asphalt, coal tar, heavy oils, roofing cements, creosote and some preservative materials. Such materials shall not remain in contact with these Sikaplan membranes.

##### The Applicator shall follow all safety regulations as required by OSHA and any other applicable authority having jurisdiction. Roof and walkways may be slippery when icy, snow covered, or wet. Working on surfaces under these conditions is hazardous. Appropriate safety measures must be implemented prior to working on such surfaces. Always follow OSHA and other relevant fall protection standards when working on roofs.

##### Where applicable, the Applicator shall arrange for pullout tests in accordance with the latest versions of the SPRI/ANSI Standard Field Test Procedures FX-1 and IA-1 for fasteners and adhesives, respectively, to verify condition of the deck/substrate and to confirm expected pullout values.

##### The Sikaplan membrane shall not be installed under the following conditions without consulting Sika Corporation’s Technical Dept. for precautionary steps:

###### The roof assembly permits interior air to pressurize the membrane underside.

###### Any exterior wall has 10% or more of the surface area comprised of opening doors or windows.

###### The wall/deck intersection permits air entry into the wall flashing area.

##### Special consideration should be given to construction related moisture. Sika Corporation is not responsible for damage when exposed to construction related moisture.

## BIDDING REQUIREMENTS

##### Pre-Bid Meeting:

A pre-bid meeting shall be held with the Owner's Representative and involved trades to discuss all aspects of the project. The Applicator's field representative or roofing foreman for the work shall be in attendance.

##### Site Visit:

Bidders shall visit the site and carefully examine the areas in question as to conditions that may affect proper execution of the work. All dimensions and quantities shall be determined or verified by the Applicator. No claims for extra costs will be allowed because of lack of full knowledge of the existing conditions unless agreed to in advance with the Owner or Owner's Representative.

## WARRANTIES

##### Sika Corporation Warranty

Upon successful completion of the work to Sika Corporation's satisfaction and receipt of final payment, the Sika Corporation Warranty shall be issued.

[NOTE TO SPECIFIER: SELECT DESIRED WARRANTY, MEMBRANE ONLY OR SYSTEM. ONLY PRODUCTS PURCHASED FROM SIKA CORPORATION ARE COVERED UNDER SYSTEM WARRANTY.]

###### Membrane Warranty

###### System Warranty

##### Contractor Warranty

## WARRANTY DURATIONS

[NOTE TO SPECIFIER: SPECIFY EITHER 5, 10, 15, OR 20 YEAR DURATION BELOW FOR SIKA CORPORATION WARRANTY. CONSULT SIKA CORPORATION - ROOFING FOR ASSISTANCE.]

##### Sika Corporation’s warranty shall be in effect for a \_\_\_\_\_ year duration.

# PRODUCTS

### GENERAL

##### Components of the roof system shall be products of Sika Corporation as indicated on the Detail Drawings and specified in the Contract Documents.

##### Components that are other than those supplied or manufactured by Sika Corporation may be submitted for review and acceptance by Sika Corporation. Sika Corporation’s acceptance of any other product is only for a determination of compatibility with Sika Corporation products and not for inclusion in the Sika Corporation warranty. The specifications, installation instructions, limitations, and restrictions of the respective manufacturers must be reviewed by the Owner’s Representative for acceptability for the intended use with Sika Corporation products.

##### Consult respective product data sheets and selection guides for additional information.

### MEMBRANE

##### Membrane shall conform to:

###### ASTM D-4434 (latest version), "Standard for Polyvinyl Chloride Sheet Roofing". Classification: Type III.

##### Sikaplan PVC thermoplastic membrane

###### Type of Membrane

1. Sikaplan Fastened
2. Sikaplan Fastened Feltback
3. Sikaplan Fastened 3 oz. Felt
4. Sikaplan Fastened FR Feltback

[NOTE TO SPECIFIER: FOR 20 YEAR WARRANTY DURATION MINIMUM 60 MIL MEMBRANE IS REQUIRED.]

###### Membrane Thickness

1. 45 mil (1.1 mm)
2. 60 mil (1.5 mm)

##### Color of Membrane

###### Sikaplan Fastened

1. EnergySmart White
2. EnergySmart Reflective Gray
3. EnergySmart Tan

##### Typical Physical Properties

###### Refer to individual Sikaplan Fastened Product Data Sheets for physical property values.

### INSULATIONS / ROOF BOARDS

##### Insulation

###### Sarnatherm

Rigid polyisocyanurate insulation board with glass fiber reinforced felt facers, meeting ASTM C-1289 Type II, Class 1, Grade 2 (20 psi) or Grade 3 (25 psi).

###### Sarnatherm CG

Rigid polyisocyanurate insulation board with coated polymer bonded glass fiber mat facers, meeting ASTM C-1289 Type II, Class 2, Grade 2 (20 psi) or Grade 3 (25 psi).

[NOTE TO SPECIFIER: A SEPARATION LAYER OF POLYISOCYANURATE OR GYPSUM ROOF BOARD MUST BE PLACED BETWEEN POLYSTYRENE BOARDS AND SIKAPLAN MEMBRANE.]

###### Sarnatherm EPS

Rigid expanded polystyrene foam insulation board, meeting ASTM C-578 Type II or IX, minimum 20 psi compressive strength.

###### Sarnatherm XPS

Closed-cell extruded polystyrene foam insulation board, meeting ASTM C-578 Type VI or VII, minimum 20 psi compressive strength.

###### Rockwool Toprock® DD

Dual-density stone wool insulation board, meeting ASTM C-726.

##### Roof Boards

###### Sarnatherm Roof Board A-III

High density polyisocyanurate 1/2” (12.7 mm) roof board with coated glass facers, meeting ASTM C-1289 Type II, Class 4, Grade 1.

###### Sarnatherm Roof Board H

High density polyisocyanurate 1/2” (12.7 mm) roof board with coated glass facers, meeting ASTM C-1289 Type II, Class 4, Grade 1.

###### Sarnatherm Roof Board R

High density polyisocyanurate 1/2” (12.7 mm) roof board with coated glass facers, meeting ASTM C-1289 Type II, Class 4, Grade 1.

###### Sarnatherm Roof Board M

High density polyisocyanurate 1/4” (6.4 mm) roof board with coated glass facers, meeting ASTM C-1289 Type II, Class 4, Grade 1 or Grade 2 or Grade 3.

###### Densdeck® Roof Board

Gypsum roof board with fiberglass mat facers, meeting ASTM C-1177.

###### DensDeck® Prime Roof Board

Gypsum roof board with a primed fiberglass mat facer on one side, meeting ASTM C-1177.

###### Securock® Ultralight Glass-Mat Roof Board

Gypsum roof board with fiberglass mat facers, meeting ASTM C-1177.

###### Securock® Ultralight Coated Glass-Mat Roof Board

Gypsum roof board with primed fiberglass mat facers, meeting ASTM C-1177.

### ATTACHMENT COMPONENTS

##### Insulation / Roof Board Attachment Plates

###### Sikaplan Board Plate

3” (76 mm) round steel plate with a Galvalume coating, used with #12, #14, and #15 Sikaplan fasteners to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to the roof deck.

###### Sarnaplate GypTec

26 gauge, 3” (76 mm) round steel plate with a Galvalume coating, used with Fastener Polymer GypTec to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to gypsum and cementitious wood fiber roof decks.

##### Membrane Attachment Discs

###### Sikaplan Disc

20 gauge, 2-3/8” round steel plate used with Sikaplan fasteners to attach membrane to the roof deck.

###### Sarnadisc RhinoBond

3” round polymer coated steel plate used to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to the roof deck or structural purlins prior to the installation of membrane to the roof deck.

###### Sarnadisc RhinoBond Treadsafe

3” round polymer coated steel plate with a polymer tube used to attach compressible insulation to the roof deck or structural purlins prior to the installation of membrane to the roof deck.

###### Sarnadisc GypTec

20 gauge, 2” (51 mm) round steel plate with a Galvalume coating, used with Fastener Polymer GypTec to attach membrane to gypsum and cementitious wood fiber roof decks.

##### Fasteners

###### Sikaplan Board Fastener #12

#12 corrosion-resistant fastener used with Sarnaplates to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to the roof deck.

###### Sikaplan Fastener #14

#14 corrosion-resistant fastener used with Sarnaplates to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to the roof deck.

###### Sikaplan Fastener #15

#15 corrosion-resistant fastener used with Sarnaplates to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to the roof deck.

###### Fastener CD-10

Nail-in, corrosion-resistant fastener used with Sarnaplates to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to structural concrete.

###### Fastener Polymer GypTec

Molded product made of fiberglass-filled nylon used with Sarnaplate GypTec to attach Sarnatherm insulation, Sarnatherm roof boards, gypsum roof boards, or other Sika approved boards to certain gypsum and cementitious wood fiber roof decks.

###### Fastener Retrodriller

Threaded drill point fastener made of carbon steel, used with Sarnadiscs or Sikaplan Disc to in-seam attach membrane into structural steel purlin.

### DECK PRIMERS

##### Vapor Retarder Primer SB

Solvent-based primer used to prime wood, concrete, primed gypsum boards and decks, prior to the application of Sika’s self-adhered vapor retarders.

##### Vapor Retarder Primer VC

VOC compliant\*, solvent-based primer used to prime wood, concrete, gypsum boards and decks, prior to the application of Sika’s self-adhered vapor retarders.

\*Check local jurisdiction for VOC compliance.

##### Vapor Retarder Primer WB

Polymer emulsion water-based primer used to prime wood, concrete, gypsum decks, and approved gypsum boards prior to the application of Sika’s self-adhered vapor retarders.

##### Vapor Retarder Primer TA

Blend of bitumen and solvent based primer for use prior to applying Sika’s torch-applied vapor retarders.

##### Vapor Retarder Primer BE

Bituminous emulsion (water based) primer for use prior to applying Sika’s torch-applied vapor retarders.

### VAPOR RETARDERS

[NOTE TO SPECIFIER: CONDENSATION AND MOISTURE MIGRATION INTO THE ROOF SYSTEM MUST BE CONTROLLED SO THAT IT DOES NOT COMPROMISE THE PERFORMANCE OF THE INSULATION AND OTHER COMPONENTS OF THE ASSEMBLY. SIKA CORPORATION IS NOT RESPONSIBLE FOR DAMAGE RESULTING FROM CONDENSATION OR OTHER CONSTRUCTION RELATED MOISTURE.]

##### Vapor Retarder PE 10

10 mil (0.25 mm) thick polyethylene vapor retarder/air barrier.

##### Vapor Retarder SA 31

31 mil (0.8 mm) thick self-adhered SBS modified bitumen vapor retarder/air barrier with a tri-laminated woven polyethylene facer. Can also serve as temporary roof protection exposed for up to three (3) months.

##### Vapor Retarder SA 106

106 mil (2.7 mm) thick self-adhered SBS polymer modified bitumen vapor retarder/air barrier with a non-woven polyester mat reinforcement and fine mineral aggregate (sand) topside. Can also serve as temporary roof protection exposed for up to six (6) months.

##### Vapor Retarder TA 138

138 mil (3.5 mm) thick torch applied SBS polymer modified bitumen vapor retarder with a non-woven polyester mat reinforcement and fine mineral aggregate (sand) topside. Can also serve as temporary roof protection exposed for up to six (6) months.

##### Ply Sheet TA 87

87 mil (2.2 mm) thick torch applied SBS polymer modified bitumen with a fiberglass mat reinforcement and fine mineral aggregate (sand) topside and polyolefin burn-off film underside. Can also serve as temporary roof protection exposed for up to six (6) months.

##### Ply Sheet HA 87

87 mil (2.2 mm) thick hot applied SBS polymer modified bitumen with a fiberglass mat reinforcement and fine mineral aggregate (sand) topside and underside, can also serve as temporary roof protection exposed for up to six (6) months. Can also be adhered with Sika approved cold applied adhesives.

##### Ply Sheet HA 118

118 mil (3.0 mm) thick hot applied SBS polymer modified bitumen with a fiberglass mat reinforcement and fine mineral aggregate (sand) topside and underside. Can also serve as temporary roof protection exposed for up to six (6) months. Can also be adhered with Sika approved cold applied adhesives.

### VAPOR RETARDER ADHESIVES

##### Asphalt

Hot application of Type III or Type IV asphalt

##### Vapor Retarder Adhesive CA

Cold applied polyether based adhesive used to adhere Sika’s vapor retarders that are typically adhered with hot asphalt. It is used in applications where hot asphalt is not advised and/or not permitted.

### FLASHING MATERIALS

##### Wall / Curb Flashing

###### Sikaplan Fastened Membrane

###### G 459 Flashing Membrane

For use over residual asphalt or other contaminated surfaces.

###### Detail Membrane

###### Sarnaclad

###### Sarnacol 2170 Adhesive

Solvent-based reactivating adhesive used to attach membrane to flashing substrate.

###### Sarnacol 2170 VC Adhesive

Solvent-based, VOC compliant\*, reactivating adhesive used to attach membrane to flashing substrate.

\*Check local jurisdiction for VOC compliance.

###### Sarnafelt

Leveling and/or separation layer that is necessary behind G 459 Flashing Membrane when the flashing substrates are rough or incompatible with the flashing membrane.

##### Perimeter Edge Flashing

[NOTE TO SPECIFIER: SELECT FASCIA AND/OR COPING METAL AND SPECIFY COLOR. SIKA CORPORATION – ROOFING HAS AGREEMENTS WITH OTHER PERIMETER EDGE METAL SUPPLIERS. CHECK WITH SIKA CORPORATION – ROOFING FOR APPROVED PERIMETER EDGE METAL SUPPLIERS.]

###### Sarnaclad

24 gauge, G90 galvanized steel with PVC-coating on one side for heat-weldability.

###### Edge Grip Fascia

Three-piece assembly of retainer base plate and snap on fascia cover with concealed splice plates.

###### Edge Grip Extruded Fascia

Three-piece assembly of extruded retainer base plate and snap on fascia cover with concealed splice plates.

###### Wall Grip Coping

Metal coping assembly of formed aluminum or galvanized steel cap and 20 gauge galvanized steel cleats.

###### Wall Grip Coping Plus

Metal coping assembly of formed aluminum or galvanized steel cap and 16 gauge galvanized steel cleats.

###### Metal-Era One Edge

Two-piece assembly of steel base rail and aluminum or steel snap-on fascia cover with spring clips.

###### Metal-Era One Drip Edge

Two-piece assembly of galvanized steel cleat and Sarnaclad PVC coated galvanized steel.

###### Metal-Era Perma-Tite System 200 / 300

Two-piece assembly of steel water dam / gravel stop and fascia cover with spring clips.

###### Metal-Era Perma-Tite Coping

Aluminum or steel snap-on coping cover with concealed splice plates.

##### Miscellaneous Flashing

###### Sarnacircles

Round circle patch.

###### Sarnacorners - Inside

Injection molded inside corner.

###### Sarnacorners - Outside

Injection molded outside corner.

###### Sarnastack Universal

Injection molded stack/pipe boot to flash pipes, vent stacks and cylindrical penetrations.

###### Sarnastack Split A, B, C

Prefabricated stack/pipe boot open along one side to flash pipes, vent stacks and cylindrical penetrations when access is obstructed.

###### Open Post Flashing

Prefabricated pipe boot open along one side to flash rooftop conduits, pipes, and cylindrical penetrations when access is obstructed.

###### Sikaplan Termination Bar

3/4” wide extruded aluminum bar used to terminate Sikaplan roofing membranes at walls and edges.

###### Sarnadrain with U-Flow

Seamless one-piece heavy-duty aluminum drain with a coated flange for hot-air welding of Sikaplan membranes.

[NOTE TO SPECIFIER: LIQUID FLASHING IS ONLY WARRANTED TO A MAXIMUM OF 20 YEARS.]

###### Liquid Flashing Primer

Two-component polymethyl methacrylate-based (PMMA) primer used to promote the adhesion of Liquid Flashing SW and Liquid Flashing WW over wood and concrete surfaces.

###### Liquid Flashing Fleece

Non-woven, needle-punched polyester fleece used as the reinforcement for Sika’s liquid flashing details.

###### Liquid Flashing Catalyst

Reactive agent based on dibenzoyl peroxide to induce curing of Sika’s Liquid Flashing SW, Liquid Flashing WW, and Liquid Flashing Primer when mixed.

###### Liquid Flashing SW (summer-grade white)

Two-component polymethyl methacrylate-based (PMMA). The ambient temperature at application must be between 59°F (15°C) and 104°F (40°C). The surface temperature at application must be between 59°F (15°C) and 122°F (50°C).

###### Liquid Flashing WW (winter-grade white)

Two-component polymethyl methacrylate-based (PMMA). The ambient and surface temperatures at application must be between 23°F (-5°C) and 68°F (20°C).

### WALKWAY PROTECTION

##### Sarnatred-V

Polyester reinforced, 96 mil (2.4 mm) thick, weldable membrane with surface embossment similar to a chevron pattern. Used as a protection layer from rooftop traffic.

##### Crossgrip XTRA

Rolled-out walkway protection mat loose laid on top of completed roof assemblies consisting of 5/8” (16 mm) thick flexible PVC with cross-directional textured ribs.

##### Concrete Pavers

Normal weight concrete pavers specifically designed and produced for rooftop application. For large areas the use of paver pedestals or a drainage panel protection layer between the Sarnafil roof membrane and the pavers is required. For narrow walkways, a welded-in-place protection layer of Sarnafil membrane is required under the concrete pavers.

### MISCELLANEOUS ACCESSORIES

##### Aluminum Tape

2” (51 mm) wide pressure-sensitive aluminum tape used as a separation layer between small areas of asphalt contamination and the membrane and as a bond-breaker under the coverstrip at Sarnaclad joints.

##### Multi-Purpose Tape

Tape used to seal membrane at penetrations and securements, metals, or Vapor Retarder PE 10.

##### Perimeter Warning Tape

2” (51 mm) wide reflective tape with a release liner used in required areas. Exceeds reflectivity 3 requirements and Federal spec. L-S-300, Class 1.

##### Perimeter Warning Membrane

4” (10.2 cm) wide yellow Sarnafil G 410 Membrane used in required areas.

##### Seam Cleaner

Used to clean adhesive out of seams. It is not to be used as a general membrane cleaner. It is also used to clean metal and reactivate existing Liquid Flashing prior to the application of new Liquid Flashing.

##### Rhinobond PS Cardboard Disc

Coated cardboard disc used in the installation of Sarnafil S 327 or Sikaplan RhinoBond roofing systems. It is intended to protect Sika approved polystyrene fanfold roofing underlayments from heat during the induction welding process.

##### Sarnastop

1” wide extruded aluminum, low profile bar used with certain Sarnafasteners to secure membrane to the roof deck or to walls/curbs at terminations, penetrations and at angle changes of the substrate.

### SEALANTS AND PITCH POCKET FILLERS

##### Sikaflex-1a

Moisture-cured, one-component polyurethane-based, non-sag elastomeric sealant used in wall, curb and drain terminations. It is also used as a sealant at pipe penetrations and under certain metal flashings. Sikaflex-1a can be used as a pourable sealer pocket filler.

##### Sikasil SG-20

One-component silicone adhesive.

##### Sarnafiller

Two-component urethane adhesive for pitch pocket toppings.

##### Mastic TG

Cold applied, fiber reinforced high strength SBS modified bitumen mastic that is specially formulated to detail around penetrations and flashings where Sika vapor retarders and ply sheets are used as a temporary roof.

### MISCELLANEOUS FASTENERS AND ANCHORS

All fasteners, anchors, nails, straps, bars, etc. shall be post-galvanized steel, aluminum or stainless steel. Mixed metal type components shall be assembled in such a manner as to avoid galvanic corrosion. Fasteners for attachment of metal to masonry shall be expansion type fasteners with stainless steel pins.

### RELATED MATERIALS

##### Wood Nailer

Code compliant wood nailers shall be installed at the perimeter of the entire roof and around such other roof projections and penetrations as specified on Project Drawings. Thickness of nailers must match the height of the insulation and roof board to achieve a smooth transition.

##### Plywood

When bonding directly to plywood, a minimum 1/2” (13 mm) CDX (C side out), smooth-surfaced exterior grade plywood with exterior grade glue shall be used. Rough-surfaced plywood or high fastener heads will require the use of Sarnafelt behind the flashing membrane. Plywood shall have a maximum moisture content of 19% by weight on a dry weight basis.

# EXECUTION

#### PRE-CONSTRUCTION CONFERENCE

The Applicator, Owner's Representative/Designer and Manufacturer(s) shall attend a pre-construction conference.

#### SUBSTRATE CONDITION

##### Applicator shall be responsible for acceptance or provision of proper substrate to receive new roofing materials.

##### Applicator shall verify that the work done under related sections meets the following conditions:

###### Roof drains and scuppers have been reconditioned or replaced (as applicable) and installed properly.

###### Roof curbs, nailers, equipment supports, vents and other roof penetrations are properly secured and prepared to receive new roofing materials.

##### The substrate shall be clean, smooth, dry, free of water, ice and snow and free of flaws, sharp edges, loose and foreign material, oil, grease and other contaminants. Roofing shall not start until all defects have been corrected.

#### SUBSTRATE PREPARATION

The roof deck and existing roof construction must be structurally sound to provide support for the new roof system. The Owner's Representative shall ensure that the roof deck is secured to the structural framing according to local building code or insurance requirements and in such a manner as to resist all anticipated loads in that location.

##### New Construction

###### Steel Deck

The roof deck shall conform and be installed to current local building code or insurance requirements.

###### Wood Deck

The roof deck shall be minimum 1-1/2” (38 mm) thick lumber or 15/32” (12 mm) thick plywood. Deck shall be installed according to local code requirements.

###### Poured Structural Concrete Deck

The surface shall be dry and free of moisture, have a level finish, and shall be free of dust, excess moisture, oil-based curing agents and loose debris. Under no circumstances shall a sealer be used in lieu of a curing agent. Sharp ridges or other projections above the surface shall be removed before roofing. In accordance with the ICRI Technical Guideline No. 310.2R-2013, a concrete surface profile range of CSP 3 to CSP 6 is required for Vapor Retarders SA 31, SA 106, and TA 138; a concrete surface profile range of CSP 2 to CSP 6 is required for Ply Sheets TA 87, HA 87, and HA 118.

###### Poured Lightweight (Cellular or Insulating) Concrete Substrate

The surface shall be installed per lightweight concrete manufacturer’s guidelines. The wet and dry densities shall be in accordance with the manufacturer's requirements. Sharp ridges or other projections above the surface shall be removed before roofing.

###### Precast / Prestressed Concrete Panel Deck

The surface shall have a smooth and level finish and shall be free of dust, moisture, oil or loose debris. All joints between precast units shall be grouted. Any differentials in height between precast units shall be feathered for a smooth transition. Sharp ridges or other projections above the surface shall be removed before roofing.

###### Cementitious Wood Fiber Deck

The roof deck shall be installed in accordance with the deck manufacturer’s requirements and industry practice. The surface shall have a smooth and level finish and shall be free of dust, moisture, and loose debris. All voids and joints shall be grouted. Any differentials in height between precast units shall be feathered for a smooth transition. Sharp ridges or other projections above the surface shall be removed before roofing. Panels shall be secured to structural supports as recommended by the deck manufacturer.

##### Reroofing with Removal of Existing Roofing System

All existing roofing, base flashing, deteriorated wood blocking or deteriorated metal flashings shall be removed. Remove only that amount of roofing and flashing which can be made weathertight with new materials during a one-day period or before the onset of inclement weather.

###### Steel Deck

All rusted or deteriorated decking shall be brought to the attention of the Owner's Representative to determine method of treatment or replacement. Surface-only rusted metal shall be sanded and treated with rust-inhibiting paint. Sections that have rusted deeper than the surface or are not structurally sound shall be removed and replaced. Deck type shall match existing and the attachment shall conform to local code requirements.

###### Wood Deck

All rotted or deteriorated wood shall be removed and replaced. The deck thickness shall be 1-1/2” (38 mm) lumber or 15/32” (12 mm) plywood or match existing deck if greater. Deck type and attachment shall conform to local code requirements. Fastener heads shall be recessed into the wood surface.

###### Poured Structural Concrete Deck

The surface shall be dry and free of moisture, have a level finish, and shall be free of dust, excess moisture, and loose debris. Sharp ridges or other projections above the surface shall be removed before roofing. In accordance with the ICRI Technical Guideline No. 310.2R-2013, a concrete surface profile range of CSP 3 to CSP 6 is required for Vapor Retarders SA 31, SA 106, and TA 138; a concrete surface profile range of CSP 2 to CSP 6 is required for Ply Sheets TA 87, HA 87, and HA 118.

###### Poured Lightweight (Cellular or Insulating) Concrete Substrate

Sharp ridges or other projections above the surface shall be removed before roofing. Fastening for recover board shall be into structural deck below insulating fill (see steel/concrete deck requirements).

###### Precast / Prestressed Concrete Deck

The roof deck shall be smooth, even, free of dust, dirt, excess moisture or oil and be structurally sound. All joints between precast units shall be grouted. Any differentials in height between precast units shall be feathered for a smooth transition. Any deteriorated decking shall be repaired.

###### Cementitious Wood Fiber Deck

The roof deck face shall be smooth, even, free of excess moisture, and structurally sound. Joints over bulb-tees shall be grouted. Grouting shall be done with materials supplied or recommended by the deck manufacturer. All wet or deteriorated sections of decking shall be removed and replaced. Deck planks shall be secured to structural supports as recommended by deck manufacturer.

##### Reroofing with Removal of Existing Single-Ply Membrane

The Owner's Representative and Applicator shall determine the condition of the roof deck and existing insulation. Deteriorated decking or wet or deteriorated materials are to be removed and replaced. After removal of single-ply roof, inspect insulation boards and reuse only if dry and in stable condition. Add a Sika Corporation approved recover board or new insulation board. Fasten recover board or top layer of insulation in accordance with Sika Corporation's requirements.

##### Recover Over Existing Single Ply Membrane

The Owner's Representative and Applicator shall determine the condition of the roof deck and existing insulation. Deteriorated decking or wet or deteriorated materials are to be removed and replaced. Remove all debris from the existing single-ply roof and cut into 10 ft x 10 ft panels (3.0 m x 3.0 m), or cut 6” (15.2 cm) circles down center of each sheet, every 5 to 8 ft (1.5 to 2.4 m). Install a layer of a Sika Corporation approved roof board or new insulation board over the cut single-ply and then fasten the board according to Sika Corporation's requirements.

###### Install a layer of a Sika Corporation approved recover board or a new insulation board over the fastened 10 ft x 10 ft (3.0 m x 3.0 m) panels and then fasten the board according to Sika Corporation's requirements. For Type III hot asphalt attachment of new insulation board, priming of the old roof surface after preparation is necessary.

##### Recover Over Existing Bitumen Roofing

The Owner's Representative and Applicator shall determine the condition of the existing roof deck and old roof system. Areas with deteriorated decking or wet materials are to be removed and replaced.

[NOTE TO SPECIFIER: LOOSE GRAVEL SHALL BE REMOVED UNLESS INSTRUCTED BY SPECIFIER.]

###### On graveled surfaces, all debris shall be removed. All blisters shall be removed and sealed or cut, fastened down and sealed. Any accumulation of bitumen or other irregularities shall be scratched and removed so as to produce a smooth surface.

###### On smooth surfaced roofs, the surface must be clean and dry. All blisters shall be removed and sealed or cut, fastened down and sealed. For Type III hot asphalt attachment of new insulation board, priming of the old roof surface after preparation is necessary.

###### Coal-tar pitch or heavily resaturated roofs may require removal. Contact Sika Corporation Technical for coal-tar pitch or heavily resaturated reroof preparation requirements.

#### WOOD NAILER INSTALLATION

##### Install continuous code compliant wood nailers at the perimeter of the entire roof and around roof projections and penetrations as shown on the Detail Drawings.

##### Wood nailers or wood blocking for penetrations, curbs, or snow protection systems shall be installed prior to the installation of the roof membrane whenever possible.

#### VAPOR RETARDER INSTALLATION

[NOTE TO SPECIFIER: IF USED AS A TEMPORARY ROOF, POSITIVE SLOPE TO DRAIN IS REQUIRED.]

Refer to vapor retarder Product Data Sheets (PDS) and *Vapor Retarder Installation* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

##### Vapor Retarder PE 10

Overlap loose laid sheets 4” (10.2 cm) and extend up the perimeter and deck penetrations. Seams and penetrations shall be sealed with Multi-Purpose Tape.

##### Vapor Retarder SA 31

All surfaces except for steel require priming. Lay out sheets so side laps are overlapped by 3” (76 mm) and end laps are overlapped by 6” (15.2 cm). Peel back release liner, press onto substrate, and roll with a minimum 100 lb roller.

##### Vapor Retarder SA 106

All surfaces except for steel require priming. Lay out sheets so side laps are overlapped by 3” (76 mm) and end laps are overlapped by 6” (15.2 cm). Peel back release liner, press onto substrate, and roll with a minimum 100 lb roller.

##### Vapor Retarder TA 138

Prime concrete surfaces. Lay out sheets so side laps are overlapped by 3” (76 mm) and end laps overlapped by 6” (15.2 cm). Torch the bottom side of the sheet and install into substrate.

##### Ply Sheet TA 87

Prime concrete surfaces. Torch the bottom side of the sheet, install into substrate, and walk on or roll the surface with a minimum 100 lb roller. Sheets shall be laid out so side laps are overlapped by 6” (15.2 cm) and end laps are overlapped by 12” (30.5 cm).

##### Ply Sheet HA 87 and Ply Sheet HA 118

Prime concrete surfaces. Adhere sheets with Type III or Type IV asphalt in accordance with ARMA guidelines. Ply Sheet HA 87 and HA 118 can also be cold applied with Vapor Retarder Adhesive CA.

##### Sarnavap 5000E SA FR

Install sheets parallel to metal deck profiles so side laps lie on top flanges. Lay out sheets so side and end laps are overlapped by 2” (51 mm). Install a 6” (15.2 cm) wide strip of Sarnavap 5000E SA FR or metal plate perpendicular to the deck profiles and roll direction to support the end of the sheets. Peel back release liner, press onto substrate, and roll with a minimum 100 lb roller.

#### INSULATION / ROOF BOARD INSTALLATION

General Criteria:

###### Boards shall be installed according to local building code, insurance requirements, and manufacturer's instructions.

###### Boards shall be neatly cut to fit around penetrations and projections.

###### Install tapered insulation in accordance with insulation manufacturer's shop drawings.

###### Do not install more board than can be covered with membrane by the end of the day or the onset of inclement weather.

###### When two or more layers of insulation and/or roof boards are used, stagger joints at least 12” (30.5 cm) in both directions between layers.

###### Refer to individual Product Data Sheets (PDS) and *Insulation or Roof Board Installation* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

##### Mechanical Attachment

Boards may be loose laid, but top-most layer shall be mechanically fastened to the deck with approved fasteners and plates according to the wind uplift rating requirements and associated fastening patterns.

#### SIKAPLAN FASTENED MEMBRANE INSTALLATION

The surface of the insulation, roof board, or substrate shall be inspected prior to installation of the Sikaplan roof membrane. The substrate shall be clean, dry, and free from debris and smooth with no surface roughness or contamination. Broken, delaminated, wet or damaged boards shall be removed and replaced.

##### General Criteria

###### Sikaplan Fastened membrane shall be attached with Sikaplan Fasteners and Sarnadiscs or Sikaplan Discs to withstand project specified design pressures.

###### Tack welding of Sikaplan Fastened full or half-width rolls for purposes of temporary restraint during installation is not permitted and may result in voiding of Sika Corporation warranty.

###### Sheet layout shall not buck water.

###### Hot-air weld overlaps according to Sika Corporation’s recommendations. Seam test cuts shall be taken at least 3 times per day.

###### Refer to Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions

##### Sikaplan Fastened System

###### Sikaplan fasteners and Sarnadiscs or Sikaplan Discs are installed along the edge of the membrane on the fastening line at a spacing determined by Sika Corporation and the Owner’s Representative/Designer.

###### Fasteners shall clamp the Sikaplan Fastened membrane tightly to the substrate.

###### Adjacent rolls shall be overlapped as outlined on individual Product Data Sheets (PDS) and *In-Seam Disc Placement Details / Membrane Installation* section of Sika Sarnafil Roofing Applicator Handbook for specified plate and fastener combination.

##### Rhinobond System

###### Sikaplan Fastened membrane is laid out over properly installed substrate attached with specified Sarnadisc Rhinobond plates.

###### Membrane is then induction welded to the specified Sarnadisc Rhinobond. After weld is complete, immediately apply magnetic heat sink.

#### HOT-AIR WELDING OF MEMBRANE OVERLAPS

##### All membrane overlaps shall be hot-air welded. The membrane shall be clean and dry prior to hot-air welding.

##### Field membrane overlaps for automatic machine-welding will vary in width depending on the plate and fastener combination used. A minimum of 4” (10.2 cm) wide overlap is required when hand-welding details.

##### 1” (25 mm) wide cross-section samples of welded seams shall be taken at least two times a day, once in the morning and once in the afternoon.

##### Refer to *Welding* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

#### MEMBRANE FLASHING INSTALLATION

All flashings shall be installed concurrently with the roof membrane as the job progresses. No temporary flashings shall be allowed without the prior written approval of the Owner's Representative and Sika Corporation. Approval shall only be for specific locations on specific dates. If any water is allowed to enter under the newly completed roofing, the affected area shall be removed and replaced at the Applicator's expense. Flashing shall be adhered to compatible, dry, and smooth surfaces free of dirt, dust, and debris. Use caution to ensure adhesive fumes are not drawn into the building.

##### All flashings should extend a minimum of 8” (20.3 cm) above finished roofing level. Submit requests for exceptions in writing to the Owner's Representative and Sika Corporation Technical Department for signed approval.

##### No bitumen shall be in contact with the Sikaplan membrane.

##### All flashing membranes shall be mechanically fastened along the counter-flashed top edge with Sarnastop or approved Sarnadisc at 6 - 12” (15.2 – 30.5 cm) on center.

##### Flashings shall be terminated according to Sika Corporation recommended details.

##### All adhered flashings that exceed 45” (1.14 m) in height shall receive additional securement, unless applying Sarnafil G 410 SA membrane to plywood, DensDeck Prime, glass-faced polyisocyanurate, or smooth poured concrete with a concrete surface profile range of CSP 2 to CSP 6 according to ICRI Technical Guideline No. 310.2R-2013.

##### Refer to *Typical Flashing Procedures* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

#### LIQUID FLASHING INSTALLATION

##### Application Guidelines

Liquid Flashing has a strong odor. Precautions should be taken to prevent odors and/or vapors from entering the building/structure, including but not limited to turning off and sealing air intake vents and other means of ingress for odors and/or vapors into the building/structure during product application and cure. Refer to individual Product Data Sheets (PDS) and *Liquid Flashing Procedures* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

##### Installation Notes

###### Prepare the surface to be flashed by cleaning the area to like-new condition.

###### Pre-cut vertical and horizontal liquid flashing fleece to fit around the penetration with 2” (51 mm) overlaps.

###### Thoroughly mix the Liquid Flashing and the Liquid Flashing Catalyst with a slow speed mixer.

###### Apply the catalyzed liquid flashing with a 55 mil base layer. Place the pre-cut fleece into the wet Liquid Flashing making sure to saturate the fleece. Apply a 25 mil finishing layer over the fleece.

##### Inspection and Quality Control

Refer to Sika Sarnafil Technical Bulletin 19-02 for detailed inspection procedures.

#### SARNACLAD METAL BASE FLASHINGS / EDGE METAL INSTALLATION

##### All flashings shall be installed concurrently with the roof membrane as the job progresses. No temporary flashings shall be allowed without the prior written approval of the Owner's Representative and Sika Corporation. Approval shall only be for specific locations on specific dates. If any water is allowed to enter under the newly completed roofing due to incomplete flashings, the affected area shall be removed and replaced at the Applicator's expense.

##### Metal details, fabrication practices and installation methods shall conform to the applicable requirements of the following:

###### ANSI SPRI ES-1 (latest issue).

###### Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) - latest issue.

##### Pre-formed metal flashing shall be installed according to metal manufacturer’s guidelines.

##### Metal, other than that provided by Sika Corporation, is not covered under the Sika Corporation warranty.

##### Sarnaclad and other metal flashings shall be formed and installed per the Detail Drawings. Refer to individual Product Data Sheets (PDS) and *Metal Flashings* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

#### WALKWAY INSTALLATION

##### Sarnatred-V

Probe all existing deck membrane seams which are to be covered by Sarnatred-V. Install walkway in straight lines by either adhering and welding or just welding to the field membrane.

##### Crossgrip XTRA

Probe all existing membrane seams which are to be covered by Crossgrip XTRA. Crossgrip XTRA is installed loose laid. Connecting clips are available for attaching roll ends together.

##### Concrete Pavers

Probe all existing membrane seams which are to be covered by concrete pavers. Using a separate piece of Sarnafil membrane as a protection layer, weld all edges in place. Place normal weight concrete pavers on the protection membrane. In areas of high wind exposure the pavers shall be strapped together with stainless steel metal straps that are flush with the paver surface.

##### Refer to individual Product Data Sheets (PDS) and *Walkway Installation* section of Sika Sarnafil Roofing Applicator Handbook for detailed installation instructions.

#### PERIMETER WARNING INSTALLATION

##### Application areas must be cleaned to a like-new condition. For detailed installation instructions, refer to individual Product Data Sheets (PDS).

##### Tape: Perimeter Warning Tape is applied with hand pressure to the top of PVC roofing membrane in the areas required.

##### Membrane: Perimeter Warning Membrane is hot-air welded to the top of PVC roofing membrane in the areas required.

#### TEMPORARY CUT-OFF

##### All flashings shall be installed concurrently with the roof membrane in order to maintain a watertight condition as the work progresses. All temporary cut-offs shall be constructed to provide a watertight seal. The new membrane shall be carried into the temporary cut-off. Temporary cut-off shall be sealed to the deck or substrate so that water will not be allowed to travel under the new or existing roofing. When work resumes, the contaminated membrane shall be cut out.

##### If inclement weather occurs while a temporary cut-off is in place, the Applicator shall provide the labor necessary to monitor the situation to maintain a watertight condition.

##### If any water is allowed to enter under the newly-completed roofing, the affected area shall be removed and replaced at the Applicator's expense.

##### Refer to *Overnight Tie-In* section of Sika Sarnafil Roofing Applicator Handbook for detailed instructions.

#### COMPLETION

##### Prior to demobilization from the site, the work shall be reviewed by the Owner's Representative and the Applicator. All defects noted and non-compliances with the Specifications or the recommendations of Sika Corporation shall be itemized in a punch list. These items must be corrected immediately by the Applicator to the satisfaction of the Owner's Representative and Sika Corporation prior to demobilization.

##### All Warranties referenced in this Specification shall have been submitted and have been accepted by the owner or owner’s representative at time of contract award.

#### DETAILS

##### Refer to usa.sika.com/sarnafil.

**DISCLAIMER**

**Prior to each use of any Sika product, the user must always read and follow the warnings and instructions on the product’s most current Product Data Sheet, product label and Safety Data Sheet which are available online at usa.sika.com/sarnafil or by calling Sika's Technical Service Department at 800-451-2504. Nothing contained in any Sika materials relieves the user of the obligation to read and follow the warnings and instruction for each Sika product as set forth in the current Product Data Sheet, product label and Safety Data Sheet prior to product use.**

With respect to any guide specifications prepared and provided by Sika, such guide specifications are generic and nature and are provided as a general guide for informational purposes only to architects or roof designers/specifiers. Sika guide specifications are not intended to replace sound engineering and architectural practices and should not be relied upon for that purpose. Sika assumes no liability with respect to the provision of this guide specification, the preparation of the guide specifications, the design of the roofing or waterproofing system, the preparation and approval of the details and shop drawings, or for determining their suitability for a particular project or application. The architect, consultant and/or engineer or design professional for a particular project bears the sole responsibility for the design of the roofing or waterproofing system, for the preparation of the specifications, the preparation and approval of the details and shop drawings, and for determining their suitability for a particular project or application.

**SIKA MAKES NO WARRANTY OF ANY KIND, EITHER EXPRESS OR IMPLIED, AS TO THE CONTENTS OF THESE GUIDE SPECIFICATIONS. SIKA SHALL NOT BE RESPONSIBLE UNDER ANY LEGAL THEORY TO ANY THIRD PARTY FOR ANY DIRECT OR CONSEQUENTIAL DAMAGES OF ANY KIND ARISING FROM THE USE OF THESE GUIDE SPECIFICATIONS.**