ROOFING SPECIFICATION PREPARED BY SIPLAST, INC.

PC-227 ELASTOMERIC ROOF COATING

This specification is provided as a general guide for use of Siplast products based on typical building conditions and standard roofing practices.  Siplast is strictly a manufacturer of roofing systems and has no experience, training or expertise in the areas of architecture/engineering or in the area of consulting with respect to matters related to such areas.  Siplast recommends that the Owner's representative independently verify the accuracy and appropriateness of a specification provided for a specific project.

December 1, 2022

SECTION  09 96 53   ELASTOMERIC COATING

PART I  GENERAL

  - SECTION INCLUDES:

- Preparation of modified bitumen roof system to receive elastomeric coating

- Application of elastomeric coating to prepared modified bitumen substrate

  - RELATED SECTIONS

- Section 07 52 00 – Modified Bituminous Membrane Roofing

  - REFERENCE STANDARDS

References in these specifications to standards, test methods and codes, are implied to mean the latest edition of each such standard adopted.  The following is an abbreviated list of associations, institutions, and societies which may be used as references throughout this specification section.

ASTM	American Society for Testing and Materials

Philadelphia, PA

NRCA	National Roofing Contractors Association

Rosemont, IL

OSHA	Occupational Safety and Health Administration

Washington, DC

UL	Underwriters Laboratories

Northbrook, IL

USEPA	United States Environmental Protection Agency

Washington, DC

USGBC	United States Green Building Council

Washington, DC

  - SUBMITTALS

- Submit product data sheets verifying physical and mechanical properties of the coating material.

- Submit material safety data sheets for the elastomeric coating material and accessory products to be using in conjunction with the coating application.

  - QUALITY  ASSURANCE

- Acceptable Contractor:  Contractor shall be certified in writing by the coating manufacturer to install the specified elastomeric coating.

- Local Regulations:  Conform to regulations of public agencies, including any specific requirements of the city and/or state of jurisdiction.

- The elastomeric roof coating shall be eligible to achieve 1 credit point according to the SS Credit 7.2: Heat Island Effect: Roof as recorded in 2009 LEED for New Construction & Major Renovations.  In addition, the elastomeric coating shall meet the approval requirements of the U.S. EPA Energy Star program.

  - PRODUCT  DELIVERY,  STORAGE  AND  HANDLING

- Containers and Packaging:  Deliver materials in original sealed containers, clearly marked with manufacturer’s logo, full product name; and lot number(s).

- Storage:  Store pallets upright on a clean, flat surfaces at temperatures between 40oF  (4ºC) and 100oF (38ºC) with careful handling to prevent damage.  Exposure of product to temperatures outside this range may affect product shelf life and quality of finished product.

- Protection:  Protect the pails of elastomeric coating from temperatures outside the range described in 1.06-B and other damage during transit, handling, storage, and installation.

  - PROJECT  CONDITIONS

- Application Rates:  The minimum specified application rates for material usage are for ideal conditions.  Application rates may vary depending on substrate and application method.

- Surface Conditions:  Do not apply materials unless surfaces to receive the elastomeric coating are clean, dry and prepared as specified.

- Coating Manufacturer/Regulatory Agency Requirements:  Install the coating in strict accordance with all published safety, weather, or applicable regulations of the manufacturer and local, state, federal agencies which have jurisdiction.  Follow the coating supplier’s application guidelines at all times.

- Application Equipment Manufacturer Requirements:  If mechanical equipment is used to apply the coating system, follow the application equipment manufacturer’s guidelines.

- Weather Restrictions:  Do not apply the elastomeric coating when the ambient temperature is less than 50ºF (10ºC) or if weather will not permit the coating to dry prior to exposure to precipitation or freezing temperatures.

- Heavy Puddles.  Heavy puddles of coating on the roof surface are not acceptable.

- Drainage Restrictions:  Ensure that the substrate to receive the elastomeric coating provides positive drainage prior to application of the coating system.

  - GUARANTEE/GUARANTEE ADDENDUM

- Elastomeric Roof Coating Warranty:  Upon successful completion of the project, and after all post installation procedures have been completed, furnish the Owner with the manufacturer's 5 year limited materials warranty.  The warranty shall cover replacement of the elastomeric coating as a result of the following causes:

1.	Deterioration of the coating materials resulting from ordinary wear and tear by the elements.

2.	Deterioration of the coating materials resulting from manufacturing defects in said materials.

>	Siplast 5-year PC-227 Elastomeric Coating Materials Warranty

PART II  PRODUCTS

  - COATING SYSTEM/PRODUCTS

- Elastomeric Coating System:  An elastomeric coating system composed of 100% acrylics designed for spray, brush or roller application over modified bitumen roof systems.  The coating system shall exhibit the following physical and mechanical properties following the curing period:

  - Solids content by volume (min.)  50%  (ASTM D6083)

  - Solids content by weight (min.)  65%  (ASTM D6083)

  - Coating System Tensile strength @ 73F (min)  250 psi  (ASTM D6083)

  - Coating System Elongation at break (73F)  250%  (ASTM D6083)

  - Coating System Permeance (max.) 15 perms  (ASTM D6083)

>	Siplast PC-227 Elastomeric Roof Coating

  - RELATED MATERIALS

- Related Materials - General:  Flashing, adhesives, elastomeric sealant compounds, primers, and similar materials shall be approved by the supplier of the coating system.

- Substrate Cleansing Agent:  A concentrated, non-corrosive, biodegradable, water-soluble cleaner used to prepare membrane surfaces prior to elastomeric coating application.

PART III   EXECUTION

  - SUBSTRATE EXAMINATION

- Substrate Inspection:  Inspect the substrate to receive the coating to ensure that surfaces are clean, smooth, sound, and free of moisture, dirt, debris, or contamination.  Verify that all roof penetrations, mechanical equipment, cants, edge metal, and other on-roof items are properly installed and secure.  Verify that all air conditioning and air intake vents are suitably protected or closed.

- Protection Of Surrounding Areas:  Protect areas surrounding the area to receive the elastomeric coating from overspray.

  - SUBSTRATE PREPARATION

- Membrane/Flashing Preparation/Repairs:  Repair damaged or deteriorated areas of the existing membrane/flashing system using materials to match the existing according to the membrane manufacturer's specifications.  Asphalt or torch applied membranes shall be exposed to the elements for a minimum of 30 days prior to coating application.

- Surface Cleansing:  Clean the surface of the existing roof, ensuring that the surface is clean, sound, dry and free of any contaminating materials that would interfere with proper adhesion of the coating.  This may require a low-pressure wash, scrubbing, brooming, power-brooming or power vacuuming.  Rinse the substrate with copious amounts of clean water  and allow to dry before application of coating materials.

- Application of Cleansing Agent.  Apply the cleansing agent, diluted to a ratio of at least 10 parts water to 1 part cleansing agent, to the substrate at the rate of 150 to 200 square feet per gallon.  Allow the solution to stand for approximately 5 minutes.  Pay particular attention to low areas.  Low areas and depressions in the substrate or any area containing excessive dirt or oils may require repeat applications.  Scrub the entire surface to be cleaned vigorously and completely using a stiff-bristled broom.  Before the cleansing agent dries, wash the surface with copious amounts of clean water  Allow the roof surface to dry completely prior to application of the elastomeric coating system.

  - APPLICATION OF ELASTOMERIC COATING SYSTEM

- Apply two coats of PC-227 Elastomeric Roof Coating using spray, brush, or roller to create a seamless roof coating.

  - Apply the first coat at the rate of 1.5 gallon per 100 square feet and allow to dry.  Drying time is normally 4 to 12 hours, depending on sunlight, ambient temperatures and relative humidity.

  - Apply the second coat using a cross hatch technique at a the rate of 1.5 gallon per 100 square feet.

  - Cut-in all edges evenly and in a uniform manner so as to provide an aesthetically pleasing appearance.

  - PROTECTION/CLEANING

- Surfaces not intended to receive the PC-227 Elastomeric Roof Coating shall be protected during the application of the system.  Should this protection not be effective, or not be provided, the respective surfaces shall be restored to their proper conditions by cleaning, repair or replacement.

END SECTION 09 96 53