Roofing Specification

For:

Guide Specification

Parapro Green Roofing System

Prepared by:

Siplast

1000 East Rochelle Blvd.

Irving, Texas 75062

(800) 922-8800

This specification is provided as a general guide for use of Siplast products based on typical building conditions and standard roofing practices.  Siplast is strictly a manufacturer of roofing systems and has no experience, training or expertise in the areas of architecture/engineering or in the area of consulting with respect to matters related to such areas.  Siplast recommends that the Owner's representative independently verify the accuracy and appropriateness of a specification provided for a specific project.

October 15, 2010

SECTION 07560  FLUID-APPLIED GREEN ROOFING AND FLASHING  (Rev 10/2009)js

PART 1  GENERAL

1.01  SECTION INCLUDES:

A.	Preparation of Substrate to Receive Roofing Materials

B.	Modified Bitumen Ply Sheet Application to Prepared Substrate

C.	PMMA Flashing Application

D.	PMMA Roof Membrane Application

1.02  RELATED SECTIONS

A.	Section [-----] - Submittals

B.	Section [-----] - Rough Carpentry

C.	Section [-----] – Concrete Roof Decks

D.	Section [-----] - Sheet Metal Flashing Components And Roofing Accessories

E.	Section [-----] - Sheet Metal Flashing and Trim

F.	Section [-----] - Sheet Metal Roofing Specialties

G.	Section [-----] – Green Roof Overburden

1.03  REFERENCE STANDARDS

Agencies which may be used as references throughout this specification section include:

ASTM	American Society for Testing and Materials

Philadelphia, PA

FM	Factory Mutual Engineering and Research

Norwood, MA

NRCA	National Roofing Contractors Association

Rosemont, IL

CERTA	Certified Roofing Torch Applicator Program

National Roofing Contractors Association

Rosemont, IL

Midwest Roofing Contractors Association

Lawrence, KS

OSHA	Occupational Safety and Health Administration

Washington, DC

UL	Underwriters Laboratories

Northbrook, IL

ACI	American Concrete Institute

Hills, MI

ICRI	International Concrete Repair Institute

Des Plaines, IL

1.04  SUBMITTALS

*  NOTE:	Coordinate submittal requirements with general provisions.  Modify submittals to suit specific project requirements.

A.	Submittals Prior to Contract Award:

1.	Letter from the proposed primary roofing manufacturer confirming that the bidder is an acceptable Contractor authorized to install the proposed system.

2.	Letter from the primary roofing manufacturer stating that the proposed application will comply with the Manufacturer's requirements in order to qualify the project for the specified guarantee.

1.05  QUALITY ASSURANCE

A.	Acceptable Contractor:  Contractor shall be certified in writing by the roofing materials manufacturer to install the primary roofing products.

B.	Product Quality Assurance Program:  Primary roofing materials shall be manufactured under a quality management system that is monitored regularly by a third party auditor under the ISO 9001 audit process.

C.	Project Acceptance:  Submit a completed manufacturer's application for roof guarantee form along with shop drawings of the roofs showing all dimensions, penetrations, and details.  The project must receive approval by the membrane manufacturer, through this process, prior to shipment of materials to the project site.

D.	Scope of Work:  The work to be performed under this specification shall include but is not limited to the following:  Attend necessary job meetings and furnish competent and full time supervision, experienced roof mechanics, all materials, tools, and equipment necessary to complete, in an acceptable manner, the roof membrane/flashing installation in accordance with this specification.  Comply with the latest written application instructions of the manufacturer of the primary roofing products.

E.	Local Regulations:  Conform to regulations of public agencies, including any specific requirements of the city and/or state of jurisdiction.

F.	Manufacturer Requirements:  The membrane/flashing system manufacturer shall provide direct trained company personnel to attend necessary job meetings, perform periodic inspections as necessary, and conduct a final inspection upon successful completion of the project.

1.06  GUARANTEE/WARRANTY

A.	Roof Membrane Guarantee:  Upon successful completion of the project, and after all post installation procedures have been completed, furnish the Owner with the manufacturer's ten-year labor and materials membrane guarantee.  The guarantee shall be a term type, without deductibles or limitations on coverage amount, and shall be issued at no additional cost to the Owner.  This guarantee shall not exclude random areas of ponding from coverage.

>	Siplast Parapro 10-year Roof Membrane Guarantee

1.07  PRODUCT DELIVERY STORAGE AND HANDLING

A.	Delivery:  Deliver materials in the manufacturer's original sealed and labeled containers and in quantities required to allow continuity of application.

B.	Storage:  Store closed containers in a cool, dry area away from heat, direct sunlight, oxidizing agents, strong acids, and strong alkalis.  Do not store resins or catalyst at temperatures below 32°F (0°C) or above 85°F (29°C).  Keep away from open fire, flame or any ignition source.  Store in a well ventilated area.

C.	Handling:  Handle all materials in such a manner as to preclude damage and contamination with moisture or foreign matter.  Keep away from open fire, flame, or any ignition source.  Vapors may form explosive mixtures with air.  Avoid skin and eye contact with this material.  Avoid breathing fumes when above the Threshold Limit Value (TLV).  Do not eat, drink, or smoke in areas where roofing materials are stored or applied.

D.	Damaged Material:  Any materials that are found to be damaged or stored in any manner other than stated above shall be automatically rejected, removed and replaced at the Contractor's expense.

1.08  PROJECT/SITE CONDITIONS

A.	Requirements Prior to Job Start

1.	Notification:  Give a minimum of 5 days notice to the Owner and manufacturer prior to commencing any work and notify both parties on a daily basis of any change in work schedule.

2.	Permits:  Obtain all permits required by local agencies and pay all fees which may be required for the performance of the work.

3.	Safety:  Familiarize every member of the application crew with all fire and safety regulations recommended by OSHA, NIOSH, NRCA and other industry or local governmental groups.  Workers shall wear a long sleeve shirt with long pants and work boots.  Workers shall use only butyl rubber or nitrile gloves when mixing or applying PMMA products.  Safety glasses with side shields are required for eye protection.  Use local exhaust ventilation to maintain worker exposure below the published Threshold Limit Value (TLV).  If the airborne concentration poses a health hazard, becomes irritating or exceeds recommended limits, use a NIOSH approved respirator in accordance with OSHA Respirator Protection requirements published under 29 CFR 1910.134.  The specific type of respirator will depend on the airborne concentration.  A filtering face piece or dust mask is not appropriate for use with this product if TLV filtering levels have been exceeded.

B.	Environmental Requirements

1.	Precipitation:  Do not apply roofing materials during precipitation or in the event there is a probability of precipitation during application.  Take adequate precautions to ensure that materials, applied roofing, and building interiors are protected from possible moisture damage or contamination.

3.	Temperature Restrictions – self-adhesive sheets:  The minimum required substrate temperature at point of application is 40F (4C).  Maintain a minimum roof membrane material temperature above 50F (10C).  In low temperature conditions, materials keep materials warm prior to application.  Suspend application in situations where the self-adhered base ply cannot be kept at temperatures allowing for proper adhesion or the substrate temperature will not allow for proper adhesion.

4.	Temperature Restrictions – PMMA-based Materials:  Do not apply catalyzed resin materials if there is a threat of inclement weather.  Follow the resin manufacturer's specifications for minimum and maximum ambient, material and substrate temperatures.  Do not apply catalyzed resin materials unless temperatures fall within the resin manufacturer's published range.

C.	Protection Requirements

1.	Membrane Protection:  Provide protection against staining and mechanical damage for newly applied roofing and adjacent surfaces.

PART 2  PRODUCTS

2.01  ROOFING SYSTEM ACCESSORIES

A	Primers Sealants and Adhesives for Bitumen Products

1.	Asphalt Primer:  An asphalt, solvent blend conforming to ASTM D 41 Type I or II requirements and meeting local VOC regulations.

>	PA-1125 Asphalt Primer by Siplast; Irving, TX

2.	Asphalt Primer:  An asphalt/solvent blend meeting ASTM D 41, South Coast Air Quality District and Ozone Transport Commission requirements.

>	PA-917 LS Asphalt Primer by Siplast; Irving, TX

3.	Primer for Self-Adhesive Sheets:  A quick drying, low-VOC, water-based, high-tack primer specifically designed to promote adhesion of roofing and waterproofing sheets to approved substrates. Primer shall meet South Coast Air Quality District and Ozone Transport Commission requirements.

>	TA-119 Primer by Siplast; Irving, TX

4.	Elastomeric Sealant:  A moisture-curing, non-slump elastomeric sealant designed for roofing applications.  The sealant shall be approved by the roof membrane manufacturer for use in conjunction with the roof membrane materials.  Acceptable types are as follows:

>	PS-304 Elastomeric Sealant by Siplast; Irving, TX

C.	Resin Accessories

1.	Cleaning Solution/Solvent:  A clear solvent used to clean and prepare transition areas of in-place catalyzed resin to receive subsequent coats of resin and to clean substrate materials to receive resin.

>	Pro Prep by Siplast; Irving, TX

2.	Preparation Paste:  A PMMA based paste used for remediation of depressions in substrate surfaces or other irregularities.

>	Pro Paste Resin by Siplast; Irving, TX

3.	Repair Mortar:  A two-component, PMMA based, aggregate filled mortar used for remediation of depressions or patching concrete substrates.

>	Pro Repair Mortar by Siplast; Irving, TX

4.	Color Finish Resin:  A pigmented, polymethylmethacrylate (PMMA) based resin to provide a desired color finish over the flashing system.

>	Pro Color Finish by Siplast; Irving, TX

D.	PMMA Primers

1.	Primer for Vertical Concrete, Wood and Plywood Substrates:  A fast-curing PMMA-based primer for use in vertical applications over concrete, concrete repair materials and masonry and for approved wood, plywood and rigid insulation substrates.

>	Pro Primer W by Siplast; Irving, TX

2.	Primer for Horizontal Concrete Substrates:  A fast-curing PMMA-based primer for use over horizontal concrete substrates.

>	Pro Primer T by Siplast; Irving, TX

3.	Primer for Asphaltic Substrates:  PMMA-based primer for use over asphaltic materials to serve as a bleed-blocker.

>	Pro Primer R by Siplast; Irving, TX

E.	Accessories

1.	Tape:  A white, flexible, coated cotton gaffers tape designed for treatment of insulation panel joints, deck/wall transitions and joints in flashing substrates.

2.	Joint Tape:  A thermoplastic/rubber based sheet having a woven polyester backing used to treat joints between rigid insulation or flashing substrate panels.  The sheet shall have a minimum width of 4 inches.

>	Eternabond Webseal by Eternabond, Inc., Mundelein, IL

2.02  ROOFING SYSTEM COMPONENTS

*  NOTE:	Select a roof system to meet individual project requirements.  Contact Siplast for further information regarding roof system selection guidelines.

A.	Roofing Membrane Assembly:  A membrane assembly consisting of a liquid applied, flexible, polymethylmethacrylate (PMMA) based monolithic membrane formed by the combination of liquid PMMA-based resin and fleece fabric.

>	Siplast Parapro Roof System

1.	Resin for Field Membrane Construction:  A flexible, polymethylmethacrylate (PMMA) based resin for use in combination with fleece fabric to form a monolithic, reinforced roofing membrane.

a)	Thickness (avg):  90 mils (2.3 mm) at 0.31 kg/ft² (3.3 kg/m²) coverage rate (ASTM D 5147, section 5). The values listed below are based upon a 90 mil (2.3 mm) resin thickness.

b)	Weight (min per 100 ft² of coverage):  68.4 lb (3.3 kg/m²)

c)	Peak Load (avg) @ 73°F (23ºC):  70 lbf/in (12.3 kN/m)  (ASTM D 5147 section 6)

d)	Peak Load (avg) @ 73°F (23ºC):  90 lbf/inch (15.8 kN/m)  (ASTM D 412, dumbbell)

e)	Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D 5147, section 6)

f)	Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D 412, dumbbell)

g)	Shore A Hardness (avg): 81 (ASTM D 2240)

h)	Water Absorption, Method I (24h @ 73°F):  0.8% (ASTM D 570)

i)	Water Absorption, Method II (48h @ 122°F):  1.2% (ASTM D 570)

j)	Low temperature flexibility @ 23 F (-5°C):  PASS (ASTM D 5147, section 11)

k)	Dimensional Stability (max):  0.15% (ASTM D 5147, section 10)

l)	Tear Strength (avg):  90 lbf (0.4 kN) (ASTM D 5147, section 7)

m)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

>	Parapro Roof Resin by Siplast; Irving, TX

2.	Fleece for Membrane Reinforcement:  A non-woven, 110 g/m², needle-punched polyester fabric reinforcement as supplied by the membrane system manufacturer.

>	Pro Fleece by Siplast; Irving, TX

B.	Roofing Membrane Assembly:  A membrane assembly consisting of one ply of a prefabricated, reinforced, homogeneous Styrene-Butadiene-Styrene (SBS) block copolymer modified asphalt membrane applied over a prepared substrate, covered with a liquid applied, flexible, polymethylmethacrylate (PMMA) based monolithic membrane formed by the combination of liquid PMMA resin and fleece fabric.  The reinforcement mats in the SBS ply shall be impregnated/saturated and coated each side with an SBS modified bitumen blend.  The cross sectional area of the SBS sheet material shall contain no oxidized or non-SBS modified bitumen.  The adhesive layer of torch-grade membranes shall be manufactured using a process that embosses the surface with a grooved pattern to provide optimum burn-off of the plastic film and to maximize application rates.  The top surface of the modified bitumen ply sheet shall be coated with a white acrylic coating to enhance resin bond and to minimize surface temperatures.  The composite system, including SBS modified bitumen ply sheet and reinforced PMMA, shall pass 500 cycles of ASTM D 5849 Resistance to Cyclic Joint Displacement (fatigue) at 14F (-10C).  Passing results shall show no signs of membrane cracking or interply delamination after 500 cycles.  The system shall pass 200 cycles of ASTM D 5849 after heat conditioning performed in accordance with ASTM D 5147.

>	Siplast Parapro Roof System with Paradiene 20 TG P base ply

1.	Modified Bitumen Ply Sheet

a)	Thickness (avg):  114 mils (2.9 mm)  (ASTM D 5147)

b)	Thickness (min):  110 mils (2.8 mm)  (ASTM D 5147)

c)	Weight (min per 100 ft² of coverage):  73 lb (3.6 kg/m²)

d)	Maximum filler content in elastomeric blend:  35% by weight

e)	Low temperature flexibility @ -15º F (-26º C) - PASS  (ASTM D 5147)

f)	Peak Load (avg) @ 73ºF (23ºC):  30 lbf/inch (5.3 kN/m) (ASTM D 5147)

g)	Peak Load (avg) @ 0ºF (-18ºC):  75 lbf/inch (13.2 kN/m) (ASTM D 5147)

h)	Ultimate Elongation (avg.) @ 73ºF (23ºC):  50%  (ASTM D 5147)

i)	Dimensional Stability (max):  0.1%  (ASTM D 5147)

j)	Compound Stability (min):  250ºF (121ºC)  (ASTM D 5147)

k)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

l)	Reinforcement:  fiberglass mat or other meeting the performance and dimensional stability criteria

m)	Top Surfacing:  factory applied acrylic coating

>	Paradiene 20 TG P, by Siplast; Irving, TX

2.	Self-Adhesive Modified Bitumen Flashing Reinforcing Sheet

a)	Thickness (avg):  102 mils (2.6 mm)  (ASTM D 5147)

b)	Thickness (min):  98 mils (2.5 mm)  (ASTM D 5147)

c)	Weight (min per 100 ft² of coverage):  69 lb (3.4 kg/m²)

d)	Maximum filler content in elastomeric blend:  35% by weight

e)	Low temperature flexibility @ -15º F (-26º C) - PASS  (ASTM D 5147)

f)	Peak Load (avg) @ 73ºF (23ºC):  30 lbf/inch (5.3 kN/m) (ASTM D 5147)

g)	Peak Load (avg) @ 0ºF (-18ºC):  75 lbf/inch (13.2 kN/m) (ASTM D 5147)

h)	Ultimate Elongation (avg.) @ 73ºF (23ºC):  50%  (ASTM D 5147)

i)	Dimensional Stability (max):  0.1%  (ASTM D 5147)

j)	Compound Stability (min - sheet):  250ºF (121ºC)  (ASTM D 5147)

k)	Compound Stability (min – adhesive coating):  212ºF (100ºC)  (ASTM D 5147)

l)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

m)	Reinforcement:  fiberglass mat or other meeting the performance and dimensional stability criteria

n)	Back Surfacing:  polyolefin release film

o)	Top Surfacing:  factory applied acrylic coating

>	Paradiene 20 SA P by Siplast; Irving, TX

3.	Resin for Field Membrane Construction:  A flexible, polymethylmethacrylate (PMMA) based resin for use in combination with fleece fabric to form a monolithic, reinforced roofing membrane.

a)	Thickness (avg):  90 mils (2.3 mm) at 0.31 kg/ft² (3.3 kg/m²) coverage rate (ASTM D 5147, section 5). The values listed below are based upon a 90 mil (2.3 mm) resin thickness.

b)	Weight (min per 100 ft² of coverage):  68.4 lb (3.3 kg/m²)

c)	Peak Load (avg) @ 73°F (23ºC):  70 lbf/in (12.3 kN/m)  (ASTM D 5147 section 6)

d)	Peak Load (avg) @ 73°F (23ºC):  90 lbf/inch (15.8 kN/m)  (ASTM D 412, dumbbell)

e)	Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D 5147, section 6)

f)	Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D 412, dumbbell)

g)	Shore A Hardness (avg): 81 (ASTM D 2240)

h)	Water Absorption, Method I (24h @ 73°F):  0.8% (ASTM D 570)

i)	Water Absorption, Method II (48h @ 122°F):  1.2% (ASTM D 570)

j)	Low temperature flexibility @ 23 F (-5°C):  PASS (ASTM D 5147, section 11)

k)	Dimensional Stability (max):  0.15% (ASTM D 5147, section 10)

l)	Tear Strength (avg):  90 lbf (0.4 kN) (ASTM D 5147, section 7)

m)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

>	Parapro Roof Resin by Siplast; Irving, TX

4.	Fleece for Membrane Reinforcement:  A non-woven, 110 g/m², needle-punched polyester fabric reinforcement as supplied by the membrane system manufacturer.

>	Pro Fleece by Siplast; Irving, TX

C.	Roofing Membrane Assembly:  A roof membrane assembly consisting of one ply of a prefabricated, reinforced, homogeneous Styrene-Butadiene-Styrene (SBS) block copolymer modified asphalt membrane applied over a prepared substrate, covered with a liquid applied, flexible, polymethylmethacrylate (PMMA) based monolithic membrane formed by the combination of liquid PMMA resin and fleece fabric.  The reinforcement mats in the SBS ply shall be impregnated/saturated and coated each side with an SBS modified bitumen blend.  The cross sectional area of the SBS sheet material shall contain no oxidized or non-SBS modified bitumen.  The back of the modified bitumen base ply shall be coated with factory applied polymer modified asphalt self-adhesive coating covered with a removable film.  The top surface of the modified bitumen ply sheet shall be coated with a white acrylic coating to enhance resin bond and to minimize surface temperatures.  The composite roof system, including SBS modified bitumen ply sheet and reinforced PMMA, shall pass 500 cycles of ASTM D 5849 Resistance to Cyclic Joint Displacement (fatigue) at 14F (-10C).  Passing results shall show no signs of membrane cracking or interply delamination after 500 cycles.  The roof system shall pass 200 cycles of ASTM D 5849 after heat conditioning performed in accordance with ASTM D 5147.

>	Siplast Parapro Roof System with Paradiene 20 SA P base ply

1.	Self-Adhesive Modified Bitumen Ply and Flashing Reinforcing Sheet

a)	Thickness (avg):  102 mils (2.6 mm)  (ASTM D 5147)

b)	Thickness (min):  98 mils (2.5 mm)  (ASTM D 5147)

c)	Weight (min per 100 ft² of coverage):  69 lb (3.4 kg/m²)

d)	Maximum filler content in elastomeric blend:  35% by weight

e)	Low temperature flexibility @ -15º F (-26º C) - PASS  (ASTM D 5147)

f)	Peak Load (avg) @ 73ºF (23ºC):  30 lbf/inch (5.3 kN/m) (ASTM D 5147)

g)	Peak Load (avg) @ 0ºF (-18ºC):  75 lbf/inch (13.2 kN/m) (ASTM D 5147)

h)	Ultimate Elongation (avg.) @ 73ºF (23ºC):  50%  (ASTM D 5147)

i)	Dimensional Stability (max):  0.1%  (ASTM D 5147)

j)	Compound Stability (min - sheet):  250ºF (121ºC)  (ASTM D 5147)

k)	Compound Stability (min – adhesive coating):  212ºF (100ºC)  (ASTM D 5147)

l)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

m)	Reinforcement:  fiberglass mat or other meeting the performance and dimensional stability criteria

n)	Back Surfacing:  polyolefin release film

o)	Top Surfacing:  factory applied acrylic coating

>	Paradiene 20 SA P by Siplast; Irving, TX

2.	Self-Adhesive Modified Bitumen Flashing Reinforcing Sheet

a)	Thickness (avg):  102 mils (2.6 mm)  (ASTM D 5147)

b)	Thickness (min):  98 mils (2.5 mm)  (ASTM D 5147)

c)	Weight (min per 100 ft² of coverage):  69 lb (3.4 kg/m²)

d)	Maximum filler content in elastomeric blend:  35% by weight

e)	Low temperature flexibility @ -15º F (-26º C) - PASS  (ASTM D 5147)

f)	Peak Load (avg) @ 73ºF (23ºC):  30 lbf/inch (5.3 kN/m) (ASTM D 5147)

g)	Peak Load (avg) @ 0ºF (-18ºC):  75 lbf/inch (13.2 kN/m) (ASTM D 5147)

h)	Ultimate Elongation (avg.) @ 73ºF (23ºC):  50%  (ASTM D 5147)

i)	Dimensional Stability (max):  0.1%  (ASTM D 5147)

j)	Compound Stability (min - sheet):  250ºF (121ºC)  (ASTM D 5147)

k)	Compound Stability (min – adhesive coating):  212ºF (100ºC)  (ASTM D 5147)

l)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

m)	Reinforcement:  fiberglass mat or other meeting the performance and dimensional stability criteria

n)	Back Surfacing:  polyolefin release film

o)	Top Surfacing:  factory applied acrylic coating

>	Paradiene 20 SA P by Siplast; Irving, TX

3.	Resin for Field Membrane Construction:  A flexible, polymethylmethacrylate (PMMA) based resin for use in combination with fleece fabric to form a monolithic, reinforced roofing membrane.

a)	Thickness (avg):  90 mils (2.3 mm) at 0.31 kg/ft² (3.3 kg/m²) coverage rate (ASTM D 5147, section 5). The values listed below are based upon a 90 mil (2.3 mm) resin thickness.

b)	Weight (min per 100 ft² of coverage):  68.4 lb (3.3 kg/m²)

c)	Peak Load (avg) @ 73°F (23ºC):  70 lbf/in (12.3 kN/m)  (ASTM D 5147 section 6)

d)	Peak Load (avg) @ 73°F (23ºC):  90 lbf/inch (15.8 kN/m)  (ASTM D 412, dumbbell)

e)	Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D 5147, section 6)

f)	Elongation at Peak Load (avg) @ 73°F:  35% (ASTM D 412, dumbbell)

g)	Shore A Hardness (avg): 81 (ASTM D 2240)

h)	Water Absorption, Method I (24h @ 73°F):  0.8% (ASTM D 570)

i)	Water Absorption, Method II (48h @ 122°F):  1.2% (ASTM D 570)

j)	Low temperature flexibility @ 23 F (-5°C):  PASS (ASTM D 5147, section 11)

k)	Dimensional Stability (max):  0.15% (ASTM D 5147, section 10)

l)	Tear Strength (avg):  90 lbf (0.4 kN) (ASTM D 5147, section 7)

m)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

>	Parapro Roof Resin by Siplast; Irving, TX

4.	Fleece for Membrane Reinforcement:  A non-woven, 110 g/m², needle-punched polyester fabric reinforcement as supplied by the membrane system manufacturer.

>	Pro Fleece by Siplast; Irving, TX

B.	Flashing Membrane Assembly:  A flashing membrane assembly consisting of a liquid applied, flexible, polymethylmethacrylate (PMMA) based monolithic membrane formed by the combination of liquid PMMA-based resin and fleece fabric.

>	Siplast Parapro Waterproofing System

1.	Resin for Flashing Applications:  A flexible, polymethylmethacrylate (PMMA) based resin combined with a thixotropic agent for use in combination with non-woven, 110 g/m², needle-punched polyester fabric reinforcement to form a monolithic, reinforced flashing membrane.

>	Parapro 123 Flashing Resin by Siplast; Irving, TX

2.	Fleece for Flashing Reinforcement:  A non-woven, 110 g/m², needle-punched polyester fabric reinforcement as supplied by the membrane system manufacturer.

>	Pro Fleece by Siplast; Irving, TX

PART 3 EXECUTION

3.01  SUBSTRATE EXAMINATION/PREPARATION

*  NOTE:	Rigid insulation and installation methods should be covered in a separate specification section.  See the Siplast Rigid Insulation and Base Sheet Usage Guide section of the Siplast Engineered Roofing Systems Manual for information regarding approved rigid insulation and applicable installation methods.

A.	General:  Ensure that substrates are free from gross irregularities, loose, unsound or foreign material such as dirt, ice, snow, water, grease, oil, bituminous products, release agents, laitance, paint, loose particles/friable matter, rust or any other material that would be detrimental to adhesion of the catalyzed primer and/or resin to the substrate.  Some surfaces may require scarification, shotblasting, or grinding to achieve a suitable substrate.  Wipe surfaces with a clean cloth saturated with the specified cleaner/solvent to remove grease, oils or dust that may affect adhesion and to cured PMMA surfaces to receive a subsequent coat of resin.

B.	Concrete Substrate Requirements:  Structural concrete shall be cured a minimum of 28 days in accordance with ACI-308, have a minimum compressive strength of 3,500 psi (24 N/mm2) and have a moisture content that conforms with the waterproofing system manufacturer’s requirements prior to commencement of work.

*  NOTE:	The Contractor must carefully verify the suitability of a concrete substrate.  High moisture content or a substandard surface condition may result in inadequate adhesion of the roofing system.

*  NOTE:	Lightweight structural concrete or concrete that does not offer bottom-side venting is not a suitable substrate for direct application of the roofing system materials.  Contact Siplast for information on applicability and/or recommended treatment of lightweight structural concrete or concrete that does not provide bottom-side venting.  The presence of an underlying slotted metal deck or drainage mat does not constitute bottom-side venting.

*  NOTE:	Curing compounds containing waxes, oils, silicones or other materials that may inhibit adhesion of the waterproofing system should not be used.

C.	Moisture Content Evaluation:  Evaluate the level of moisture in the substrate to determine that the moisture content is acceptable for application of the specified waterproofing system.  Concrete substrates shall have a maximum moisture content of 6% by weight and a maximum internal relative humidity of 75%.

D.	Adhesion Testing for Concrete Substrates to Receive Resin Materials:  Test the concrete substrate using a device conforming to ASTM D 4541 using a 50 mm dolly adhered with the specified catalyzed primer.  Utilize the same concrete preparation methods as that which will be used prior to application of the roofing for areas to be evaluated for adhesion.  Ensure that a minimum adhesion value of 220 psi is obtained before application of the PMMA primer.  If multiple areas or substrates are involved in the scope of work, evaluate each to determine suitability.  Maintain testing/evaluation records.

E.	Preparation of Newly Placed Concrete Substrates to Receive a Direct Application of Resin Materials:  Newly placed concrete shall be cured a minimum of 28 days in accordance with ACI-308, and have a minimum compressive strength of 3,500 psi (24 N/mm2).  Following evaluation for moisture content and confirmation that the moisture content is at a acceptable level, shot-blast or scarify/shot blast the surface to provide a sound substrate free from laitance and to generate a concrete surface profile of CSP-2 to CSP-4 as defined by the ICRI.  Grinding may be used as a preparation method for localized areas that cannot be reached by a shot blasting equipment provided that a surface profile of CSP-2 to CSP 4 can be generated.  Repair spalls and voids on vertical or horizontal surfaces using the specified primer and preparation paste.

F.	Preparation of Existing Concrete/Masonry Substrates to Receive a Direct Application of Resin Materials:  Existing concrete substrates shall have a minimum compressive strength of 3,500 psi (24 N/mm2).  Following evaluation for moisture content and confirmation that the moisture content is at an acceptable level, shot blast or scarify/shot-blast concrete or masonry surfaces to provide a sound substrate free from laitance and residue from bitumen, coal tar, primer, coatings, adhesives, sealer or any material that may inhibit adhesion of the specified primer.  Generate a concrete surface profile of CSP-2 to CSP-4 as defined by the ICRI.  Grinding may be used as a preparation method for localized areas that cannot be reached by a shot blasting equipment provided that a surface can be prepared to a CSP-2 to CSP 4.  Repair spalls and voids on vertical or horizontal surfaces using the specified primer and preparation paste.

G.	Preparation of Concrete Substrates to Modified Bitumen Base Ply:  Poured reinforced concrete shall be cured a minimum of 28 days in accordance with ACI-308, with a minimum compressive strength of 3,500 psi (24 N/mm2).  Concrete decks shall be fully cured, dry, frost-free, broom-cleaned, free from release/curing agents and smooth enough to allow for full adhesion of the ply sheet.  Ensure that the moisture content is at a level suitable for proper application of the primer and roofing system components.  Level projections or depressions that may interfere with proper application of roofing system components.  Prime the deck with the specified asphalt primer at the rate of 1 gallon per 100-400 square feet and allow to dry thoroughly.

H.	Repair and Leveling of Concrete Substrate to Receive Resin Materials:  Before application of the roofing membrane, and after priming, fill all joints, cracks, voids, fractures, depressions, small indentations, and low areas in the substrate using the specified paste or repair mortar.

I.	Static Crack and Cold Joint Preparation:  Clean cracks/joints and treat with the specified PMMA primer.  Fill the cracks and joints using the specified preparation paste prior to membrane/flashing application.

*  NOTE:	Contact Siplast for specific information regarding crack evaluation and treatment.

J.	"Self-Adhered" Ply Sheet Application:  Unroll the base ply, and set the roll into place utilizing minimum 3 inch side and end laps.  Fold one end of the roll back onto itself by 24 inches.  Peel the release film off of the back of the 24 inch end section of the sheet and lay into place, pressing the 24 inch end section of the sheet firmly into place over the substrate.  Pull the release film free from the underside of the remainder of the sheet while pressing the material into place with a follow tool as the film is being removed, leaving the end laps unadhered.  Prior to adhering the end laps, cut a dog ear angle at each end lap on overlapping selvage edges.  Torch seal or heat weld end laps, ensuring that the self-adhesive blend on the underside of the overlapping sheet and the top surface of the underlying sheet flow into a layer of continuously bonded or fused modified bitumen.  Using a clean trowel, apply top pressure to top seal T-laps immediately following sheet application.  Stagger end laps a minimum of 3 feet.  Laps of the base ply shall not be left exposed overnight.  The base ply application shall be immediately followed by the application of the finish ply.  A phased application between the base and finish plies is not approved.  In cases where rapid onset of inclement weather occurs, seal exposed lap edges with a torch or hot-air welder and trowel.

K.	Torch-Applied Ply Sheet Application:  Bond the modified bitumen ply sheet to the prepared substrate, utilizing minimum 3 inch side and end laps.  Apply each sheet directly behind the torch applicator.  Cut a dog ear angle at the end laps on overlapping selvage edges.  Using a clean trowel, apply pressure to top seal T-laps immediately following sheet application.  Stagger end laps a minimum of 3 feet.  Follow manufacturer’s specifications regarding maximum exposure periods prior to application of the liquid-applied finish membrane.

L.	Preparation of Steel/Aluminum Substrates:  Grind to generate a "white-metal" surface and remove loose particles.  Extend preparation area a minimum of 1/2-inch (13 mm) beyond the termination of the roofing/flashing system.  Notch steel surfaces to provide a rust-stop where detailed.

*  NOTE:	Consider the use of primer and paint to treat the prepared area not covered with resin to prevent corrosion of steel surfaces.

M.	Rigid Plastic Flashing Substrates:  Evaluate the plastic for compatibility with the resin materials.  Lightly abrade the surface to receive the flashing system, clean plastic substrates using the specified the cleaner/solvent and allow to dry.  Extend the preparation area a minimum of 1/2 inch (13 mm) beyond the termination of the flashing system.

N.	Preparation of Wood/Plywood Flashing Substrates to receive Resin:  Tape the joints between plywood or wood panels using the specified tape and prime wood/plywood surfaces to receive the specified flashing system with the specified PMMA-based primer and allow primer to set prior to application of the flashing system.

3.02  MIXING OF RESIN PRODUCTS

A.	Preparation/Mixing/Catalyzing Resin Products:  Pour the desired quantity of resin into a clean container and using a spiral mixer or mixing paddle, stir the liquid for the time period specified by the resin manufacturer.  Calculate the amount of catalyst powder needed using the manufacturer's guidelines and add the pre-measured catalyst to the resin component.  Mix again for the time period specified by the resin manufacturer, ensuring that the product is free from swirls and bubbles.  Ensure that air is not entrained into the product during the mixing process.  To avoid aeration, do not use a spiral mixer unless the spiral section of the mixer can be fully contained in the liquid during the mixing process.  Mix only enough product to ensure that it can be applied before expiration of resin pot life.

B.	Preparation/Mixing/Catalyzing Aggregate-Filled Resin Products:  Pour the entire desired quantity of resin into a clean container and slowly add the pre-measured quantity of aggregate using a spiral mixer or mixing paddle, stirring the mixture for the time period specified by the resin manufacturer.  If catalyst is not a component of the aggregate mixture, calculate the amount of catalyst powder needed using the manufacturer's guidelines and add the pre-measured catalyst to the resin/aggregate mixture.  Mix again for the time period specified by the resin manufacturer, ensuring that the product is free from swirls and bubbles.  Ensure that air is not entrained into the product during the mixing process.  To avoid aeration, do not use a spiral mixer unless the spiral section of the mixer can be fully contained in the liquid during the mixing process.  Mix only enough product to ensure that it can be applied before expiration of resin pot life.

3.03  PREPARATION PASTE AND PRIMER MIXING/APPLICATION

A.	Primer Application:  Apply primer resin using a roller or brush at the minimum rate specified by the primer manufacturer over prepared substrates.  Apply primer resin at the increased rate specified by the primer manufacturer over DensDeck and DensDeck Prime.  Increase application rates over other absorbent substrates.  Do not let resin pool or pond.  Do not under-apply or over-apply primers as this may interfere with proper primer catalyzation.  Make allowances for saturation of roller covers and application equipment.

B.	Paste Application:  Allow the primer to set and apply catalyzed preparation paste using a trowel.  Before application of resin over the catalyzed paste surface, the specified cleaner/solvent, wipe the surface of the paste using the specified cleaner/solvent and allow to dry.  Treat the surface again if not followed up by resin application within 60 minutes.

3.04  FLASHING AND FIELD MEMBRANE APPLICATION

A.	Base Flashing Application

1.	Using masking tape, mask the perimeter of the area to receive the flashing system.  Apply resin primer to substrates requiring additional preparation and allow primer to set.

2.	Pre-cut fleece to ensure a proper fit at transitions and corners prior to membrane application.

3.	Apply an even, generous base coat of flashing resin using a roller at the minimum rate specified by the resin manufacturer to prepared surfaces requiring flashing coverage.  Work the fleece into the wet, catalyzed resin using a brush or roller to fully embed the fleece in the resin and remove trapped air.  Lap fleece layers a minimum of 2 inch (5 cm) and apply an additional coat of catalyzed resin between layers of overlapping fleece.  Again using a roller, apply an even top coat of catalyzed resin at the minimum rate specified by the resin manufacturer immediately following embedment of the fleece, ensuring full saturation of the fleece.  Ensure that the flashing resin is applied to extend beyond the fleece (maximum 0.25 inch (6 mm)). Remove the tape before the catalyzed resin sets.  Make allowances for saturation of roller covers and application equipment.

4.	Should work be interrupted for more than 12 hours or the surface of the catalyzed resin becomes dirty or contaminated by the elements, wipe the surface to be lapped with new flashing resin using the specified cleaner/solvent.  Allow the surface to dry for a minimum 20 minutes and a maximum 60 minutes before continuing work.

B.	Field Membrane Application

1.	Using the specified cleaner/solvent, wipe flashing membrane surfaces to be lapped with field membrane.  Allow the surface to dry for a minimum 20 minutes before continuing work.

2.	Apply an even, generous base coat of field membrane resin using a roller at the minimum rate specified by the resin manufacturer to prepared surfaces.  Work the fleece into the wet, catalyzed resin using a roller to fully embed the fleece in the resin and remove trapped air.  Lap fleece layers a minimum of 2 inch (5 cm) and apply an additional coat of catalyzed resin between layers of overlapping fleece.  Again using a roller, apply an even top coat of catalyzed resin at the minimum rate specified by the resin manufacturer immediately following embedment of the fleece, ensuring full saturation of the fleece.  Make allowances for saturation of roller covers and application equipment.  Allow 2 hours cure time prior to exposing the membrane to foot traffic.

C.	Color Finish Application

1.	Ensure that the  flashing membrane and has been in place for a minimum 2 hours.  Using the specified cleaner/solvent, wipe membrane surfaces to receive the color finish layer.  Allow the surface to dry for a minimum 20 minutes before continuing work.

2.	Apply an even top coat of catalyzed color finish resin at the minimum rate specified by the resin manufacturer.  Allow 2 hours cure time prior to exposing the membrane to foot traffic.

3.05  FIELD QUALITY CONTROL AND INSPECTIONS

A.	Site Condition:  Leave all areas around job site free of debris, roofing materials, equipment and related items after completion of job.

B.	Notification Of Completion:  Notify the manufacturer by means of manufacturer's printed Notification of Completion form of job completion in order to schedule a final inspection date.

C.	Water Test:  Prior to the application of the overburden plug the drains and scuppers, and flood the waterproofing surface with water a minimum of 1 to 2 inches deep.  Leave the water for a minimum of 24 hours to ensure the system is leak free.

* NOTE:	Precautions must be taken to determine if the structure can hold the weight of the water for the duration of the test.

D.	Final Inspection

* NOTE:	The roof membrane system must be inspected by the manufacturer's representative prior to installation of the overburden system.  The manufacturer's representative will compile required punch list items indicating any deficiencies in the roof membrane and flashing membrane system that shall be corrected before the installation will be accepted.

1.	Post-Installation Meeting:  Hold a meeting at the completion of the project, attended by all parties that were present at the pre-job conference.  A punch list of items required for completion shall be compiled by the Contractor and the manufacturer's representative.  Complete, sign, and mail the punch list form to the manufacturer's headquarters.

E.	Issuance Of The Guarantee:  Complete all post installation procedures and meet the manufacturer's final endorsement for issuance of the specified guarantee.