GUIDE SPECIFICATION

Paradiene 20/30 FR Roof System

PA-311 Adhesive & PA-100 Asphalt Applications

Prepared by:

Siplast, Inc.

1000 East Rochelle Boulevard

Irving, Texas 75062

(800) 922-8800

Please see the Siplast Technical Guide or contact Siplast Technical Support for further information regarding slope limitations and specific application requirements for Paradiene 20/30 FR roof systems.

This specification is provided as a general guide for use of Siplast products based on typical building conditions and standard roofing practices.  Siplast is strictly a manufacturer of roofing systems and has no experience, training or expertise in the areas of architecture/engineering or in the area of consulting with respect to matters related to such areas.  Siplast recommends that the Owner's representative independently verify the accuracy and appropriateness of a specification provided for a specific project.

January 6, 2003

SECTION 07550   MODIFIED BITUMEN MEMBRANE ROOFING   (Rev 01/06/2003)

PART 1  GENERAL

1.01  SECTION INCLUDES

A.	Base Sheet Application

B.	Roof Membrane Application

C.	Roof Flashing Application

1.02  RELATED SECTIONS

A.	Section [-----] - Submittals

B.	Section [-----] - Rough Carpentry

C.	Section [-----] - Roof Decks

D.	Section 07220 - Lightweight Insulating Concrete Roof Insulation

*  NOTE:	See the Siplast Engineering Design Manual for information regarding lightweight insulating concrete and applicable installation methods.

E.	Section [-----] - Rigid Roof Insulation

*  NOTE:	See the Siplast Insulation Guide section of the Siplast Engineered Roofing Systems Manual for information regarding approved rigid insulation and applicable installation methods.

F.	Section [-----] - Sheet Metal Flashing Components And Roofing Accessories

G.	Section [-----] - Sheet Metal Flashing and Trim

H.	Section [-----] - Sheet Metal Roofing Specialties

I.	Section [-----] - Temporary Roofs/Vapor Retarders*

*  NOTE:	A vapor retarder can be an important component in roof systems where climatic and building interior conditions require the prevention of vapor condensation within the roof assembly.

1.03  REFERENCE STANDARDS

References in these specifications to standards, test methods, codes etc., are implied to mean the latest edition of each such standard adopted.  The following is an abbreviated list of associations, institutions, and societies which may be used as references throughout these specifications.

ASTM	American Society for Testing and Materials

Philadelphia, PA

FM	Factory Mutual Engineering and Research

Norwood, MA

NRCA	National Roofing Contractors Association

Rosemont, IL

OSHA	Occupational Safety and Health Administration

Washington, DC

SMACNA	Sheet Metal and Air Conditioning Contractors National Association

Chantilly, VA

UL	Underwriters Laboratories

Northbrook, IL

1.04  SUBMITTALS

All submittals which do not conform to the following requirements will be rejected.

*  NOTE:	Coordinate submittal requirements with general provisions.  Modify submittals to suit specific project requirements.

A.	Submittals Prior to Contract Award:

1.	Letter from the proposed primary roofing manufacturer confirming that the bidder is an acceptable Contractor authorized to install the proposed system.

2.	Letter from the primary roofing manufacturer stating that the proposed application will comply with the Manufacturer's requirements in order to qualify the project for the specified guarantee.

1.05  QUALITY ASSURANCE

A.	Acceptable Products:  Provide primary roofing products, including each type of sheet, all manufactured in the United States, supplied by a single manufacturer which has been successfully producing the specified types of primary products for not less than 10 years.  Provide secondary or accessory products which are acceptable to the manufacturer of the primary roofing products.

*  NOTE:	Coordinate the desired fire and windstorm rating with the Underwriters Laboratories Roofing Materials and Systems Directory and the Factory Mutual System Approval Guide.

B.	Product Quality Assurance Program:  Primary roofing materials shall be manufactured under a quality management system that is monitored regularly by a third party auditor under the ISO 9001:2000 audit process.  A certificate of analysis for reporting/confirming the tested values of the actual material being supplied for the project will be required prior to project close-out.

C.	Agency Approvals:  The proposed roof system shall conform to the following requirements.  No other testing agency approvals will be accepted.

1.	Underwriters Laboratories Class [-----] acceptance of the proposed roofing system (including mopping asphalt or cold adhesive) without additional requirements for gravel or coatings.

2.	Factory Mutual Approval Standard 4470 listing for the proposed membrane system.  The roof membrane configuration shall be approved by FM for Class 1-SH (severe hail) exposure.  The roof configuration (including fastening of base sheet, insulation, etc.) shall be approved by FM for minimum 1-[----] wind uplift construction.

D.	Project Acceptance:  Submit a completed manufacturer's application for roof guarantee form along with shop drawings of the roofs showing all dimensions, penetrations, and details.  The form shall contain all the technical information applicable to the project including deck types, roof slopes, base sheet and/or insulation assemblies (with method of attachment, and fastener type), and manufacturer's membrane assembly proposed for installation.  The form shall also contain accurate and complete information requested including proper names, addresses, zip codes and telephone numbers.  The project must receive approval, through this process, prior to shipment of materials to the project site.

E.	Scope of Work:  The work to be performed under this specification shall include but is not limited to the following:  Attend necessary job meetings and furnish competent and full time supervision, experienced roof mechanics, all materials, tools, and equipment necessary to complete, in an acceptable manner, the roof installation in accordance with this specification.  Comply with the latest written application instructions of the manufacturer of the primary roofing products.  In addition, application practice shall comply with requirements and recommendations contained in the latest edition of the Handbook of Accepted Roofing Knowledge (HARK) as published by the National Roofing Contractor's Association, amended to include the acceptance of a phased roof system installation.

F.	Local Regulations:  Conform to regulations of public agencies, including any specific requirements of the city and/or state of jurisdiction.

G.	Manufacturer Requirements:  The primary roofing materials manufacturer shall provide direct trained company personnel to attend necessary job meetings, perform periodic inspections as necessary, and conduct a final inspection upon successful completion of the project.

1.06  PRODUCT DELIVERY STORAGE AND HANDLING

A.	Delivery:  Deliver materials in the manufacturer's original sealed and labeled containers and in quantities required to allow continuity of application.

B.	Storage:  Store materials out of direct exposure to the elements.  Store roll goods on a clean, flat and dry surface.  All material stored on the roof overnight shall be stored on pallets.  Rolls of roofing must be stored on ends.  Store materials on the roof in a manner so as to preclude overloading of deck and building structure.  Store materials such as solvents, adhesives and asphalt cutback products away from open flames, sparks or excessive heat.  Cover all material using a breathable cover such as a canvas.  Polyethylene or other non-breathable plastic coverings are not acceptable.

C.	Handling:  Handle all materials in such a manner as to preclude damage and contamination with moisture or foreign matter.  Handle rolled goods to prevent damage to edges or ends.

D.	Damaged Material:  Any materials that are found to be damaged or stored in any manner other than stated above will be automatically rejected, removed and replaced at the Contractor's expense.

1.07  PROJECT/SITE CONDITIONS

A.	Requirements Prior to Job Start

1.	Notification:  Give a minimum of 5 days notice to the Owner and manufacturer prior to commencing any work and notify both parties on a daily basis of any change in work schedule.

2.	Safety:  Familiarize every member of the application crew with all fire and safety regulations recommended by OSHA, NRCA and other industry or local governmental groups.

B.	Environmental Requirements

1.	Precipitation:  Do not apply roofing materials during precipitation or in the event there is a probability of precipitation during application.  Take adequate precautions to ensure that materials, applied roofing, and building interiors are protected from possible moisture damage or contamination.

2.	Temperature Restrictions - asphalt:  At ambient temperatures of 40(F (4(C) and below, special precautions must be taken to ensure that the specified Type IV asphalt maintains a minimum acceptable 400(F (204(C) at the point of sheet application.  The asphalt must not be overheated to compensate for cold conditions.  The use of insulated handling equipment is strongly recommended.  Hot luggers, mop carts, and kettle-to-roof supply lines should be insulated.  Hand mops should be constructed with a smaller yarn head to facilitate short moppings.  Luggers and mop carts should never be more than half filled at all times.

3.	Temperature Restrictions - cold adhesive:  At low temperatures, the specified cold adhesive becomes more viscous, making even distribution more difficult. The optimal temperature of the adhesive at point of application is 70(F (21(C).  To facilitate application when ambient temperatures are below 50(F (10(C), store the adhesive and roll goods in a warm place immediately prior to use.  Roll or broom the sheets to ensure contact with the underlying adhesive.  Suspend application in situations where the adhesive cannot be kept at temperatures allowing for even distribution.

C.	Protection Requirements

1.	Membrane Protection:  Provide protection against staining and mechanical damage for newly applied roofing and adjacent surfaces throughout this project.

2.	Torch Safety:  Designate one person on each crew to perform a daily fire watch.  The designated crew member shall watch for fires or smoldering materials on all areas of roof construction  Continue the fire watch after roofing material application has been suspended for the day.

3.	Debris Removal:  Remove all debris daily from the project site and take to a legal dumping area authorized to receive such materials.

4.	Site Condition:  Complete, to the owner's satisfaction, all job site clean-up including building interior, exterior and landscaping where affected by the construction.

1.08  GUARANTEE

A.	Roof Membrane Guarantee:  Upon successful completion of the project, and after all post installation procedures have been completed, furnish the Owner with the manufacturer's ten year labor and materials membrane guarantee.  The guarantee shall be a term type, without deductibles or limitations on coverage amount, and shall be issued at no additional cost to the Owner.  This guarantee shall not exclude random areas of ponding from coverage.

>	Siplast ten year Roof Membrane Guarantee

PART 2  PRODUCTS

2.01  ROOFING SYSTEM ASSEMBLY/PRODUCTS

NOTE:	Rigid insulation and installation methods should be covered in a separate specification section.  See the Siplast Rigid Insulation and Base Sheet Usage Guide section of the Siplast Engineered Roofing Systems Manual for information regarding approved rigid insulation and applicable installation methods.

A.	Base Sheet

NOTE:	Select a specific base sheet to meet individual project requirements.  Contact Siplast for further information regarding approved base sheets.

1.	Sheathing Paper:  A rosin coated building paper used as the underlayment for base sheets conforming to ASTM D 549.

2.	Base Sheet:  A fiberglass reinforced, specially oxidized asphalt coated sheet, having an minimum weight of 85 lb/sq.

>	Siplast Irex 40

3.	Base Sheet:  A fiberglass scrim/fiberglass mat reinforced, specially oxidized asphalt coated sheet, having an minimum weight of 85 lb/sq.

>	Siplast Irex HT

4.	Modified Base Sheet:  A fiberglass reinforced, Styrene-Butadiene-Styrene (SBS) modified asphalt coated sheet having a minimum weight of 30 lb/sq.

>	Siplast Parabase Plus

5.	Base Sheet:  A fiberglass reinforced, asphalt coated sheet with a polyolefin film backing, having a minimum weight of 20 lb/sq.  The sheet shall conform to ASTM D 4601, Type II requirements.

>	Siplast Parabase FS

6.	Venting Base Sheet:  A fiberglass reinforced, asphalt coated sheet with a polyolefin film backing, having a minimum weight 20 lb/sq.  The sheet shall have 1 1/2 inch perforations on 5 inch centers through the field of the sheet to provide bonding of the roof system to the substrate only through the perforations.

>	Paravent FS

2.02  DESCRIPTION OF SYSTEMS

A.	Roofing Membrane Assembly:  A roof membrane assembly consisting of two plies of a prefabricated, reinforced, homogeneous Styrene-Butadiene-Styrene (SBS) block copolymer modified asphalt membrane, applied over a prepared substrate.  Both reinforcement mats shall be impregnated/saturated and coated each side with an SBS modified bitumen blend.  The roof system shall pass 500 cycles of ASTM D 5849 Resistance to Cyclic Joint Displacement (fatigue) at 14(F (-10(C).  Passing results shall show no signs of membrane cracking or interply delamination after 500 cycles.  The roof system shall pass 200 cycles of ASTM D 5849 after heat conditioning performed in accordance with ASTM D 5147.  The assembly shall possess waterproofing capability, such that a phased roof application, with only the modified bitumen base ply in place, can be achieved for prolonged periods of time without detriment to the watertight integrity of the entire roof system.

>	Siplast Paradiene 20/30 FR roof system

1.	Modified Bitumen Base and Stripping Ply

a)	Thickness (avg):  91 mils (2.3 mm)  (ASTM D 5147)

b)	Thickness (min):  87 mils (2.2 mm)  (ASTM D 5147)

c)	Weight (min per 100 ft² of coverage):  62 lb (3.0 kg/m²)

d)	Maximum filler content in elastomeric blend - 35% by weight

e)	Low temperature flexibility @ -13F (-25C):  PASS  (ASTM D 5147)

f)	Maximum Load (avg) @ 73F (23C):  30 lbf/inch (5.3 kN/m) (ASTM D 5147)

g)	Maximum Load (avg) @ 0F (-18C):  70 lbf/inch (12.3 kN/m) (ASTM D 5147)

h)	Elongation @ 5% Maximum Load (avg.) @ 73F (23C):  50%  (ASTM D 5147)

i)	Dimensional Stability (max):  0.1%  (ASTM D 5147)

j)	High Temperature Stability (min):  250F (121C)  (ASTM D 5147)

k)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

l)	Reinforcement:  fiberglass mat or other meeting the performance and dimensional stability criteria

>	Siplast Paradiene 20

2.	Modified Bitumen Finish Ply

a)	Thickness  (avg):  130 mils (3.3 mm)  (ASTM D 5147)

b)	Thickness at selvage (coating thickness) (avg):  98 mils (2.5 mm)  (ASTM D 5147)

c)	Thickness at selvage (coating thickness) (min):  94 mils (2.4 mm)  (ASTM D 5147)

d)	Weight (min per 100 ft² of coverage):  90 lb (4.4 kg/m²)

e)	Maximum filler content in elastomeric blend:  35% by weight

f)	Low temperature flexibility @ -13 F (-25 C):  PASS  (ASTM D 5147)

g)	Maximum Load (avg) @ 73F (23C):  30 lbf/inch (5.3 kN/m) (ASTM D 5147)

h)	Maximum Load (avg) @ 0F (-18C):  75 lbf/inch (13.2 kN/m)  (ASTM D 5147)

i)	Elongation @ 5% Maximum Load (avg.) @ 73F (23C):  55%  (ASTM D 5147)

j)	Dimensional Stability (max):  0.1%  (ASTM D 5147)

k)	High Temperature Stability (min):  250F (121 C)  (ASTM D 5147)

l)	Granule Embedment (max loss):  2.0 grams per sample  (ASTM D 5147)

m)	Approvals:  UL Class listed, FM Approved (products shall bear seals of approval)

n)	Reinforcement:  fiberglass mat or other meeting the performance and dimensional stability criteria

o)	Surfacing:  ceramic granules

>	Siplast Paradiene 30 FR

*  NOTE:	Pre-select the granule color finish of the Paradiene 30 finish ply.

B.	Flashing Membrane Assembly:  A flashing membrane assembly consisting of a prefabricated, reinforced, Styrene-Butadiene-Styrene (SBS) block copolymer modified asphalt membrane with a continuous, channel-embossed metal-foil surfacing.  The finish ply shall conform to ASTM D 6298 and the following physical and mechanical property requirements.

>	Siplast Veral flashing system, aluminum finish

*  NOTE:	Veral flashing systems are available in aluminum, Spectra™ Polar White, stainless steel and copper foil finishes.  Siplast also offers granule-surfaced flashing systems.  Contact Siplast for more information regarding these products.

1.	Metal-Clad Modified Bitumen Flashing Sheet

a)	Thickness (avg):  142 mils (3.6 mm)  (ASTM D 5147)

b)	Thickness (min):  138 mils (3.5 mm)  (ASTM D 5147)

c)	Weight (min per 100 ft² of coverage):  92 lb (4.5 kg/m²)

d)	Coating Thickness – back surface (min):  40 mils (1 mm)  (ASTM D 5147)

e)	Maximum filler content in elastomeric blend:  35% by weight

f)	Low temperature flexibility @ 0 F (-18 C):  PASS  (ASTM D 5147)

g)	Maximum Load (avg) @ 73F (23C):  85 lbf/inch (15 kN/m)  (ASTM D 5147)

h)	Maximum Load (avg) @ 0F (-18C):  180 lbf/inch (31.7 kN/m)  (ASTM D 5147)

i)	Elongation @ 5% Maximum Load (avg) @ 73F (23C):  45%  (ASTM D 5147)

i)	Tear-Strength (avg):  120 lbf (0.54 kN)  (ASTM D 5147)

j)	Dimensional Stability (max):  0.2%  (ASTM D 5147)

k)	High Temperature Stability (min):  225F (107C)  (ASTM D 5147)

l)	Cyclic Thermal Shock Stability (maximum):  0.2%  (ASTM D 6298)

m)	Approvals:  UL Approved, FM Approved (products shall bear seals of approval)

n)	Reinforcement:  fiberglass scrim mat or other meeting the performance and dimensional stability criteria

o)	Surfacing:  aluminum metal foil

>	Siplast Veral Aluminum

Flashing Reinforcing Ply - (Same as roof system base ply)

2.03  ROOFING ACCESSORIES

A.	Roofing Adhesives

1.	Mopping Asphalt:  Type IV asphalt certified for full compliance with the requirements listed in Table I, ASTM D 312.  Each container or bulk shipping ticket shall indicate the equiviscous temperature, EVT, the finished blowing temperature, FBT, and the flash point, FP.  Mopping asphalt shall be approved in writing by the roof membrane manufacturer.

>	Siplast PA-100 Asphalt by Siplast/Icopal; Irving, TX

2.	Membrane Cold Adhesive:  A blend of special adhesive asphalts and safe, high-flash, quick drying solvents that meets or exceeds ASTM D 4479, Type II requirements.

>	Siplast PA-311 Adhesive by Siplast/Icopal; Irving, TX

B.	Bituminous Cutback Materials

1.	Primer:  A high flash, quick drying, asphalt solvent blend which meets or exceeds ASTM D 41 requirements.

>	Siplast PA-1125 Asphalt Primer by Siplast/Icopal; Irving, TX

2.	Mastics:  An asphalt cutback mastic, reinforced with non-asbestos fibers, used as a base for setting metal flanges conforming to ASTM D 4586 Type II requirements.

>	Siplast PA-1021 Plastic Cement by Siplast/Icopal; Irving, TX

C.	Sealant:  A moisture-curing, non-slump elastomeric sealant designed for roofing applications.  The sealant shall be approved by the roof membrane manufacturer for use in conjunction with the roof membrane materials.  Acceptable types are as follows:

>	Siplast PS-304 Elastomeric Sealant by Siplast/Icopal; Irving, TX

D.	Ceramic Granules:  No. 11 grade specification ceramic granules of color scheme matching the granule surfacing of the finish ply.

E.	Metallic Powder:  A finely graded metal dust as supplied or approved by the membrane manufacturer, used for covering of bitumen overruns over the foil surfaced membrane.

F.	Walktread:  A prefabricated, puncture resistant polyester core reinforced, polymer modified bitumen sheet material topped with a ceramic-coated granule wearing surface.

1.	Thickness: 0.217 in (5.5 mm)

2.	Weight: 1.8 lb/ft² (8.8 kg/m²)

3.	Width: 30 in (76.2 cm)

>	Paratread Roof Protection Material by Siplast / Icopal; Irving, TX

G.	Fasteners

NOTE:	Contact Siplast for further information regarding approved base sheet fasteners for specific substrates.

PART 3 EXECUTION

3.01  PREPARATION

A.	General:  Sweep or vacuum all surfaces, removing all loose aggregate and foreign substances prior to commencement of roofing.

*  NOTE:	Edit this section to address specific job conditions which may affect the scope of work.

3.02  SUBSTRATE PREPARATION

NOTE:	Select a specific base sheet application method to meet individual project requirements.  Contact Siplast for further information regarding base sheet fastening diagrams for field, corner and perimeter zones.

A.	Base Sheet/Rosin Sheet Securement to Prepared Substrate:  Lay the rosin sheet in tandem with the asphalt base sheet over entire area to be roofed, lapping sides 3 inches and ends 6 inches.  Using the specified fasteners, fasten each sheet every 9 inches through laps and stagger fasten the remainder of the sheet in 2 rows on nominal 12 inch centers with fasteners in each row on 12 inch centers.

B.	Base Sheet/Rosin Sheet Securement to Prepared Substrate:  Lay the rosin sheet in tandem with the asphalt base sheet over entire area to be roofed, lapping sides 3 inches and ends 6 inches.  Using the specified fasteners, fasten each sheet every 7 1/2 inches through laps and stagger fasten the remainder of the sheet in 2 rows on nominal 12 inch centers with fasteners in each row on 10 inch centers.

C.	Base Sheet Securement to Prepared Substrate:  Lay the base sheet over entire area to be roofed, lapping sides 3 inches and ends 6 inches.  Using the specified fasteners, fasten each sheet every 9 inches through laps and stagger fasten the remainder of the sheet in 2 rows on nominal 12 inch centers with fasteners in each row on 12 inch centers.

D.	Base Sheet Securement to Prepared Substrate:  Lay the base sheet over entire area to be roofed, lapping sides 3 inches and ends 6 inches.  Using the specified fasteners, fasten each sheet every 7 1/2 inches through laps and stagger fasten the remainder of the sheet in 2 rows on nominal 12 inch centers with fasteners in each row on 10 inch centers.

E.	Venting Base Sheet Application to Prepared Substrate:  Lay the venting base dry over the area to be roofed, lapping sides and ends a maximum of 1 inch.

NOTE:	Rigid insulation and installation methods should be covered in a separate specification section.  See the Siplast Rigid Insulation and Base Sheet Usage Guide section of the Siplast Engineered Roofing Systems Manual for information regarding approved rigid insulation and applicable installation methods.

3.03  ROOF MEMBRANE INSTALLATION

*  NOTE:	This specification is limited to projects having a maximum roof slope of 1/2 inch for hot asphalt applications and maximum roof slope of 2 1/2 inches for cold adhesive and torch applications.  Contact Siplast for specifications to meet higher or lower slope requirements.

A.	Membrane Application:  Apply roofing in accordance with roofing system manufacturer's instructions and the following requirements.  Application of roofing membrane components shall immediately follow application of base sheet and/or insulation as a continuous operation.

B.	Aesthetic Considerations:  An aesthetically pleasing overall appearance of the finished roof application is a standard requirement for this project.  Make necessary preparations, utilize recommended application techniques, apply the specified materials (i.e. granules, metallic powder), and exercise care in ensuring that the finished application is acceptable to the Owner.

C.	Priming:  Prime metal flanges (all jacks, edge metal, lead drain flashings) and concrete and masonry surfaces with a uniform coating of ASTM D 41 asphalt primer.

D.	Kettles and Tankers:  Kettles and tankers shall be equipped with accurate, fully readable thermometers.  Do not heat asphalt to or above its flash point.  Avoid heating at or above the FBT, should conditions make this impractical, heating must be no more than 25ºF below the EVT and no more than 25ºF above EVT.

E.	Asphalt Temperatures:  If the EVT information is not provided, the following asphalt temperature shall be observed.  Maximum heating temperature shall be 525ºF (274ºC).  Minimum application temperature shall be 400ºF (204ºC).

F.	Asphalt Moppings:  Ensure that all moppings do not exceed a maximum of 25 lb./square.  Mopping shall be total in coverage, leaving no breaks or voids.

G.	Membrane Adhesive Application:  Membrane adhesive can be applied by roller, squeegee or spray unit.  Apply cold adhesive in a smooth, even, continuous layer without breaks or voids.  Utilize an application rate of 2 to 2 1/2 gal/sq (0.6 to 1.0 l/m²) over irregular or porous substrates.  Utilize an application rate of 1 1/2 to 2 gal/sq (0.6 to 0.8 kg/m²) for interply applications.  Double the adhesive application rate at the end laps of granule surfaced sheets.

H.	Bitumen Consistency:  Cutting or alterations of bitumen, primer, and sealants will not be permitted.

*  NOTE:	Choose the following application techniques that are applicable for the  proposed roof membrane assembly.

I.	Roofing Application:  Apply all layers of roofing free of wrinkles, creases or fishmouths. Exert sufficient pressure on the roll during application to ensure prevention of air pockets.

*  NOTE:	Use the following items 1-3 for applications incorporating sheets applied perpendicular to the slope of the roof.

1.	Apply all layers of roofing perpendicular to the slope of the deck.

2.	Fully bond the base ply to the prepared substrate, utilizing minimum 3 inch side and end laps.  Apply each sheet directly behind the *[asphalt/cold adhesive] applicator.  Cut a dog ear angle at the end laps on overlapping selvage edges.  Using a clean trowel, apply top pressure to top seal T-laps immediately following sheet application.  Stagger end laps a minimum of 3 feet.

3.	Fully bond the finish ply to the base ply, utilizing minimum 3 inch side and end laps.  Apply each sheet directly behind the *[asphalt/cold adhesive] applicator.  Stagger end laps of the finish ply a minimum 3 feet.  Cut a dog ear angle at the end laps on overlapping selvage edges.  Using a clean trowel, apply top pressure to top seal T-laps immediately following sheet application.  Stagger side laps of the finish ply a minimum 12 inches from side laps in the underlying base ply.  Stagger end laps of the finish ply a minimum 3 feet from end laps in the underlying base ply.

*  NOTE:	Use the following items 1-3 for applications incorporating sheets applied parallel to the slope of the roof.

1.	Apply all layers of roofing parallel to the slope of the deck.

2.	Fully bond the base ply to the prepared substrate, utilizing minimum 3 inch side and end laps.  Apply each sheet directly behind the *[asphalt/cold adhesive] applicator.  Cut dog ear angles on underlying end laps at the finish edge and the overlapping selvage edges.  Using a clean trowel, apply top pressure to top seal T-laps immediately following sheet application.  Stagger end laps a minimum of 3 feet.

3.	Fully bond the finish ply to the base ply, utilizing minimum 3 inch side and end laps.  Apply each sheet directly behind the *[asphalt/cold adhesive] applicator.  Stagger end laps of the finish ply a minimum 3 feet.  Cut dog ear angles on underlying end laps at the finish edge and the overlapping selvage edges.  Using a clean trowel, apply top pressure to top seal T-laps immediately following sheet application.  Stagger side laps of the finish ply a minimum 12 inches from side laps in the underlying base ply.  Stagger end laps of the finish ply a minimum 3 feet from end laps in the underlying base ply.

4.	Maximum sheet lengths and special fastening of the specified roof membrane system may be required at various slope increments where the roof deck slope exceeds 1/2 inch per foot. The manufacturer shall provide acceptable sheet lengths and the required fastening schedule for all roofing sheet applications to applicable roof slopes.

J.	Granule Embedment:  Broadcast mineral granules over all bitumen overruns on the finish ply surface, while the bitumen is still hot or the adhesive is soft, to ensure a monolithic surface color.

K.	Flashing Application - Masonry Surfaces:  Flash masonry parapet walls and curbs using the reinforcing sheet and the metal foil flashing membrane.  After the base ply has been applied to the top of the cant, fully adhere the reinforcing sheet, utilizing minimum 3 inch side laps and extend a minimum of 3 inches onto the base ply surface and 3 inches up the parapet wall above the cant.  After the final roofing ply has been applied to the top of the cant, prepare the surface area that is to receive flashing coverage by torch heating granular surfaces or by application of asphalt primer; allowing primer to dry thoroughly.  Torch apply the metal foil-faced flashing into place using three foot widths (cut off the end of roll) always lapping the factory selvage edge.  Stagger the laps of the metal foil flashing layer from lap seams in the reinforcing layer.  Extend the flashing sheet a minimum of 4 inches beyond the toe of the cant onto the prepared surface of the finished roof and up the wall to the desired flashing height.  Exert pressure on the flashing sheet during application to ensure complete contact with the wall/roof surfaces, preventing air pockets; this can be accomplished by using a damp sponge or shop rag.  Check and seal all loose laps and edges.  Nail the top edge of the flashing on 9 inch centers.  (See manufacturer's schematic for visual interpretation).

L.	Flashing Application - Wood Surfaces:  Flash wood or plywood parapet walls and curbs using the reinforcing sheet and the metal foil flashing membrane.  The reinforcing sheet shall have minimum 3 inch side laps and extend a minimum of 3 inches onto the base ply surface and to the top of the parapet wall or curb.  Nail the reinforcing sheet through the field of the sheet to the vertical wood surface on 12 inch centers from the top of the cant to top of the wall or curb.  Fully adhere the remainder of the flashing reinforcing sheet that extends over the cant and roof level.  After the final roofing ply has been applied to the top of the cant, prepare the surface area that is to receive flashing coverage by torch heating granular surfaces or by application of asphalt primer; allowing primer to dry thoroughly.  Torch apply the metal foil-faced flashing into place using three foot widths (cut off the end of roll) always lapping the factory selvage edge.  Extend the flashing sheet a minimum of 4 inches beyond the toe of the cant onto the prepared surface of the finished roof and up the wall to the desired flashing height.  Exert pressure on the flashing sheet during application to ensure complete contact with the wall/roof surfaces, preventing air pockets; this can be accomplished by using a damp sponge or shop rag.  Check and seal all loose laps and edges.  Nail the top edge of the flashing on 9 inch centers.  (See manufacturer's schematic for visual interpretation).

M.	Use of Metallic Powder:  Broadcast metallic powder over all bitumen overruns on the metal foil membrane surface while the bitumen is still hot to ensure a monolithic surface color.

N.	Water Cut-Off:  At end of day's work, or when precipitation is imminent, construct a water cut-off at all open edges.  Cut-offs can be built using asphalt or plastic cement and roofing felts, constructed to withstand protracted periods of service.  Cut-offs must be completely removed prior to the resumption of roofing.

O.	Sealant:  Apply a smooth continuous bead of the specified sealant at the exposed finish ply edge transition to metal flashings incorporated into the roof system.

3.04 FIELD QUALITY CONTROL AND INSPECTIONS

A.	Site Condition:  Leave all areas around job site free of debris, roofing materials, equipment and related items after completion of job.

B.	Notification of Completion:  Notify the manufacturer by means of manufacturer's printed Notification of Completion form of job completion in order to schedule a final inspection date.

C.	Final Inspection/Post-Installation Meeting:  Hold a meeting at the completion of the project, attended by all parties that were present at the pre-job conference.  A punch list of items required for completion shall be compiled by the Contractor and the manufacturer's representative.  Complete, sign, and mail the punch list form to the manufacturer's headquarters.

D.	Issuance of the Guarantee:  Complete all post installation procedures and meet the manufacturer's final endorsement for issuance of the specified guarantee.