ROOFING GUIDE SPECIFICATION PREPARED BY SIPLAST, INC.

TERANAP WATERPROOFING MEMBRANE SYSTEM

OVER A STRUCTURAL CONCRETE DECK

This specification is provided as a general guide for use of Siplast, Inc. products based on typical building conditions and standard roofing practices. This guide specification is not a substitute for professional design services. The information in this guide specification must be reviewed/approved by a design professional and modified as necessary and appropriate for each project. Each project has unique requirements and Siplast, Inc. recommends that the Owner's representative independently verify the accuracy and appropriateness of the specification provided for a particular project. Each selection or deletion made to this guide specification should be carefully considered. Users of this guide specification assume sole responsibility for its use.

January 1, 2023

SECTION 07 13 52 – STYRENE BUTADIENE STYRENE MODIFIED BITUMINOUS MEMBRANE WATREPROOFING

PART 1 - GENERAL

  - RELATED DOCUMENTS

- The project plans, details and general Contract requirements apply to this Section.

  - SUMMARY

- Items Included:

- SBS modified bituminous membrane waterproofing.

- Related Sections:

- [Section 06 10 00 "Rough Carpentry"] [Section 061053 "Miscellaneous Rough Carpentry"] for wood nailers, curbs, and blocking, and for wood-based, structural-use roof deck panels.

- Section 06 16 00 "Sheathing" for wood-based, structural-use roof deck panels.

- Section 07 62 00 "Sheet Metal Flashing and Trim" for sop and field formed metal roof flashings and counter flashings.

- Section 07 71 00 "Roof Specialties" for premanufactured metal copings, roof edge fascia, gravel stops, reglets, roof edge flashings, and counter flashings.

- Section 07 92 00 "Joint Sealants" for joint sealants, joint fillers, and joint preparation.

  - REFERENCES

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT STANDARD REFERENCES.

  - PREINSTALLATION MEETINGS

- Pre-installation Roofing Conference at Jobsite:  Hold a meeting with the Owner, Construction Manager, Architect, Roofing Contractor, Roofing Manufacturer's Representative, and other applicable trades to discuss the means and methods related to roofing installation.  The Roofing Contractor shall examine the substrate that will receive the specified roofing materials and confirm its suitability for attachment of the specified roofing system.

  - SUBMITTAL OF ALTERNATE SYSTEMS

- Consideration of Alternate Systems:  Submit primary waterproofing systems to be considered as equals to the specified waterproofing system no less than 10 days prior to bid date.  Primary waterproofing systems which have been reviewed and accepted as equals to the specified waterproofing system will be listed in an addendum prior to bid date; only then will equals be accepted at bidding.  Submittals shall include the following:

Identify fire and hail ratings in Items 6 and 8 below.

- Two 3 inch x 5 inch samples of the primary waterproofing and flashing sheets.

- Latest edition of the waterproofing system manufacturer's specifications and installation instructions.

- Evidence that the manufacturer of the proposed waterproofing system utilizes a quality management system that is ISO 9001 certified.  Documentation of ISO 9001 certification of foreign subsidiaries without domestic certification will not be accepted.

- Evidence and description of manufacturer's quality control/quality assurance program for the primary waterproofing products supplied.  The quality assurance program description shall include all methods of testing for physical and mechanical property values.  Provide confirmation of manufacturer's certificate of analysis for reporting the tested values of the actual material being supplied for the project prior to issuance of the specified guarantee.

- Descriptive list of the materials proposed for use.

- Evidence of Underwriters' Laboratories Class [-----] acceptance of the proposed waterproofing system (including mopping asphalt or cold adhesive) without additional requirements for gravel or coatings.

- Evidence that the waterproofing configuration (including fastening of insulation) has been tested by an accredited independent testing agency to meet the design wind load pressure indicated in Part 1.07 C2.

- The waterproofing membrane configuration shall be approved by FM Global for [Class 1-SH (severe hail) exposure] [Class 1-VSH (very severe hail) exposure].

- Letter from the proposed primary waterproofing manufacturer confirming that a phased waterproofing application, with only the modified bitumen base ply in place for a period of up to 10 weeks, is acceptable and approved for this project.

- List of 3 of the proposed primary waterproofing manufacturer's projects, located in the United States, of equal size and degree of difficulty which have been performing successfully for a period of at least 10 years.

- Letter from the proposed primary waterproofing manufacturer confirming that the filler content in the elastomeric blend of the proposed waterproofing membrane and flashing components does not exceed 35% in weight.

- Complete list of material physical and mechanical properties for each sheet including: weights and thicknesses; low temperature flexibility; peak load; ultimate elongation; dimensional stability; compound stability; high temperature stability; granule embedment and resistance to thermal shock for foil faced products.

- Evidence that the waterproofing system shall pass 500 cycles of ASTM D5849 Resistance to Cyclic Joint Displacement (fatigue) at 14F (-10C).  Passing results shall show no signs of membrane cracking or interply delamination after 500 cycles.  The waterproofing system shall pass 200 cycles of ASTM D5849 after heat conditioning performed in accordance with ASTM D5147.

- Sample copy of the proposed guarantee.

- Technical Product Data:  Submit the manufacturer’s technical product data sheets for each type of product.

- Shop Drawings:  Include plans, sections, and shop drawings/details for all applicable conditions.

- Product Samples:  Submit product samples of the specified base, finish, flashing reinforcing, and flashing membrane plies.

  - INFORMATIONAL SUBMITTALS

- Qualification Data:

- Installer:  Submit written confirmation that they have a minimum of 2 years of experience in successfully installing the same or similar roofing materials and be certified in writing by the roofing materials manufacturer to install the primary roofing products.

- Manufacturer:  Submit written confirmation that the manufacturer of the primary roofing products has been successfully producing the specified types of primary products for not less than 10 years with a consistent composition for a minimum of 5 years.

- System Qualification:

- Intent to Warrant Letter: Submit a signed letter on the waterproofing membrane manufacturer’s letterhead, confirming that specified waterproofing system complies with the guarantee requirements indicated in Part 1.11 and the criteria indicated in Part 2.2 Roof Membrane Sheet Materials.

- Cyclic Fatigue:  Submit confirmation that the proposed roof system will pass 500 cycles of ASTM D5849 Resistance to Cyclic Joint Displacement (fatigue) at 14˚F (-10˚C), and 200 cycles after heat conditioning (performed in accordance with ASTM D5147), showing no signs of membrane cracking or interply delamination.

- Sample Guarantee:  Submit a sample copy of the manufacturer’s proposed Guarantee.

  - CLOSEOUT SUBMITTALS

- Maintenance Data: Submit the manufacturer’s care and maintenance guide.

- Executed Guarantee:  Provide the Owner with an executed version of the specified guarantee.

  - QUALITY ASSURANCE

- Fire Rating:  Submit evidence of exterior fire-test exposure by an approved third-party testing agency in accordance with ASTM E108 or UL 790 guidelines.

Indicate Class A, B, or C for the fire rating where the brackets appear in item 1 below.

- Class [----]

- Wind Uplift Rating:  Submit evidence by an approved third-party testing agency that the roof configuration has been tested to meet the following specified wind uplift design.

Select item “1” for FM Global rated systems, or item “2” if using a different code approval agency or independent laboratory testing.  Indicate the wind uplift design criteria where the brackets appear.

- Class 1, 1-[----] windstorm construction.

- Minimum design wind load pressure of - [----] psf.

  - DELIVERY, STORAGE, AND HANDLING

- Delivery:  Deliver roofing materials to Project site in original containers with seals unbroken and labeled with manufacturer's name, product brand name and type, date of manufacture, approval or listing agency markings, and directions for storing and mixing with other components.

- Storage:  Store liquid materials in their original undamaged containers in a clean, dry, protected location and within the temperature range required by roofing manufacturer.

- Protect stored liquid material from direct sunlight, heat, open fire, ignition sources, oxidizing agents, strong acids, and strong alkalis.

- Discard and legally dispose of liquid material that cannot be applied within its stated shelf life.

- Protection:  Protect roof insulation materials from physical damage and from deterioration by sunlight, moisture, soiling, and other sources.  Comply with the insulation manufacturer's written instructions for handling, storing, and protecting materials during installation.

- Handling:  Handle and place roofing materials and equipment in a manner to avoid permanent deflection of deck.

  - FIELD CONDITIONS

- Weather Limitations: Proceed with installation only when existing and forecasted weather conditions permit roofing to be installed in accordance with manufacturer's written instructions and warranty requirements.

- Membrane Protection:  Provide protection against staining and mechanical damage for newly applied roofing and adjacent surfaces throughout this project.

- Debris Removal:  Remove all debris daily from the project site and take to a legal dumping area authorized to receive such materials.

- Site Condition:  Complete, to the owner's satisfaction, all job site clean-up including building interior, exterior and landscaping where affected by the construction.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT TORCH SAFTEY GUIDELINES.

  - GUARANTEE

- Manufacturer’s Guarantee: Provides that the Manufacturer will repair leaks through the covered waterproofing materials due to material or workmanship defects, subject to certain exclusions, during the specified time period. Refer to guarantee for complete coverage and restrictions.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT GUARANTEE COVERAGE.

- Special Project Warranty: Submit waterproofing contractor’s warranty signed by the Installer, including all components of the waterproofing and insulation system for the following warranty period:

      - Warranty Period: [---] years from date of Substantial Completion.

PART 2 - PRODUCTS

  - MANUFACTURERS

A.	Manufacturer: A roof system by the following manufacturer is approved for application.

- Siplast, Inc.

  - ROOFING MEMBRANE SHEET MATERIALS

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT BASE PLY.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT FINISH PLY.

  - BASE FLASHING SHEET MATERIALS

- Flashing Reinforcing Ply and Cant Backer: An ASTM D6163, Type I, Grade S homogenous membrane with a glass-fiber reinforcing mat impregnated/saturated and coated each side with SBS modified bitumen blend with a factory applied polymer modified asphalt self-adhesive on the back surface of the sheet to provide full adhesion to the total surface area of the substrate.  The back side of the base ply shall be surfaced with a removable film.

- Paradiene 20 SA by Siplast, Inc.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT FLASHING PLY.

- Liquid Flashing System:  The specified liquid flashing system shall consist of a catalyzed PMMA-based membrane fully reinforced with a non-woven polyester fleece that is installed over a prepared substrate.

- Parapro 123 Flashing by Siplast, Inc.

- Liquid Flashing System:  The specified liquid flashing system shall consist of an STP-based membrane fully reinforced with a non-woven polyester fleece that is installed over a prepared substrate.

- Paraflex 531 Liquid Flashing by Siplast, Inc.

  - PRIMERS

- Asphalt Primer: Primer shall meet ASTM D41 criteria.

- PA-1125 Asphalt Primer by Siplast, Inc.

- Low VOC Asphalt Primer: Primer shall meet ASTM D41 criteria and South Coast Air Quality District and Ozone Transport Commission requirements.

- PA-917 Primer by Siplast, Inc.

- Primer for Self-Adhesive Membranes:  Primer for self-adhesive membranes shall be a single component, water-based resinous primer formulated to condition masonry, wood, plywood, concrete, asphaltic, and gypsum surfaces to facilitate adhesion of self-adhesive membranes.

- TA-119 Primer by Siplast, Inc.

  - AUXILIARY ROOFING MATERIALS

Delete auxiliary roofing materials listed below, as necessary, to meet individual project requirements. Use PA-311 R for solvent based adhesive or SFT Adhesive for solvent-free adhesive.  (Note:  PA-311 series adhesives are not for use with systems having Teranap 1M Film.)

- Roofing Asphalt: ASTM D312, Type [III or IV].

- Cold-Applied Asphalt Adhesive: An asphalt, solvent blend conforming to ASTM D4479, Type II requirements.

- PA-311 R Adhesive by Siplast, Inc.

- Membrane Adhesive:  A single-component, moisture curing, low-odor adhesive designed for application of the specified roof membrane system.

- SFT Adhesive by Siplast, Inc.

Delete auxiliary roofing materials listed below, as necessary, to meet individual project requirements.  Use PA-1021 and PA-828 for solvent based cement or SFT Cement for solvent-free adhesive.  (Note:  PA-828 Flashing Cement is not for use with Veral Aluminum or Teranap 1M Film.)

- Asphalt Roofing Cement: An asphalt cutback mastic, reinforced with non-asbestos fibers, used as a base for setting metal flanges conforming to ASTM D4586 Type II requirements.

1.	PA-1021 Plastic Cement by Siplast, Inc.

- Flashing Cement:  A slump resistant, asphalt cutback flashing adhesive, reinforced with non-asbestos fibers, conforming to ASTM D4586 Type II requirements.

1.	PA-828 Flashing Cement by Siplast, Inc.

- Flashing Cement:  A single-component, moisture curing, low-odor adhesive formulated in a grade for application of flashing materials.

1.	SFT Cement by Siplast, Inc.

- Sealant:  A moisture-curing, self-leveling elastomeric sealant designed for roofing applications.

1.	PS-209 Elastomeric Sealant

- Sealant:  A moisture-curing, non-slumping elastomeric sealant designed for roofing applications.

- PS-715 NS Elastomeric Sealant

- Ceramic Granules:  No. 11 grade specification ceramic granules of color scheme matching the granule surfacing of the finish ply.

Delete Item J below if a mechanically attached base sheet is not specified.

- Base Sheet Fasteners for Wood/Plywood Decks:

- A 12 gauge, spiral or annular threaded shank, zinc coated steel roofing fastener having a minimum 1 inch metallic head.

a.	Simplex Cap Nail by Simplex Nails, Inc.

  - INSULATION ACCESSORIES

- Insulation Cant Strips: A cant strip composed of expanded volcanic minerals combined with waterproofing binders, meeting ASTM C728 criteria.  The top surface shall be pre-treated with an asphalt based coating.  The face of the cant shall have a nominal 4 inch dimension.

  - OVERBURDEN COMPONENTS

Delete items as necessary to match the desired hardscape criteria.  If specifying a vegetated overburden system, which can be specified in Section 07 33 63, then keep Item A below and delete all other components.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT A PROTECTION LAYER.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT INSULATION.

- Vegetated Overburden System:  See Specification Section 07 33 63.

- Prefabricated Drainage Mat:  A two-part prefabricated sheet drain and protection board consisting of a formed polystyrene core covered on one side with a woven polypropylene filter fabric, designed for high compression applications.

- Paradrain Drainage Mat by Siplast

- Filter Fabric:  A nonwoven, chemical resistant geotextile made up of a network of polypropylene fibers, designed for preventing the passage of ballast fines, soils, or other loose overburden material into the insulation and waterproofing systems below the fabric on protected membrane waterproofing assemblies.

- Paradrain W Filter Fabric by Siplast

- Stone Ballast:  River washed rock used to ballast the insulation assembly shall meet the ASTM D448 #57 requirements.  Diameter of the rock particles shall maintain a nominal 3/4 inch to a maximum 1-1/2 inch range.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT A PAVER SYSTEM.

PART 3 - EXECUTION

  - EXAMINATION

- Substrate Qualification:  The installing contractor shall examine all substrates where the specified roofing and flashing system will be applied and confirm their suitability to receive the specified roofing materials.

  - PREPARATION

- Sweep or vacuum all surfaces, removing all loose aggregate and foreign substances prior to commencement of roofing.

Keep item B if specifying a tear-off, partial tear-off, or re-cover.  Delete numbered conditions, as necessary to match project conditions.

- Remove all of the following existing conditions:

- Surface gravel

- Roof membrane

- Insulation

- Base flashings

- Edge metal

- Flanged metal flashings

- Cants

- Walkways

- Nonfunctional penetrations/curbs

- Drain assemblies

- Vapor retarder

- Metal trim, counter flashing

- Primer for Self-Adhesive Flashing Reinforcing Ply:  Apply the specified tacky primer by roller or spray in an even film. Refer to the manufacturer’s literature for the approved rate of application over various substrate types. Allow the primer to dry until it leaves a slightly sticky surface without transfer when touched.  Cutting or alteration of the primer is not permitted.

- Asphaltic Primer:  Prime metal and concrete and masonry surfaces with a uniform coating of the specified asphalt primer according to the manufacturer’s published application rate.  Cutting or alteration of the primer is not permitted.

  - INSTALLATION OF WATERPROOFING, GENERAL GUIDLEINES

Keep items A and B, as appropriate, for cold adhesive and/or hot asphalt application.

- Asphalt Heating and Application:  Do not heat asphalt to or above its flash point.  Avoid heating at or above the FBT, should conditions make this impractical, heating must be no more than 25ºF  below the EVT and no more than 25ºF above EVT.  Follow the asphalt manufacturer’s published maximum heating temperature and minimum application temperature guidelines.  Ensure that all moppings do not exceed a maximum of 25 lb/sq.  Mopping shall be total in coverage, leaving no breaks or voids.

- Adhesive Application:  Apply membrane cold adhesive by roller, squeegee or spray unit in a smooth, even, continuous layer without breaks or voids.  Utilize an application rate for each ply as published by the roof membrane manufacturer.  Double the adhesive application rate at the end laps of granule surfaced sheets.  Where solvent-based adhesive is applied, refer to the manufacturer’s inter-ply flashing detail at the locations that are to receive the specified catalyzed acrylic resin primer/flashing system.  Cutting or alteration of the adhesive is not permitted.

- General Appearance:  Ensure that the finished roofing application has an aesthetically pleasing overall appearance and is acceptable to the Owner.

  - APPLICATION OF BITUMINOUS ROOFING MEMBRANE

Select parallel or perpendicular sheet orientation in Item A below.  Select application method for membrane plies below.

- Apply all layers of roofing with side laps running [parallel/perpendicular] to the direction of the slope.  Exert sufficient pressure on the roll during application to ensure prevention of air pockets, wrinkles, creases or fishmouths.  Refer to the manufacturer’s guidelines for maximum sheet lengths and special fastening of the head laps where the roof deck slope exceeds 1/2 inch per foot.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT BASE PLY APPLICATION METHODS TO MEET THE SPECIFIED REQUIREMENTS.

HOVER CURSOR HERE AND RIGHT CLICK TO SELECT FINISH PLY APPLICATION METHODS TO MEET THE SPECIFIED REQUIREMENTS.

  - APPLICATION OF FLASHING AND STRIPPING

- Modified Bitumen Flashing System:  Apply the specified base flashing materials in accordance with the manufacturer’s standard details.  Notify the design team immediately of any flashing heights below 8 inches.  For torch applied base flashings, apply a 12-inch self-adhesive cant backing sheet extending 6 inches onto the field of the roof area and a minimum of 6 inches up the vertical surface utilizing minimum 3 inch laps.  Set the non-combustible cant into place dry prior to installation of the roof membrane base ply and subsequent flashing system.  Flash walls and curbs using the reinforcing sheet and flashing membrane.  Exert pressure on the flashing sheet during application to ensure complete contact with the vertical/horizontal surfaces, preventing air pockets.  Check and seal all loose laps and edges.  Nail the top edge of the flashing on 9 inch centers.  (See the manufacturer's schematic for visual interpretation).

- Liquid Flashing System:  Install the specified liquid-applied flashing system in accordance with the membrane system manufacturer’s printed installer’s guidelines and other applicable written recommendations as provided by the manufacturer.

  - APPLICATION OF SEALANT

- Apply a smooth continuous bead of the specified sealant at the exposed finish ply edge transition to metal flashings incorporated into the roof system.

  - APPLICATION OF OVERBURDEN COMPONENTS

Retain the following items based on selection of the overburden components specified in Part 2 and delete non-applicable items.

- Membrane Protection Layer:  Place the specified polyethylene slip sheet unadhered directly over all areas of the newly applied membrane, extending to walls, curbs, and other related junctures.  Lap the polyethylene sheets a minimum 6 inches at the sides and ends.

- Drainage Mat:  Place the specified drainage mat with the polyethylene filter fabric side up, unadhered directly over all areas of the newly applied membrane, extending to walls, curbs, and other related junctures.

- Protection Board:  Place the protection board unadhered directly over the waterproofing surface with the end joints staggered.  Install the panels to fit tightly; leaving a maximum opening between panels of 3/8 inch.  Closely abut walls, penetrations, and projections leaving a maximum opening between panels and projections of 3/4 inch.

- Insulation:  Place the specified insulation unadhered with the channeled edges down.  Install the panels to fit tightly; leaving a maximum opening between panels of 3/8 inch.  Closely abut walls, penetrations, and projections leaving a maximum opening between panels and projections of 3/4 inch.  In multiple-layer configurations the bottom layer must be the thickest layer of the insulation system, and have a minimum thickness of 2 inches.  Stagger the panel joints between insulation layers.

- Filter Fabric:  Place the specified filter fabric unadhered directly over the insulation.  Overlap edges and ends of the fabric a minimum of 1 foot.  Extend the fabric a minimum 3 inches above the stone/gravel ballast at all penetrations with the exception of drains.  Do not lap the fabric within 6 feet of the perimeter of the area.  Immediately install ballast over the fabric to prevent heat-buildup beneath the fabric.  High temperatures may result in damage to the underlying insulation panels.  The use of a light-color tarp must be considered if fabric is to be exposed in hot weather or when exposed to severe UV.

- Ballast:  Installation of gravel ballast must concur with the instructions of the insulation manufacturer.  Distribute the gravel ballast evenly over the insulation/filter fabric at a minimum rate of 1000 lb/sq.  Provide for a ballast distribution at the roof perimeter of 2000 lb/sq in an area extending 4 feet in from the perimeter.

- Pedestals/Pavers:  Install the pedestals/pavers following the instructions and requirements of the insulation and pedestal/paver manufacturer, as well as the specified wind uplift criteria, including specifications as applicable for adhesion of pedestals, perimeter securement and incorporation of metal fabricated restrainments at the perimeter.  For applications that require mechanical attachment of the corners of the paver to the pedestal base, ensure that the fastener is snug without overtightening.

  - FIELD QUALITY CONTROL

- Notify the manufacturer of job completion in order to schedule a final inspection date.  Hold a meeting at the completion of the project, attended by all parties that were present at the pre-job conference.  A punch list of items required for completion shall be compiled by the manufacturer's representative.  Complete, sign, and send the punch list form to the manufacturer's headquarters.

- Leave all areas around job site free of debris, roofing materials, equipment and related items after completion of job.

- Complete all post installation procedures and meet the manufacturer's requirements for issuance of the specified guarantee.

END OF SECTION 07 13 52