Zono-Patch

Lightweight Insulating Concrete Patching Compound

Prepared by:

Siplast, Inc.

1000 East Rochelle Blvd.

Irving, Texas 75062

(800) 922-8800

This specification is provided as a general guide for use of lightweight insulating concrete patching products based on typical building conditions and standard construction practices.  Siplast is strictly a manufacturer of roofing and insulation systems and has no experience, training or expertise in the areas of architecture/engineering or in the area of consulting with respect to matters related to such areas.  Siplast recommends that the Owner's representative independently verify the accuracy and appropriateness of a specification provided for a specific project.

January 1, 2011

PART 1:  GENERAL

1.01  SUMMARY

A.	Furnish labor, materials, equipment, and services necessary for the complete and proper repair of incidental surface damage, unintended low areas, rough cold joints and fastener holes in [new/existing] lightweight insulating concrete substrates.

1.02  RELATED SECTIONS

A.	Section  [-----] – Lightweight Insulating Concrete Roof Decks

B.	Section  07220 – Lightweight Insulating Concrete Roof Insulation

C.	Section  [-----] – [-------] Roofing

1.03  SUBMITTALS

A.	Submit manufacturer's instructions for proper placement of the proposed lightweight insulating concrete patching compound.

1.04  DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in the supplier’s original unopened packages, fully identified as to manufacturer, brand or other identifying data.

B.	Store bagged patching products in a dry location until ready for application.

C.	Familiarize every member of the application crew with the manufacturer's material safety data sheets and safety regulations as required by governing codes and regulations.

1.05 PROJECT/SITE CONDITIONS

A.	Do not install the lightweight insulating concrete patching compound during periods of precipitation, when air temperatures are below 32 degrees F (0ºC), or when air temperatures are expected to fall below 32 degrees F (0ºC) any time within 24 hours following application of the product.

PART 2:  PRODUCTS

2.01  MATERIALS

A.	A lightweight insulating concrete patching compound incorporating cementitious binders, low density fine aggregates, and additives supplied by a single manufacturer.

>	Zono-Patch Lightweight Insulating Concrete Patching Compound by Siplast, Inc., Irving, TX  (800) 922-8800

B.	Potable water that is clean and free of deleterious amounts of acid, alkali and organic materials.

PART 3:  EXECUTION

3.01  EXAMINATION/PREPARATION OF SURFACES THAT REQUIRE PATCHING

A.	Remove debris from the area and remove deteriorated roof deck material down to a sound substrate.

B.	For improved bonding, moisten the existing lightweight insulating concrete surface with water or a 1:1 dilution of acrylic or PVA concrete bonding agent.  The extent of moistening will depend on the nature of the surface to be repaired.   Highly porous, dusty surfaces will require more preparation.  If moistening is insufficient, the Zono-Patch will stiffen too quickly to finish.

3.02  MIX DESIGN/PRODUCT PREPARATION

A.	One five gallon container of Zono-Patch requires approximately 3 gallons of water for mixing.  For larger quantities, utilize a mix ratio of 5 parts Zono-Patch powder to 3 parts water.  The quantity of water may be adjusted to control the consistency and handle ability of the material during application.  Adding more water will make the product more fluid; less water will make it stiffer.  Sufficient water should be added to create a wet mix that is easily trowelled and finished to a smooth surface.

B.	In a suitable container or mortar mixer, add water in a quantity suitable to achieve the desired batch size.  Add dry Zono-Patch powder to the water and mix until the wet slurry is of a smooth, lump-free, creamy consistency.  If a container is used, a “jiffy” mixer attached to a drill motor is recommended.

*  NOTE:	Zono-Patch powder must always be added to water.  Adding water to powder will result in an unmixable combination.

3.03  APPLICATION

A.	Following mixing and utilizing product that has the proper stiffness for the specific application, pump or pour the Zono-Patch into place.  Finish the surface of the Zono-Patch to a smooth surface.

B.	Trowel finish any edges to provide a smooth transition to the surface of the existing substrate.